## Slide 1
It is a Great Time to Be a Rocket Engineer
Gregg Jones
NASA Marshall Space Flight Center (MSFC)
March 26-27, 2019

## Slide 2: When I graduated
Lockheed Martin and Boeing
Aerojet, Rocketdyne, Pratt & Whitney
European Space Agency
Russian Space Agency

## Slide 3: Commercial Space Today
Over 75 New Space companies on the Wikipedia
  Does not include Boeing, Lockheed, United Launch Alliance, Aerojet Rocketdyne and Northrop Grumman
Very active and working with NASA

## Slide 4: SLS LIFT CAPABILITIES
Foundation for a generation of deep space exploration
Maximum Thrust
11.9M lbs
8.8M lbs
8.8M lbs
8.8M lbs
** Not including Orion/Service Module volume
Payload Volume
34,910 ft3 (988 m3)
18,970 ft3 (537 m3)
10,100 ft3 (286m3)**
N/A**
Payload to TLI/Moon
> 45 t (99k lbs)
37–40 t (81k–88k lbs)
34–37 t (74k–81k lbs)
> 26 t (57k lbs)
Low Earth Orbit (LEO) represents a typical 200 km circular orbit at 28.5 degrees inclination
Trans-Lunar Injection (TLI) is a propulsive maneuver used to set a spacecraft on a trajectory that will cause it to arrive at the Moon. A spacecraft performs TLI to begin a lunar transfer from a low circular parking orbit around Earth.
The numbers depicted here indicate the mass capability at the Trans-Lunar Injection point.
SLS Block 2 Cargo
SLS Block 1B Cargo
SLS Block 1B Crew
SLS Block 1 Crew
SLS Block 2 Crew
10,100 ft3 (286m3)**
> 45 t (99k lbs)
11.9M lbs
> 26 t (57k lbs)
9,030 ft3 (256m3)
8.8M lbs
SLS Block 1 Cargo
Payload to LEO
130 t (287k lbs)
105 t (231k lbs)
105 t (231k lbs)
95 t (209k lbs)
130 t (287k lbs)
95 t (209k lbs)
Notes: (Note: new 8.4m fairing on Block 2)
Block 1 and EM-1 will be a great early test of SLS, Orion and ground systems, but it’s just the beginning.
The basic SLS design has room to grow and we are working on that already with the Block 1B design that will be our workhorse for lunar missions – EUS, RS-25, USA, etc.
We’re not a low Earth orbit rocket. We’re a deep space transportation system. Block 1 will have more than 26 metric tons (57,320 lb) of payload to the Moon. Block 1B will have 34 to 40 metric tons (74,957 – 88,185 lb) to the Moon, depending on whether its crew or cargo configuration. Block 2 cargo will have more than 45 metric tons (99,208 lb) payload to the Moon. That is by far more capability than any existing rocket.
The benefits of heavy lift are obvious for something as challenging as space exploration. The ability to transport large payloads reduces payload complexity and operational complexity from the ground all the way to space. It saves time and money and increases our chances for mission success.

## Slide 5: SLS – enabling human exploration exploration class: deep space CAPABILITIES
Volume
Nearly four times more volume than any contemporary heavy lift vehicle
Only vehicle that can carry the Orion and a co-manifested payload to the Moon
Orion with Science
Missions
8m x 27m fairing with large aperture telescope
Reduce transit times by half or greater to the outer solar system
Enables larger payloads to deep space destinations
Departure Energy
Block 1B: Can launch 60% more mass than any contemporary launch vehicle
Block 2: Mars-enabling capability of greater than 45 metric tons to Trans Lunar Injection
Mass
Contemporary Heavy Lift
SLS Block 1B
SLS Block 2
Notes: These three areas are the primary “unique capabilities” of SLS which enable or enhance exploration class missions in ways other vehicles cannot.
VOLUME
•Space Launch System will be able to offer payload accommodations with nearly four times more volume than any contemporary launch vehicle enabling large habitats, telescopes, and other payloads not previously possible*
MASS
•Space Launch System will offer an initial capability of greater than 26 metric tons (57,320 lb) to Trans-Lunar Injection; current U.S. launch vehicle maximum is ~20 t**
•Evolved version of SLS will offer Mars-enabling capability of greater than 45 metric tons (99,208 lb) to TLI
ENERGY
•SLS offers reduced transit times to the outer solar system by half or greater (2-3 years for Europa instead of 7-8)
•SLS enables larger payloads to deep space destinations
MORE THAN MEETS THE EYE
All rockets are not created equal, and there’s even more to SLS advantages than volume, mass and departure energy.
Its unmatched capability will reduce the complexity, cost, and risk associated with payload design, ground infrastructure, and in-space operations and provide the best opportunity for mission success.
*Based on 255 m3 for standard 5-meter Delta IV vs. SLS 8.4 m wide 27m long-fairing at 988 m3
**Citing an average of several sources on Falcon Heavy including ACO estimates at 19.4, the “Rocket Garden” chart from August 2018 which shows 22.2 t. SpaceX does not show TLI for FH on their website.

## Slide 6: SOLID ROCKET boosterS
Notes: Large image:
Qualification Motor QM-2 test in Promontory, Utah at Northrop Grumman’s facility in June of 2016.
Top Inset image:
Booster production continues at prime contractor Northrop Grumman’s facilities, where technicians are applying photogrammetric markings on completed segments for the five-segment solid rocket booster motors for the first integrated mission of SLS and Orion.
Bottom inset image:
Moving a completed booster segment at Northrop Grumman in UT where it awaits completion of remaining segments to ship to Kennedy Space Center.
Status:
Two full-scale static hot-fire tests have been conducted and are paving the way for qualification.
  The first test (March 2015) tested the propellant at a temperature of about 90 degrees.
  The second test (June 2016) tested the propellant at about 40 degrees
At Northrop Grumman in Utah, all 10 EM-1 motor segments have been cast with propellant and several are completely painted, finished and are awaiting shipment to Kennedy Space Center.
Both nozzles are finished at Northrop Grumman facilities in UT.
At Kennedy, the forward and aft skirts are being refurbished and outfitted for flight. TVC has been installed in the left-hand aft skirt and teams recently completed a hot fire test on an aft skirt pathfinder in preparation for final assembly and checkout.
Upper and lower TVC frames have been installed in the right-hand aft skirt.
Booster separation motors is complete on the left-hand aft skirt.
At Marshall, the avionics recently finished qualification testing and will be tested with vehicle avionics later this year.
Booster segments are now being cast for EM-2.
Booster fun facts:
- Each 177 feet or 17 stories tall – taller than the Statue of Liberty
- Each is 12 feet in diameter.
- Each booster burns through 1,385,000 pounds of propellant in two minutes – that’s an average of 5.5 tons of propellant every second.
- Each booster’s thrust is greater than 14 four-engine Boeing 747s at full take-off power.
- During flight, the temperature of the motor chamber gases reach more than 5,000°F – hot enough to boil steel!

## Slide 7: ENGINES
Notes: Images: RS-25 testing at SSC (large), EM-1 engine processing complete (top), development engine with 3-D printed Pogo accumulator (bottom)
Basics: 4 RS-25 engines vs 3 for shuttle, 109% thrust vs 104.5%, new controller and software and nozzle insulation, more than 500,000 lbs thrust each, more than 1 million seconds total ground and flight time.
Program starts with 14 flown engines and 2 new serial number engines built from spares.
STATUS
Program has been hot-fire testing the RS-25 engines since 2015 to ensure the engines can perform under the different SLS pre-launch conditions, higher heating environment, and flight thrust profiles, and also to qualify the new EM-1 controllers. More than 20 tests, more than 10,000 seconds hot fire time as of March 2018.
All 4 EM-1 engines processing complete. All 4 EM-1 controllers and all 4 EM-2 controllers green run tested. Processing of EM-2 engines has started.
Most recent test (2/21/18) took the RS-25 to 113% thrust, the highest ever, and it continued to function nominally (with no issues).
Concurrent work is under way on developing a new more affordable, expendable variant of the RS-25 that costs at least 30 percent less and operates at 111% (521,000 lb) thrust. It incorporates new materials and new manufacturing processes, as well as new technology like 3D printing. First test was late 2017 and again in early 2018 of a 3D printed pogo accumulator on a ground test engine.
New test series to begin in August that will include the pogo accumulator plus a new HIP (Hot Isostatic Pressure) – Bonded main combustion chamber that reduces production time and cost.

## Slide 8: CORE STAGE
Notes: NASA’s Michoud rocket factory that built the Apollo rockets and Space Shuttle tanks is once again a land of giants.
Top Left:
Rocket tanks experience extreme temperatures from cold propellants and friction created as NASA's deep space rocket, the Space Launch System, soars through Earth’s atmosphere to space. An innovative robotic system sprayed thermal protection foam on the tank, shown here, that will hold the cryogenic liquid oxygen propellant for Exploration Mission-1 (EM-1), the first integrated flight of SLS and the Orion spacecraft. Now that its thermal protection system application is complete, engineers recently moved the tank to install sensors and prepare it to be vertically stacked with the intertank and forward skirt. Once stacked, these three pieces will form half of the 212-foot-tall rocket core stage, which has four RS-25 engines that produce two million pounds of thrust.
Bottom left:
Engineers installed intertank SLS structural test hardware into a test stand at Marshall Space Flight Center where testing recently began. The test version of the SLS intertank is being pushed, pulled and bent with millions of pounds of force to ensure it can withstand the forces of launch and ascent. The test hardware is structurally identical to the flight version of the intertank that will connect the core stage's two colossal fuel tanks, serve as the upper-connection point for the two solid rocket boosters and house critical avionics and electronics.
Right:
Liquid Hydrogen tank preparing to be primed before thermal protection system application (foam insulation.)
Hardware Status:
Boeing has completed manufacturing of the engine section and intertank test articles. Engine section testing was completed in early 2018. Intertank testing began summer 2018.
Boeing is finishing the LH and LOX tank test articles for shipment in 2018 and 2019.
Structural work is complete on the engine section, LH tank, intertank, LOX tank and forward skirt for the 212-foot EM-1 core stage, and all are being outfitted with internal hardware and instrumentation for flight.
SITF-Q completed software testing as part of intertank functional tests in 2018, and forward skirt testing was completed summer 2018 to demonstrate avionics system harnesses – first major core stage component ready for flight.
Core Stage Pathfinder built in 2017 and barged to Michoud to begin practice operations. Test moves with core stage GSE set for fall/winter 2018.
B-2 test stand at Stennis Space Center continuing to get ready for core stage green run.
Ground support equipment in testing.
Basics:
The SLS Core Stage will be the tallest rocket stage ever flown. When completed, the Core Stage will be 212 feet tall (64.6 m) and 27.6 ft. (8.4 m) in diameter.
It will weigh 2.3 million pounds when fueled
The liquid hydrogen tank measures more than 130 feet tall, comprises almost two-thirds of the core stage and holds 537,000 gallons of liquid hydrogen cooled to minus 423 degrees Fahrenheit.
The Core Stage is being built by prime contractor Boeing at Michoud Assembly Facility outside New Orleans, LA, using state-of-the-art manufacturing tools, including the world’s largest friction-stir welding tool, the Vertical Assembly Center.

## Slide 9: Commercial Resupply
Develop Commercial Launch Capabilities starting 2008
Deliver supplies to the International Space Station
$3.4 Billion Development and up to $14 Billion for flights
Space X, Orbital Science, and Sierra Nevada
Antares 230
Falcon 9
Atlas 5

## Slide 10: Commercial Crew
Started in 2010
Current Contract Phase $6.8 Billion
Test Flight Planning Dates: SpaceX Demo-1 (uncrewed): March 2, 2019 Boeing Orbital Flight Test (uncrewed): NET April 2019 Boeing Pad Abort Test: NET May 2019 SpaceX In-Flight Abort Test: June 2019 SpaceX Demo-2 (crewed): July 2019 Boeing Crew Flight Test (crewed): NET August 2019

## Slide 11: Space X Demo 1 Completed

## Slide 12: Back To The Moon

## Slide 13: Gateway

## Slide 15: Humans Return to the Moon

## Slide 16: When I started
RL10
Tube Wall Chambers
SSME
10 Years Later
ED Nickel
Compression Brazed
RD-180

## Slide 17: Future is Additive Manufacturing
Channel-cooled Nozzles
Pumps
Combustion Chambers
Injectors
Valves

## Slide 18: Metal AM Processes: Powder Bed Based
Selective Laser Melting (SLM)
  Basic Process: Uses a layer-by-layer powder-bed approach in which the desired component features are sintered and subsequently solidified using a laser. Used widely in combustion devices applications.
  Advantages: Allows for high resolution, fine features, including complex internal designs to be fabricated, such as cooling channels
  Disadvantages: The scale for SLM is limited and does not provide a solution for all components
Electron Beam Melting
  Basic Process: Similar to SLM, but uses an electron beam instead of a laser. Not frequently used in combustion devices applications.
  Advantages: Build is performed under vacuum, which can be useful for reactive materials such as titanium
SLM Fabrication Process Overview.

## Slide 19: AM Thrust Chamber Injectors: Overview
MSFC has developed a total of 10 unique AM injectors between 2012-2018
  Materials: Inco 625, Inco 718, Monel K-500
  Element Types: swirl coax, shear coax, FOF
  Number of Elements: ranging from 6 to 62
  Diameters: ranging from 1.125” to 7.5”
  Hot fire tests performed on 7 of these 10 AM injectors
To date, all MSFC injector designs have been manufactured with a powder-bed process.
Advantages of AM application to injectors:
  Reduction of reducing part count, braze/weld operations, cost, and schedule
  Allows non-conventional manifolding schemes and element designs
Challenges of AM fabrication of injectors:
  Feature size resolution (particularly radial to the build direction)
  Excessive surface roughness
  Removing powder prior to heat treatments (even stress relief) is both necessary and challenging
100lbf LOX/Propane Nanolaunch Injector. Built 2012. Tested 2013.
1.2K LOX/Hydrogen Injector First Tested in June 2013. >7200 seconds hotfire
20K LPS Subscale Injector.
Tested August 2013
Methane 4K Injector with printed manifolds, parametric features. Tested Sept 2015.
LOX/Methane Gas Generator Injector, Tested Summer 2017
35K AMDE Injector with Welded Manifolds, Tested 2015

## Slide 20: Affordable Hardware = More Testing
Pathfinder approach for comparing AM against conventionally machined injectors
  To evaluate structural and performance capabilities of AM in liquid rocket injector applications, two early test programs were initiated at NASA MSFC to directly compare the operating characteristics of conventionally manufactured 20 Klbf LOX/H2 swirl coaxial element injectors to those of similarly designed SLM manufactured injectors.
  Results of hot-fire testing showed characteristic exhaust velocity efficiencies for the two different manufacturing techniques to be within measurement error.
Follow-on efforts included successful hot fire test firings of a range of element types (swirl coaxial, shear coaxial, impinging), propellant combinations (LOX/H2, LOX/CH4, LOX/C3H8), and thrust classes (100 lbf to 35K lbf) to validate AM use in these applications.
Water Flow of the AMDE Injector LOX Circuit; Hot Fire Test of the AMDE Injector.
Four Thrusters with 1200 lbf Shear Coaxial Injectors.
Stable performance of AM Injectors and Efficiency Approaching Traditional (98-99%)

## Slide 21: AM Combustion Chambers: Overview
MSFC has developed over 10 unique AM chambers between 2013-2018
  Materials: Inco 625, Inco 718, GRCop-84, C-18150, Monel K-500
  Propellants: LOX/GH2, LOX/LCH4, LOX/RP-1
  Additive Process: SLM and SLM/DED
  Over 110 starts and 6100+ seconds of hot fire test test.
Chambers have been fabricated using SLM powder bed AM technique, with a few test articles incorporating DED techniques for a bimetallic end product.
21
Total Accumulated Hot-fire Time on Copper-alloy Chambers = >6100 sec
2017
2016
2018
META4
26 sec
1.2K Workhorse
2365 sec
MET1
25 sec
LOX/RP1 Faceplate
25 sec
LCUSP 3.0
45 sec
1.2K Commercial Liners
2500 sec
LCUSP 2.2
102 sec
META4 #2
134+ sec
Feasibility Hardware
2013 – 2015

## Slide 22: AM Combustion Chambers: Methane Engine SLM Chamber Development
Inco 625 Pathfinder: Included pressure and temperature ports along the length of one coolant channel to gather critical data for thermal models.
META4: Full-length, regeneratively cooled GRCop-84 chamber developed for LOX/LCH4 in-space applications; fabricated in two sections and welded together due to SLM build height limitations
META4X4: Second iteration of META4 concept; same thrust level but smaller package with a bolted center interface in place of a welded joint
MET1: Scaled down approach from META4 for smaller in-space missions or for clustering together to provide multiples of 1 Klfb thrust; could be printed in one build with no mid-section interface
Inco 625 Pathfinder
META 4 and META 4X4
MET1

## Slide 23: AM Combustion Chambers: Bimetallic AM Combustion Chambers
The Low Cost Upper Stage-Class Propulsion (LCUSP) project developed SLM fabrication of GRCop84 and DED Electron Beam Free Form Fabrication (EBF3) with Inco 625 manufacturing technologies to produce a combustion chamber at a lower cost and schedule.
  Chamber was designed and fabricated by MSFC, GRC, and LaRC, and hot-fire tested at MSFC.
  LOX/LH2, nominal thrust of 35,000 lbf.
  Demonstrated key manufacturing technologies in a relevant environment, taking the AM LCUSP chamber and the one piece AM cooled nozzle to 100% of design conditions.
LCUSP Unit Between EBF3 Deposition Steps

## Slide 24
Low Cost Upper Stage-Class Propulsion (LCUSP)
Hot Fire Video

## Slide 25: AM Channel-Cooled Nozzles: Overview
NASA is investigating AM methods for targeting increased scale required for current NASA and commercial space program channel wall nozzle applications.
Channel-cooled nozzles present a unique manufacturing challenge due to the scale and complexity required at these scales.
90”
46”
Nozzle Exit Diameters
70”
56”
SSME/RS-25
J-2X, Regen Only
RD-180
RL-10A-4
Current AM Build
Boxes
10x10x10
16x24x19

## Slide 26: Metal AM Processes: Directed Energy Deposition (DED)
Freeform fabrication technique focused on near net shapes as a forging or casting replacement and also near-final geometry fabrication. Can be implemented using powder or wire as additive medium.
Blown Powder Deposition / Hybrid
Melt pool created by laser and off-axis nozzles inject powder into melt pool; installed on gantry or robotic system
Electron Beam Deposition (wire)
An off-axis wire-fed deposition technique using electron beam as energy source; completed in a vacuum.
Laser Wire Deposition
A melt pool is created by a laser and uses an off-axis wire-fed deposition to create freeform shapes, attached to robot system
Arc-Based Deposition (wire)
Pulsed-wire metal inert gas (MIG) welding process creates near net shapes with the deposition heat integral to a robot

## Slide 27: AM Channel-Cooled Nozzles: Development at MSFC
Several AM methods are being investigated for forming the inner liner, producing the coolant channels, and fabricating the manifolds and combinations of channels and manifolds:
Arc-based additive deposition and LWDC integrated into channel wall nozzle for hot-fire.
DED Blown Powder Nozzle and DED Nozzle during feasibility hot-fire test.
Nozzle Component Description | Propellants | Additive Process | Material | Starts | Hot-fire Time (sec)
1,200 lbf LWDC Regen Nozzle, PH034 | LOX/GH2 | LWDC | SS347 | 4 | 160
1,400 lbf LWDC Regen Nozzle, Additive Liner, PH034 | LOX/GH2 | LWDC | Inco 625 | 9 | 880
Integrated Nozzle Film Coolant Ring (INFCR), PF086 | LOX/GH2 | SLM | Inco 625 | 12 | 147
1,200 lbf DED Regen Nozzle, PH034 | LOX/GH2 | DED | Inco 625 | 1 | 15
800 lbf Radiatively-cooled Nozzle, PD020C | LOX/GH2 | SLM | Inco 718 | 1 | 30
 |  |  | TOTAL | 23 | 1232
  Laser Wire Direct Closeout (LWDC)
  Arc-Based Wire Deposition
  Blown Powder Deposition (BPD)
  Selective Laser Melting (SLM)

## Slide 28: Fuel Turbopump
Testing
Pump Unit 1 (D101) – 25 Starts / 245 seconds
Unit 2 Pump (D201) – 31 Starts / 359 seconds
Unit 3 (D301) – Soon to be tested
1st Stage Impeller
Additively Manufactured Ti6-4
Pump Inlet Housing
Additively Manufactured Inconel 718
2nd Stage Impeller
Additively Manufactured Ti6-4
Main Pump Housing
Additively Manufactured Inconel 718
Turbine Exit Guide Vanes
Additively Manufactured Inconel 718
Pump Crossover
Additively Manufactured Inconel 718
Turbine Blisk
Additively Manufactured Inconel 718
Turbine End Damping Seal
Additively Manufactured Inconel 718

## Slide 29: Carbon-Carbon Nozzles

## Slide 30: Carbon-Carbon Nozzles
Nozzle Extension Installed on Thrust Chamber Assembly
  Full assembly at MSFC TS-115.
  View of tantalum backer split ring, graphite split ring, and overall interface region.
  C-C extensions attached to aft flange of combustion chamber using GES Graphite (PFI-25 and PFI-45) split rings.
  Grafoil, grade GTB flexible graphite, 0.060” thick compressed seal at interface between graphite and combustion chamber flange.
  Tantalum split-ring backer plate at aft end of graphite split ring.

## Slide 31: Great Time to Be a Rocket Engineer
Going back to the Moon
Tons of Space Companies – both large and small
Price of manufacturing going down
More room to innovate
More testing

## Slide 32
Contact: Gregg Jones
NASA MSFC
256.544.2225
Gregg.W.Jones@nasa.gov

## Slide 33: Acknowledgements
Paul Gradl
Jessica Wood
Dale Jackson
Chip Kopicz
Sandy Greene
Ian Johnston
Cory Medina
Will Brandsmeier
Kevin Baker
Dwight Goodman
Shawn Skinner
Adam Willis
Bob Witbrodt
Armando Martinez
Matt Cross
Rory Jones
William Till
Robert Hickman
Dave Ellis
Bob Carter
Brad Lerch
Ivan Locci
Laura Evans
Karen Taminger
Darron Rice
Greg Barnett
Majid Babai
Zach Jones
Omar Mireles
Jim Lydon
Brian West
Phillip Steele
James Walker
David Myers
Ron Beshears
Doug Wells
Cynthia Sprader (TS115 Crew)
Ryan Wall (TS116 Crew)
Paul Dumbacher (Test Cell crew)
David Olive
Steve Wofford
Mike Shadoan
Carol Jacobs (retired)
Andy Hardin Keegan Jackson
John Vickers
John Fikes
Jim Turner
Nick Case
Greg Hyatt (DMG)
Sean Sporie (DMG)
Bryant Walker (Keystone)
Albert Hammeke (LTA)
Bhaskar Dutta (DM3D)
Joe Sims (ASRC)
Judy Schneider (UAH)
Moog
Stratasys
Incodema
Aerojet Rocketdyne
Commercial Space Partners
Chris Hill
Derek O’Neal

## Slide 34: Reference
SLS Slides – SLS Ambassadors Briefing Feb 2019 - https://www.nasa.gov/specials/ccp-press-kit/main.html
Commercial Crew - https://www.nasa.gov/specials/ccp-press-kit/main.html
Return to the moon – Human Landing Systems BAA Industry Day Feb 14, 2019
Gateway Slide – Gherstenmaier Cislunar and Gateway https://www.nasa.gov/sites/default/files/.../cislunar-update-gerstenmaier-crusan-v5a.pd...
Additive Manufacturing - Paul Gradl AIAA Additive CD Overview Charts 54th AIAA Joint Propulsion Conference