## Slide 1: Solar Sail Spacecraft Development
By: Danielle Da Costa
Mentors: Matthew Chamberlain and Gregory Dean

## Slide 2: Table of Contents
Deployable Composite Booms (DCB) Part II “Topic 2”
Experiments
  Hinge Deployment Study
  O-Hinge Study
  Moon Hinge Study
  3D Printing onto Solar Sail Membranes
  Deployment Study of Membranes with TPU and SMAs
  Future Work—Peel Testing
Obstacles
Other Work with Solar Sails
Side Projects

## Slide 3: “Topic 2” – Self Deploying Sail Membranes
Project goal:
Research advanced deployable membrane structures for potential future small spacecraft structures.
My goal:
Help create self-deploying sail membranes using 3D printing techniques and Shape Memory Alloys.
Experiment with varying hinge designs and study their deployment after being stowed.

## Slide 4: Hinge Deployment Study
Determine how well hinge deploys after being stowed for 24 hours, 48 hours, 1 week, and 2 weeks.

## Slide 5: Hinge Deployment Study
Hinge 1 opened 24 hours after bending.
Pre-Test
Post-Test

## Slide 6: Hinge Deployment Study Data
180°
103°

## Slide 7
Oval Hinge Deployment Study/ Adhesive Test
Using O-Hinge and Tilted-O-Hinge CAD files from previous intern Amy Caldwell / DLR

## Slide 8: Hinge Study / Adhesive Test
Determine how well TPU and PLA oval and moon hinges deploy after being stowed for 24 hours, 3 days, and 1 week.
TPU Oval Hinge
Thickness 0.7mm
Thin Moon Hinge (1mm)
Thickness 0.7mm
Thick Moon Hinge (2.5mm)
Thickness 0.7mm
PLA Oval Hinge
Thickness 0.5mm
Thick Moon Hinge (2.5mm)
Thickness 0.5mm
Thin Moon Hinge (1mm)
Thickness 0.5mm

## Slide 9: Hinge Study / Adhesive Test
Two different methods used for adhering hinges to sail using DOWSIL 6-1125 CV Sealant.
Glue on
Straights
Glue
Everywhere

## Slide 10: O-Hinge Study (Adhesive on Straights)
Pre-Test
Post-Test
Hinge 1 opened 24 hours after bending.

## Slide 11: O-Hinge Study (Adhesive Everywhere)
Pre-Test
Post-Test
Hinge 1 opened 24 hours after bending.

## Slide 12: O-Hinge Study
Data collected so far…
*Need to find a better way to measure angle.*
95°
180°
Notes: Fix angle on slide and finish filling in data…

## Slide 13: Moon Hinge Deployment Study/ Adhesive Test
Thick hinge data collected so far…

## Slide 14: Moon Hinge Deployment Study/ Adhesive Test
Thin hinge data collected so far…

## Slide 15: 3D Printing onto Solar Sail Membranes
TPU 95A
PLA
Using O-Hinge and Tilted-O-Hinge CAD files from previous intern Amy Caldwell / DLR

## Slide 16: Tips for 3D Printing onto Solar Sail Membranes
Do not
Just apply glue to the membrane—this causes the printer head to catch the membrane and create drag/rips.
Leave big bubbles when gluing the membrane onto the glass base—causes the head to make tears.
Leave edges of membrane unrestricted.

## Slide 17: Tips for 3D Printing onto Solar Sail Membranes
Do
Glue the membrane to the base plate, making sure the membrane is as flat as possible with minimal air bubbles.
Tape the edges of the membrane to the base plate so the printer head does not catch it and cause displacement.

## Slide 18: Directly Printing onto Sail Membrane
Printed on Black Chromium side of sail, opposite to Aluminum side of sail.
*TPU 95A seemed to adhere best with Black Chromium.
*PLA does not adhere to any sail surface.

## Slide 19: Directly Printing onto Sail Membrane
Printed on Aluminum side of sail, opposite to Black Chromium side of sail.
*TPU 95A does not adhere to Aluminum surface well, and was easy to peel off.

## Slide 20: Directly Printing onto Sail Membrane
Printed on Mylar side of sail, opposite to Aluminum side of sail.
*TPU 95A does adhere to Mylar surface well.

## Slide 21: Deployment Study of Membranes with TPU and SMAs
Oval hinge placement on possible fold lines.
Outer border prevents sail from ripping.

## Slide 22: SMA Placement
4 Short SMAs approx. length 30-40 mm.
4 Longer SMAs approx. length 40-50mm.

## Slide 23: TPU and SMA Sail Membrane Folding
Fold #1 (pictured on the right)
Fold #2 (fold lines shown on the right picture)
Fold #3 No specific pattern, but making the sail as small as possible (use wire to keep sail stowed).

## Slide 24: TPU and SMA Sail Membrane Folding
During deployment—SMAs work against Fold #2 and open the sail.
Larger SMAs located along the lower ends of the sail help make the sail flat.
Using DOWSIL adhesive with TPU on membrane causes poor deployment.
Less glue = better deployment.
*Home printer doesn’t adhere TPU to sail well (bed not heated)*

## Slide 25: TPU and SMA Sail Membrane Deployment Day 1

## Slide 26: TPU and SMA Sail Membrane
Deployment duration 135 seconds.

## Slide 27: TPU and SMA Sail Membrane Deployment Day 3

## Slide 28: TPU and SMA Sail Membrane
Deployment duration 115 seconds.

## Slide 29: Peel Testing (Future Work)
Useful for determining how well TPU adheres to sail membrane without the help of adhesive.
Would acquire the force of which TPU peels off or tears the sail.
Experimental setups can range from being basic to complex. Without the proper equipment, a basic setup is best for testing.

## Slide 30: Obstacles
Not much equipment at home limits experimentation.
Contacted SMA expert at GRC, Othmane Benafan, to obtain Shape Memory Alloys. Center closed before we received shipment.
Printer at home, Flash Forge Finder, does not have a bed heating. Prints on sail are not as good.

## Slide 31: CubeSat Solar Sail Survey
The University of Surrey
CubeSail
DeOrbitSail
InflateSail
NASA
Nanosail
ACS3
MMA Design
DragNet
University of Toronto’s Spaceflight Laboratory
CanX-7
The Planetary Society
Lightsail-1
Lightsail-2
Japan Aerospace Exploration Agency
IKAROS

## Slide 32: DLR Gravity Offloading Carts for ACS3 Boom Deployment
Printed cart parts at LaRC Works Makerspace on Prusa 3D Printers.

## Slide 33: Grounding Diagram for NASA Sounding Rocket Operations Center (NSROC)

## Slide 34: Questions?
Ask me anything!

## Slide 35: THANK YOU!
Special Thanks to my mentors Matt and Greg!
Thanks to everyone working at the Gantry and building 1293B!