## Slide 1: Co-cure-ply Materials Development (AERoBOND)
Intern: Charlotte Brandenburg
Mentor: Frank Palmieri
Co-mentor: Tyler Hudson
2020 Spring NIFS Research Symposium

## Slide 2: Challenge
Problem:
Adhesive bonding of composites is unpredictable, and requires redundant fasteners
Fastener installation creates a bottleneck in the airframe assembly line
Co-cure assembly eliminates fasteners, but is limited to simple structures
Approach:
Partially cured panels with offset resin (epoxy-rich) stoichiometry
Panels joined with a layer of hardener-rich resin and fully cured
Project history:
Initial set of 24 test panels completed prior to internship
Now narrowing in on the more successful tests
Joining Layer A
conventional materials (uncured)
Joining Layer A
partially cured
surfaces
Primary Cure
cured laminate
Co-cured structure
Secondary Cure
partially cured interface
Assembly with
Joining Layer B

## Slide 3: Objective
Project Objective:
  Achieve mechanical properties of at least 80% that of conventional composite
Internship Objectives:
  Experimentally validate predicted properties of neat resin from molecular simulation
  Manufacture composite panels for mechanical testing
  Mix large batches of resin for pre-preg production
+
API-60 Part A: 65% tetrafunctional epoxy,
20% trifunctional epoxy, 15% toughener
DDS Hardener
DETDA Hardener

## Slide 4: Approach
Uncured density:
  Resin poured into 25 mL volumetric flasks and weighed
  Remainder of the flask filled with water and weighed again to find resin volume
Cured density: Archimedes method
  Measured dry mass and weight of sample suspended in water
  Density = dry/(dry-suspended)
Tensile modulus: modified ASTM D638
  Rectangular specimen, 37 mm gage length
  5 mm/min strain rate
Bulk resin production
  Resin was heated to 100 °C in an oil bath
  Stirred for 1 hour
  Mixed with solvent on rolling mill for 3 days

## Slide 5: Results
Chart: API-60/DDS Density
| 0.5 | 0.8 | 1 | 1.5 | 2
Uncured | 1.2287 | 1.2283 | 1.2297 | 1.2443 | 1.2413
Cured | 1.2839 | 1.2902 | 1.2922 | 1.3045 | 1.3099
Chart: API-60/DDS Modulus
| 0.5 | 0.8 | 1 | 1.5 | 2
 | 905.225 | 1406.6567 | 1329.818 | 1292.06 | 1425.642
Literature modulus: 3500 MPa
@ R~0.8
Nominal Density: 3.3 g/mL
@ R~0.8

## Slide 6: Analysis/Summary
Density results are consistent with model
  Density increases with increasing R-value
  Similar numeric values
  Validated trend of the model
Modulus measurement needs additional work
  Expect a peak at R=1
  Test at higher strain rates, smaller samples
  Does proprietary toughener contribute to differences from model?
Chart: 
| 0.5 | 0.8 | 1 | 1.5 | 2
Uncured | 1.2287 | 1.2283 | 1.2297 | 1.2443 | 1.2413
Cured | 1.2839 | 1.2902 | 1.2922 | 1.3045 | 1.3099
Model: data points with curve fit
Experiment: data points

## Slide 7: Next Steps/Future Work
Next Steps:
  DMA – modulus at higher strain rates, controlled temperature
  Continue fabricating panels
Other possible future work:
  Same set of measurements on API-60/DETDA resin system

## Slide 8: Acknowledgements
  Jin Ho Kang - guidance
  Hoa Luong - panel fabrication
  Sean Britton - panel fabrication