## Slide 1: 17th International Planetary Probe Workshop (IPPW 2020) Webinar Series
Mars Sample Return and Earth Entry Vehicle
James Corliss, NASA Langley Research Center
and the EEV Team:
Langley Research Center
Ames Research Center
Jet Propulsion Laboratory
Goddard Space Flight Center
June 25, 2020

## Slide 2: Outline
Mars Sample Return Campaign Overview
  Campaign Elements
  Bringing the Samples Back to Earth
Earth Entry Vehicle Overview
  EEV History
  Unique Features and Capabilities
EEV Concept for the Current MSR Campaign
  Current EEV Design Concept
  Key On-Going EEV Design Trades
  Performance Analysis and Testing
Summary

## Slide 3: MSR Campaign Elements
Mars 2020 Sample Caching Rover
Sample acquisition and caching of at least 20 soil and rock samples
Currently in final assembly for launch in 2020
Earth Return Orbiter
Capture/Containment Module
Earth Return Module
Earth Entry Vehicle
Sample Retrieval Lander
Fetch Rover
Orbiting Sample container (OS)
Mars Ascent Vehicle
Mars 2020
Sample Retrieval Lander (SRL)
Earth Return Orbiter (ERO)
Earth Entry Vehicle

## Slide 4: MSR Campaign Architecture*

## Slide 5: Bringing the Samples Back to Earth
Atmospheric Entry
Descent
Orbiter deflection maneuver from Earth-bypass trajectory to nominal Earth-entry trajectory 1-10 days before EEV entry
EEV MM garage opened
EEV is spin-ejected to correct entry attitude
EEV passes through orbital debris field
EEV enters atmosphere (high heat and deceleration)
EEV descends through atmosphere slowing to a terminal velocity of 35-45 m/s
EEV impact lands in soft soil at UTTR (notional landing site)
EEV Release
1
2
3
4
5
6
7
ERO Deflection Maneuver
to Earth Flyby
ERO Deflection Maneuver
to Earth Entry Trajectory
Micro-Meteoroid / Orbital Debris Field
Outside Landing Zone
Landing Zone
Landing/Impact
Notional Landing Site

## Slide 6: Earth Entry Vehicle History
The original Earth Entry Vehicle (EEV) concept was developed at the NASA Langley Research Center in 1998 as an enabling technology for the 03/05 Mars Sample Return Mission (MSR).
Back planetary protection requirements demanded a sample return capsule with unprecedented reliability
Drop Testing of the First EEV Prototype at the Utah Test & Training Range (UTTR) in 2000
Unique Features / Capabilities
Passive ballistic entry and descent
No parachute
Omni-directional impact energy absorber

## Slide 7: EEV Concept for Current MSR Campaign
After
Foam-Composite Crushable Energy Absorber
Accommodates 30-Tube Orbiting Sample Container
Phenolic Impregnated Carbon Ablator (PICA) Aft-Body Thermal Protection System
Composite Cellular Structure Energy Absorber
3-D Woven Heatshield for Extreme entry Environment Technology (HEEET) Forward Thermal Protection System
Composite Rib Stiffened Aeroshell
Current EEV Design Features

## Slide 8: Key On-Going EEV Design Trades
Foam-Composite Crushable Energy Absorber
EEV Outer Mold Lines - Key Criteria
Stardust Sample Return Capsule Launched Feb. 7, 1999
Landed UTTR Jan. 15, 2006
Genesis Sample Return Capsule Launched Aug. 8, 2001
Landed UTTR Sep. 8, 2004
1. Accommodate the Mars sample container and crushable energy absorber
2. Aerodynamically stable (entry to ground)
3. High aerodynamic drag (reduce landing velocity)
EEV Design Concepts for 03/05 MSR Mission
60-Deg Sphere Cone

## Slide 9: Key On-Going EEV Design Trades
Trade Study Between 60-Deg and 45-Deg Sphere Cone EEV Concepts
The objective of this trade is to determine if a 45-degree sphere cone geometry can be accommodated in order to improve EEV subsonic aerodynamic stability.
60-Deg Sphere Cone Free-Flight Test NASA Langley Research Center
Credit: Bruce Owens - NASA LaRC
45-Deg Sphere Cone Free-Flight Test NASA Langley Research Center
Credit: Bruce Owens - NASA LaRC
60-Degree Sphere Cone EEV Concept
45-Degree Sphere Cone EEV Concept

## Slide 10: Key On-Going EEV Design Trades
Aeroshell Structure Trade
The current EEV reference design utilizes a graphite Integral Composite Stiffened Structure (ICoSS)
  Low mass
  Demonstrated technology
  Successful drop tests conducted
Notional Thin Titanium EEV Aeroshell Construction
An alternative thin titanium aeroshell structure is under consideration
  Improve tolerance to micrometeoroid impacts
  Improved thermal capability and robustness if thermal protection system incurs damage

## Slide 11: Performance Analysis and Testing
Micro-meteoroid / Orbital Debris (MM/OD) Testing
MM/OD impacts during EEV free-flight can cause damage to the EEV TPS or underlying aeroshell structure
Impact behavior is characterized with Hyper-velocity Impact Testing at White Sands and hydrocode analysis by NASA Ames
Response of damaged TPS materials and aeroshell structure characterized through arc jet testing and thermal analysis
Hypervelocity Impact Testing of HEEET Thermal Protection System

## Slide 12: Performance Analysis and Testing
TPS Arc Jet Testing
Pristine and simulated MM/OD-damaged coupons
Tested in the NASA Ames Research Center Interaction Heating Facility (IHF 360)
Validate TPS response models and characterize MM/OD damage progression through EEV entry heat pulse
PICA and HEEET exhibited graceful hole growth with no catastrophic failure under the conditions tested
Pristine PICA (Pretest)
Damaged PICA (Pretest)
Pristine HEEET (Pretest)
Damaged HEEET (Pretest)

## Slide 13: Performance Analysis and Testing
Nine Drop Tests Conducted at UTTR in November 2019 have Provided Confidence in the Soil Models being used to Predict Landing Loads

## Slide 14: Performance Analysis and Testing
Nominal LS-DYNA™ Soil Landing Simulations
Credit: Greg Vassilakos, Langley Research Center
Off-Nominal LS-DYNA™ Hard Surface Landing Simulations
Credit: Aaron Siddens, Jet Propulsion Laboratory
0°
7.5°
15°
22.5°
For nominal landings the soil absorbs the EEV kinetic energy and the impacts loads are attenuated to <1,100 g at the sample container to maintain science integrity.
For off-nominal landings onto a hard surface the EEV energy absorber limits loads to <3,000 g at the sample container to maintain back planetary protection.
EEV Landing Simulation into UTTR Great Salt Lake Desert Playa Soil

## Slide 15: Summary
Summary
  EEV design and development is continuing as planned to support the MSR Campaign schedule
Near-term Next Steps
  Continued subsonic and transonic aerodynamic testing of 60-deg and 45-deg sphere cone EEV geometries to support trade study
  Complete the composite / titanium aeroshell structure trade study
  Second series of UTTR drop tests
  MSR Campaign Concept Review in August 2020
Longer-term Plans
  Build an EEV manufacturing demonstration unit in FY21