## Slide 1
Bryson Clifford
Mentors: Dr. Yi Lin & Dr. John Connell
2020 Summer NIFS Research Symposium
Lightweight Regenerable CO2-to-Power Conversion (RECOP) System for Safer Manned Missions

## Slide 2: Challenge
2
  NASA 2020 Technology Taxonomy: TX06 Human Health, Life Support and Habitation Systems
  “Long-term, maintenance-free reliability to maintain ppCO2 below 2 mmHg without significant impacts to resource requirements, such as power, and adsorber size and integration with CO2 reduction equipment.”
International Space Station
xEMU Suits
ECLSS
PLSS

## Slide 3: Challenge
Environmental Control & Life Support System (ECLSS)
  CO2 removal
  Temperature & humidity control
  Waste management
  Urine recovery
Portable Life Support System (PLSS)
  “MetOx” canisters (since 1998)
  Rapid Cycle Amine (RCA) swing-bed technology (testing from 2006-present for xEMU)
Dimensions: 13.46” x 9.78” x 3.42”
International Space Station (ISS)
Space Suit (for xEMU)

## Slide 4: Project Objective
Holey graphene (hG)
(NASA patented advanced material)
Air Cathode (compressed hG + wire mesh current collector)
Regenerable CO2-to-Power (RECOP) Project
Aim to selectively remove CO2 from the air and and electrochemically generate power with reversible battery chemistry.
Li-CO2 coin cell battery
Battery assembly

## Slide 5: Fall 2019 Objective
Objectives: (a) system analysis on target application and (b) collect initial Li-CO2 battery data.
(Theoretical) Values | Space Suit (per EVA*) | ISS (per day*)
CO2 Generated (kg) | 0.700 | 22.950
Total Li Required (kg) | 0.146 | 4.830
Power Generated (W) | 199 | 2,160
Specific Energy (Wh/kg) | 2,016 (based on Li2CO3) | 
* per day & per EVA notation does not apply to the amount of Li required for each application
70 kWh Tesla battery uses 63 kg of Lithium Cobalt Oxide LiCoO2: ~ 12 kg Li needed
https://www.quora.com/How-much-lithium-in-kg-is-used-in-an-electric-car

## Slide 6: Spring 2020 Objective
Objective: Quantify and characterize the consumption and release of CO2 during discharge and charge of Li-CO2 batteries, respectively.
Metal vacuum chamber
Plastic purge chamber
CO2
O2
Pure O2 or CO2 or mixed gas compositions
Hiden Analytical gas analyzer

## Slide 7: Summer 2020 (Virtual) Objective
Objectives: (a) initial drop-in replacement design of RECOP for target applications, (b) Li-CO2 battery review article: Current Progress toward “Mars Air Batteries”, (c) support data processing and graph automation for experimental battery tests.
ICES-2018-54 “Methodology for Extravehicular Activity (EVA) Technology Identification, Prioritization, and Maturation”
CAMRAS = CO2 And Moisture Removal Amine Swingbed

## Slide 8: Results: Objective (a)
Aim to draw direct comparison between:
  RECOP and battery & RCA (xPLSS)
  RECOP and CAMRAS (ISS)
Assess feasibility of RECOP as a dual drop-in replacement (CO2 scrubber and power supply).
  i.e. weight, active material mass, volume, power, voltage, etc.
“Exploration Portable Life Support System (xPLSS)”, EVA Technology Workshop 2017, Colin Campbell, NASA\EC.
Rapid Cycle Amine Swingbed
Battery Packs

## Slide 9: Results: Objective (b)
Aim to compile a comprehensive Li-CO2 summary, including:
  History
  Mechanism (discharge, charge, etc.)
  Electrolyte
  Air cathode (carbon, carbon-free, catalyst types – metal, metal-free, hybrid)
  Flexible battery application
  Influence of gas composition
Search criteria (present-2017):
  Li-CO2
  Lithium-CO2
  Lithium-carbon dioxide
  Li-carbon dioxide
90+ papers found, 50+ cited
Current Progress toward “Mars Air Batteries”

## Slide 10: Results: Objective (c)
Aim to automate as much data processing as possible:
  Discharge graphs
  Cycle graphs
  Able to sort and handle various exported report types

## Slide 11: Results: Objective (c)
Improve efficiency and ease of data evaluation for all parties.
Macro pros:
  Script can be used multiple times on same excel file
  Graphs can be adjusted/edited post processing
  Graph and data are sourced linked
Cycle graph sample:
Discharge graph sample:

## Slide 12: Summary & Future Work
Excel macro tips:
Drop-in RECOP design:
Continuous updates of xPLSS and CAMRAS specs for accurate theoretical design of RECOP.
RECOP testing under same trace contamination conditions as xEMU and ISS.
Continued (in-person) testing of hG-based Li-CO2 batteries.
Stackoverflow.com
Automateexcel.com
Manually record macros to see code

## Slide 13: Acknowledgements
Colin Campbell (PLSS Team Lead)
Samuel Russell (PLSS Battery Expert)
Joel Alexa (vacuum chamber modifications)
April Rains, Brandon Walker, Christian Plaza-Rivera, and Liz Barrios (virtual lab mates!)
Universities Space Research Association (USRA)
NIFS Program Coordinators
AMPB Branch