## Slide 1: Delamination Depth Imaging for Quasi-static and Fatigue Load Testing Using Passive Thermography Joseph N. Zalameda and William P. Winfree NASA Langley Research Center Hampton, VA 23681
QNDE Virtual Conference August 25-26, 2020

## Slide 2: Outline
Introduction
Passive Thermography
  Single Stringer Panel Quasi-static Loading
    Imaging for Damage Growth with Ultrasonic and X-ray CT Comparisons
  Single Stringer Panel Fatigue (Cyclic) Loading
    Imaging for Damage Growth
Reduction of Thermal Data for Damage Depth
  Model Fit to the Thermal Data (Fatigue and Quasi-static Loading)
Conclusions

## Slide 3: Single Stringer Panel Quasi-static Loading
Skin is 12 plies (0.22 cm thick), stiffener flange is woven composite 12 plies (0.24 cm thick), camera is synchronized to loading, 640 x 512 cooled InSb sensor, 25 mm Ge optics, and load is acquired for each frame, frame rate of camera is 80 -180Hz, applied load to over 1,000 pounds typically over 15 – 25 minutes.
IR Camera
Single Stringer Panel

## Slide 4: Single Stringer Panel Quasi-static Loading Thermal Responses
7.6 cm
Before Failure
Next Image:
Elapsed Time = 0.056 seconds
Ultrasonic Inspection
7.6 cm
Time (Seconds)
Temperature (Counts)
Instantaneous Heating
Single Pixel Plot
Instantaneous Heating Image

## Slide 5: 1-Dimensional Series Solution for a Planar Heat Source and Thermoelastic Heat Source
Heat Source
from Damage
at depth = l
T (t)
depth = p
Stiffener Flange
Skin
Heat Flux
Infrared Camera
Thickness = L
Winfree, W. P., Zalameda, J. N., and Michael R. Horne, “Simulations of Thermal Signatures of Damage Measured during Quasi-Static Loading of a Single Stringer Panel”, AIP Conference Proceedings 2102, 120007 (2019); https://doi.org/10.1063/1.5099849, Published Online: 08 May 2019.
Notes: The transient heating can be modeled with a simple 1-d thermal model

## Slide 6: Model Fit to Data and Imaging of Damage Depth
Time (Seconds)
Temperature (Counts)
Single Pixel Plot with Model Fit
Data:
Model:
2.5 cm
Position (pixels)
Thickness (cm)
Line Plot
Thermal Thickness Image
0.0 cm
0.4 cm
Position (pixels)
X-ray CT Cross Section Slice
0.24 cm Depth
Skin Side
Stiffener Flange Side
0.29 cm Depth
Crack at Multiple Interfaces
Center of Crack
Notes: The transient heating can be modeled with a simple 1-d thermal model

## Slide 7: Single Stringer Panel with Fatigue Loading
Skin is 12 plies (0.22 cm thick), stiffener flange is woven composite 12 plies (0.24 cm thick), frequency of loading = 2 Hz, and maximum compressive load is -25,000 pounds, camera is synchronized to loading, 640 x 512 cooled InSb sensor, 25 mm Ge optics, and load is acquired for each frame.

## Slide 8: Data Processing for Rapid Growth Damage Response (Single Stringer)
Frequency of loading = 2 Hz. Y[k] is the averaged thermal image, x[k + j] is the raw acquired thermal images (80 Hz), j is the acquired image number, k is the averaged image number, i is the processed image number, N = 40 is the number of boxcar averages, j is the acquired image number, delay = 25 is the offset subtracted averaged image.
Parameter for processing behaves as a simple notch filter.
Delay is sufficient to capture transient thermal response 12.5 seconds or less.
Notes: Non periodic processing, is same but use 40 averaged images to filter out the periodic response (behaves as a simple notch filter), any signal at 2 Hz and its harmonics are removed, use longer delay subtraction of 25 averaged images.

## Slide 9: Comparison of Periodic to Rapid Growth Thermal Responses with Model Fit Results
Time (Seconds)
Temperature (Counts)
Instantaneous Heating
Averaged Pixels Plot
4.1 cm
Transient
Heating
Notes: Single stringer panel, left is periodic response dominated by the TE heating, right is the non-periodic response with the 2 hz TE heating filtered out., see this rapid growth heating at 422.5 seconds and it stays for over 10 seconds.

## Slide 10: Conclusions
Passive thermography has been shown to be an effective real time NDE technique for composite panels during quasi-static and fatigue loading.
Using notch filtering, the periodic response was removed and the non-periodic (rapid growth) thermal response was captured.
Rapid growth damage depth is determined using both the instantaneous and the transient thermal responses to reduced the thermal data to a defect depth image using the recently developed model.
Notes: With passive thermography we can detect the location, size and depth of the rapid growth damage