## Slide 2: Stitched Composites with Three-Dimensional Stitch Paths
Andrew E. Lovejoy
Research Aerospace Engineer,
Structural Mechanics and Concepts Branch,
NASA Langley Research Center

## Slide 3: Authors
Andrew E. Lovejoy and Dawn C. Jegley
Structural Mechanics and Concepts Branch
NASA Langley Research Center

## Slide 4: Outline
Introduction
Integrated Structural Assembly of Advanced Composites (ISAAC) Facility
  Stitching Heads
Stitching Path Development
  Initial Stitching Path Definition
  Three-Dimensional Path Definition Process
  Example Stitched Paths
Concluding Remarks

## Slide 5: Introduction
Composite materials commonly used in aerospace structures
Methods developed to improve through-the-thickness strength and reduce delamination and impact damage
  Matrix augmentation (toughening)
    Rubber or nanoparticle toughening and carbon nanotube treatments
  Architecture augmentation
    Stitching, tufting, z-pinning, three-dimensional weaving/braiding, and needling

## Slide 6: Introduction (cont.)
NASA conducted two main stitching projects since 1990s
  Advanced Composite Technology (ACT)
  Environmentally Responsible Aviation (ERA)
Stitched graphite-epoxy material identified with potential for reducing structural weight and cost
  Commercial aircraft
  Launch vehicle dry structure
  Stiffened conformal pressure vessels
  Wind tunnel blades such as National Transonic Facility (NTF)

## Slide 7: NTF Wind Tunnel Blade
Airfoil
Root: Pinned to
wind tunnel hub
Airfoil
Platform
Fairing
Root
(Hidden)
27 in.

## Slide 8: ISAAC Facility
Rail
Rotator
Robot arm
Automated Fiber
Placement (AFP) Head
Coupon
table

## Slide 9: Stitching Heads
Vectran thread
Throat
region
Looper
Needle
End
effector
Head plate
Vectran thread
Insertion needle
Catcher
needle
End
effector
Head plate
Slider mechanism
Double-sided
Single-sided

## Slide 10: Stitching Pattern
Needle side
Tool side
Needle side
Looper side
Double-sided
Single-sided

## Slide 11: Stitching Path Development
Initial Stitching Path Definition
Three-Dimensional Path Definition Process
Example Stitched Paths

## Slide 12: Initial Stitching Path Definition
Duplicate stitching process used during the ERA project
  Straight paths in space
  Each path had to be “trained” by the operator
  Defined head path parameters for computer numeric control
    Tool point
    Stitching tool surface
“Curved” paths stitched (cylindrical panel)
  Short straight paths in direction of curvature (circumferential)
  Tool-side stitch length dependent on where on stitch path
    Longer paths, smaller radius of curvature can affect stitch formation

## Slide 13: Stitching Head Path Parameters
Tool point
Looper
Needle
End effector table
Presser foot
Catcher needle
(90-degree)
Insertion needle
(45-degree)
Stitching tool surface
Presser foot surface
Tool point
x
z
Double-sided
Single-sided

## Slide 14: Stitching Paths for Curved Panel
Stringer stitch terminations adjacent to frame
Frame stitch terminations adjacent to stringer
Frame
Stringers
7.8 in.
5.4 in.

## Slide 15: Path Definition Process
Double-sided less affected by path curvature
  Considered subset of the single-sided motion (single needle)
Single-sided used to define stitching path
  Needles ”walk” within presser foot during stitch formation
Needle Insertion
During Stitch
Needle Retraction

## Slide 16: Effects of Path Curvature (Head Rotations)
Rotation about x-axis
  Small side loads
    Increase with thickness, reduction in curvature
Rotation about y-axis
  Can affect stitch formation due to change in length
  between needle points at tool surface
  Small side loads
Rotation about z-axis
  Large side loads on insertion needle
  Most severe problems for stitching process
x
z
y

## Slide 17: Stitch Patterns, Rotation About Z-Axis
Convex path (shown)
  Insertion needle stitch length longer than catcher needle
Concave path
  Insertion needle stitch length shorter than catcher needle
Stitch 1,
catcher needle
Stitch 2,
catcher needle
Stitch 1,
insertion needle
Stitch 2,
insertion needle
Stitching path
x
y

## Slide 18: Curved Path Programming

## Slide 19: Example Paths
Segment 1
Segment 2
Slope discontinuity
Weights holding preform in place
Weights holding preform in place
Closed path
Double-curvature path

## Slide 20: Closed Path: Straight and Curved Segments

## Slide 21: Double-Curvature Path

## Slide 22: Concluding Remarks
Initial stitching path capability was straight paths
  Cannot be used for long paths on curved surfaces
    Side forces exerted on insertion needle (particularly z-axis rotation)
    Can also result in improper stitch formation
Process to define/program three-dimensional paths has been developed by decoupling translation and rotation
  Opens up the design space
    Closed curved paths (such as round access holes)
    Double-curvature paths (such as wind tunnel blades)
  Future: Logic to define when to decouple being developed