## Slide 1: Layered Electrode Architectures Enabled by Holey Graphene Hosts
Yi Lin1 and John W. Connell2
1National Institute of Aerospace, Hampton, VA 23666
2Advanced Materials & Processing Branch, NASA Langley Research Center, Hampton, VA, 23681
PRiME 2020 (Virtual)
10/06/2020
Abstract # A02-0334

## Slide 2: Batteries for Electric Aircraft
Advanced Materials and Processing Branch NASA Langley Research Center
Solid-state Li-S batteries hold the best chance to meet NASA goal for electric aircraft batteries.
500
300
200
Pack
Specific Energy
(Wh/kg)
Li-Ion SOA
400
100
350
Expansion of Electrified Aircraft Market
Current R&D Focus for Automotive Sector
Tesla Model S
NASA Goal
Initial UAM Introduction with Limited Capability
Desired Mission Capability for eVTOL and Market Expansion to Regional Aircraft
Uber UAM Goal

## Slide 3: Holey Graphene
Advanced Materials and Processing Branch NASA Langley Research Center

## Slide 4: Holey Graphene
Advanced Materials and Processing Branch NASA Langley Research Center
In-plane porosity: Improves ion transport path, reduces tortuosity
Accessible surface area: Improves gravimetric capacitance
Volume reduction: Mitigates need to create large pores/spacing
Hole-edge functionalities: Improves mesoscale wetting
Electrical Conductivity: Retains graphitic crystallinity
Intact Graphene
Holey Graphene

## Slide 5
Inherit nearly all properties of graphene
Facile through-plane ion transport
Enhanced edge functionalization
B,N-codoped hG
Angew. Chem. Int. Ed. 2017, 56, 6970.
Li-CO2 Batteries
Liming Dai
(CWRU)
Advanced Materials and Processing Branch NASA Langley Research Center
Holey Graphene: An Advanced Electrode Material
Intact Graphene
Holey Graphene
ACS Nano 2014, 8, 8255.
Supercapacitors
As-Prepared hG
Liangbing Hu
(U Maryland)
Li-Ion Battery (Anode)
Small 2015, 11, 6179.
N-doped hG
Liming Dai
(CWRU)
Li-O2 Batteries
N-doped hG
ACS Energy Lett 2016, 1, 260.
Liming Dai
(CWRU)
Carbon Dot-Supported on hG
Adv. Func. Mater. 2018, 28, 1804630
Single Fe Atom Catalysts Supported on hG
Adv. Mater. 2020, 32, 1907436.

## Slide 6
Advanced Materials and Processing Branch NASA Langley Research Center
A New Narrative: Holey Graphene is Dry Compressible
Holey Graphene
Powder
Holey Graphene
Monolithic Architectures
ACS Nano 2017, 11, 3189. (In collaboration with Prof. Liangbing Hu)

## Slide 7
Advanced Materials and Processing Branch NASA Langley Research Center
A Game Changer in Electrode Preparation
hG
N-doped hG
Monolithic Electrodes
“Sandwich”
Simple Mix
“Open-Face
Sandwich”
“Big Mac”
Composite Electrodes
Matrix (compressible): Holey graphene
Filler (non-compressible): Active or auxiliary components (e.g. catalysts, active electrode materials, other additives)
Solvent-free
Binder-free
Completion within minutes
Scalable: High mass loading
Enable complex architectures
Li Ion Batteries (Cathode)
ACS Appl. Energy Mater. 2019, 2, 2990-2997.

## Slide 8
Advanced Materials and Processing Branch NASA Langley Research Center
A Game Changer in Electrode Preparation
Li-S Batteries
Batteries & Supercaps 2019, 2, 774.
ACS Appl. Energy Mater. 2019, 2, 2990.
Li-Ion Batteries
LFP
NCM
Submitted for publication.
Supercapacitors
ACS Appl. Mater. Interfaces 2016, 8, 29478.
Versatile Applications
Nano Lett. 2017, 17, 3252.
Li-O2 Batteries

## Slide 9: Interest in Li-S, Se, and SeSx Battery Chemistry
Advanced Materials and Processing Branch NASA Langley Research Center
Power
Energy
8
O
Oxygen
15.9994
16
S
Sulfur
32.066
34
Se
Selenium
78.96
VI A
 | Conductivity (S/cm) | Specific Capacity (mAh/g)
S | 5 x 10-30 | 1675
Se | 10-5 | 675
Li-S (sulfur) and Li-Se (selenium) pairs are similar in battery chemistry
S/Se compounds are intermediate species between S and Se
S/Se hybrid chemistry may be used to achieve both energy (S) and power (Se)

## Slide 10: Dry Pressed S Cathodes Enabled by hG
Advanced Materials and Processing Branch NASA Langley Research Center
Facile solvent-free preparation of high S content, high mass loading S cathodes.
Batteries & Supercaps, 2019, 2, 774-783.

## Slide 11: High Performance S/hG Composite Cathodes
Advanced Materials and Processing Branch NASA Langley Research Center
Batteries & Supercaps, 2019, 2, 774-783.
Dry-pressed S/hG composite cathodes exhibited ultrahigh areal and volumetric performance with high S utilization efficiency.
85% S utilization

## Slide 12: Layered Cathode Architecture Improves Performance
Advanced Materials and Processing Branch NASA Langley Research Center
Al current collector
hG ”Interlayer”
S/hG Composite
Batteries & Supercaps, 2019, 2, 774-783.
Lightweight conductive interlayer (~10 wt%)
Improves current collector– cathode contact
  Electrochemistry kinetics
  Overpotential

## Slide 13: Composite, Layered, and Sandwich Electrodes
Advanced Materials and Processing Branch NASA Langley Research Center
High active material content (up to 90 wt%)
High mass loading: high areal capacity
Excellent current collector– cathode contact
Extremely facile: single-step, no mixing needed
Widely applicable: S, Se, SexSy, Li2S

## Slide 14: Starting Powders and Sandwich Discs
Advanced Materials and Processing Branch NASA Langley Research Center
Se vs. hG Powder
hG/Se/hG Sandwich Electrode
ACS Appl. Energy Mater. 2020, 3, 6374

## Slide 15: Sandwich Electrode Performance
Advanced Materials and Processing Branch NASA Langley Research Center
d
High mass loading: 17.3 mg/cm2
High Se content: 75 wt%
High Se utilization: 88%
High specific capacity: 598 mAh/gSe
High areal capacity: 10.4 mAh/cm2
Excellent rate performance: > 5 mA/cm2
Excellent reversibility
ACS Appl. Energy Mater. 2020, 3, 6374

## Slide 16: Composite vs. Sandwich Electrode
Advanced Materials and Processing Branch NASA Langley Research Center
Sandwich vs. (layered) composite architectures:
Similar performance: overpotential, utilization
Extremely facile preparation!

## Slide 17: The Fate of Sandwiched Se
Advanced Materials and Processing Branch NASA Langley Research Center
Discharge
Charge
ACS Appl. Energy Mater. 2020, 3, 6374
As-Prepared
After First Cycle
Electrochemical Redistribution

## Slide 18: Polyselenide Shuttling
Advanced Materials and Processing Branch NASA Langley Research Center
ACS Appl. Energy Mater. 2020, 3, 6374
Li Anode (First Discharge, Cross-section)

## Slide 19: Exploration of Perfluorinated Solvents
Advanced Materials and Processing Branch NASA Langley Research Center
1,1,2,2-tetrafluoroethyl-2,2,3,3-tetrafluoropropyl ether (TTE)
1,2-dimethoxyethane (DME)
1,3-dioxolane (DOL)
Common Electrolyte Solvents

## Slide 20: Exploration of Perfluorinated Solvents
Advanced Materials and Processing Branch NASA Langley Research Center
Fluorinated vs. conventional ether solvents:
Attenuated intermediate shuttling
Higher Columbic efficiency
Better cyclability
Lower rate
ACS Appl. Energy Mater. 2020, 3, 6374

## Slide 21: Electrode Morphology with Perfluorinated Solvent
Advanced Materials and Processing Branch NASA Langley Research Center
Se Cathode (Cross-section) with TTE
Li Anode (>80 cycles, Surface)
ACS Appl. Energy Mater. 2020, 3, 6374

## Slide 22: S and SeS2 Sandwich Cathodes
Advanced Materials and Processing Branch NASA Langley Research Center
ACS Appl. Energy Mater. 2020, 3, 6374
Power
Energy
8
O
Oxygen
15.9994
16
S
Sulfur
32.066
34
Se
Selenium
78.96
VI A

## Slide 23: Layered Air Cathodes for Li-O2 Batteries
Advanced Materials and Processing Branch NASA Langley Research Center
An Ideal Cathode Architecture
Abstract # A02-0489 (10/8/2020)
“Ultrahigh Areal Capacity Holey Graphene Air Cathodes for Li-O2 and Li-CO2 Batteries”

## Slide 24: Summary
Advanced Materials and Processing Branch NASA Langley Research Center
Holey graphene enables extremely facile, binder-free, solvent-free, scalable electrode fabrication via dry-press.
High mass loading and high areal capacity electrodes can be conveniently achieved.
The dry process procedure allows fabrication of layered electrode architectures where raw active material can be directly used (sandwich electrodes).
Sandwich electrodes exhibit excellent performance with electrochemical redistribution of raw materials after first discharge.
The process is widely applicable to various active materials including, but not limited to, S, Se, SeS2.

## Slide 25: Acknowledgements
Advanced Materials and Processing Branch NASA Langley Research Center
Collaborators:
    Prof. Liangbing Hu (U. of Maryland – College Park)
    Prof. Liming Dai (Case Western Reserve University – now at U. New South Wales)
Student Interns:
    Evan Walsh
    Steven Lacey (2018 Ph.D @ UMD)
    Brandon Moitoso
    Francisco Mendez Sosa
    Louisa Greenburg
    Christian Plaza-Rivera
Funding:
  NASA Convergent Aeronautics Solutions (CAS)
  NASA Langley Internal Research and Development (IRAD) Program and Center Innovation Fund (CIF)