## Slide 1: Characterization of Composite Damage using Passive Thermography Joseph N. Zalameda NASA Langley Research Center Hampton, VA 23681
NDT in Aerospace Conference Oct. 8, 2020

## Slide 2: Outline
Introduction
Passive Thermography
  Single Stringer Panel Quasi-static Loading
    Imaging for Damage Growth with Ultrasonic and X-ray CT Comparisons
Reduction of Thermal Data for Damage Depth
  Model Fit to the Thermal Data (Fatigue and Quasi-static Loading)
Single Stringer Panel Fatigue (Cyclic) Loading
    Imaging for Damage Growth
Conclusions

## Slide 3
Passive Thermography vs. Active Thermography
In a general sense both require energy: application or removal to produce temperature differences.
Active thermography implies control of the energy for the inspection (flash, quartz lamp, ultrasonic, microwave, hot air, etc.).
Passive thermography implies no control of the energy, simply observing (environmental heating, moisture detection, structural loading, etc.).

## Slide 4: Introduction: Passive Thermography for Structural Testing
Objectives
Real time inspection for early detection of onset damage and controlled growth of damage up to failure.
In-situ wide area real time inspections on composite structures during load testing using passive thermography.
Implementation of a detailed inspection (ultrasonics or X-ray CT) for through thickness detail.
Payoffs
Early detection and quantitative measurement of damage onset and growth validates test articles and feeds damage prediction models which decreases certification times.
Notes: While testing composite structures – CG with real time NDE, passive thermography lets you know the damage state of the entire structure while loading,. Stop load testing when we see damage growth and do UT or X-ray CT. also PT documents the failure of the structure
This work was done under NASA’s advanced composite project.

## Slide 5: Quasi-Static Load Configuration
Time (Seconds)
Load (Pounds)
Testing is composed of multiple load runs and each last approximately 15 to 25 minutes, acquired thermal data is approximately 60 Gigabytes of data.
Applied Load

## Slide 6: Single Stringer Panel Quasi-static Loading
Skin is 12 plies (0.22 cm thick), stiffener flange is woven composite 12 plies (0.24 cm thick), camera is synchronized to loading, 640 x 512 cooled InSb sensor, 25 mm Ge optics, and load is acquired for each frame, frame rate of camera is 80 -180Hz, applied load to over 1,000 pounds typically over 15 – 25 minutes.
IR Camera
Single Stringer Panel

## Slide 7: Processing of Thermal Data using a Delayed Subtraction
Y[k] is the averaged thermal image, x[k + j] is the raw acquired thermal image (rate = 80 Hz), j is the acquired image number, k is the averaged image number, N is the number of boxcar averages (typically 10), delay is the offset subtracted averaged image (typically 100), and i is the processed image number.

## Slide 8: Thermal Imaging of Damage Formation

## Slide 9: Single Stringer Panel Quasi-static Loading Thermal Responses
7.6 cm
Before Failure
Next Image:
Elapsed Time = 0.056 seconds
Ultrasonic Inspection
7.6 cm
Time (Seconds)
Temperature (Counts)
Instantaneous Heating
Single Pixel Plot
Instantaneous Heating Image

## Slide 10: 1-Dimensional Series Solution for a Planar Heat Source and Thermoelastic Heat Source
Heat Source
from Damage
at depth = l
T (t)
depth = p
Stiffener Flange
Skin
Heat Flux
Infrared Camera
Thickness = L
Winfree, W. P., Zalameda, J. N., and Michael R. Horne, “Simulations of Thermal Signatures of Damage Measured during Quasi-Static Loading of a Single Stringer Panel”, AIP Conference Proceedings 2102, 120007 (2019); https://doi.org/10.1063/1.5099849, Published Online: 08 May 2019.
Notes: The transient heating can be modeled with a simple 1-d thermal model

## Slide 11: Model Fit to Data and Imaging of Damage Depth
Time (Seconds)
Temperature (Counts)
Single Pixel Plot with Model Fit
Data:
Model:
2.5 cm
Position (pixels)
Thickness (cm)
Line Plot
Thermal Thickness Image
0.0 cm
0.4 cm
Position (pixels)
X-ray CT Cross Section Slice
0.24 cm Depth
Skin Side
Stiffener Flange Side
0.29 cm Depth
Crack at Multiple Interfaces
Center of Crack
Notes: The transient heating can be modeled with a simple 1-d thermal model

## Slide 12
Thermal Imaging of Damage Formation: Small Delamination

## Slide 13: Thermal Inspection Results: Small Delamination
Before Failure
Next Image:
Elapsed Time = 0.125 seconds
Ultrasonic Inspection
Time (Seconds)
Temperature (Counts)
Instantaneous Heating
2.5 cm
2.5 cm
Single Pixel Plot
Instantaneous Heating Image

## Slide 14: Thermal Imaging of Damage Depth with Comparison to X-ray CT: Small Delamination
2.5 cm
Thermal Damage Depth Image
Position (pixels)
Thickness (cm)
Line Plot
0.0 cm
0.4 cm
X-ray CT Cross Section Slice
0.2 cm Depth
Skin Side
Skin Side Strain Gauge
Stiffener Flange Side
Center of Crack
Time (Seconds)
Temperature (Counts)
Pixel Plot with Model Fit
Data:
Model:

## Slide 15: Single Stringer Panel with Fatigue Loading
Skin is 12 plies (0.22 cm thick), stiffener flange is woven composite 12 plies (0.24 cm thick), frequency of loading = 2 Hz, and maximum compressive load is -25,000 pounds, camera is synchronized to loading, 640 x 512 cooled InSb sensor, 25 mm Ge optics, and load is acquired for each frame.

## Slide 16: Data Processing for Rapid Growth Damage Response (Single Stringer)
Frequency of loading = 2 Hz. Y[k] is the averaged thermal image, x[k + j] is the raw acquired thermal images (80 Hz), j is the acquired image number, k is the averaged image number, i is the processed image number, N = 40 is the number of boxcar averages, j is the acquired image number, delay = 25 is the offset subtracted averaged image.
Parameter for processing behaves as a simple notch filter.
Delay is sufficient to capture transient thermal response 12.5 seconds or less.
Notes: Non periodic processing, is same but use 40 averaged images to filter out the periodic response (behaves as a simple notch filter), any signal at 2 Hz and its harmonics are removed, use longer delay subtraction of 25 averaged images.

## Slide 17: Comparison of Periodic to Rapid Growth Thermal Responses with Model Fit Results
Time (Seconds)
Temperature (Counts)
Instantaneous Heating
Averaged Pixels Plot
4.1 cm
Transient
Heating
Notes: Single stringer panel, left is periodic response dominated by the TE heating, right is the non-periodic response with the 2 hz TE heating filtered out., see this rapid growth heating at 422.5 seconds and it stays for over 10 seconds.

## Slide 18: Conclusions
Passive thermography has been shown to be an effective real time NDE technique for composite panels during quasi-static and fatigue loading.
A recently developed model was used to process the passive thermal data to obtain damage depth of rapid growth damage using the both the instantaneous and the transient thermal responses. This was demonstrated for quasi-static loading.
Using notch filtering, the periodic response was removed and the non-periodic (rapid growth) thermal response was captured and thus allowing the damage depth imaging.
Notes: With passive thermography we can detect the location, size and depth of the rapid growth damage