## Slide 1: Realistic Thermographic Simulation of Impact Damage with Quadrupole Method
William P. Winfree, Joseph N. Zalameda and Patricia A. Howell NASA Langley Research Center Hampton, VA 23681
2020 NDT in Aerospace Virtual Conference: October 6 – 8, 2020

## Slide 2: Overview
Simulations assist in developing an understanding of the limitations of the technique and enable quantitative characterization of subsurface flaws
Quadrupole Method is used for rapid simulation of thermographic inspection of composites
This presentation:
  Examines the sensitivity of simulation to in-plane diffusivity and delamination contact resistance
  Based on the computed tomography characterization of impact damage in a composite, simulates the thermal response
  Compares the simulation results to experimental measurements
  Iterates on contact resistance to improve agreement between simulation and experiment

## Slide 3: Quadrupole Method
Solves Laplace transform of heat equation, then inverts to temporal solution
Used extensively for 1-D layered systems
Extended to 3-D in particular for composites
  Previous methodology developed for single delamination at an interface between two layers
    Batsale, J., Maillet, D., and Degiovanni, A., International Journal of Heat and Mass Transfer 37 (1), 111, (1994).
    Bendada, A., Modelling and Simulation in Materials Science and. Engineering 10 (6), 673 (2002).
    Bendada, A., Erchiqui, F., and Lamontagne, M Inverse Problems 21 (3), 85 (2005)
    Winfree,W., Zalameda, J., Howell,P., and Cramer, E., Proc. SPIE 9861, Thermosense: Thermal Infrared Applications XXXVIII, 98610N (11 May 2016);
  Methodology developed for multiple delaminations at multiple interfaces between layers and plates that are not aligned
    Winfree, W., Zalameda, J. and Howell, P., Proc. SPIE 11004, Thermosense: Thermal Infrared Applications XLI, 110040F (2 May 2019)
    Winfree, W., Zalameda, J. and Howell, P., Thermosense: Thermal Infrared Applications XLII; 114090K (2020)

## Slide 4: One-Dimensional Model of Two Layer System with Air Gap
Layer Thermal Conductivity(K), Thermal Diffusivity(k), Thickness(d1)
Layer Thermal Conductivity(K), Thermal Diffusivity(k), Thickness(d2)
Thin Air Gap
dgap Thickness
Kair Thermal Conductivity of Air
For thin air gap, the thermal properties of the air gap can be represented by a contact resistance R
R=/Kair
In equations, R is always multiplied by thermal conductivity of layer, such that relevant term is K dgap/Kair

## Slide 5: Gap Thickness Influence on One-Dimensional Thermal Response
Two different representation of the same data
Normalized by dividing by the combined heat capacities of the two layer and the input flux. For long times approaches 1 if contact resistance is less than infinity
Normalized by dividing by the response of a semi-infinite layer with the same thermal properties and the input flux. Thermal response is 1 for early times.
First layers are 0.02 cm and 0.05 cm thick
Second layers are 0.18 cm and 0.15 cm thick

## Slide 6: Gap Width Influence on Three-Dimensional Thermal Response
First layer is 0.02 cm and thick Second layer is 0.18 cm thick
Normalized by dividing by the response of a semi-infinite layer with the same thermal properties and the input flux.
In-plane and surface normal diffusivities are both 0.005 cm2/sec
0.05 sec
0.20 sec
0.10 sec
0.40 sec
20 mm
Air Gaps Widths
40 mm
10 mm
30 mm
Diameter of circular air gaps 1 cm
Block 4 x 4 x 0.2 cm
Aspect ratio (1,1,5)
Same scaling for all surface plots

## Slide 7: Gap Width Influence on Three-Dimensional Thermal Response
First layer is 0.02 cm and thick Second layer is 0.18 cm thick
Normalized by dividing by the response of a semi-infinite layer with the same thermal properties and the input flux.
In-plane diffusivity is 0.025 cm2/sec and surface normal diffusivity is 0.005 cm2/sec
0.05 sec
0.20 sec
0.10 sec
0.40 sec
20 mm
Air Gaps Widths
40 mm
10 mm
30 mm
Diameter of circular air gaps 1 cm
Block 4 x 4 x 0.2 cm
Aspect ratio (1,1,5)
Same scaling for all surface plots

## Slide 8: Temperature Profiles Along Diagonals of Three-Dimensional Thermal Responses
10 mm
40 mm
20 mm
30 mm
Over the 10 mm air gap the thermal contrast decreases between 0.2 sec and 0.4 sec
Over the 20 mm air gap the thermal contrast does not significantly increase between 0.2 sec and 0.4 sec

## Slide 9: Three-Dimensional Thermal Response for Wedge Gap
First layer is 0.02 cm thick. Second layer is 0.18 cm thick
Surface normal diffusivity is 0.005 cm2/sec
0.05 sec
0.05 sec
0.40 sec
0.40 sec
Same scaling for all surface plots
In-plane diffusivity 0.005 cm2/sec
In-plane diffusivity 0.025 cm2/sec
Wedge air gap between first and second layers varies from 0 to 40 mm
Layer 2 cm x 2 cm
Wedge 1 cm x 1 cm

## Slide 10: Temperature Profiles Along Wedge Center
Initial time response does not reflect the shape of the wedge
Later time responses reflect the shape of the wedge
Increasing in-plane diffusivity by a factor of 5 does not dramatically change response

## Slide 11: CT Estimation of Impact Damage Composite
Composite has 18 plies
From CT data, delaminations were present at 13 different depths
Most Depths have two significant delaminations
Impact Damage has the typical “petal” appearance
Volume 3.2 cm by 3.2 cm by 0.332 cm
Aspect ration 1:1:8
View from top
Area 3.2 cm by 3.2 cm
Different Color for each depth
First three depths
Red 0.0178 cm
Green 0.0347 cm
Blue 0.0532 cm

## Slide 12: CT Data Through an Impacted Region of the of the Composite
Gap width not the same for all delaminations
Delaminations are not flat
Contrast between delamination and composite indication of gap width
This contrast is used to estimate the gap width of the delamination
0.33 cm

## Slide 13: Gaussian Fit for Calculation of Gap Width
Fit with a constant minus a Gaussian
Amplitude of the Gaussian proportional to the gap width
Point spread of CT system estimated from CT response at edge of composite

## Slide 14: CT Images and Estimated Gap Spacing
Interface 1
Interface 2
Interface 3
Interface 5
Interface 6
All CT images scaled the same
All of the gap spacing scaled from 0 to 0.050 mm
CT image
Gap thickness image

## Slide 15: Quadrupole Simulation of Impacted Composite
Gap spacings map is multiplied by the thermal conductivity of air to provide a contact resistance map at interfaces identified by CT as having a delamination
Largest gap thickness ~ 50 mm
Thermal conductivity composite: 97000 Erg/(cm K sec)
Diffusivity: 0.0044 cm2/sec
Thermal conductivity of air: 2624 Erg/(cm K sec)
Largest Kcomposite R is ~0.18 cm

## Slide 16: Comparison of Flash Thermography Simulation of Impacted Composite and Measured Response
0.1 sec
0.2 sec
0.4 sec
0.8 sec
Areas with thinner gap widths tend to fade faster in measurement than simulation
images 3.2 by 3.2 cm
Measured Response
Simulation Results

## Slide 17: Horizontal Profiles of Experimental Data and Simulation Data
Reasonable agreement early times
Poor agreement at later times
Delamination
0.532 mm
from
surface
Delamination
0.178 cm
from
surface
Quad- Simulation data
Exp – Experimental data

## Slide 18: Vertical Profiles of Experimental Data and Simulation Data
Reasonable agreement early times
Poor agreement at later times
Delamination
0.532 mm from surface
Delamination
0.178 cm
from
surface
Quad- Simulation data
Exp – Experimental data
Delamination
0.178 cm
from
surface

## Slide 19: Horizontal Profiles of Experimental Response and Simulation Results for ½ K R Value Estimated from CT
Delamination
0.532 mm
from
surface
Delamination
0.178 cm
from
surface
Quad- Simulation data
Exp – Experimental data
Much better agreement when KR is ½ the value estimate based on CT measurement and literature values for thermal conductivities

## Slide 20: Vertical Profiles of Experimental Response and Simulation Results for ½ K R Value Estimated from CT
Much better agreement assuming K R is ½ value estimated from CT
Delamination
0.532 mm
from surface
Delamination
0.178 cm
from
surface
Quad- Simulation data
Exp – Experimental data
Delamination
0.178 cm
from
surface

## Slide 21: Comparison of Flash Thermography Simulation When KR Reduced by Factor of Two
0.1 sec
0.2 sec
0.4 sec
0.8 sec
Absolute values are considerably better, however, contrast images are not dramatically different
Measured Response
Simulation Results

## Slide 22: Summary
Small changes in contact resistance result in most significant changes in the contrast
For the thermal properties of interest within the time frame of interest, large changes in in-plane diffusivity don’t significantly change the contrast
When using the K R estimated from CT and literature values for thermal conductivities, comparison of the absolute values of contrast between measurements and simulation is poor, particularly at times greater than 0.2 sec
Using ½ the K R estimated from CT and literature values for thermal conductivities, comparison of the absolute values of contrast between measurements and simulation is reasonable