## Slide 1
Developing a Framework for Using In-Process Monitoring Data to Manage Risk in AM Hardware
Erin L. Lanigan, NASA Marshall Space Flight Center November 18, 2020

## Slide 2: Presenter Bio
Erin Lanigan
Native of Lenexa, Kansas (Kansas City metro)
Bachelor’s Degree in Mechanical Engineering from the University of Kansas
Non-Destructive Evaluation Team at NASA Marshall Space Flight Center since Oct. 2017
Pursuing Master’s in Mechanical Engineering at the University of Alabama in Huntsville
Focus Areas:
Infrared flash thermography
NDE of additive manufacturing
In-situ process monitoring
AM certification
In-space manufacturing

## Slide 3: Use of In-Situ Monitoring for Managing Risk
NASA Objectives & Research Portfolio
Outlook on the Use of the Technology
Qualification Considerations

## Slide 4: Use Case - Inspectability Challenges
RS-25 Pogo Accumulator Z-Baffle
Over 100 Welds Eliminated
Nearly 35% Cost Reduction
28-Element Inconel® 625 Fuel Injector
Reduced 163 parts to 2
Schedule reduced from 1 year to 4 months
70% cost reduction
Injector Assembly
MSFC Project with Army Air and Missile Defense (AMD)
Cryogenic Heat Exchanger-Injector-Condenser Demo
NASA is most interested in in-situ monitoring for high criticality, complex parts that are difficult to inspect using traditional NDE.

## Slide 5: Use Case – In-Space Manufacturing
Another pressing need is the certification of parts manufactured in the space environment, where traditional nondestructive evaluation may not be available.
Bound Metal Deposition
TechShot, Inc. FabLab
Made in Space, Inc. Vulcan
Ground-based prototype system
Wire-Arc Additive Manufacturing

## Slide 6: Investigating In-Situ Monitoring Technologies
Small Business Innovation Research Grants
Monitoring Systems
ASTM Working Group WK73289
“Standard Guide for In-Situ Monitoring of Metal Additive Manufactured Parts”
ASTM AM Center of Excellence
Surveyed the landscape of in-situ monitoring technologies
Interviewed subject matter experts
NASA Marshall Space Flight Center | Automated defect detection
AM seeded defect creation | Correlating NDE and metallography data
EOS | Optical Tomography
& Meltpool Monitoring
ARCTOS | Thermal Tomography & High-Speed Spatter Imaging
Phase III: Made in Space, Inc. | Wire Arc AM Machine Vision
Phase II: Intelligent Optical Systems | L-PBF In-Line Laser Ultrasonics
Phase I: Relativity Space Inc. | Wire-Feed AM Real-Time Defect Detection

## Slide 7: Variety of In-Situ Monitoring Technologies
Ultrasonic Frequency Spectrum
Electromagnetic Frequency Spectrum
(No external excitation)
Monitor During Build Process
Inspection Between Build Layers
Passive
(Added excitation)
Active
Infrared/near-IR
melt pool monitoring
-
Visual
Laser profilometry
Laser ultrasonic
X-ray

## Slide 8: Monitoring Different AM Systems
Powder Bed Systems
Process:
Feedstock:
Freeform Fabrication
Laser Powder Bed Fusion (L-PBF)
Electron Beam Melting (EBM)
Selective Laser Sintering (SLS)
Metals: Nickel alloys, copper alloys, titanium alloys, etc.
Polymers: nylon, polyamide
Laser Directed Energy Deposition (DED)
Electron Beam Free Form Fabrication (EBF3)
Rapid Plasma Deposition
Additive Friction Stir Weld
Fused Filament Fabrication (FFF)
Metal powder/wire/chips
Filament: polymer, carbon fiber, biological, etc.

## Slide 9: Two Different Functions of In-Situ Monitoring
Process Control Function
Quantitative analysis of part quality
Requires a known correlation between indications, physics of the process, and actual defects in the finished part
Need to know probability of detection
  Extra step – verify actual size, location of created defects
Need to treat it like NDE – believe and investigate every indication
  Can’t dismiss anything as a false positive unless proven
vs.
Part Quality Function
Real-time warning of build problems
Use to check for process drift
Monitor effects of parameter changes, spatter, etc.
Not counting on it for quantitative part quality metrics or defect detection
  May help tell you where to look for a problem, but would require verification with NDE

## Slide 10: Challenging the Qualification Paradigm
Closed-loop process control
Often, defect observations are indirect
  Directly observing process variation, inferring final defect
  Must understand physical basis for measured phenomena
  Need to prove a causal correlation from measured indications to defect state
Probability of detection (POD) study must include secondary verification of created defects
Current qualification logic based on a locked process
For real-time parameter changes, a new approach is needed
In-process vs. post-process NDE
no longer nondestructive

## Slide 11: NASA AM Certification Approach
MSFC-SPEC-3717
MSFC-STD-3716
Policy
Procedure
NASA-STD-6016A
Requirements for traditional manufacturing – also apply to AM
NASA-STD-6030
NASA-SPEC-6033
Standard for Additively Manufactured Spaceflight Hardware by Laser Powder Bed Fusion in Metals
MSFC Technical Standard
MSFC Technical Standard
Specification for Control and Qualification of Laser Powder Bed Fusion Metallurgical Processes
NASA Technical Standard
NASA Technical Standard
Additive Manufacturing Requirements for Crewed Spaceflight Systems
Additive Manufacturing Requirements for Equipment and Facility Control

## Slide 12: Comprehensive NDE Requirement
The new NASA standards require comprehensive NDE for surface and volumetric defects, unless otherwise substantiated.
Language:
“All AM parts shall receive comprehensive nondestructive evaluation (NDE) for surface and volumetric defects within the limitations of technique and part geometry unless otherwise substantiated as part of the Integrated Structural Integrity Rationale [ISIR] of PPP [Part Production Plan] per section 7.3”
Rationale:
“NDE provides a necessary degree of quality assurance for AM parts in addition to the process controls of this NASA Technical Standard.”
“There is currently no methodology to preclude all AM process failure modes through the available process controls.”
(emphasis added)

## Slide 13: Qualified In-Situ Process Monitoring
However, passive in-situ process monitoring may be used as a quantitative indicator of part quality, if qualified by the CEO.
Language:
“Prior to use as a quantitative indicator of part quality, passive in-situ process monitoring technologies shall be qualified by the CEO to the satisfaction of NASA in a manner analogous to other NDE technologies.”
Rationale:
“All processes that are used to establish quantifiable quality assurance metrics are qualified to verify detection reliability, calibration, and implementation against established criteria. If in-situ monitoring techniques are employed for such purposes… the need for such qualification is unchanged.”
“Certification of a passive in-situ monitoring technology relies upon:
  A thorough understanding of the physical basis for the measured phenomena
  A proven causal correlation of the measured phenomena to a well-defined defective process state, and a proven level of reliability for detection of the defective process state.”
(emphasis added)

## Slide 14: Qualification Flow Chart
In-situ monitoring can factor into several aspects of part certification.
Qualification of Material Process (QMP)
  Use in sync with process development
Part Classification
  Improve inspectability for better risk posture
  Inspection process must be qualified by CEO
Part Production Plan
  Integrated Structural Integrity Rationale (ISIR):
    Can be specified as a defect screening action
    Must be qualified by CEO
Production Controls
  Could develop certain metrics to track over time
Design
  Part Classification
Part Production Plan
Pre-Production Article Evaluation
Additive Manufacturing Readiness Review
Qualified Part Process
Production Engineering Controls
Production Controls
Acceptance testing / Statistical Process Control
Digital Thread
Definition of Material Process
Qualification of Material Process
Equipment Control
Personnel Training
Material Property Suite
  Material property data
  Design values
  Process Control Reference Distribution
  Statistical Process Control Criteria
See NASA-SPEC-6033 for procedural implementation
{

## Slide 15
Risk-based part classifications for AM parts consider the risk of AM manufacturability and inspectability.
Catastrophic Failure?
Heavily Loaded?
Does the build have challenging aspects or areas that cannot be inspected?
AM Risk Classification
Notes: Part Classification system is a risk communication tool
What happens if the part fails? How severe is the stress in the part? How challenging is the part to design, build, and inspect?
. By looking at the classification we get a quick and consistent view into the risk posture for that piece of hardware.
The higher a part’s classification, the more stringent the downstream requirements become
  Non-destructive evaluation needs will differ

## Slide 16: Adaptive (Closed-Loop) Systems
Two issues for verification:
Monitor the process using sensors (e.g. meltpool thermal signature) and change a machine/process parameter (e.g. laser power) to optimize the response
Currently available in many directed energy deposition (DED) systems
Verify the sensor performance, algorithm and machine response
Verify the physics – does controlling this parameter result in a good part?
Adaptive (Closed-Loop) Systems:
(control system)
(materials)
“Active in-situ monitoring technologies that alter the defined AM process in response to monitored phenomena are not currently acceptable per this NASA Technical Standard.”
The current certification approach does not accommodate the use of adaptive systems.

## Slide 17: Control System Verification
For certifying closed-loop control systems, NASA can leverage the expertise of the spacecraft control systems community.
Black box issue:
Verify the accuracy of the sensor data
Verify the software/algorithm processing and response
Verify that the changed parameter responds correctly
For commercial systems, machine parameters may not be known, algorithms may not be accessible
Ideal approach: collaborate with machine manufacturers
Can also develop transfer function by studying inputs/outputs
Verification of a control system:

## Slide 18: Material Control Verification
Verifying that the adaptive system results in good material is a challenge that will require further study.
What parameter will you change?
Assume you’re monitoring the meltpool thermal emissions
Are you looking to keep it constant, or vary it based on part geometry?
More complex if monitoring multiple signals and/or changing multiple parameters
Qualify process for each different system, alloy, part?
What is being monitored, and to what end?
What does it really tell you about the process and the material?
Is this a good indicator of material quality?
Is the resulting microstructure/morphology consistent and repeatable?

## Slide 19: Conclusions
In summary, NASA encourages and wants to help enable the use of in-situ process monitoring for AM certification.
Use for process monitoring is highly encouraged.
→ Will help inform, develop, and prepare for part quality function
To use for quantitative part quality function, monitoring system must be qualified.
→ Main challenge: developing correlation of indication to verified defect
Qualifying closed-loop, adaptive systems will require a new approach to the QMP.
Thank you for your time!

## Slide 20
Thank you.
Erin Lanigan, NASA Marshall Space Flight Center November 18, 2020