## Slide 1: Ultrasonic nondestructive evaluation using non-contact air-coupled Lamb waves
Wenfeng Xiao
PhD Dissertation Defense
Department of Mechanical Engineering
University of South Carolina, Columbia
November 10th , 2020

## Slide 2: Acknowledgements
Advisor: Dr. Lingyu Yu
Committee: Dr. Giurgiutiu, Dr. Chao, Dr. Zhang
My family and friends
VSHM colleagues
LAMSS members
U. S. Department of Energy (DOE)
National Aeronautics and Space Administration (NASA)
University of South Carolina, ASPIRE Innovation award
*A part of the proposal is based upon work supported by National Aeronautics and Space Administration (NASA) under Award Nos. NNL09AA00A and 80LARC17C0004.
Any opinions, findings, and conclusions or recommendations expressed in this material
are those of the author and do not necessarily reflect the views of the NASA.
NASA

## Slide 3: Wrinkle inspection setup
y
O
x
60
125
190
220
x
(b)
x
O
y
Top surface
Bottom surface
Wrinkle specimen
  Dimension: 306 × 205 × 3.74 mm
  No other information is available
  Wrinkle region: more visible wrinkles
  Reference region: less visible or likely no wrinkles
Reference region
Wrinkle region
Reference region
Wrinkle region
Inspection setup
  Excitation: 120 kHz ACT with incident angle 
  Sensing: SLDV for out-of-plane velocity measurement
optimal= 15˚
Peak value
Signal strength vs. incident angle
 = 10˚
 = 17˚
Optimal incident angle tuning is conducted along x-axis direction in the reference region with  set as 10˚, 11˚, 13˚, 15˚, 17˚,19˚, and 20˚.
Courtesy of NASA Langley Research Center and Boeing

## Slide 4: Line scan inspection
Line scan along the x-axis direction is conducted with optimized setups for ACT and SLDV
Wrinkle reflections
R3 wavefield
W3 wavefield
R3 f-k spectrum
W3 f-k spectrum
Reference region
Wrinkle region
ACT
306 mm
265 mm
x
O
ACT
R2
R1
R3
O1
O2
O3
W2
W1
W3
y
Reference region: R1, R2, and R3
Wrinkle region: W1, W2, and W3
Schematic of the line scans
Inspection results:
Time-space wavefield
f-k spectrum
Wrinkle reflections
Negative wavenumbers
Negative wavenumbers
Little wrinkle reflections
Weak negative wavenumbers
Weak negative wavenumbers
Little reflections
The wrinkle defects’ signatures are successfully achieved!
Courtesy of NASA Langley Research Center and Boeing

## Slide 5: Wrinkle imaging inspection
60
125
Wrinkle pattern
90
120
Wrinkle pattern
60
90
220
190
Wrinkle pattern
60
125
Wrinkle region imaging
Reference region imaging
Reference region
Wrinkle region
ACT
306 mm
265 mm
x
O
0˚ direction
y
ACT
60
100
100
Area scans are conducted in both wrinkle regions and reference region for wrinkle inspection
The excitation moved to x = 110 mm
Wrinkle pattern from 90 to120 mm are imaged
Wrinkle pattern from 60 to 90 mm are imaged
ACT excitation at 160 mm
SLDV scans with 1 mm resolution
Imaging method:
Wave energy imaging method for quick inspection
Schematic of the area scans
Less wrinkles from 190 to 220 mm are imaged as well.
The entire wrinkles in the wrinkle region are successfully imaged
The less wrinkle in the reference region are imaged as well
The noncontact Lamb wave system has successfully inspected the wrinkle defects
Courtesy of NASA Langley Research Center and Boeing
Courtesy of NASA Langley Research Center and Boeing