## Slide 1
newly polymerized
Jacob Gissinger, Benjamin Jensen, Kristopher Wise
NASA Langley Research Center
REACTER—A Heuristic Method
for Reactive Molecular Dynamics
MRS Fall 2020
Nov. 27 – Dec. 4
F.MT04.03.07
jacob.gissinger@nasa.gov

## Slide 2: What is REACTER?
A protocol for adjusting topology during classical MD
  Add/remove specific bonds, angles, dihedrals, and impropers
  Modify all force field types as well as atomic charges
  Supports any fixed-valence force field (PCFF, OPLS, etc.)
  Reaction stabilization
Parallel implementation in LAMMPS as fix bond/react
  User inputs: molecule templates of pre- and post-reaction topology
  A map file relating atoms before and after the reaction
www.reacter.org
REACTER: A Heuristic Method for Reactive Molecular Dynamics.
Gissinger, Jensen & Wise. Macromolecules. 2020 (in press).

## Slide 3: REACTER: Standard Features
REACTER supports:
  Arbitrary reactions, any classical force field, on-the-fly minimization
Useful capabilities:
  Support for coarse-grained systems
  Limit total occurrences of a given reaction
    Use case: Stop reactions after a certain percentage of crosslinking
  Use variables for inputs (reaction cutoff, probability and frequency)
    Use case: define reaction cutoff as a function of extent of reaction
Additional options:
  Reaction constraints
  Delete user-specified atoms, based on topology

## Slide 4: Delete Atoms Based on Topology
1) Delete unwanted reaction by-products
2) Remove specific molecules based on topology (such as small rings)
deletion of condensed water molecule
nylon polycondensation

## Slide 5: Bond-Breaking Reaction Trigger
Simple criterion for mechanically-induced chain scission

## Slide 6: Reaction Constraints
Currently five constraints: Arrhenius, RMSD, distance, angle, dihedral
  Can be used to enforce a relative orientation between reacting molecules
Demo: two distance constraints enforce a certain molecular orientation

## Slide 7
Large-scale Nylon 6,6 Demo
condensed water molecules removed
Setup: 5,000x adipic acid
5,000x hexamethylenediamine
220,000 atoms
Temperature: 530 K
(actual synthesis temp)
Final density: 0.9 g/cm3
Side length: 13.3 nm
3-5 Å reaction cutoff
>99% polymerized

## Slide 8
Chain PDI ≈ 2 Overall PDI (with cycles) ≈ 3.9*
265 repeat units
>7,400 backbone
atoms
(nylon 6,6)
only backbone atoms shown
*Experimental PDI ≈ 4.
Solid-state modification of polyamide-6,6. Jeyakumar, A. Eindhoven: Technische Universiteit Eindhoven. 2012.

## Slide 9
>99% Polymerized Nylon 6,6: Chains vs. Cycles
weight % cycles:
simulation: 3.7%
experiment: 1-5%1
>250 repeat units
(>500 reactant molecules)
1Endgroup-based separation and quantitation of polyamide-6,6 by means of critical chromatography. Mengerinka, et al. Journal of Chromatography A 949, 337. 2002.
Cycles
Chains
degree of polymerization
chain ID
molecule count
degree of polymerization

## Slide 10
Nylon 6,6: Chain Morphology
(Å)
Rg2 ~ N1.1
# repeat units
end-to-end distance
radius of gyration
Value for a Gaussian chain:
degree of polymerization
Nylon 6,6: chain radii of gyration

## Slide 11: Chain Growth vs. Ring Formation
cycle constraining two chains:
physical ‘slip-link’
single topologically-constrained cycle
Nylon 6,6
cycle
cycle

## Slide 12: Uniaxial Extension with Chain Scission
Uniaxial strain
  Highly entangled system
  Craze formation
Chain scission reaction
  Relieve topological constraints
  Activated if C-N bond > 1.67Å
    Chosen empirically
  Only 6 chain scissions occurred
130 Å
1435 Å (~11:1 aspect ratio)
(nylon 6,6)

## Slide 13: Polystyrene Demo
>99% polymerized polystyrene
200,000 atoms (12,500x styrene)
>98.5% polymerized with 3.0 Å distance cutoff, before switching to 3.5 Å
Conclusion: REACTER can handle small monomers with bulky side groups
530 K
13.7 nm box
REACTER: A Heuristic Method for Reactive Molecular Dynamics.
Gissinger, Jensen & Wise. Macromolecules. 2020 (in press).

## Slide 14
Simple cross-linking mechanism of an amine to two epoxy molecules
Epoxy Crosslinking

## Slide 15
Final Epoxy Morphology
96% cross-linked
Distance cutoffs:
rxn 1: 3.5 Å, rxn 2: 5.0 Å
100 diepoxy molecules,
50 diamine molecules
Run: 200 ps at 800 K
Modeling chemical reactions in classical molecular dynamics simulations. Gissinger, Jensen & Wise. Polymer 128, 211-217. 2017.

## Slide 16: Summary and Outlook
REACTER is a useful tool for building complex morphologies
The REACTER protocol scales well
  10,000 nylon precursors true temp. (≈260 C)
  12,500 styrene molecules low cutoff 3-5 Å
Correctly predicts cyclic content, polydispersity and chain morphology
What’s next?
  More predictive reaction constraints
    Potential energy surfaces?
  Features in progress
    Additional reaction constraints
    Option to insert atoms
>99% polymerization

## Slide 17
Thank You!
www.reacter.org