## Slide 1: Additive Manufacturing of Electronics for Space Applications
Beth Paquette
NASA Goddard Space Flight Center
  beth.m.paquette@nasa.gov
  301.286.8647

## Slide 2: Outline/Agenda
Introduction: Additive Manufacturing Techniques
Next Generation X-Ray Polarimeter
Next Generation Microshutter Array
Future Work
Acknowledgements
Q & A

## Slide 3: Introduction: Additive Manufacturing Methods
Printed Hybrid Electronics: Deposit conductive and insulating inks onto an existing substrate to create circuits
Aerosol Jet

## Slide 4: Why?
Feature sizes down to 10 microns
Variety of substrates – flexible, rigid, 3-dimensional non-planar
Has the potential to reduce mass and volume

## Slide 5: Next Generation X-Ray Polarimeter (NGXP)
Original Strip Detector
Frame
3 in x 5 in Liquid Crystal Polymer (LCP)
Traces: 121µm pitch, copper cladding etched
Fan-out area
ASIC Board
Photoelectron tracks imaged using strip detectors in a gas environment
Notes: Study sources of X-Rays
Photoelectron tracks imaged using strip detectors in a gas environment
Original strip design: traces at 121-micron pitch, etched into copper cladding on a liquid crystal polymer substrate
The minimum pitch of the strips and the area required to fan the strips in to the pitch of the ASIC readout is limited by the accuracy of the etching, and limits the gas choices and pressure, thus restricting the achievable sensitivity
Reducing the pitch could reduce the Polarimeter design in size, which saves mass, and improves track resolution
A reduction in strip pitch will enable the detector sensitivity to be increased by more than a factor of three and a mission sensitivity increase by more than a factor of ten

## Slide 6: NGXP Flexible Prints
Materials:
  Gold and silver inks
  Kapton and Liquid Crystal Polymer (LCP) Substrates
Printer:
  Optomec AJ200
  Pneumatic atomizer for silver ink
  Ultrasonic atomizer for gold ink

## Slide 7: NGXP Flexible Prints
120µm pitch
0.6
inches
3.5 inches
Silver printed on Liquid Crystal Polymer
Traces 60-80µm width

## Slide 8: NGXP Flexible Prints
Silver printed on LCP
40-80µm width traces
120µm pitch
Notes: 40µm width increased to 80µm half-way through printing. Settings had to be adjusted to get thinner traces again.

## Slide 9: NGXP Flexible Prints
Gold on Kapton
Ultrasonic atomizer
200µm tip
80µm width traces
120µm pitch
Ink appeared dry and powdery. Overspray observed

## Slide 10: NGXP Flex Mechanical Tests
Bend Testing
Tensile Testing
Tape Testing
Pull directions

## Slide 11: NGXP Flex Mechanical Tests
Trace, bond and LCP breaks observed
Tensile Tests
Tape Tests

## Slide 12: NGXP Flex Observations
Printing parameters need to be adjusted over length of print
Results vary between printer operators
Gold ink more cumbersome to use, store
Adhesion of inks to LCP needs improvement

## Slide 13: NGXP Rigid Prints
Aerosol Jet Printed Silver Traces on Macor
45µm width traces and 120µm pitch

## Slide 14: NGXP Rigid Print Tests
Visual and topography imaging
Traces measured 45.5µm+/-4.4µm
Trace
Substrate
ASTM Adhesion
Class 5B and 4B observed

## Slide 15: NGXP Rigid Print X-Ray Tests
Printed Strip
Electrode layer
X-Rays move parallel to traces
Strip survived 40+ hours of X-Ray testing
Charge drifts towards the traces

## Slide 16: NGXP Rigid Print Observations
Prints on rigid substrates yielded ASTM Class 4B and 5B adhesion (minimal material removed)
Substrate topography may impact trace structure and conductivity
Prints survived X-Ray chamber

## Slide 17: Next Generation Microshutter Arrays (MSA)
High-resolution spectroscopy: Microshutters select many objects in one viewing for simultaneous observation
Microshutter Array
Silicon Substrate
128 pairs of metal pads

## Slide 18: MSA Aerosol Jet (AJ) Test Prints
Sample without insulator
Sample with insulator
Printed Silver Lines
Metal Pads
Printed Insulator
Conductivity tests were successful

## Slide 19: MSA AJ Test Prints
Printed silver lines with 20um width over insulating fillet/”ramp"
Printed Sample on Silicon Squares attached to Wafer
Scanning Electron Microscope Images by GSFC

## Slide 20: MSA AJ Test Prints
Printed silver lines with 25µm width over insulating fillet/”ramp“ [Optomec]
Left Side
1
130
Trace resistivity measured: 10 W/mm
Isolation resistance measured greater than 10 GW
Right Side

## Slide 21: Future Work
Work with syringe printer and other additive manufacturing methods to produce circuitry
Continue Conductivity and Environmental Testing
Integrate ASIC board design into NGXP
Future applications: Sounding Rocket Demonstration, CubeSat Demonstration

## Slide 22: Acknowledgements
Goddard Space Flight Center: Parts, Packaging and Assembly Branch, Meng-Ping Chang, Peng Chen, Kevin Black, Christopher Green, Joe Hill-Kittle, Keith Jahoda, Justin Jones, Mary Li, Eleanya Onuma, Cameron Parvini, Wes Powell, Margaret Samuels, Anna Zajczyk
Justin Bourassa, Mike Renn, Optomec

## Slide 23
Thank You!
Contact: beth.m.paquette@nasa.gov

## Slide 24: Acronyms
Acronym | Definition
AJ | Aerosol Jet
ASIC | Application Specific Integrated Circuit
ASTM | American Society of Testing and Materials
LCP | Liquid Crystal Polymer
MSA | Microshutter Array
NGXP | Next Generation X-Ray Polarimeter
PEEK | Polyetheretherketone