## Slide 1
Electrodynamic Dust Shield
Carlos I. Calle, Ph.D.
Electrostatics and Surface Physics Laboratory
Swamp Works
NASA Kennedy Space Center

## Slide 2: The EDS Technology
The Electrodynamic Dust Shield (EDS) is an active dust mitigation/transport system for NASA’s Exploration missions.
Uses dynamic electric fields to remove dust from surfaces.
Multiple phases
Can be made transparent, flexible, applied to metals
1
3
2
+
dust particle motion

## Slide 3
EDS Implementations: Optical Systems & Viewports – TRL 5
RASSOR EDS Mount
Works well in conjunction with passive dust mitigation methods/coatings
Uses include:
  Camera lenses, optical instruments
  Viewports, visors
  Solar panels, solar cells
  Curved surfaces such as solar concentrators
  Thermal radiators, thermal painted surfaces
  Flexible materials, fabrics
Glass EDS at vacuum
Glass EDS in space
9”diameter ITO/PET EDS Tested at Desert RATS.

## Slide 4
EDS Implementations: Solar Panels – TRL 5
RASSOR EDS Mount
Kapton EDS in space
Glass EDS/PV and PV setup with JSC-1A lunar stimulant. Efficiency was restored to 95% of original value.
Solar panel response to 50–75 mm JSC-1A dust deposition and removal under high vacuum conditions with a 3-phase ITO-glass EDS with four different electrode spacings.**
Glass EDS/PV and PV setup with JSC-1A lunar stimulant

## Slide 5
EDS Implementations: Thermal Radiators – TRL 5
RASSOR EDS Mount
Kapton EDS in space
One-Phase Al-FEP EDS
Cu-Kapton EDS on Al with AZ-93 Thermal Paint
Kapton EDS in space

## Slide 6: EDS Implementations: Fabrics – TRL 4
50-75 µm simulant on 2-phase CNT-cotton fabric EDS, 1500 V, 10 Hz, <10 s, air test.*
Dust removal experiments with EDS with CNT thread electrodes on Ortho-Fabric material.**

## Slide 7
Glass EDS Vacuum test
EDS Electronics – TRL 5
High voltage power supply
(50 mm x 50 mm x 25 mm)
Mass: 58 g
Kapton EDS Vacuum test
RASSOR EDS Mount
Size: Power supply: 5 cm x 5 cm x 2 cm
Power: EDS shields  ~ mW to remove dust
EDS Power supply  2-4 W maximum
Modes of Operation:
EDS can be operated continually for surfaces needed to be free of dust that are highly sensitive (optics, lenses, etc.)
EDS can be operated momentarily to remove settled dust for less susceptible systems (solar panels, radiators, etc.)
Power Signal:
  EDS operates between ~900-1200 volts in air, but could operate up to 4 kV in vacuum with efforts at minimizing that potential underway
      Signals are 10 Hz square wave with fast rise times (still being optimized for vacuum)

## Slide 8
RGF and ISS Experiments
Electronics control unit
Vacuum chamber
Video recording computer
Tested with Apollo samples on Reduced Gravity Flights
Flying as a payload for the Materials ISS Experiment (MISSE) 11 and 15
Developing payload for NASA’s Commercial Lunar Payload Services Lander (CLPS) program
  Reduced Gravity Flight (RGF) Experiments were performed under lunar and Martian gravity
  MISSE 11 and 15: to test materials and construction of the EDS subassemblies to evaluate impact of exposure to the space environment

## Slide 9: EDS demonstration on a CLPS Mission
Launch date: June 2023
The main objective is to demonstrate the operation of two EDS Systems on the lunar surface:
  EDS for a small camera to be located under the lander’s deck
  EDS on a white aluminum panel to be located on a lander’s footpad
The camera EDS will consist of indium tin oxide electrodes on a glass panel coated with a space-rated dielectric.
The Footpad EDS will consist of thin copper electrodes on polyimide film with a white polyimide dielectric cover. This multilayer film will be affixed to an aluminum panel.
The EDS panels will be activated and controlled with compact high voltage power supplies co-located with each EDS.
A Digital Storage Unit (DSU) will provide power, data communications, and data storage for EDS and camera operations.

## Slide 10
Prototype 60” x 40” ITO on clear polymer (Poly Adaptive, LLC)
Clear 9”-diameter EDS on Viewport, 14” x 17” Cu/Kapton EDS for thermal radiators installed on lunar habitat prototype at Desert Research and Technology Studies (Desert RATS).
Scaling Up the Technology

## Slide 11
10-micron dust simulant removal on Reduced Gravity Flight at vacuum
EDS on a Reduced Gravity Flight