## Slide 1: Small Satellites Protecting Components, Enabling Communications
Dr. D. Laurence Thomsen III (Larry) NASA Langley Research Center, Advanced Materials and Processing Branch, 6A West Taylor Street, Hampton, VA 23681; 757-864-4211, d.l.thomsen@nasa.gov
27 January 2021

## Slide 2: CubeSat Market: $0.5B-1B over 3yrs
Over 1700 small satellites forecasted for 2017-2023 (www.spaceworksforecast.com)
Over 500 over next 3 yrs into polar low earth orbit (PLEO) (www.spaceworksforecast.com)
Typical CubeSats costs $1-2M* (https://esto.nasa.gov/techval_space.html)
*NASA ESTO Office reported it is $1-$1.5M per U at the 2017 SmallSat Conference and is updating its figure.
CubeSat value at risk: $0.5-1B in the next three years alone
Image Credits: www.nasa.gov
Notes: Polar low earth orbit: most radiation in low earth orbit, cubesats have virtually no shielding
(70% commercial, 10% government, and 20% Academic.)
from development, launch, and operations.

## Slide 3: LaRC Z-Shielding Increases CubeSat Mission Lifetimes
Extends typical CubeSat missions from 3 months to years
A 18-36x reduction of total ionizing dose and removal of internal charging effects.
Increases return on investment
NASA Tech-Transfer web releases of LaRC Z-Shielding
Z-shielding Technology pitch: https://www.youtube.com/watch?v=oHA8j5bpFcU&t=21s
Webinar: https://www.youtube.com/watch?v=RrqDocGqawQ
https://techgatewire.larc.nasa.gov/2017/01/26/radiation-protection-material-webinar/
Image Credit: NASA
Notes: in comparison to commercial CubeSat aluminum shielding
with risk reduction of satellite failures from total ionizing dose and internal electrostatic discharge, a historical spacecraft killer.

## Slide 4: Shielding is not common today
CubeSat missions have been short, mostly experimental
There are size and material constraints in the "standard" CubeSat packaging
Mostly in low, short-lived orbits, such as deployed from ISS
The actual satellites have been viewed as "disposable"
Notes: Previously, considered short tech demo academic experiments
Attitude Control, Star Trackers, Propulsion, High Bandwidth radios, deployable solar arrays
Increase in SmallSat Industry Attendance at Conferences
Now Longer Orbit Lifetimes, more time for data or space debris
Shielding matters for risk reduction

## Slide 5: But that can and is changing quickly
The satellites themselves are now more capable
Higher orbits are now available
Longer orbit life calls for longer functional life for the satellite
Shielding now matters

## Slide 6: Proliferation of Small Satellites in Polar Low Earth Orbit
SpaceX has now launched more than 1000 Starlink satellites to date
Amazon Web Services and OneWeb building Constellations
January 20th, 2021: SpaceX launched 60 Starlink satellites to orbit from Kennedy Space Center, completing the seventeenth Starlink mission. www.starlink.com
Image Credit: SpaceX
Image Credit: SpaceX
Image Credit: Marco Langbroek, https://sattrackcam.blogspot.com/2019/05/wowowow-spectacular-view-of-spacex.html
First Starlink Deployment on 23 May 2019

## Slide 7: Shields-1, Space Radiation Effects Experiments NORAD ID 43850
Presently, Shields-1 operates with LaRC Z-Shielding providing radiation protection for the electronics over 2 years in polar low earth orbit.
Shields-1 onboard Rocket Lab USA, Electron Rocket, NASA ELaNaXIX Mission, 16 December 2018 Launch
Image Credit: Rocket Lab USA
Shields-1 in PPOD deployer, 2nd from bottom, inside Electron Rocket Fairing before encapsulation
https://www.rocketlabusa.com/missions/completed-missions/elana-19/ https://www.youtube.com/watch?v=KZwLJMPuos8
https://www.youtube.com/watch?v=WSCAE-hEa9M
Image Credit: NASA
Image Credit: Rocket Lab USA

## Slide 8: Shields-1 from Idea to Spaceflight
ElaNaXIX Mission Readiness Acceptance
  New Shielding Structure completed a 10g Vibrational Test (NASA 10 GEVS). Risk Reduction for multiple launch vehicle rideshares
  Met Fit Checks for PPOD Deployer
  Met Bakeout and outgassing requirements
  Met anodization requirements including hard anodized rail requirements
Successful deployment and current operations
Image Credit: NASA

## Slide 9: Shields-1: Radiation Shielding Experiments
Vault Electronics
  To measure total ionizing dose (TID) over time and monitor system electronics performance.
Atomic Number (Z)-Grade Radiation Shielding
  To measure total ionizing dose of Z-grade radiation shielding and compare to baseline aluminum for at least 3 samples each.
Image Credit: AGI
Notes: For the system electronics performance, the effort has been to chart the SD card performance over time with the voltage and current measurements. UMICH has reported that SD Card failures typically occur from increasing current draw on the card. This engineering data has not been integrated. The regulator performance will be attempted to monitor. The current and voltage measurements need to be characterized with respect to a regulated voltage source. On board we only have reference resistors in the research payload, which will be attempted to use for baselining the regulators. At this time this data has not been integrated with the dosimeter data.

## Slide 10: Shields-1 Vault Experiment
The Shields-1 electronics enclosure (vault) dosimeter is located inside the vault with Resistance Temperature Detector (RTD)
Dosimeter
and RTD
Shields-1 Vault Z-Shielding effectiveness:
75.6 +/- 3.2 Rad/Yr (3.02 g/cm2) for polar low earth orbit
All Earth orbits, inter-planetary, Mars, and Moon relevance with SPE protections for TID Reduction on commercial parts
Over 18 times reduction from typical Al Shielding (0.198 cm, 0.535 g/cm2) with a 2 times under estimated AP8 AE8 radiation model and no protection from solar proton events
Thickness (Volume) savings when compared to Aluminum for Shields-1 first generation Z-Shielding 56.1% and comparable Thin Z-Shields prototype material = 77.1% savings
Image Credit: NASA

## Slide 11: Shields-1 Summary
Vault Experiment:
  75.6 +/- 3.2 Rads/Yr in polar low earth orbit, versus 1380 Rads/yr for typical 0.198 cm (78 mil) aluminum commercial CubeSat Structure, 18 times reduction in Total Ionizing Dose (TID), which is likely under estimated by a factor of 2, per modeling limitations
  Thickness (Volume) savings when compared to Aluminum for Shields-1 first generation Z-Shielding 56.1% and comparable Thin Z-Shields prototype material = 77.1% savings
  Z-Shielded Vault estimated mission lifetime increased for commercial TID parts. Typical low earth orbit hardness design guidelines suggest 2-10 kRad commercial part hardness, with some parts even below 2 KRad. Typical NASA radiation design margin 2. This suggests Shields-1 has a TID mission design life of 1000/75.6 = 13.2 year TID radiation design life.
    Typical Commercial CubeSat System: with 2-10 kRad hardness guideline and Radiation Design Margin guideline has a combined 1 kRad/year estimated dose rate guideline, has a 1000/1380 = 0.72 year (8.7 months) TID radiation design life. If Radiation Design Margin is 3 = 667 / 1380 = 0.48 year (5.8 months).
    This calculation does not include solar activity, which worst case could introduce over 700 Rad for a typical 0.2 cm (0.08 in) Aluminum in a CubeSat. (Solar Activity Increasing through Max in 2025)
Notes:   Significance: Reduced TID associated Mission Failure Risks. Increased Mission Assurance for the science data return on investment.
  Vampola noted no experimental radiation data below L 1.2 for electrons and L 1.17 for protons, which is approximately 840 km altitude, the DMSP satellite data in the AP8 and AE8 models.

## Slide 12: Shields-1 Vault Experimental Results
Reference: Donald Thomsen, Kevin Somervill, Mark Jones, Raymond T. Lueg, William G. Girard, Alexander D. Scammell, Jing Pei, James W. Cutler, Robert G. Bryant, “Shields-1 Initial Space Operations, a NASA CubeSat Launch Initiative ELaNaXIX Mission”, SmallSat Conference, 2019, Logan, Utah, 7 August 2019.
Teledyne mdosimeter: http://www.teledynemicro.com/product/radiation-dosimeter
Preliminary results: estimated dose rate per year: 75.6 +/- 3.2 Rad/Yr
Suggests Z-Shielding Vault behaves similarly to a spherical shielding model
Reduces total ionizing dose on sensitive electronic parts
High Count = 256 counts (steps) of Medium
Med Count = 256 counts (steps) of Low
High count step = 256 x 256 x 14.3 +/- 0.6 mRad/step = 0.94+/-0.04 Rad/step
Each step represents a turnover of the mdosimeter high counter

## Slide 13: Z-Grade Radiation Shielding Experiment
Infinite slab, geometry approximation
>95% incident radiation through shielding sample
Large sample field of views, thick backing
UDOS | Shielding | Areal Density (g/cm2)
1 | Al | 6.00
2 | Al | 3.00
3 | AlTiTa | 3.02
4 | AlTiTa | 2.08
5 | AlTi | 1.33
6 | Al | 1.26
7 | Al | 1.69
Shielding Samples Behind mDosimeters (UDOS)s
LaRC
Z-Shielding Vault
LaRC Z-Shielding Test Samples
LaRC Shields-1 CubeSat Structure
Image Credit: NASA

## Slide 14: Z-Grade Radiation Shielding Thickness Comparisons
Chart: Comparison of Z-Shielding Materials and Aluminum Baseline
| 2.2200000000000002 | 1.1100000000000001 | 0.46500000000000002 | 0.624
 | 70.0277 | 73.5659 | 90.8939 | 84.2532
 | 81.9479 | 84.3301 | 89.6875
Al (1.26 g/cm2)
AlTi (1.33 g/cm2)
AlTiTa
(2.08 g/cm2)
Al (1.69 g/cm2)
Al (3.00 g/cm2)
Al
(6.00 g/cm2)
AlTiTa
(3.02 g/cm2)
Total ionizing dose over a 17 day accumulation period
Polar Low Earth Orbit, 85 deg inclination, 500 km altitude
Recent Thinner NASA Z-Shielding:
Thin Z-Shields LEO-Light (0.203 cm)
Thin Z-Shields LEO (0.203 cm)
Thin Z-Shields GEO (0.254 cm)
Notes: The Z-shielding performance as a function of thickness enables low volume shielding solutions for multiple polar orbiting scenarios where traditional aluminum thicknesses limit electronic card sizes. These measurements occurred at solar minimum, where shielding performance needed for solar maximum has not been demonstrated.

## Slide 15: Shields-1: Shielding Dose Rate Comparisons
TID ELaNaXIX Mission Environment: 1 year duration at 500 km altitude and 85o inclination
(UDOS 1-7 collected TID over a 17 day period for total dose rate, UDOS 0 over 2 months)
UDOS | Slab Shielding | Areal Density (g/cm2) | Thickness (cm) | Experimental TID (Rad (Si))/ Year | Modeled TID (Proton (p) & Electron (e)) (Rad (Si)) 2pistr omnidirectional | Modeled TID Total (Rad (Si) | Modeled TID with 6 g/cm 2 Backslab Rad (Si) Added
1 | Al | 6.00 | 2.22 | 70.0 +/-3.0 | 13.48+/-0.06 p, 0.21 +/- 0.03 e | 13.69 +/- 0.07 | 27.38 +/- 0.11
2 | Al | 3.00 | 1.11 | 73.6 +/-3.2 | 21.77+/-0.09 p, 0.36 +/-0.03 e | 22.13 +/- 0.09 | 35.82 +/-0.11
3 | AlTiTa | 3.02 | 0.483 | 81.9 +/-3.4 | 25.68+/- 0.10 p, 0.18 +/- 0.04 e | 25.86 +/-0.10 | 39.55 +/-0.13
4 | AlTiTa | 2.08 | 0.429 | 84.3 +/-2.5 | 28.79 +/- 0.10 p, 0.15 +/- 0.03 e | 28.94 +/- 0.10 | 42.63 +/-0.13
5 | AlTi | 1.33 | 0.378 | 89.7 +/-2.7 | 32.77+/-0.11 p, 6.36+/-0.25 e | 39.03 +/- 0.27 | 52.72 +/-0.28
6 | Al | 1.26 | 0.465 | 90.9 +/-2.7 | 32.24 +/- 0.11p, 8.79+/- 0.29e | 41.03 +/- 0.31 | 54.72 +/-0.32
7 | Al | 1.69 | 0.624 | 84.3 +/-2.5 | 28.67 +/- 0.10 p, 2.00 +/- 0.14 e | 30.67 +/-0.14 | 44.36 +/- 0.16
 | Sphere | Shielding | Relevant | Shielding | for Comparison |  | 
 | Al# | 0.535 | 0.198 | n/a | 117 +/- 4 p, 1266+/-47 e | 1383+/-47 | n/a
 | Z-Shield LEO Light* | 1.05 | 0.203 | n/a | 104.2 +/-3.1 p, 45.5+/-8.7 e | 149.7+/-9.2 | n/a
 | Z-Shield LEO | 2.15 | 0.203 | n/a | 95.1+/- 2.7 p, 10.7 +/- 4.0 e | 105.8+/-4.8 | n/a
 | Z-Shield GEO^ | 3.00 | 0.254 | n/a | 81.7 +/-2.9 p, 0 e | 81.7+/-2.9 | n/a
0 | Z-Shield Vault | 3.02 | 0.483 | 75.6 +/- 3.2 | 75.6+/- 6.1 p, 0 e | 75.6+/-6.1 | n/a
 | Al | 3.00 | 1.11 | n/a | 64.7 +/- 8.4 p, 1.5 +/- 1.5 e | 66.2 +/-8.5 | n/a
Notes: references for the NASA PD-ED-1258, “Space Radiation Effects on Electronic Components in Low-Earth Orbit” and NASA PD-ED-1260, “Radiation Design Margin Requirement”. In low earth orbit below ~840 km the AP8 and AE8 models don’t cover the low earth orbit environment, where the CSLI traditional orbit altitudes exist from 500 km to 300 km for polar low earth orbit and ISS orbit.
The structures typically sold by commercial companies described have 0.078 in thick aluminum. I am finding that the 0.078 in Aluminum for a spherical model has a total ionizing dose for a year in the ELaNaXIX mission environment has an estimated dose for the AP8min-AE8max model of 1383 +/- 47. The Aerospace Proton (AP) 8 – Aerospace Electron (AE)8 model has limitations, according to Alfred Vampola from the Aerospace Corporation for inner zone electron models at the NASA Langley Research Center’s Space Environment Workshop, 1988:
For Inner Electron Models:
“The current NSSDC models which provide useful inner zone (L = 1.2 to 2.4) electron data are AE5 [6], for solar minimum, AE6 [10] for solar maximum, and AE8 [9] for solar minimum and maximum. The energy range of these models is from 0.04 MeV to 5 MeV, although present techniques can not make reliable measurements of electrons with energies above 2 MeV below about L=1.55 in the inner zone. They are empirical models, being based on in-situ measurements of the fluxes. To produce the models, data is acquired from investigators, corrected, edited, averaged, interpolated, extrapolated, etc; in other words, it is all very thoroughly massaged. Some estimate of its reliability is also made, but such a step is very subjective.” “The accuracy of the models is very good, better than a factor of two, for energies below 1 MeV and L < 1.65….Above 2 MeV, the fluxes are extrapolations and their accuracy is unknown.” pg. 378
L. Vampola, “The Space Particle Environment”, NASA/SDIO Space Environmental Effects on Materials Workshop, NASA Conference Proceedings 3035, part 2, NASA Langley Research Center, Hampton, VA June 28 – July 1, 1988, pg. 367.
For Proton models, “ The current proton models are AP8MIN and AP8MAX, again representing the solar minimum and maximum periods. The major effect of the solar variation is the variation in atmospheric density at lower altitudes: at solar maximum, the higher scale height of the atmosphere decreases the energetic proton fluxes. The models are probably accurate to 50% or better. They cover the energy range from 100 keV to 400 MeV and the L range from 1.17 to 7.” pg. 379
L. Vampola, “The Space Particle Environment”, NASA/SDIO Space Environmental Effects on Materials Workshop, NASA Conference Proceedings 3035, part 2, NASA Langley Research Center, Hampton, VA June 28 – July 1, 1988, pg. 367.
This value is approximately 3 times lower than estimated by Vampola et al. A spherical model is a typical conservative geometrical model for a satellite electronics enclosure. (ref. Hastings and Garrett et al and . NASA PD-ED 1258 reports typical parts hardness from 2-10 kRads. NASA PD-ED-1260 recommends a design margin of 2. Further, there is no experimental data used in the AP models for the orbital altitudes below ~840 km, which can assist in determining a better estimate for the total ionizing dose environment for many of the typical low earth orbit CubeSat missions, because the models rely on empirical data. There is no empirical data that has been used to update the AP models below 840 km. The low earth orbiting satellites used were 7 DMSP satellites at 840 k and TIROS and NOAA with 4 satellites orbiting at 850 km. (D. Bilitza, D.M. Sawyer, and J.H. King, “Trapped Particle Flux models at NSSDC/WDC-A-R&S)”, NASA/SDIO Space Environmental Effects on Materials Workshop, NASA Conference Proceedings 3035, part 2, NASA Langley Research Center, Hampton, VA June 28 – July 1, 1988, appendix.)
Shields-1 data that has been accumulating over the last year has the potential to contribute to low earth orbit space environment data over 300 km lower in altitude than the satellites used for the AP AE models. Already data collected on the spacecraft with all sensors operating have approximately 3 months of averaged radiation data, which is approximately half of the estimated data needed for the temporal guidance described by Vampola et al. This would be solar minimum data. Future concepts of operations for Shields-1 could be focused at ensuring 3 more months of radiation data can be obtained to contribute to NSSDC. NESC has expressed an interested in funding the data caputre for NSSDC, as described in the current Shields-1 data analysis work package.
NSSDC = National Space Science Data Center
For AP9 AE 9, https://www.vdl.afrl.af.mil/programs/ae9ap9/issues-and-limits.php.
“The model currently contains no solar cycle dependence, in particular with regard to LEO region proton variations. This will be addressed in a future version.
Uncertainties in the LEO region protons for energies <20 MeV are large, due to variability in the satellite sensor data, and sparse data coverage.
There are significant uncertainties in particle flux gradients for altitudes in the LEO region (i.e. <800km), affecting both AE9 and AP9 models.
The error bars for the inner zone electrons are poorly constrained at all energies. The Van Allen Probes sensors have detected no electrons with energies >1.5 MeV; past measurements of such are ambiguous. It is unknown if this current environment state is temporary or the nominal condition.”

## Slide 16: Solar Activity Forecast: Solar Minimum Today and Maximum estimated for 2025
https://www.swpc.noaa.gov/news/solar-cycle-25-forecast-update
Image Credit: NASA
Notes: The Shields-1 mission demonstrates the feasibility of adding low volume shielding into the CubeSat/SmallSat Structure. The majority of all CubeSats and SmallSats have no significant radiation protection to reduce the TID of both trapped belt and SPE protons.

## Slide 17: Solar Particle Event Animation
https://spaceplace.nasa.gov/solar-activity/en/
Image Credit: NASA

## Slide 18: Solar Particle Event (SPE) Radiation Estimate: Polar Low Earth Orbit
Low volume Z-Shielding reduces potentially SPE catastrophic impacts on commercial parts
Shields-1 Protects Commercial Parts: thin shielded CubeSats have increased risk for TID critical part failures during Solar Max, such as commercial regulators, memory, and processors.
Image Credit: NASA
Chart: Thickness (cm)
| 0.19800000000000001 | 0.46500000000000002 | 0.77 | 1.1100000000000001
Rad (Si) | 750 | 432 | 276 | 183
 | 451 | 338 | 253
Al (0.535 g/cm2)
SPE Proton Dose by King Model
Notes: We are currently operating at Solar Minimum. The solar cycle will begin again with solar activity increasing early in this decade. (https://www.swpc.noaa.gov/products/solar-cycle-progression). Historically, numerous satellites have had anomalies and failures during increased solar activity. All polar orbiting CubeSat and Small Satellite Missions will experience increased solar particle event radiation over the poles, where there is no protection from the Van Allen Belts. Shields-1 Vault has enough shielding to reduce short duration high dose rate TID levels, where thin shielded CubeSats become at risk for TID failures due to reaching TID limits for the commercial parts. The only NASA commercial part guidelines were prepared for commercial part use at ISS orbits (NASA PD 1258, “Space Radiation Effects on Electronic Components in Low Earth Orbit”, August 1996.), where the Van Allen Belts protect from SPE Solar proton radiation and the only significant radiation contribution is the South Atlantic Anomaly, where commercial parts have time to anneal some of the accumulated TID effects.
This plot was produced using the King Model Solar Particle Event, using Spenvis MULASSIS for shieldings with spherical geometries.
CubeSats and SmallSats being planned or implemented in projects today with commercial parts need to address the risk associated with the upcoming solar cycle progression of increased solar activity.
Shields-1 and associated Z-Shielding possibilities have demonstrated the ability to prepare for hazardous radiation orbits, whether trapped belt or increased solar activity radiation

## Slide 19: Z-Shielding Characteristics
Low atomic number materials graded or layered to higher atomic number materials
One piece structure
  Continuous metallic properties: thermal and electrical continuity
  Manufacturing methods: diffusion bonding, welding, plasma spray
  Machining examples: milling, hot wire, and water jet
  Thickness reduced by over half compared to Aluminum baselines
Al Ti Ta
Z-Shielding layered example
Space Radiation
High Energy protons and electrons
Attenuated protons and electrons
For many low earth orbits: electron radiation can be effectively shielded and the risks for internal charging substantially reduced with Z-Shielding

## Slide 20: Z-Grade Shielding Materials and Technology Development
Z-Grade Shielding from Titanium and Tantalum Diffusion Bonding
256 Hrs. (Diffusion Zone 5 mils Thick)
U.S. Patent No. 10,600,522, 24 March 2020, “Method of Making Thin Atomic (Z) Grade Shields”, D.L. Thomsen III.
U.S. Patent No. 10,039,217, 31 July 2018, “Methods of Making Z-Shielding.” D.L. Thomsen III, R.J. Cano, B.J. Jensen, S.J. Hales, and J.A. Alexa.
U.S. Patent Application No. 20170032857, 2 February 2017, “Atomic Number (Z) Grade Shielding Materials and Methods of Making Atomic Number (Z) Grade Shielding.” D.L. Thomsen III, S.N. Sankaran, and J.A. Alexa.
D.L. Thomsen III, W. Kim, and J.W. Cutler. “Shields-1, A SmallSat Radiation Shielding Technology Demonstration”, 29th AIAA/USU Conf. on Small Sat., SSC15-XII-9, August 2015.
U.S. Patent No. 8,661,653, 4 March 2014, “Methods of Making Z-Shielding.” D.L. Thomsen III, R.J. Cano, B.J. Jensen, S.J. Hales, and J.A. Alexa.
LaRC
Z-Shielding Vault
LaRC Z-Shielding Test Samples
LaRC Shields-1 CubeSat Structure
Product
Relevant Publications:
Image Credit: NASA
Notes: 3 Licenses have been generated for “Methods of Making Z-Shielding”: Space Boosters LLC (commercial license), Z-Rated (commer, and Burlington Medical (evaluation license. “Methods of Making Z-Shielding” was an RD100 Finalist in 2017 and an honorable mention for the NASA Government Invention of the Year in 2018.

## Slide 21: Methods of Making Atomic Number Z-grade Radiation Shielding
Titanium 6-4 (Ti) Tantalum (Ta) Copper (Cu)
Metal Plasma Sprayed Carbon Fiber Fabrics
Schematic of Z-grade Lay-up with Fiber Metal Laminate
Ta on IM-7 Carbon Fiber (CF) Fabric
SEM cross-sectional image
Thickness ~196 - 210mm
Ta
CF
U.S. Patent 8,661,653, 4 March 2014, “Methods of Making Z-Shielding.” D.L. Thomsen III, R.J. Cano, B.J. Jensen, S.J. Hales, and J.A. Alexa.
LaRC Ta Carbon Fiber Laminate, prepared by Vacuum Assisted Resin Transfer Molding (VARTM)
Image Credit: NASA
Image Credit: NASA

## Slide 22: Summary
Z-Shielding structures enable a low volume approach to reducing total ionizing dose (TID) with structural properties
Reduced TID reduces risk of failures associated with ionizing radiation
Shields-1 has increased the development level of one piece Z-Shielding structures with space heritage and all the completed testing requirements associated with Space Flight.
Opportunities for further development:
  Development of material suppliers: Standard Metallurgy and Machine Tooling
  Structure adaptations for the commercial, Academice, and government sectors’ Space Missions Bus and Instrument Application
  Increased structure and spot Shielding applications enable reduced TID failure risks and increases return on investment with longer operational lifetimes
  Tech Transfer Opportunities: Commercial, evaluation licenses, and material transfer agreements: http://technology.nasa.gov
  Potential Cooperative Agreements for Technology Development for not just aerospace applications but other commercial, government, and academic radiation shielding applications

## Slide 23: Acknowledgements
J Cutler (UMich)
W Kim (JPL)
B. Blake (Aerospace Corp.)
B. Crain
A. Goff (Luna Innovations)
S. Princiotto (Teledyne)
M. Wrosch (Vanguard Space)
ELaNaXIX Mission NASA CubeSat Launch Initiative
NASA Wallops Flight Facility CubeSat Ground Operations
R. Bryant (LaRC)
M. Jones
R. Lueg
K. Somervill
W. Girard
T. Burns
C. Rhoades
M. Cooney
N. Miller
B. Seufzer
V. Stewart
H. Soto
S. Thibeault
A. Thornton
S. Gayle
C. Fay
M Banchy
D. Keck
J. Applin

## Slide 24: Back-ups

## Slide 25: Spacecraft Overview with Experiments
Excerpt: Shields-1 Brochure, NASA NP-2015-04-608-LaRC

## Slide 26: Spacecraft Overview with Experiments
Excerpt: Shields-1 Brochure, NASA NP-2015-04-608-LaRC

## Slide 27: Spacecraft Overview with Experiments
Excerpt: Shields-1 Brochure, NASA NP-2015-04-608-LaRC

## Slide 28: Aluminum (Al) Incidence Angle Dependence on Total Ionizing Dose (TID)
Chart: Incident Angle (Degrees)
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85
0.857 g/cm2 | 204.1111 | 177.0556 | 143.6111 | 163.6944 | 141.9722 | 142.9722 | 130.5 | 120.1111 | 105.5 | 96.1389 | 81.9722 | 70 | 60.0556 | 50.1944 | 41.3889 | 31.8889 | 23.4389 | 13.6806
1.28 g/cm2 | 78.8611 | 81.25 | 88.3056 | 81.6667 | 76.7222 | 76 | 70.8611 | 66.4444 | 60.1111 | 56.5833 | 50.6667 | 45.5278 | 40.5556 | 34.3056 | 28.5556 | 23.2667 | 17.4139 | 9.2194
2 g/cm2 | 47.2222 | 47.1111 | 47.6944 | 49.8333 | 49.4167 | 46.0833 | 44.8056 | 42.4722 | 39.3889 | 36.8889 | 33.5556 | 30.6667 | 27.1889 | 24.0333 | 20.8167 | 16.7833 | 11.8833 | 5.5278
3 g/cm2 | 52.1667 | 45.0278 | 28.4167 | 35.0833 | 32.8333 | 32.0556 | 30.3889 | 29.25 | 27.725 | 26.0694 | 24.5083 | 22.5194 | 20.4667 | 18.0972 | 15.0833 | 11.9389 | 7.6139 | 3.4972
Chart: Incident Angle (Degrees)
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85
0.857 g/cm2 | 5200 | 5119.4444 | 4955.5556 | 4655.5556 | 4250 | 3758.3333 | 3208.3333 | 2616.3889 | 2023.3333 | 1453.0556 | 940.2778 | 527.5 | 233.2778 | 70.5556 | 8.4333 | 0.17933 | 3.3583e-07 | 0
1.28 g/cm2 | 1105.5556 | 1084.4444 | 1028.6111 | 937.2222 | 821.1111 | 683.6111 | 538.6111 | 395 | 264.0556 | 155.6667 | 75.8333 | 27.8611 | 6.3111 | 0.67389 | 0.0073417 | 2.5011e-07 | 0 | 0
2 g/cm2 | 76.9167 | 74.6389 | 68.0833 | 57.8333 | 32.6667 | 21.075 | 11.7278 | 5.4194 | 1.945 | 0.46583 | 0.058583 | 0.00092667 | 1.8647e-06 | 0 | 0 | 0 | 0 | 0
3 g/cm2 | 0.86472 | 0.81583 | 0.685 | 0.50417 | 0.16783 | 0.06725 | 0.018236 | 0.0023697 | 0.00011017 | 3.225e-06 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Incident angle dependence used to determine shielding FOV slab diameters.
In order to receive greater than 95% of the proton radiation through a shielding slab the incident angles need to be at least 75 degrees.
No electrons contribute to dose from incident angles greater than 70 degrees.
SPENVIS: Shieldose-2 from AP8min-AP8Max Model Al half-sphere results with trigonometric determined incident angle dependencies of areal density in a slab geometry for GTO.
Reference: D.L. Thomsen III, W. Kim, and J.W. Cutler. “Shields-1, A SmallSat Radiation Shielding Technology Demonstration”, 29th AIAA/USU Conf. on Small Sat., SSC15-XII-9, August 2015.

## Slide 29: Calibration Calculations
Vault Dosimeter (uDos0) during full sun phase with all other dosimeters in operation: 14.4 +/- 0.4 (operated at 26.0 +/- 1.4 deg) and 14.3 +/- 0.6 (during the two months in operation at an average lower temperature)
UDos1-7: 14.2 +/- 0.4 (all dosimeters operated at 20.5-20.8 deg C with 1.0 deg C standard deviation) The temperature was stabilized by the spacecraft spin and the full sun environment, during the periods the data was collected for the dose depth curve measurements.
The main propagated error contribution came from the initial dosimeter calibrations at 26 deg C, described on next slide.
The thermal drift correction from 26.0 deg to 20.5-20.8 deg C was calculated from 0.3%/deg C as described in the Teledyne Microdosimeter User Manual and added to the 26 deg C calibration.
Areal density error from errors in material thicknesses, which were measured to at least with 4 digits of precision across the material in at least 5 places do not increase the propagated error further.

## Slide 30: Co60 Calibrated Dosimeters
Calibrated at Aerospace Corporation at 26 deg C with a 100 Curie Cobalt-60 Irradiator at 0.82 m from the source. Each microdosimeter was exposed at a rate of 32,778 urads/sec for 90 seconds.

## Slide 31: Z-Grade Radiation Shielding Compared to Baseline Aluminum
Chart: Comparison of Z-Shielding Materials and Aluminum Baseline
| 6 | 3 | 3.02
 | 70.0277 | 73.5659 | 81.9479
2.08 1.33 1.26 1.69 | 84.3301 | 89.6875 | 90.8939 | 84.2532
Total ionizing dose over a 17 day accumulation period
Polar Low Earth Orbit, 85 deg inclination, 500 km altitude
Al (0.465 cm)
AlTi (0.378 cm)
AlTiTa
(0.429 cm)
Al (0.624 cm)
Al (1.11 cm)
Al (2.22 cm)
AlTiTa (0.483 cm)
Notes: The majority of the radiation contribution has been from the South Atlantic Anomaly, slide 24. Z-Shielding performed within error of aluminum samples at lower areal densities, which can be explained by the shielding performance for removing the outer electrons at high latitudes. At higher areal densities the aluminum performance better as expected for shielding protons more effectively from the South Atlantic Anomaly

## Slide 32: Dosimetry with the South Atlantic Anomaly (SAA)
Image Credit: NASA
Shielding Samples Behind mDosimeters (mDOS)s
Relative Radiation levels
0
100
1st Pass
2nd Pass (near SAA Center)
AlTiTa (2.08 g/cm2)
3rd Pass
1st Pass
2nd Pass (near SAA Center)
3rd Pass
Al (1.69 g/cm2)
1st Pass
2nd Pass (near SAA Center)
3rd Pass
Al (6.00 g/cm2)
Lower total dose rate
Total dose rate similar to Al (1.69 g/cm2)
Pass differences between samples
Notes: AlTiTa (2.08 g/cm2) dose rates differ than the Aluminum samples during the 3rd Pass, where there is no apparent dose rate increase. The total dose for AlTiTa (2.08 g/cm2) over this 12 hr period was 0.1036 Rad and 0.1056 Rad for Al (1.69 g/cm2), and 0.0995 Rad for Al (6.00 g/cm2)

## Slide 33: Radiation Measurements over the Poles: Influenced by Space Weather
7/22/19 04:23 UTC
SAA Contributions
Notes: On 7/22/2019: There was a minor geomagnetic disturbance over the poles due to solar wind activity. The orange line is a dosimeter behind a thin aluminum shield of 1.33 g/cm2. It is highlighted at 7/22/19 04:23 UTC, because it was over the South Pole at the time and showed a variation in the distance between the inflection points of the curve. The inflection points of the curve are related to the satellite orbital position over the poles (max radiation, i.e steepest slope). and the equator (min radiation). The blue line is a dosimeter behind a 6.0 g/cm2 shield. The blue line iterations over time have less variance of the inflection point distances which is related to the orbital period, suggesting minimal effects from a geomagnetic disturbance, which may elevate electron radiation, but would have little or no effect on the dosimeter behind the thicker shielding.

## Slide 34: Radiation Measurement over Satellite Position and Space Weather
Image Credit: AGI
Notes: The NOAA satellite environment slide lower right for 7/22/2019, show the geomagnetic disturbance timing, which shows the it was occurring .

## Slide 35: Geolocation over South Pole
22 Jul 2019
04:23
NOAA Space Weather Report: minor geomagnetic storm from solar wind hitting Earth, 21-22 July 2019
Image Credit: AGI
Notes: Shields-1 was over the South Pole on 7/22/2019 at 04:23 UTC, which is during the period of the geomagnetic disturbance. This was a minor disturbance. I would hypothesize that much greater radiation measurements would occur over a larger geomagnetic disturbance in the near future, as solar activity is expected to increase from the current minimum. On the NOAA Universal Time axis. The tick marks are 3 hrs, which indicates the estimated Kp was elevated, although it was minor. The minor elevated Kp indicates that solar weather was disturbing the geomagnetic field.
Based on the King’s SPE modeled results for solar protons, high solar activity from solar particle events would increase the dose rate over the poles, so that all dosimeter channels would be operating for low, medium, and high during a solar particle event.

## Slide 36: PLO SPE Dose Compared with Trapped Radiation
Sphere Shielding | Areal Density (g/cm2) | Thickness (cm) | Trapped Belts TID Total (Rad (Si)/Year) | SPE King Sphere Model, (Rad (Si))
Al | 0.535 | 0.198 | 1383+/-47 # | 750+/-5
Al | 1.26 | 0.465 | 90.9 +/-2.7 | 432 +/- 7
Al | 1.69 | 0.624 | 84.3 +/-2.5 | 345 +/- 9
Al | 3.02 | 1.11 | 73.6 +/-3.2 | 183 +/- 11
AlTi | 1.33 | 0.378 | 89.7 +/-2.7 | 451 +/- 6
AlTiTa20 | 2.08 | 0.429 | 84.3 +/-2.5 | 338 +/- 6
AlTiTa40 | 3.02 | 0.483 | 81.9 +/-3.4 | 253 +/- 6
For typical thin CubeSat shielding 0.20 cm (0.080 in), yearly trapped dose is 1383 Rad with 750 Rad from SPE increases total dose to 2133 Rad. Adding a two fold increase for the trapped belt radiation uncertainty brings the total radiation near the TID lifetime of many commercial parts after an SPE
Z-Shielding enables TID reduction for trapped belt radiation and SPEs with low volume
Enables TID protection for commercial parts in multiple orbits
# Spenvis Mulassis AP8 min AE8 Max Modeled Sphere Result
Bold Shields-1 Experimental Results
SPE King Model radiation estimates with SPENVIS MULASSIS sphere geometry
Notes: All CubeSats and SmallSats with commercial electronic parts today being planned and fabricated will have heightened risk for TID induced parts failures due to upcoming solar activity in the next solar cycle. Shields-1 is currently the only CubeSat where significant radiation protection has been implemented into the design and structure for reducing TID risks for both trapped belt and solar protons for commercial part TID risk reductions.

## Slide 37: GTO Modeled Radiation Example
2p steradian = 180 degrees radiation (front only)
Geosynchronous Transfer Orbit (GTO) Environment: 1 year at 36000 km apogee, 240 km perigee, and 23o inclination.
Extreme Radiation Environment where satellite moves through the maxima of the inner proton and outer electron belts.
11 hour orbital period, spends most time in outer electron belt
SPENVIS MULASSIS AP8min AE8max Model: Slab Orientation
https://spenvis.oma.be
Image Credit: NASA
Notes: The low volume Z-Shielding Enables CubeSat missions in GTO and subsequent GEO orbits with commercial parts for TID risk reduction.

## Slide 38: Z-Shielding Estimated Performance GTO Environment 1 of 2
Slab Shielding | Areal Density (g/cm2) | Thickness (cm) | Modeled TID (Proton (p) & Electron (e)) (Rad (Si))2pistr omnidirectional | Modeled TID Total (Rad (Si)
Al | 0.535 | 0.198 |  | 
Al | 1.26 | 0.465 | 918 +/- 125 p, 2385 +/- 88 e | 3303 +/- 153
Al | 1.67 | 0.624 | 662 +/- 101 p, 581 +/- 38 e | 1243 +/- 108
Al | 2.08 | 0.770 | 451 +/- 80 p, 308 +/- 24 e | 759 +/- 84
Al | 2.60 | 0.963 | 355 +/- 63 p, 186 +/- 14 e | 541 +/- 65
Al | 3.02 | 1.11 | 302 +/- 50 p, 204 +/- 16 e | 506 +/- 52
Al | 6.00 | 2.22 | 201 +/- 40 p, 88 +/- 9 e | 289 +/- 41
AlTi | 1.33 | 0.378 | 947 +/- 130 p, 1834 +/- 78 e | 2781 +/- 152
AlTiTa10 | 1.76 | 0.404 | 786 +/- 152 p, 223 +/- 28 e | 1009 +/- 152
AlTiTa20 | 2.08 | 0.429 | 587 +/- 81 p, 80 +/- 12 e | 667 +/- 82
AlTiTa30 | 2.60 | 0.454 | 626 +/- 103 p, 73 +/- 13 e | 699 +/- 108
AlTiTa40 | 3.02 | 0.483 | 516 +/- 87 p, 47 +/- 11 e | 563 +/- 88
GTO Environment: 1 year at 36000 km perigee, 240 km apogee and 23o inclination
Notes: GTO is typically required to enter long term Geosynchronous Orbit (GEO) to transfer from GTO, a highly elliptical orbit, to the daily operatonal GEO orbit for many applicatons and even out of low earth orbit. GTO has a more hazardous radiation environment than GEO, because it traverses the center of the inner proton and outer electron orbits. Modeled using SPENVIS MULASSIS AP8min AE8max slab model which is a 2pi steradian omnidirectional model. The low volume Z-shielding enables CubeSats and SmallSats to be developed with commercial parts for GTO and GEO Orbits. As shown in the tables, Shielding areal densities

## Slide 39: Z-Shielding Estimated Performance GTO Environment 2 of 2
Slab Shielding | Areal Density (g/cm2) | Thickness (cm) | Modeled TID (Proton (p) & Electron (e)) (Rad (Si)) 2pistr omnidirectional | Modeled TID Total (Rad (Si)
AlTa10 | 1.76 | 0.499 | 212 +/-24 p, 768 +/- 127 e | 980 +/- 129
AlTa20 | 2.08 | 0.525 | 626 +/- 94 p, 98 +/- 15 e | 724 +/- 95
AlTa30 | 2.60 | 0.550 | 456 +/- 75 p, 34 +/- 10 e | 490 +/- 76
AlTa40 | 3.02 | 0.576 | 403 +/- 64 p, 57 +/- 12 e | 460 +/- 65
AlTiTa10Ti | 1.15 | 0.203 | 1084 +/- 128 p, 1373 +/- 72 e | 2457 +/- 147
AlTiTa20Ti | 1.49 | 0.203 | 953 +/- 126 p, 294 +/- 31 e | 1247 +/- 130
AlTiTa30Ti | 2.58 | 0.228 | 695 +/- 95 p, 116 +/- 16 e | 811 +/- 96
AlTiTa40Ti | 3.00 | 0.254 | 698 +/- 106 p, 100 +/- 17 e | 798 +/- 107
Notes: The shielding with the most aluminum versus titanium had improved performance at the expense of thickness reduction.