## Slide 1: Enabling Sustained Presence Using Recyclables (ESPUR)
44th Annual Meeting of the Adhesion Society, Virtual
February 22-25, 2021
1NASA Langley Research Center, Hampton, VA 23681, USA
2NASA Internship, Fellowship, and Scholarship Program, NASA Langley Research Center, Hampton, VA, 23681, USA
Christopher J. Wohl1, Bryce L. Horvath1, Peter M. Strohmaier2, Sarah E. Gorski2, Haley M. Ketteler2, Alec B. Werner2, Nasef A. Junaid2,
and Sidney L. Eichelberger2

## Slide 2: Reusable Materials for Space Exploration
In-space manufacturing will be critical to enable increased mission endurance and future mission independence from Earth.
The Problem: Mission resupply becomes increasingly difficult as we reach further from Earth
  Extended timeline from recognition of need to site arrival
  Risk mitigation is inhibited by launch mass limitations
The Need:
  In-space manufacturing capability amenable to a broad array of applications
Quantitative Impact: development of recyclable/reusable material will enable launch mass savings, longer mission duration, and greater mission Earth-independence
Image credit: NASA

## Slide 3: Challenge
Spares on Earth
Spares on ISS
ISS Model
Corrective
Preventative
Failures
Re-Supply
Losses
Spares Aboard
On-Board Fabrication, Reuse, Recycling
ESPUR Mission
Diagram adapted from: Owens, Andrew, and Olivier De Weck. "Systems Analysis of In-Space Manufacturing Applications for the International Space Station and the Evolvable Mars Campaign." AIAA SPACE 2016. 2016. 5394.

## Slide 4: The ESPUR Concept
Enable Sustained Presence Beyond Low Earth Orbit (LEO)
Via Recyclable Feedstocks
Andrew Owens and Olivier De Weck. "Systems Analysis of In-Space Manufacturing Applications for the International Space Station and the Evolvable Mars Campaign", AIAA SPACE 2016, AIAA SPACE Forum, (AIAA 2016-5394)

## Slide 5: Components of ESPUR Material
Key
Epoxy Microparticle
Copoly(carbonate-urethane) polymer coating
Diels Alder Functionalities
Notes: discuss that ESPUR made PCU, and coated Epoxy particles with it, but we have not yet tested PCU-coated microparticles (mechanical testing), nor have we incorporated diels alder functionalities to the coated particles

## Slide 6: Tunability of ESPUR Material
50 mm
Copoly(carbonate urethane) polymer
  Thermal properties
  Mechanical properties
  Rheological properties
Epoxy microparticles
  Particle size
  Particle coating thickness
  Particle organization
Polycarbonate
Urethane Linkage
Image credit: NASA

## Slide 7: Polymer Coating-CPCU
2011, Macromol. Rapid Commun., 32, 1379-1385.
2012, Green Chem., 14, 1728-1735.
Image credit: NASA
A
B
Notes: Polycarbonate hard-block synthesis example

## Slide 8: Tunability of ESPUR Material
Copoly(carbonate urethane) polymer
  Thermal properties
  Mechanical properties
  Rheological properties
Epoxy microparticles
  Particle size
  Particle coating thickness
  Particle organization
Flory-Fox Equation
R2=0.93
Polycarbonate
Urethane Linkage

## Slide 9: Tunability of ESPUR Material
Copoly(carbonate urethane) polymer
  Thermal properties
  Mechanical properties-determined to be dependent on polycarbonate molecular weight
  Rheological properties
Epoxy microparticles
  Particle size
  Particle coating thickness
  Particle organization
Polycarbonate
Urethane Linkage
Low Molecular Weight Polycarbonate
Tg > RT
High Molecular Weight Polycarbonate
Tg < RT
Image credit: NASA

## Slide 10: Tunability of ESPUR Material
Polycarbonate
Urethane Linkage
Chart: Carbonate Oligomer Molecular Weight, g/mol
| 771.6 | 340.1 | 445.18 | 3915.41 | 1590.07
 | 1152 | 2460 | 1350 | 8.57 | 338
Copoly(carbonate urethane) polymer
  Thermal properties
  Mechanical properties-closely follows a trend enabling estimation of mechanical properties a priori
  Rheological properties
Epoxy microparticles
  Particle size
  Particle coating thickness
  Particle organization

## Slide 11: Tunability of ESPUR Material
Polycarbonate
Urethane Linkage
*Number of cycles refers to number of times feedstock has been healed, reused/recycled or reshaped.
Healing Efficiency | Number of Cycles*
10 Cycles
Chart: Target Healing Efficiency (%)
| First Few Cycles | Remaining Cycles
 | 90 | 85
2 GPa
5 MPa
Copoly(carbonate urethane) polymer
  Thermal properties
  Mechanical properties-TARGET mechanical properties and healing efficiency calculated from literature examples
  Rheological properties
Epoxy microparticles
  Particle size
  Particle coating thickness
  Particle organization

## Slide 12: Tunability of ESPUR Material
Copoly(carbonate urethane) polymer
  Thermal properties
  Mechanical properties
  Rheological properties-properties comparable to PLA at much lower temperatures
Epoxy microparticles
  Particle size
  Particle coating thickness
  Particle organization
Polycarbonate
Urethane Linkage
Viscosity of PLA filament from: Zhu, Pu, "Polymer Materials Via Melt Based 3D Printing: Fabrication and Characterization" (2018). All Theses. 2895.
https://tigerprints.clemson.edu/all_theses/2895

## Slide 13: Tunability of ESPUR Material
Copoly(carbonate urethane) polymer
  Thermal properties
  Mechanical properties
  Rheological properties
Epoxy microparticles
  Particle size-particles are synthesized using precipitation polymerization. Repeatability and scalability have both been addressed up to 0.5 kg scale.
  Particle coating thickness
  Particle organization
Chart: Monomer Weight %
| 0.1 | 0.05 | 0.2 | 7.4999999999999997E-2 | 0.15 | 0.3 | 0.5 | 0.4
DAT | 4.1615 | 1.936 | 9.3931 | 3.5503 | 6.1735 | 8.9364 | 5.2175 | 5.6497

## Slide 14: Tunability of ESPUR Material
Copoly(carbonate urethane) polymer
  Thermal properties
  Mechanical properties
  Rheological properties
Epoxy microparticles
  Particle size
  Particle coating thickness- controlled by concentration of reactive species with polymerization occurring in the presence of particles
  Particle organization
Chart: Percentage of total number of particles
Uncoated
Coated
Chemical Bonding
Hydrogen Bonding
Image credit: NASA

## Slide 15: Tunability of ESPUR Material
Copoly(carbonate urethane) polymer
  Thermal properties
  Mechanical properties
  Rheological properties
Epoxy microparticles
  Particle size
  Particle coating thickness
  Particle organization-leveraging concepts from Shannon Entropy, scale-free research to enable generation of durable 3D architectures
S.A. Beznosyuk et al., Informational Approach to Self-Assembling Aggregation of Colloidal Nanoparticles, Materials Science and Engineering C, 2009, 29, 884-888.
Compressive Load

## Slide 16: Reversible Click Chemistry
Maleimide-furan reaction
Prog. Polym. Sci. 2013, 38, 1-29.
Maleimide
  Derived from maleic anhydride
Furfuryl amine
  Naturally-derived
B. Zhang, et. al., Polym. Chem., 2015,6, 7368-7372

## Slide 17: Maleimide End-Cap Synthesis
B. Zhang, et. al., Polym. Chem., 2015,6, 7368-7372

## Slide 18: NMR Analysis of Intermediates*
*Final product has been synthesized. NMR analysis has been completed but spectrum cannot be shown due to lack of laboratory access

## Slide 19: Ready for the Next Phase of Research … Proof of Concept*
+
+
*Picture taken in March, 2020
Image credit: NASA

## Slide 20: Conclusions/Next Steps
In-space manufacturing can be a game-changing approach to realize long duration missions beyond low Earth orbit (LEO)
Utilization of recyclable feedstocks to extend mission lifetimes and reduce risk seems like a natural extension
Next Steps
  Need to develop CPCU formulations for filament extrusion toward 3D printing applications
  Need to evaluate the efficacy of click-chemistry functionalities integrated into CPCU
  Need to demonstrate reversible assembly

## Slide 21: Acknowledgements
Advanced Materials and Processing Branch
  Joseph G. Smith Jr., John W. Connell
NASA Marshall Space Flight Center
  Tracie Prater, Michael Fisk
NIFS Program, IRAD Program
Carlex Morales Cruz
Spring, 2018
Matthew Swift
Summer, 2018
Image credit: NASA
Team Lightning Bugs,
Ben Zusmann
Jonah Sayre
Jailyn Hernandez
Spring, 2019
Nasef Junaid
Fall 2019
Sidney Eichelberger
Fall, 2019
Charity Williams
Summer, 2019
Alec Werner
Summer, 2019 2020
Haley Ketteler
Summer, 2020
Sarah Gorski
Summer & Fall, 2020
Spring, 2021