## Slide 1: Simultaneous Development and Robust Optimization of a Microstructure Dependent Material Model
Karl Garbrecht1, Nolan Strauss1, Geoffrey Bomarito2, Patrick Leser2, Jacob Hochhalter1
1 University of Utah
2 NASA Langley Research Center
Leveraging Sequential Monte-Carlo Methods to Enhance Symbolic Regression Analysis

## Slide 2: Multi-Scale Material Models
Macroscale Response = f(Continuum Properties) =
Design Scale of Interest
https://en.wikipedia.org/wiki/Fracture
https://en.wikipedia.org/wiki/Forging
f(Physical, Meso, Micro Properties)
Scale of
Variables
Notes: .

## Slide 3: Homogenized Parameters
- texture tensor 1
cos sim / projection
magnitude, mean/var
1 - S. Kotha, D. Ozturk 2019 (presentation of several microstructural homogenization parameters)
Parameter homogenization
provides method around microscale modeling
loss of fidelity
potentially abstract variables
additional processing steps
- mean
- variability
Texture
Scalars
Tensors, Vectors, Scalars
Grain Size

## Slide 4: Symbolic Regression
Genetic Programming Symbolic Regression (GPSR) - proposes, evaluates, and evolves solutions given fitness function and training data
+
b
a
SIN
*
X
Initial Solution Generation
Potential Solutions
Evolution
Evaluation
Propose New Models
Model Represented as a Directed Acyclic Graph
Chromosome | 6 | 5 | 4 | 3 | 2 | 1 | 0
Main | + | * | a | sin() | a | b | X
Topological | 5 | 4 | - | - | - | - | -
 | 1 | 3 | - | 0 | - | - | -

## Slide 5: GPSR Traditional Regression
Effectively, regression analysis without specifying model form
Similar to traditional regression:
  response will be given as a function of selected input variables (implicit possible)
  data quality important (size, scaling, variability, domain sample locations)
  extrapolation and interpolation accuracy unknown
Unlike traditional regression:
  coefficient significance/feature selection is automated
  no closed form solution: computationally expensive, no guarantee of optimum solution
  larger data set required (possibly much larger)
  currently developing technique, less established

## Slide 6: Data Collection and Generation
Continue to Machine Learning
VPSC
Microscopy Data
Calibrate with Measured Data
Response Variables
Create Training Data
Independent Variables
Response Variables
&
https://en.wikipedia.org/wiki/Tensile_testing
Mechanical Test Data
Homogenized
Material Parameters
Measured Data
Measured &
Modeled Data

## Slide 7: GPSR Solution Results
Error Metric | Results
MAPE | 0.78
MSE | 140
Test 1
Scatter Plot of 500 Randomly Sampled Data Points vs. GPSR Predicted Solution
Plot of 3 Randomly Sampled Specimen Stress-Strain Training Data vs. GPSR Predicted Solution
ε = Plastic Strain (%) α = Texture Alignment β = Texture Alignment Variability
MAPE = Mean Absolute Percent Error (%)
MSE = Mean Square Error (MPa^2)
ε = True Plastic Strain (%) σ = True Stress (MPa)

## Slide 8: GPSR Results Discussion
Deterministic Algorithm: deterministic fitness
  can find linear or nonlinear multi- dimensional solutions
  prone to generate complex or overfitted models with many parameters and terms
  must select “best” model out of final pool of models
Probabilistic Algorithm: Bayesian fitness
  allows for unbiased model comparisons wrt observed data
  evaluation includes model complexity
Complexity vs Fitness

## Slide 9: GPSR with Sequential Monte Carlo (SMC)
Set Equation Priors Around Optimized Parameters
Sequentially Temper Posterior and Evaluate Equation
Selection via Bayesian Comparison
Initial Solution Generation
Potential Solutions
Evolution
Evaluation
Propose New Models
Bayesian Reformulation of Evaluation
- Iteratively Increase T,
- Then use Fractional Bayes Factor3 (FBF) for model selection
3 – A. O’Hagan, 1995
9

## Slide 10: SMC Implementation
Probability Weighted Particle Filtering

## Slide 11: SMC-GPSR Solution Results
Error Metric | Results
MAPE | 2.2
NMLL | 410
Scatter Plot of 500 Randomly Sampled Data Points vs. GPSR Predicted Solution
Plot of 3 Randomly Sampled Specimen Stress-Strain Training Data vs. GPSR Predicted Solution
ε = Plastic Strain (%) α = Texture Alignment
MAPE = Mean Absolute Percent Error (%)
NMLL = Normalized Marginal Log Likelihood
ε = True Plastic Strain (%) σ = True Stress (MPa)

## Slide 12: SMC-GPSR Results Discussion
Direct comparison difficult due to different hyperparameters (HP)
 | Islands | Population | Generations | Data Set Size | Test Error (%) | Training Error (%) | Time
Parallel GPSR | 50 | 3,000 | 4,000 | 2,000 | 0.78 | 0.75 | 11 hr
GPSR | 1 | 100 | 1000 | 100 | 6.5 | 6.2 | 2 min
GPSR | 1 | 100 | 100 | 100 | 4.0 | 3.6 | <0.5 min
SMC – GPSR | 1 | 100 | 100 | 100 | 2.2 | 2.0 | 1.5 hr
SMC – GPSR | 1 | 100 | 100 | 100 | 2.3 | 2.2 | 1.5 hr
Initial Observations of SMC-GPSR Implementation
good performance vs generation (more testing required due to influence of initialization)
models generalized from small data set
computationally expensive
additional HPs associated with SMC
HP
Run

## Slide 13: Conclusions and Continuing Efforts
With current serial implementation:
GPSR with Bayesian selection feasible
significant increase in run time to achieve equivalent results to deterministic GPSR
Continuing Efforts:
full-scale testing of parallel implementation
formal evaluation against GPSR
improve algorithm efficiency

## Slide 14: Acknowledgments and Reference
Shravan Kotha, Deniz Ozturk. 2019. Somnath Ghosh. “Parametrically homogenized constitutive models (PHCMs) from micromechanical crystal plasticity FE simulations, part I: Sensitivity analysis and parameter identification for Titanium alloys”. International Journal of Plasticity, vol.120, p. 296-319. ISSN 0749-6419.
Thi Le Thu Nguyen, Francois Septier, Gareth W. Peters, and Yves Delignon. 2015. “Efficient Sequential Monte-Carlo Samplers for Bayesian Inference”. IEEE Transactions on Signal Processing, vol. 64, no. 5, p. 1305-1319, DOI: 10.1109/TSP.2015.2504342.
O'Hagan, A. 1995. “Fractional Bayes Factors for Model Comparison”. Journal of the Royal Statistical Society: Series B (Methodological), vol. 57: p. 99-118. DOI: 10.1111/j.2517-6161.1995.tb02017.
Acknowledgments
References
The authors are grateful for experimental data made available by MID3AS Additive Manufacturing Challenge and project support from NASA Grant 80NSSC20M0128