## Slide 1: Rapid Inspection & Characterization Summary Report
Brief Summary of Completion / Accomplishment:
Automated NDE Systems – Functional Demonstrations: Completed functional demos for two systems, the GIRAFFE infrared flash-based thermal inspection unit coupled with a 2D ultrasonic scanning inspection system and the PULSAR laser ultrasonic system. In the case of the GIRAFFE system, the instrument was disassembled and shipped to an aircraft maintenance facility where it was reassembled and used to inspect a portion a Boeing VC-25 in the current fleet used for Air Force One presidential aircraft. In both cases, the inspection data were verified to ensure the technology produced expected results. The systems performed as expected and were deemed functionally operational.
Characterized In-Situ NDE Capability during AFP: Completed experiments to characterize the detection capabilities of the inspection system for Foreign Object Debris (FOD) consisting of poly backing paper. Pieces of the poly backing paper were inserted into an uncured composite layup mockup, and inspected with the In-Situ IR thermography system. The test results successfully demonstrated using thermographic methods, FOD pieces as small as 1/16th inch by ½ inch tall could be detected through a layer of uncured composite.
Integrated NDE Framework – Open Sourced: an open-source, integrated tool suite and associated framework that streamlines the inspection and defect disposition process through model-assisted inspection optimization, automated defect analysis of NDE data, and mapping of NDE data into finite element analysis software was demonstrated on a stiffened panel with impact damage.
Beginning TRL 2, Final TRL 5-6

## Slide 2: Rapid Inspection & Characterization Publications
Author(s) | Title | Where presented
Christopher Sacco, Anis Baz Radwan, Ramy Harik, Michel Van Tooren | Automated Fiber Placement Defects: Automated Inspection and Characterization | SAMPE 2018
Francisco Hernando Quintanilla and Cara Campbell-Leckey | Lebedev Scheme for Ultrasound Simulation in Composites | Ultrasonics, Volume 86, Pages 28-40, May 2018
Harold A. Haldren, Daniel F. Perey, William T. Yost, K. Elliott Cramer, and Mool C. Gupta | Swept-Frequency Ultrasonic Phase Evaluation of Adhesive Bondingi ni Tri-Layer Structures | The Journal of the Acoustical Society of America, Vol. 145, Issue 3, Mar 2019
Christopher Saccoa, Ramy Harika, Elizabeth Gregory | On Machine Learning in Engineered Materials | Composite Structures / Elsevier, April 2019
V. Hafiychuk, K. Wheeler and K. Gee | Computational Non-destructive Evaluation Improving Ultrasonic Interrogation of Complex Geometry Composite Parts | NASA/TM-2019-220197, June 2019
K. E. Cramer, Daniel F. Perey, Joshua L. Brown | The Application of Line Scan Thermography Using Multiple Collaborative Robots | Review of Progress in QNDE, July 2019
Peter D. Juarez, Elizabeth D. Gregory | In Situ Thermal Inspection of Automated Fiber Placement Manufacturing | CAMX 2019, Sept 2019
Ryan Canfield, Matthew O'Donnell, Ivan Pelivanov, Thomas Muller-Wirts, Jan Ahrens, Jill Bingham, Gary Georgeson, Barry Fetzer | Distance and angle correction system (DACS) for a kHz A-scan rate pump-probe laser-ultrasound inspection | NDT&E International Journal – Elsevier, 2020
Patricia A. Howell, Editor | NDE Methods and Capabilities Handbook | NASA/TM-2020-220568; Vol. 1 and 2, Feb 2020
Christopher Sacco, Anis Baz Radwan, Andrew Anderson, Ramy Harik, and Elizabeth Gregory | Machine Learning in Composites Manufacturing: Case Study of Automated Fiber Placement Inspection | Journal of Manufacturing and Materials Processing, Mar 2020
Lingyu Yu and Zhaoyun Ma | Various Types of Defects Detection in Flat and Curved Laminated Composite Plates Using Nonintrusive Lamb Wave System | ASME Journal of Nondestructive Evaluation, Diagnostics and Prognostics of Engineering Systems, Jan 2021

## Slide 3
Composites: Rapid Inspection & Characterization
Problem
Development and appplication of inspection of composite structures is labor intensive, which lengthens the product development cycle.
Objective
Develop and demonstrate nondestructive evaluation (NDE) systems and enabling technologies to fully inspect and rapidly disposition findings in complex composite structures.
Results
Developed NDE tools (Low-cost, non-contact laser ultrasound system on robot; Infrared thermography coupled with ultrasound system for global/local inspection; Collaborative Robot inspection system)
Developed on-head, in-process inspection system, to detect and report anomalies during automated fiber placement.
Demonstrated a framework for automation of NDE data acquisition, defect characterization, and transfer of data to structural analysis
Published “NDE Methods and Capabilities Handbook” with consensus guidance on applicability, cost, speed of various inspection methods
Significance
Automated inspection and disposition procedures increase throughput on inspection, provide better quality control, and provide more information early in manufacturing development
Robotic and In-process inspection increases efficiency and enables machine learning
Thermal-based on-head inspection during automated fiber placement
Automated UT Enhancement to IR Inspection (GIRAFFE)
Defects
Auto Defect classification & recording