## Slide 1: Presence of Metal Aerosols on the International Space Station
Amanda Rodell

## Slide 2: Overview
Passive Aerosol Samples
  Methods
  Analysis
  Locations
Calculations
Comparison to OSHA Regulations
Notes: Stop using question intonation

## Slide 3: Passive Aerosol Samplers (PAS)
Positioned on Bacterial Filter Elements (BFEs)
Placed only in the US orbital section
PAS Sample Size: 3.75 cm2
  Typical Filter Size: 751.74 cm2
  Ratio: ≈1:200
2018 PAS-D US LAB Bay 3
2018 PAS-B NOD2D3
Notes: Carbon tape for SEM sample

## Slide 4: Sampler Description
7 Passive Aerosol Samplers
  5 samples inside each sampler
2016 Samples were taken over 2,4-,8-,16-,and 32-day periods with each duration being taken over samples 1 through 5 respectively
2018 Samples were taken over a 26-day period
For analysis, the data was modified to units per day to simplify the comparison process

## Slide 5: Sample Analysis
Analyzed by Scanning Electron Microscopy (SEM) and Energy Dispersive X-Ray Spectroscopy (EDS)
Particle Information Collected: Composition, Size, Weight, and Shape
RJ Lee Group, prepared for Meyer, M. E., Ph.D., “NASA ISS Sampling and Particle Characterization Study - Payload 2 Passive Aerosol Samplers (PAS),” Unpublished Data, 2018

## Slide 6: Occupational Air Pollution Limits
Presented in milligrams per cubic meter for an 8-hour workday
  Also presented less commonly in parts per million (ppm)
Highest level of a given pollutant an employee can be exposed to without increasing the risk of adverse health effects

## Slide 7: Sampler Locations 2016
Node 1 – Eating
Node 2 – Docking
Node 3 – Exercise and Hygiene
US Lab – Lab Experiments
Permanent Multipurpose Module (PMM) – Storage

## Slide 8: Sampler Locations 2016
Passive Sampler ​ | Location​ | Relevant Activity​ | Date of Active Sampling​
PAS B​-16 Day Sample | Node 1 Deck 1​ (NOD1D3) | Eating​ | 12/8/16​
PAS D​-16 Day Sample | Node 3 Deck 3​ (NOD3D3) | Exercise & Hygiene ​ | 12/15/16​
PAS E -32 Day Sample | Permanent Multipurpose Module (PMM​) | Storage​ | 12/22/16​
PAS F​-32 Day Sample | Node 2 Deck 2​ (NOD2D3) | Docking ​ | 11/29/16 & 12/15/16​
PAS G​-8 Day Sample | Node 3 Forward 3​ (NOD3F3) | Exercise & Hygiene​ | 11/29/16​
PAS J​-32 Day Sample | US Lab Bay 1 Starboard Deck​ (LAB1SD1) | Experiments​ | 12/8/16 & 12/22/16​
PAS K-16 Day Sample | US Lab Bay 3 Port/Deck (LAB1PD3) ​ | Exercise & Hygiene​ | N/A​

## Slide 9: Sampler Locations 2018
Node 1 – Eating
Node 2 – Sleeping and Docking
Node 3 – Exercise and Hygiene
US Lab – Lab Experiments

## Slide 10: Sampler Locations 2018
Passive Sampler ​ | Location​ | Relevant Activity​
PAS B (NOD2D3)​ | Mid-bay HEPA Return​ | Sleeping & Docking​
PAS D (LAB1PD3)​ | US Lab Bay 3 Port/Deck ​ | Lab Experiments ​
PAS E (NOD1D3)​ | ​ | Eating​
PAS F (NOD3D3)​ | Mid-bay HEPA ​ | Exercise & Hygiene​
PAS G (NOD3F3)​ | ​ | Exercise & Hygiene​
PAS H (NOD3OA3)​ | Overhead Supply Diffuser​ | Exercise & Hygiene​
PAS K (NOD3O2)​ | Upper Plenum Assembly​ | Exercise & Hygiene​

## Slide 11: Aluminum Passive Aerosol Sampler 2018
Chart: 
| H-1 | H-2 | H-3 | H-4 | H-5
Al-Cl-Zr | 68.0307 | 11.5394 | 1.4004 | 6.3053 | 3.1938
Al-Fe | 0.78832 | 0.012367 | 10.233 | 0 | 0.027489
Al-Ni-Zn | 0 | 0 | 0 | 0 | 0
Al-Si-Fe | 28.9602 | 0.63949 | 3.9955 | 14.1642 | 3.4659
Al-Sn | 10.8908 | 0.00066529 | 0.00017283 | 0.00031832 | 0.052582
Al-Zn | 0.12559 | 0.26005 | 0.0014707 | 0.015128 | 0.80612
Chart: 
| D-1 | D-2 | D-3 | D-4 | D-5
Al-Cl-Zr | 62.5176 | 489.6293 | 525.2196 | 269.9707 | 66.2657
Al-Fe | 9.9032e-05 | 0.027071 | 0.012198 | 0.046691 | 0.019473
Al-Ni-Zn | 0 | 0 | 0 | 0.0089029 | 0
Al-Si-Fe | 2.837 | 0.032015 | 0.10863 | 0.77228 | 1.23
Al-Sn | 0 | 0 | 0 | 0 | 0
Al-Zn | 0 | 0.042533 | 1.0402 | 7.4968 | 36.4067
Chart: 
| E-1 | E-2 | E-3 | E-4 | E-5
Al-Cl-Zr | 5.5818 | 2.3847 | 42.8167 | 161.5426 | 77.0853
Al-Fe | 0.029223 | 0.28728 | 0.092194 | 0.37744 | 0.19763
Al-Ni-Zn | 0.005451 | 0.43649 | 0.020432 | 0.72749 | 0.141
Al-Si-Fe | 0.2364 | 2.6314 | 10.6317 | 10.5072 | 1.6888
Al-Sn | 0.0015554 | 0 | 0 | 0 | 0
Al-Zn | 0.010417 | 0.013337 | 1.0581 | 0.13942 | 0.011611
Chart: 
| F-1 | F-2 | F-3 | F-4 | F-5
Al-Cl-Zr | 997.3718 | 81.3388 | 8.1458 | 7.3556 | 29.1197
Al-Fe | 0.015694 | 2.2422 | 0.014155 | 0.0074301 | 0.13242
Al-Ni-Zn | 0 | 0 | 0 | 0.19502 | 0.73653
Al-Si-Fe | 2.3314 | 32.2791 | 4.8814 | 9.3111 | 7.1231
Al-Sn | 0 | 0 | 0 | 0 | 0
Al-Zn | 2.6212 | 0.049478 | 0 | 0.0007878 | 0.068145
Chart: 
| G-1 | G-2 | G-3 | G-4 | G-5
Al-Cl-Zr | 86.4551 | 58.4163 | 50.3808 | 75.8225 | 88.5199
Al-Fe | 0.64307 | 0.0012574 | 0.054593 | 21.0655 | 0
Al-Ni-Zn | 0 | 0 | 0 | 0 | 0
Al-Si-Fe | 0.03887 | 0.019193 | 20.8965 | 8.0601 | 0.3961
Al-Sn | 0 | 0 | 0 | 0 | 0
Chart: 
| K-1 | K-2 | K-3 | K-4 | K-5
Al-Cl-Zr | 81.842 | 5.2526 | 8.1571 | 6.3144 | 5.9442
Al-Fe | 0.042218 | 0.20779 | 0.17931 | 0.44452 | 2.0319
Al-Ni-Zn | 0 | 0 | 0 | 0 | 0
Al-Si-Fe | 1.1789 | 4.3215 | 1.2889 | 1.8112 | 11.5572
Al-Sn | 0 | 0 | 0 | 0 | 0
Al-Zn | 0.37993 | 0.026225 | 0 | 0.33132 | 0.11317
F NOD3D3 (Hygiene)
E NOD1D3 (Eating)
G NOD3F3 (Hygiene)
H NOD3OA3 (Hygiene)
K NOD3O2 (Hygiene)
D LAB1PD3 (Experiments)
Chart: ng/cm2/day
| B-1 | B-2 | B-3 | B-4 | B-5
Al-Cl-Zr | 11.9677 | 8.7066 | 168.5859 | 15.8189 | 7.0079
Al-Fe | 0.00054366 | 0.45134 | 0.0097414 | 0.079308 | 0.040655
Al-Ni-Zn | 0 | 0 | 0 | 0 | 0
Al-Si-Fe | 4.6992 | 2.2135 | 1.0997 | 6.0833 | 1.2635
Al-Sn | 0 | 0 | 1.0576 | 0 | 0
Al-Zn | 0.042122 | 0 | 0 | 0 | 0.00028983
B NOD2D3 (Sleeping)
Notes: Al-Cl-Zr: PAS F-1 has 1134 particles, this is not the most several other locations have >1000 particles (like E-5 and E-4), so the particles from this section might be larger in comparison to the others. For PAS G, the total particle count is between 300 and 500, and for PAS D it goes from 100 to 500 (D-3 has 292 particles)

## Slide 12: Elemental Summaries
The values for each sampler were averaged to minimize the effect of any outliers.
With Elemental Summaries, we can locate dominating species or locations
  Example: Al-Cl-Zr dominate Aluminum particles
Chart: 2018 Aluminum
| NOD2D3 (Sleeping) | LAB1PD3 (Lab) | NOD1D3 (Eating) | NOD3D3 (Hygiene) | NOD3F3 (Hygiene) | NOD3OA3 (Hygiene) | NOD3O2 (Hygiene)
Al-Cl-Zr | 42.4174 | 282.7206 | 57.8822 | 224.6663 | 71.9189 | 18.0939 | 21.502
Al-Fe | 0.11632 | 0.021107 | 0.19675 | 0.48237 | 4.3529 | 2.2122 | 0.58115
Al-Ni-Zn | 0 | 0.0017806 | 0.26617 | 0.18631 | 0 | 0 | 0
Al-Si-Fe | 3.0718 | 0.99599 | 5.1391 | 11.1852 | 5.8822 | 10.245 | 4.0316
Al-Sn | 0.21151 | 0 | 0.00031107 | 0 | 0 | 2.1889 | 0
Al-Zn | 0.0084823 | 8.9973 | 0.24657 | 0.54792 | 0.016639 | 0.24167 | 0.17013

## Slide 13: Calculation Overview
Goal: Estimate concentration of aerosols from PAS mass per unit area
Information used:
  Duration of sample: Assume that deposition occurs at a constant rate throughout the sample period
  Surface Area of Filters: Assuming that the samples are a valid estimate for particle distribution and there would be a uniform distribution over the entire filter
  Average Volumetric Flow Rate: Assuming that particles are evenly distributed through the air and a well mixed environment

## Slide 14
Venta USA (venta-usa.com)
Notes: Make the square more transparent
Put down visual aid or something along those lines

## Slide 15: OSHA Comparison Conversion
Concentration of particles bearing a given element on the sample
Duration of sample. This allows us to get a theoretical ug/cm2/day
Surface area of filters. Assuming that the samples are a valid estimate for particle distribution and there would be a uniform distribution over the entire filter.
Average volumetric flow rate of air per filter per day. Assuming that particles are evenly distributed through the air
Exposure that will be compared to OSHA limitations.
Notes: Bring up the uncertainty
Explain the rational behind it, be more specific , point out assumptions and why we did, what we did
-air flow is different in every filter
-ug/cm2 that are used are averaged

## Slide 16: 8 Hour Exposure ≠ 24 Hour Exposure
12 Breaths Per Minute
Tidal Volume: 0.5 L per Breath
Volume Per Day: 8.64 m3
Volume Per 8 Hours: 2.88 m3
Multiply OSHA limits by volume per 8 hours
Multiply ISS levels by volume per 24 hours
Biology. Authored by: OpenStax. Provided by: OpenStax College. Located at: http://cnx.org/contents/185cbf87-c72e-48f5-b51e-f14f21b5eabd@9.44:1/Biology. License: CC BY: Attribution
Notes: Assume that the air is evenly mixed throughout the ISS, even though they spend 8 hours in NODE 2 sleeping

## Slide 17: Results

## Slide 18: Element vs Percent of OSHA Limit
Chart: 2016 & 2018 Percent of OSHA Limit
| Aluminum | Titanium | Vanadium | Chromium | Manganese | Iron | Cobalt | Nickel | Copper | Zinc | Bromine | Strontium | Zirconium | Molybdenum | Silver | Cadmium | Indium | Tin | Antimony | Cesium | Barium | Lanthanum | Cerium | Neodymium | Tungsten | Platinum | Gold | Lead | Bismuth
2016 | 0.00027478 | 1.3528e-06 | 3.1036e-05 | 0.0036287 | 0.065995 | 0.0076682 | 0.00057701 | 8.7459e-06 | 0.00033362 | 0.018146 | 0.095117 | 1.3374e-05 | 0.00060128 | 7.184e-08 | 1.8412e-06 | 0 | 4.2914e-07 | 0.00010782 | 8.7281e-07
2018 | 0.0015271 | 4.1874e-05 | 9.9927e-05 | 0.010143 | 0.043301 | 0.006691 | 0.0001986 | 2.5115e-05 | 0.0005552 | 0.059072 | 0.1434 | 0.00035552 | 0.00041039 | 4.4514e-07 | 0.00014644 | 1.1669e-08 | 3.2611e-08 | 0.0044928 | 5.155e-06
Notes: Change the scale and put in where the osha limit (in a red line)
Change to non-scientific notation

## Slide 19
Chart: 2016 & 2018 Percent of OSHA Limit
| Aluminum | Titanium | Vanadium | Chromium | Manganese | Iron | Cobalt | Nickel | Copper | Zinc | Bromine | Strontium | Zirconium | Molybdenum | Silver | Cadmium | Indium | Tin | Antimony | Cesium | Barium | Lanthanum | Cerium | Neodymium | Tungsten | Platinum | Gold | Lead | Bismuth
2016 | 0.00027478 | 1.3528e-06 | 3.1036e-05 | 0.0036287 | 0.065995 | 0.0076682 | 0.00057701 | 8.7459e-06 | 0.00033362 | 0.018146 | 0.095117 | 1.3374e-05 | 0.00060128 | 7.184e-08 | 1.8412e-06 | 0 | 4.2914e-07 | 0.00010782 | 8.7281e-07
2018 | 0.0015271 | 4.1874e-05 | 9.9927e-05 | 0.010143 | 0.043301 | 0.006691 | 0.0001986 | 2.5115e-05 | 0.0005552 | 0.059072 | 0.1434 | 0.00035552 | 0.00041039 | 4.4514e-07 | 0.00014644 | 1.1669e-08 | 3.2611e-08 | 0.0044928 | 5.155e-06
Notes: Extend y-axis to 100
Make it 1 digit after the E
Put in a bonus slide with elements where there are no osha limits/no data
Look into elements where there are “no data” and see if they might be a concern to human health
For paper, put in future work/possibilities
-error bars, sources of error,

## Slide 20: Cadmium
OSHA 8-hour Limit: 0.005 mg/m3
ISS Estimated Levels:
  2016: 0.0016 ug/m3
  2018: 0.0024 ug/m3
    51% increase from 2016 to 2018
Possible Sources
  Electroplating Steel
  Rechargeable Ni-Cd Batteries
  Plastic Stabilizer
Chart: 2018 Cadmium
| NOD1D3 (Eating) | NOD2D3 (Sleeping) | LAB1PD3 (Lab) | NOD3D3 (Hygiene) | NOD3F3 (Hygiene) | NOD3OA3 (Hygiene) | NOD3O2 (Hygiene)
Cd-bearing | 0.42764 | 0.014364 | 0.0011309 | 0.0019174 | 0.00047653 | 4.8833 | 0.087787
Cd-rich | 1.3927 | 0.51251 | 16.3215 | 1.337 | 0.20073 | 48.5673 | 0.062141
Chart: 2016 Cadmium
| NOD1D3 (Eating) | NOD2D3 (Docking) | LAB1SD1 (Lab) | LAB1PD3 (Hygiene) | NOD3D3 (Hygiene) | NOD3F3 (Hygiene) | PMM (Storage)
Cd-bearing | 0 | 0 | 0 | 0 | 0.10025 | 0 | 0
Cd-rich | 0 | 0 | 0.023395 | 0.0017305 | 27.7674 | 21.0642 | 0
Notes: Try to put the graphs in the same order (NOD1, NOD2, etc.)
State 1000 difference between mg to ug
Put possible sources of elements

## Slide 21: Cadmium
RJ Lee Group, prepared for Meyer, M. E., Ph.D., “NASA ISS Sampling and Particle Characterization Study - Payload 2 Passive Aerosol Samplers (PAS),” Unpublished Data, 2018

## Slide 22: Nickel
OSHA 8-hour Limit: 0.05 mg/m3
ISS Estimated Levels:
  2016: 0.011 ug/ m3
  2018: 0.0072 ug/ m3
    34% decrease from 2016 to 2018
Possible Sources
  Steel Production
  Electroplating
  Household uses
    Jewelry, Clothing Buttons, Cooking Utensils
Chart: 2018 Nickel - Ni-rich
| NOD1D3 (Eating) | NOD2D3 (Sleeping) | LAB1PD3 (Lab) | NOD3D3 (Hygiene) | NOD3F3 (Hygiene) | NOD3OA3 (Hygiene) | NOD3O2 (Hygiene)
Ni-rich | 20.4813 | 6.4713 | 164.1211 | 27.6363 | 1.5836 | 1.2259 | 1.353
Chart: 2016 Nickel - Ni-rich
| NOD1D3 (Eating) | NOD2D3 (Docking) | LAB1SD1 (Lab) | LAB1PD3 (Hygiene) | NOD3D3 (Hygiene) | NOD3F3 (Hygiene) | PMM (Storage)
Ni-rich | 0.4141 | 0.060881 | 0.0011919 | 329.1961 | 0.77289 | 9.2323 | 0.0014427
Notes: Get pictures from analysis of particles to get some idea
Round to 2 numbers after the 0’s
Put estimate down

## Slide 23: Nickel
RJ Lee Group, prepared for Meyer, M. E., Ph.D., “NASA ISS Sampling and Particle Characterization Study - Payload 2 Passive Aerosol Samplers (PAS),” Unpublished Data, 2018

## Slide 24: Silver
OSHA 8-hour Limit: 0.01 mg/m3
ISS Estimated Levels:
  2016: 0.00060 ug/ m3
  2018: 0.0020 ug/ m3
    225% increase from 2016 to 2018
Possible Sources
  Water Disinfection
  Thermal and Electrical Conductor
Chart: Silver 2018
| NOD1D3 (Eating) | NOD2D3 (Sleeping) | LAB1PD3 (Lab) | NOD3D3 (Hygiene) | NOD3F3 (Hygiene) | NOD3OA3 (Hygiene) | NOD3O2 (Hygiene)
Ag-bearing | 0.19137 | 0.093879 | 0.14148 | 0.68701 | 0.0055108 | 0.094006 | 1.5993
Ag-rich | 0.070984 | 0.040259 | 0 | 0.00791 | 0.0024963 | 0 | 0.00261
Ag-S | 7.5601 | 11.3053 | 3.1032 | 0.37303 | 6.2802 | 23.9248 | 0.62383
Ag-S-Cl | 0.11104 | 0.017479 | 0.077918 | 0.0096257 | 0.0041652 | 0.015035 | 0.053861
Ag-Si-S | 0.23749 | 0.04536 | 0.0016619 | 0.6592 | 0.0010213 | 0.16013 | 3.3075
Chart: 2016 Silver
| NOD1D3 (Eating) | NOD2D3 (Docking) | LAB1SD1 (Lab) | LAB1PD3 (Lab) | NOD3D3 (Hygiene) | NOD3F3 (Hygiene) | PMM (Storage)
Ag-bearing | 0.0018515 | 2.5121 | 8.0388e-05 | 0.0042976 | 0.0021128 | 0.0021023 | 0
Ag-rich | 0.96452 | 0 | 0.0022184 | 0.020512 | 0.037448 | 3.3928 | 0.00040673
Ag-Zn | 0 | 0 | 11.545 | 0.16743 | 0 | 0.026319 | 0
Notes: Check in

## Slide 25: Silver
RJ Lee Group, prepared for Meyer, M. E., Ph.D., “NASA ISS Sampling and Particle Characterization Study - Payload 2 Passive Aerosol Samplers (PAS),” Unpublished Data, 2018

## Slide 26: Conclusions
Cadmium, Nickel, and Silver are the elements closest to their OSHA limits
All elemental estimated concentrations are below 1% of their OSHA permissible exposure limits
Causes of increases or decreases in concentrations are uncertain and will need further investigation.
Sampling will be repeated in December 2021

## Slide 27: Acknowledgments
Dr. Luz Marina Calle
Dr. Wenyan Li
Dr. Marit Meyer
NASA Office of STEM Engagement
Internship Coordinators
Exploration Systems and Development Office
RJ Lee Group

## Slide 28: Thank You
Amanda Rodell
Amanda.J.Rodell@Nasa.gov
Arzf5@mst.edu

## Slide 29: Additional Graph Information
All metals listed in graphs were detected on an ISS PAS
  Analysis data wasn’t available, or OSHA limit not established
Metals without OSHA Limits: Neodymium, Lanthanum, Tungsten,& Strontium
Metal's data unavailable: Vanadium, Manganese, Cobalt, Hafnium, Indium, & Gold

## Slide 30: Elements without regulations
Possible Health Affects
  Neodymium:
  Lanthanum:
  Tungsten:
  Strontium: