## Slide 1: Breakout Session 1
  Qualified Material Process and Material Property Suite for Additive Manufacturing
  Bring Your Questions!
Sam Cordner
MSFC Materials Engineer
Doug Wells
MSFC Structural Materials Engineer,
Technical Specialist – Damage Tolerance
Public Use - Quality Leadership Forum 2021 - 27 May 2021

## Slide 2: AM Certification: Governing Principles
Understanding and Appreciation of the AM process
Integration across disciplines and throughout the process
Discipline to define and follow the plan
Control what you do :: Evaluate what you get

## Slide 3: Classification

## Slide 4: Building a Foundation
Planning for AM certification does NOT start with a part
AM Control Plan should define how the foundation for certification is structured and how it operates
  Equipment and Facility Controls
  Personnel Training
  Process/Machine Qualification
  Material Properties
  Statistical Process Controls

## Slide 5: Qualified Material Process (QMP)
Begins as a Candidate QMP
Defines aspects of the basic, part agnostic, fixed AM process:
  Feedstock
  Fusion Process
  Thermal Process
Enabling Concept
  Machine qualification and re-qualification, monitored by…
  Process control metrics, SPC, all feeding into…
  Design values
Sub-QMP-A, B or C
Sub-QMP-A, B or C
Sub-QMP-A, B or C
Foundational Process Controls
MPS
Data
SPC Criteria
PCRD
Data
Design
Properties
PPP
Design Process
ECP
Qualification Maintenance Calibration
Training Plan
Training
Definition of
Material Process
Machine 2
Machine 3
Machine “n”
Qual. of Material Process
Feedstock
Specification
AM Process
Post-AM Process
QMP-A, B or C
Machine 1
Registration
(A or B)
NASA-STD-6033

## Slide 6: The QMP becomes the Foundation!

## Slide 7: QMP Tables

## Slide 8: Material Properties
The Material Property Suite (MPS) consists of four inter-related entities:
Data Repository
Design Values
Process Control Reference Distribution (PCRD)
SPC acceptance criteria for witness testing

## Slide 9: Material Properties
Material properties and design values in additive manufacturing require modifications to the approach typical of traditional metallic materials, with requirements more similar to that used in composites CMH-17
Important distinctions arise due to the sensitive nature of the process and individualistic aspect of AM machines. Each machine is a foundry!
Traditional supplier roles and responsibilities shift with the AM machine making the final material product form and part. (Casting analogy)
  AM Process Vendor is responsible for material integrity

## Slide 10: Material Properties – Data Repository
Includes data from
  Qualification testing
  Material Characterization
  Pre-production Article Evaluations
Contains all data needed for
  Setting Design Values
  Property equivalence evaluations and QMP Registration
  Setting the Process Control Reference Distribution
Grouping of data
Group data by
QMP = Material/process/heat treat
“Combinable” conditions for design

## Slide 11: Material Properties – Design Values
Design Values
Statistically substantiated
Applicable sources of variability included
Utilizes all appropriate data sources in Repository
May include additional margin for safety
Design
Values
m
DV

## Slide 12: Material Properties – PCRD
Process Control Reference Distribution
Statistically describes nominal witness behavior of a machine
Utilizes all appropriate sources of witness coupon data in Repository
Used to set acceptance criteria for witness tests
PCRD
m
s

## Slide 13: Material Properties – SPC
Statistical process controls are important in sustaining certification rationale
Statistical equivalency evaluations substantiate design values and process stability build-to-build
  Process qualification
  Witness testing
  Integration to existing material data sets
  Pre-production article evaluations
Equivalency of material performance is an anchor to the structural integrity rationale for additively manufactured parts
The dark and scary place most manufacturers are NOT used to operating….

## Slide 14: Material Properties Suite
Statistical Process Control
Acceptance Criteria
Derived from PCRD
Acceptance criteria for
witness tests
PCRD
m
s
SPC Acceptance Criteria for Witness Testing
Design
Values
DV
m

## Slide 15: Material Properties Suite – PCRD and SPC Criteria
Witness test acceptance is not intended to be based upon design values or “specification minimums”
Acceptance is based on witness tests reflecting properties in the MPS used to develop design values
Suggested approach
  Acceptance range on mean value
  Acceptance range on variability (e.g., standard deviation)
  Limit on lowest single value

## Slide 16: Registering a QMP to an MPS

## Slide 17: Bootstrapping a QMP and MPS
When new AM processes are first established, an MPS may not yet exist to conduct the registration process. In such cases, the material test data generated to produce the QMP are also used to generate the initial MPS (i.e., bootstrapping), and the QMP is registered to the new MPS by default.
Additional data generated from the QMP are used to populate preliminary MPS PCRDs and other material properties to enable registration of additional QMPs.

## Slide 18: Foundation Complete!!
A basis to begin designing AM parts with certification intent is feasible once the foundation is laid.
Foundation is now ready to support AM part development in an environment with suitable rigor to establish certification.

## Slide 19: Conclusions
QMP’s define the material state for one machine
MPS define the overall material property. It can be broken up in different ways depending on needs
QMP and MPS are the foundations for material control and material design values
Control what you do::Evaluate what you get

## Slide 20
Back Up Slides

## Slide 21: Table 14

## Slide 22: Table 15

## Slide 23: Table 16

## Slide 24: Summary of Methodology

## Slide 25: Applicability
Adaptive technologies—where process parameters change based on active feedback during the manufacturing process—are not allowed without a tailored, point-design methodology.
  e.g. Electron beam powder bed fusion (E-PBF)

## Slide 26: High Consequence of Failure
A part shall be designated as Class A, High Consequence of Failure, if failure of the part leads to a catastrophic hazard or the part is defined as Mission Critical Hardware by the Program Office.
Class A parts shall not:
  Be made from polymeric materials
  Be fasteners
  Contain printed threads.

## Slide 27: Negligible Consequence of Failure
Parts not designated Class A or Class C shall be designated as Class B.
Class B parts shall not:
  Be fasteners
  Contain printed threads.

## Slide 28: Negligible Consequence of Failure
A part shall be designated as Class C, Negligible Consequence of Failure, provided that ALL of the following criteria (see the next slide) are satisfied:
  Failure of part does not lead to any form of hazardous or unsafe condition.
  Failure of part does not eliminate a critical redundancy.
  Part does not serve as primary or secondary containment.
  Part does not serve as redundant structures for fail-safe criteria per NASA-STD-5019.
  Part is not designated “Non-Hazardous Leak Before Burst” per NASA-STD-5019.
  Failure of part does not cause debris or contamination concerns per NASA-STD-6016 .
  Part meets requirements for off-gassing, flammability, and compatibility requirements as described in NASA-STD-6016.
  Failure of part causes only minor inconvenience to crew or operations.
  Failure of part does not alter structural margins or related evaluations on other hardware.
  Failure of part does not adversely affect other systems or operations.
  Failure of part does not affect minimum mission operations.

## Slide 29: Exempt Parts
A part shall be designated as Exempt provided that all of the following criteria are satisfied, and it meets all criteria for Class C, which exempts it from all other requirements in this NASA Technical Standard:
  The part does not require any form of structural assessment.
  The part does not permanently interface to, or attach to, the launch vehicle, spacecraft, habitable module, or any subsystems thereof.
  Except for use in habitable crew spaces, the part does not provide any functionality or serve any purpose to the launch vehicle, spacecraft, or any subsystems thereof.

## Slide 30: Secondary Classification
Secondary classification is for Class A and B parts only and is used to determine appropriate levels of process control
A
B
Structural Demand
AM Risk
AM Risk
Structural Demand
AM Risk
Class
A2
Class
A4
Class
A3
Class
A1
Class
B2
Class
B1
High
High
High
High
High
Low
Low
Low
Low
Low
AM Risk
Class
B4
Class
B3
High
Low

## Slide 31: Structural Demand - Metals
Structural Demand
AM Risk
AM Risk
Class
A2
Class
A4
Class
A3
Class
A1
High
High
High
Low
Low
Low
Material Property | Criteria for Low Structural Demand
Loads environment | Defined or bounded loads environment
Environmental degradation | Only due to temperature
Ultimate strength | Minimum margin* ≥ 0.3
Yield strength | Minimum margin* ≥ 0.2
Point strain | Local plastic strain < 0.005
High cycle fatigue, improved surfaces | Cyclic stress range (including any required factors) ≤ 80% of applicable fatigue limit
High cycle fatigue, as-built surfaces | Cyclic stress range (including any required factors) ≤ 60% of applicable fatigue limit
Low cycle fatigue | No predicted cyclic plastic strain
Fracture mechanics life | 20x life factor
Creep strain | No predicted creep strain
*Margin = [sdesign/(soperation * safety factor)] – 1 | 

## Slide 32: Structural Demand - Polymers
Structural Demand
AM Risk
AM Risk
Class
A2
Class
A4
Class
A3
Class
A1
High
High
High
Low
Low
Low
Analysis Input/Material Property | Criteria for Low Structural Demand
All Materials | 
Loads Environment | Defined or bounded loads environment
Environmental Degradation | Only due to temperature and moisture, if specific environmental performance data exist. Design environment temperature does not cross the Tg.
Fatigue | Cyclic stress range (including any required factors) ≤ 50% of applicable fatigue limit
Sustained stress/creep strain | No sustained stress† and no predicted creep strain
Material with elongation at failure ≥ 3% in application environment | 
Ultimate strength | Minimum margin* ≥ 0.5
Yield strength‡ | Minimum margin* ≥ 0.3
Material with elongation at failure < 3% in application environment | 
Ultimate strength# | Minimum margin* ≥ 2.0
†Includes assembly stress (tight snap fit connections, shrink fits, fastener preloads) and operational stress
‡Yield strength defined by secant modulus to specified strain, by specified offset strain, or as otherwise defined by structural assessment requirements
#Ultimate strength assessed against local maximum principal stress at stress concentrations (brittle material design rules) for low ductility materials
*Margin = [sdesign/(soperation * safety factor)] – 1

## Slide 33: AM Risk
Additive Manufacturing Risk determination will be unique to each material and type of process
AM risk = HIGH, if cumulative AM Risk score >=5
Structural Demand
AM Risk
AM Risk
Class
A2
Class
A4
Class
A3
Class
A1
High
High
High
Low
Low
Low
 | Metallic |  | Polymer |  |  | 
 | L-PBF | DED | L-PBF | Score For |  | 
Additive Manufacturing Risk |  |  |  | Yes | No | Score
All surfaces and volumes can be reliably inspected, or the design permits adequate proof testing based on stress state? | X | X | X | 0 | 5 | 
As-built surface can be fully removed on all fatigue-critical surfaces? | X | X |  | 0 | 3 | 
Surfaces interfacing with support structures are fully accessible and the as-built surface removed? | X | X | X | 0 | 3 | 
Structural walls or protrusions are the equivalent of ≥ 8 trace, (e.g., melt pool, bead, scan path) widths in cross section? | X |  | X | 0 | 2 | 
Structural walls or protrusions are the equivalent of ≥ 2 trace, (e.g., melt pool, bead, scan path) widths in cross section? |  | X |  | 0 | 2 | 
Critical regions of the part do not require support structure? | X | X | X | 0 | 2 |