## Slide 1: OCE Engineering Research & Analysis Program
Hot Structure Concepts and Materials for Space Exploration Project
Sandra P. Walker, Structural Mechanics and Concepts Branch
and
Kristopher E. Wise, Advanced Materials and Processing Branch
NASA Langley Research Center
July 29, 2021

## Slide 2: Background
State-of-the-Art Thermal Protection System (TPS)
  Ablative TPS material
  Not reusable
  Relatively thick TPS
  TPS bonded to underlying carry structure
  TPS is brittle - no load carrying capability
  TPS has been manufactured in tiles due to its brittle nature
Carbon-Carbon (C/C) Hot Structure Capability
  Can be reusable for some applications - heat flux conditions
  More dimensionally stable and lower volume requirements
  Structural material - can carry large loads at high temperatures
  Potential to provide lighter weight, integrated TPS/structure solution with reduced manufacturing/fabrication time/cost
  Shortcomings: large material variability and low interlaminar tension (ILT) and shear (ILS) strength
Mars Science Laboratory Heat Shield
Notes: Engineering R&A Goals- Initiative seeks to restore NASA’s investments in basic engineering capabilities in targeted critical areas of discipline-based basic engineering research

## Slide 3: Hot Structure Project Overview
Goal: Deliver advanced knowledge and capability towards developing lightweight, reusable, and dimensionally stable hot structures concepts to enable advanced space exploration missions.
Focus: Improving 2D C/C material system
Two-fold Approach: Improve the performance of hot structures by advancing the computational design of C/C materials and by improving the fundamental understanding of thermal stress response in hot structure concepts
Nozzle Extension
Hot Structure Heatshield
Potential Applications:
  Develop Computational Tools for Modeling the Fabrication Process - make better 2D C/C material – lower variability
  Thermal-Structural Concept Development
  - make better C/C structures – improve ILT and ILS response
Hypersonic Cruise Vehicle
Project Duration: April 8 to Sept 30, 2020 (~ 6 months)
Notes: Engineering R&A Goals- Initiative seeks to restore NASA’s investments in basic engineering capabilities in targeted critical areas of discipline-based basic engineering research

## Slide 4: Team Membership
Name | Role | Organization
Core Team |  | 
Sandra Walker | Project Lead | NASA Langley Research Center
Kris Wise | Computational Tools Lead | NASA Langley Research Center
James Smith | Damage Modeling/Analysis | NASA Johnson Space Center
Carl Poteet | Thermal-Structural Analyst | NASA Langley Research Center
Lauren Raffanello | Thermal-Structural Analyst | NASA Langley Research Center
Andrew Lovejoy | Fabrication/Testing | NASA Langley Research Center
Ronald Kreuger | Damage Mechanics/Analyst | NIA Research Fellow
Jacob Gissinger | Material Modeling/Fluid Dynamics | NASA Postdoctoral Program Fellow
Consultants/Partners |  | 
Stan Bouslog | Thermal Structures Consultant | NASA Johnson Space Center
Steve Rickman | Project/Thermal Consultant | NASA Johnson Space Center
Wally Vaughn | C/C Material System Consultant | NASA Langley Research Center
James Ratcliffe | Damage Testing Consultant | NASA Langley Research Center
David Glass | C/C Materials Consultant | NASA Langley Research Center
Business Management |  | 
Pam Throckmorton | Budget | NASA Langley Research Center
Notes: 8 core team members – who contributed on the project
Then there were also five consulting team members

## Slide 5: Computational Tools for Modeling the Fabrication Process *
Effort focused on developing and applying modeling approaches to help reduce manufacturing time and cost while improving part quality and performance
Examples of problems to be addressed:
  Number of infusion/carbonization cycles required to reach full density
    Matrix resin char yield, structure and connectivity of porosity
  Post-production machining required to correct geometric defects
    Residual stresses and their dependence on thermal history
      Intra and interlayer, fiber/matrix interface, etc.
  Coating compatibility and adhesion for certain applications
    Nuclear Thermal Propulsion, rocket nozzle extensions, leading edges
* POC: Kris Wise, Computational Tools Lead

## Slide 6: Computational Tools for Modeling the Fabrication Process
Approach: Leverage in-house modeling and experimental capabilities along with external collaborations to develop a multiscale understanding of the material system
In-house modeling capabilities
  Quantum mechanical modeling (reactions, properties)
    Small systems, short times, high accuracy
  Classical molecular dynamics (MD) simulations
    Much larger systems and times, accuracy dependent on parameterization
  Reactive MD simulations
    Similar to classical MD, but incorporates chemical reactivity
  Micromechanics and Finite Element Model (FEM)-based fracture mechanics
    Covered later in talk
In-house experimental capabilities: Resin synthesis, composite fabrication, carbonization, structural characterization and mechanical testing

## Slide 7: Overview of Process Modeling Plans
Develop Computational Fluid Dynamic (CFD) model for matrix precursor flow into representative fiber preform structure
Improve CFD model by capturing the effect of stepwise progression of carbon matrix formation within the fiber preform
Adapt REACTER tool to model pyrolysis process for selected precursor chemistry in classical MD simulations
Demonstrate ability to predict structure and morphology of pyrolysis product, both in isolation and in presence of fiber surface
Develop coarse grained representation of initiation and growth of carbon matrix on and between fibers
Starting matrix preform structure
Matrix precursor infusion
Polymer cure and pyrolysis
Predict structure and properties of final composite
Green text: goals for first year
Variables to consider:
Matrix precursor chemistry
Preform structure
Cure/pyrolysis conditions
Infusion parameters (P, T)
Etc…

## Slide 8: Matrix Precursor Infusion Modeling
Example of two-phase flow through fibrous material using BIM
The boundary integral method (BIM) is a highly accurate but computationally expensive method for modeling multiphase flow
The interface (and only the interface) between two fluids is discretized with a mesh
A graph neural network may lend itself to training on BIM data (a mesh is a graph)
A graph-convolutional network may be able to accurately simulate flow through fibrous media, such as woven carbon fiber, at a fraction of the computational cost
BIM model has been demonstrated, machine learning element is still in the very early stages
U∞ : Far-field flow velocity, Ca : Capillary number, t : Simulation time (L/|U∞|)

## Slide 9: Polymer Cure and Pyrolysis
Method Development: REACTER
Gissinger, Jensen & Wise. Macromolecules 53, 22, 9953–9961 (2020).
www.reactor.org
Epoxy Crosslinking Reaction
Collection of new tools for adjusting topology during classical Molecular Dynamics (MD)
  Adding/removing specific bonds, angles, dihedrals, and impropers
  Modifying all force field types as well as atomic charges
  Stabilizing system energy after topology change
  Support for any fixed-valence force field (PCFF, OPLS, etc.)
Parallel implementation in LAMMPS MD package as fix bond/react
Required user input
  Templates of pre- and post-reaction topologies
  A map file relating atoms before and after the reaction

## Slide 10: Polymer Cure and Pyrolysis
Method Development: REACTER
Deletion of Reaction Byproducts
Modeling Bond Scission Reactions
Other Useful Features:
Deleting reaction byproducts
  Water molecules in condensation reactions
  Gas phase byproducts in carbonization
Simulating bond scission reactions
  Mechanical failure in polymers and composites
Computation performance is essentially the same as classical MD, no QM required!

## Slide 11: Polymer Cure and Pyrolysis
Method Development: REACTER
Quantum-informed Reaction Constraints
Potential energy constraint allows REACTER to replicate quantum-accurate bond breaking
Will be applied to ultimate strength calculations of thermosets and composites

## Slide 12: Polymer Cure and Pyrolysis
Polymerization/Carbonization of polyarylacetylene (PAA)
PAA cyclotrimerization reaction
Carbonization moves
Diethynylbenzene polymerized via linear and cyclotrimerization reactions

## Slide 13: Polymer Cure and Pyrolysis
After ~99% polymerization and ~14.5K carbonization reactions
Partially graphitized structure can be starting point for later-stage graphitization simulations
Density: 1.0 g/cm3
Box Size: (13.8 nm)3
Nano-ribbon Formation in polyarylacetylene (PAA)
Slice is 7 Å thick; only rings shown
1:1 Ratio

## Slide 14: Polymer Cure and Pyrolysis
6.7 nm
Connell, J. W., Smith Jr, J. G., Hergenrother, P. M., & Rommel, M. L. (2000). Neat resin, adhesive and composite properties of reactive additive/PETI-5 blends. High performance polymers, 12(2), 323-334.
32K atoms/416 molecules
Density: 1.5-1.8 g/cm3
Box Size: (6.7 nm)3
Polymerization/Carbonization of PERA-1
During carbonization simulation, small molecules are deleted
  Shifts reaction in favor of carbonization
  Average bond orders used to determine species (molecule type)
  Feature added to LAMMPS’ ReaxFF implementation
Temperature Ramp Cycle:
  300K → 3000K at 10 K/ps
  Hold at 3000K for 270 ps
  3000K → 300K at 10 K/ps

## Slide 15: Polymer Cure and Pyrolysis
3952 atoms/52 molecules,
Density=1.07 g/cm3
PERA-1 Carbonized Structures
Fused 5, 6, and 7-membered rings form at onset of graphitization

## Slide 16: Polymer Cure and Pyrolysis
Graphene sheets
Polymer
Technique able to reproduce morphologies observed in transmission electron microscopy images of carbon fibers
Graphene layers are often used to represent carbon fiber surfaces in atomistic simulations
REACTER is being used to create more realistic representations of carbon fibers
Higher Fidelity Representations in Composite Simulations

## Slide 17: On-going Process Modeling Work
Ongoing work supported by the Superlight-weight Aerospace Composites (SAC) project under the STMD Game Changing Development (GCD) program
Continued development of flow modeling for matrix precursor infusion
  Creation of accurate fiber preform geometries
    Computational and based on X-ray CT structures
  Exploration of applying machine learning techniques to accelerate BIM method
Larger simulations of PAA and PERA-1 polymerization and carbonization
Refinement of carbon fiber surface model to improve fiber-matrix representation
Simulations of polymerization/carbonization in presence of carbon fiber surface
Exploration of alternative matrix chemistries with higher char yields in collaboration with synthetic chemists

## Slide 18: Thermal-Structural Concept Development
Objective: Improve thermal stress response to increase operational load capability of hot structures
Analysis Approach:
  Parametric study initiated to study critical thermal stress response in typical/simplified hot structure application
  Investigate use of stitching to improve interlaminar behavior
Apply knowledge towards making better hot structure concepts

## Slide 19: Thermal-Structural Concept Development 2D C/C Material Properties
Initiated effort with consideration of 2D C/C material system
  Synthesized material property data reports
  Needed C/C fabric lamina data to generate high fidelity Finite Element Models (FEM) to evaluate thermal stress response
  Material property set needed for high-fidelity analysis
    Lamina and quasi-isotropic laminate properties
    Coefficient of Thermal Expansion, CTE(T)
    Carbon fiber properties
    Static fracture properties
  References included 7 papers and presentations
  Some properties calculated/estimated based on existing properties
Established a complete C/C and carbon fiber material property data spreadsheet needed for use in high-fidelity finite element thermal-structural analysis

## Slide 20: Thermal-Structural Concept Development Parametric Study- Thermal Stress Analyses
Need to identify critical conditions/locations when interlaminar stresses become severe
  Mechanical loads
  Thermal loads
  Geometric attributes
  Material system configuration
  Boundary conditions
Initiated parametric study on cylindrical curved sections
Initial focus on the shoulder region of a planetary entry heat shield

## Slide 21: Thermal-Structural Concept Development Parametric Study: Thermal Stress Analyses
Generated simplified finite element model
Geometric parametric variables
  Shoulder radius: RSHOULDER
  Vehicle radius: RVEHICLE
  Shoulder thickness
  Circumferential length
  Boundary conditions
Loading Condition variables included thermal, pressure and combined load cases
Example load cases:
Radial Thermal Gradient
Circumferential Thermal Gradient
Applied Pressure
Notes: The parametric range of geometric values evaluated in this study for the half circle and vehicle radii were chosen to somewhat encompass the range of possible radii for advanced hot structure concepts on future aerospace vehicles. Values where analyses were performed included: 1-inch, 5-inch and 10-inch for the shoulder radius and 18-inch, 45-inch, 180-inch, and 1000-inch for the vehicle radius. As a point of reference, existing aerospace vehicles where hot structure concepts could be considered include the Mars Science Lab (MSL), which has an approximately 5-inch shoulder radius and 90-inch vehicle radius. Also, for comparison Orion has approximately a 10-inch shoulder radius and 100-inch vehicle radius, Pioneer Venus had an approximately 45-inch vehicle radius, and Mars Sample Return had an approximately 18-inch vehicle radius. Furthermore, the large radius of 1000-inch used in this study was to evaluate a large radius that would approach a plain-strain solution; that would be somewhat representative of a leading edge on a hypersonic vehicle, or a winged entry vehicle with control surfaces.

## Slide 22: Thermal-Structural Concept Development Parametric Study: Thermal Stress Results
Case | Shoulder Radius (inches) | Vehicle Radius (inches) | Thickness (inches) | Pressure (psi) | Temperature Distribution | Condition | Margin of Safety | Interface Layer
1 | 1 | 90 | 0.17 | 20 | Radial Linear Gradient | Max ILT Stress | -0.01 | 6
 |  |  |  |  |  | Min ILT Stress | -0.03 | 7
2 | 5 | 90 | 0.17 | 20 | Radial Linear Gradient | Max ILT Stress | 0.49 | 6
 |  |  |  |  |  | Max ILS Stress | 0.80 | 6
 |  |  |  |  |  | Min ILT Stress | 0.45 | 7
 |  |  |  |  |  | Min ILS Stress | 0.70 | 7
2b | 5 | 90 | 0.34 | 20 | Radial Linear Gradient | Max ILT Stress | 0.06 | 12
 |  |  |  |  |  | Min ILT Stress | 0.04 | 13
3 | 10 | 90 | 0.17 | 20 | Radial Linear Gradient | Max ILS Stress | -0.08 | 6
 |  |  |  |  |  | Min ILS Stress | -0.16 | 8
Preliminary analysis identified cases where excessive interlaminar stresses occur
More refined analysis needed to design tests/test matrix for experimental study

## Slide 23: Thermal-Structural Concept Development Stitched C/C: Stitching Thread
Prior experimental study yielded preliminary results indicating some benefits of stitching on interlaminar strength
Preliminary micro-mechanics model developed to estimate material properties of carbon thread constructed from carbon fiber
Normalized Strain
Normalized Stress
2-strand thread
3-strand thread
4-strand thread
T300 Carbon fiber properties
Tsai-Wu Damage Model
Results indicated greater strength with less strands
Results indicated greater strain to failure with more strands
T300 Carbon fiber has been procured
Need to have thread manufactured for experimental validation
Estimated T300 Thread Strength, 7 twists/in
2-strand 3-strand 4-strand
Normalized Strain
Normalized Stress

## Slide 24: Thermal-Structural Concept Development Stitched C/C Laminate Analysis
Illustration of stitching C/C laminate:
Plane strain model developed to evaluate stitching
Progressive failure analysis performed
Preliminary results indicated a two order of magnitude increase in fracture toughness
Fracture toughness value can be used as effective value for stitched laminates in unstitched model
3D FEM initiated and can be further developed to evaluate optimal stitch parameters
L=109 mm
Width=5 mm
H=2.159 mm (per layer)
Starter crack 7 mm ahead of first stitch
Stitch element
Full Model
Top solid elements removed
stitching
First stitch failed
Several stitches failed

## Slide 25: Thermal-Structural Concept Development Fracture Mechanics FEM
Higher fidelity 3D model of a Double Cantilever Beam (DCB) specimen
Stitches modeled using spring elements
Computed Mode I energy release rate, GI
Results indicate stitches shielded the delamination front – crack did not propagate
Results published in NASA CR
Need to validate through experimental study
Spring elements
Delamination
front
Bonded
nodes
GI
Specimen width, B

## Slide 26: Concluding Remarks
Computational Tools for Modeling the Fabrication Process
  Developed and demonstrated boundary element based CFD simulations of viscous polymer flow into a simplified representation of a woven carbon fiber preform
  Adapted a molecular dynamics simulation method created for modeling polymerization to address pyrolysis and demonstrated its use for the conversion of phenolic resin to amorphous char
  Work on-going under current GCD project
Thermal-Structural Concept Development
  Parametric studies on curved hot structure concepts initiated
  Micromechanical models of stitching thread developed
  Initiated Fracture-mechanics model development to evaluate effect of stitching
  Carbon fiber and 2D carbon fabric procured for fabrication of test specimens

## Slide 27: References and Publications
References for Computational Tools for Modeling Fabrication Process
Gissinger, J. R.; Jensen, B. J.; Wise, K. E. “Modeling Chemical Reactions in Classical Molecular Dynamics Simulations” Polymer, 128, 211-217, 2017.
Gissinger, J. R.; Jensen, B. D.; Wise, K. E. “REACTER: A Heuristic Method for Reactive Molecular Dynamics” Macromolecules, 53, 9953, 2020.
References for C/C material property spreadsheet
Glass, D. E., Vaughn, W. L., Development of an Advanced Carbon-Carbon (ACC-6) Material Property Database, JANNAF Conference, 2020.
Vaughn, Wallace L, et. al., Interlaminar and In-plane Shear Strengths and Moduli of Carbon-Carbon Composites, The 42nd Annual Conference on Composites Materials, and Structures, January 22-25, 2017, Cape Canaveral, FL
Vaughn, Wallace L, et. al., Mechanical Properties of a Cut Ply Quasi-60 Carbon-Carbon Composite, The 43nd Annual Conference on Composites Mateials, and Structures, January 30th, 2018, Cape Canaveral, FL
https://toraycma.app.box.com/s/ru9sr1uzk0nw6vhilrt8hrmofytpjm1r
Sauder, Cedric, Jacques Lamon, and Rene Pailler. "Thermomechanical properties of carbon fibres at high temperatures (up to 2000 C)." Composites Science and Technology 62.4 (2002): 499-504.
Colmer, T., et al. “Dependence of Fracture Toughness on Delamination Direction in Carbon/Carbon Laminates,” Proceedings of the Joint Army, Navy, NASA, Air Force (JANNAF) Meeting, Dayton, USA, 2019.
Smith, A.J., et al. “Measurements of Mixed Mode-I/II Interlaminar Fracture Toughness of 2D-Woven Carbon/Carbon Laminates,” Proceedings of the 44rd Annual Conference on Composites, Materials, and Structures, Cocoa Beach, 2020.
New Publication
Kruger, R., Analysis of Delamination Growth in Stitched and Unstitched Double Cantilever Beam Specimens Made of Carbon-Carbon Composites, NASA CR-20210011852, March 2021.