## Slide 1: Lunar Simulant Deposition for Evaluating Adhesion
Lunar Surface Science Workshop Virtual Session 10:
Fundamental and Applied Lunar Surface Research in Physical Sciences
August 18-19, 2021
1National Institute of Aerospace, Hampton, VA 23666, USA
2NASA Langley Research Center, Hampton, VA 23681, USA
Lopamudra Das1 and Christopher J. Wohl2,*
*Corresponding Author: c.j.wohl@nasa.gov
**All images are credited to NASA unless otherwise indicated

## Slide 2: The rest of the “Langley Lunar Dust Brigade”
Valerie L. Wiesner1
Keith L. Gordon1
Glen C. King1
Sang H. Choi1
Jonathan J. Hernandez2
Kathryn M. Crossett3
Researchers at nearly every NASA Center and throughout academia and private industry
1NASA Langley Research Center, Hampton, VA 23681, USA
2National Institute of Aerospace, Hampton, VA, 23666, USA
3NASA NIFS Intern, NASA Langley Research Center, Hampton, VA 23681, USA
Place Photo Here*
*Remote work makes group photos tough

## Slide 3: Evaluating passive dust mitigation materials
What do we want to study?
Apollo astronaut glove covered in lunar dust
Image credit: NASA
Flanagan and Goree, Dust release from surfaces exposed to plasma, Physics of Plasma 13, 123504, 2006. Schwan, J., et al., The charge state of electrostatically transported dust on regolith surfaces, Geophy. Res. Lett., 44, 3059, 2017. Godyak. V,. Ferromagnetic enhanced inductive plamsa source. J. Phys. D: Appl. Phys., 46, 283001, 2013. Wang. X et al. https://sservi.nasa.gov/articles/video-dust-charging-and-mobilization/
Image credit: modified from NASA source
Artemis
Dust Particle ………………..
Candidate
Materials
Technology …………
Interaction
Forces …………………………….
?

## Slide 4: How will adhesion force be characterized?
Schematic
Actual Instrument

## Slide 5: How will adhesion force be characterized?
FAccel
FAdh
Fmg
Particle will detach when FAccel is ≥ FAdh
m = particle mass
a = acceleration
f = sonic wand frequency
A = sonic wand amplitude
Sonic Wand Motion

## Slide 6: What is an ideal system to study?
Adhesion forces
Van der Waals
Electrostatic
Magnetic
Chemical
Mechanical
Ideal case: isolated particle

Contributing forces
Gravitation (Earth)
Capillary (ambient atmosphere)

Actual case: aggregated particles
Contributing forces
Cohesion force
Mechanical interlocking
Deformation

Hypothetical case: particle monolayer
Contributing forces
Cohesion force
Mechanical interlocking


## Slide 7: Surface simulant contamination techniques
Aerosolization
Schematic
Vibratory filtration
Schematic
Vibratory motion
Tapping
motion
Simulant
Sieve

## Slide 8: Simulant deposition through aerosolization
Sample preparation
  Weigh simulant to be dispersed in aerosolization chamber (50-250 mg)
  Pour simulant onto ceramic Hirsch funnel positioned within the aerosolization chamber
  Place samples in aerosolization chamber
  Aerosolize simulant with two short bursts from compressed air canister
  Wait for simulant to settle before removing samples and collecting microscopy images

## Slide 9: Simulant deposition through vibratory filtration
Sample preparation
  Weigh simulant to be dispersed in vibratory sieve shaker (0.2-2 g)
  Pour simulant onto sieve
    Sieve No #450 (32 mm openings)
    Sieve No #500 (50 mm openings)
  Assemble sieve(s) and samples, and areal screen in shaker system
  Adjust sieve amplitude settings
  Run shaker system for specific number of tapping sequences
  Wait for simulant to settle before removing samples and collecting microscopy images

## Slide 10: Surface simulant contamination techniques
Aerosolization*
Vibratory filtration*
Sample # | 10 | 35
Simulant mass | 1 g | 1 g
Number of sieves | 2 (#450 and #500) | 2 (#450 and #500)
Amplitude | 5 | 4
Number of taps | 20 | 300
Sample # | 39 | 42
Simulant mass | 250 mg | 50 mg
Sample # 10
Sample # 35
Sample # 39
Sample # 42
*All substrates were glass

## Slide 11: Surface simulant contamination techniques
Aerosolization
Vibratory filtration
Simulant mass | 1 g
Number of sieves | 2 (#450 and #500)
Amplitude | 4
Number of taps | 300
Sample # 44
Sample # 36
Sample | 49 | 50
Simulant mass | 150 mg | 150 mg
Substrate | Glass | Titanium
Sample # 49
Sample # 50

## Slide 12: Surface simulant contamination techniques
Aerosolization
Vibratory filtration
Simulant mass | 250 mg
Simulant mass | 1 g
Number of sieves | 2 (#450 and #500)
Amplitude | 4
Number of taps | 300
Before sonication prep
After sonication prep
Before sonication prep
After sonication prep

## Slide 13: Aerosolization technique: simulant mass study
Sample # 39
250 mg
Sample # 40
100 mg
Sample # 42
50 mg
Sample # 45
150 mg
Sample # 46
75 mg
Decreasing clusters (generally)
Increasing simulant mass

## Slide 14: Determined ideal approach to simulant surface contamination for adhesion study
Step 1. Prepare samples
Step 2. Deposit simulant
Step 3. Resolve cohesion
Sonic wand samples on sample holder
Sample deposition screen
Aerosolization technique selected
Low displacement sonication

## Slide 15: Acknowledgements
Advanced Materials and Processing Branch
  John W. Connell
NASA Lunar Surface Innovation Initiative
  Niki WerkHeiser, Michael Johansen, Erica Montbach, Kristen John, Cameron Hartman
NASA Internship, Fellowship, Scholarship (NIFS) /STEM Takes Flight (STF) Programs
Image credit: NASA
Next passive mitigation technology evaluation laboratory