## Slide 1: Modeling of Solid Electrolyte for NASA SABERS Project
April A Rains
Dr. Vesselin Yamakov, Dr. Yi Lin and Dr. John Connell
2021 Summer NIFS Research Symposium

## Slide 2: Solid-state Architecture Batteries for Enhanced Rechargeability and Safety SABERS
High performance all solid-state battery research focused on electric aircraft battery requirements
R. Viggiano, D. Dornbusch, J. Wu, J. Connell, Y. Lin, V. Yamakov. “Solid-state Architecture Batteries for Enhanced Rechargeability and Safety (SABERS) - A Transformative Solution to Meet Challenging Aerospace Requirements”, 2021 AIAA Aviation Forum (Virtual), 06/15/20 – 06/19/20.

## Slide 3: Aviation Battery Requirements
Safety
Scalable
High energy density
Low weight packaging
Discharge rate performance
https://www.usfa.fema.gov/blog/cb-061819.html

## Slide 4: How to meet the battery requirements?
All Solid-State Li-S batteries
  Innovative holey graphene scaffold
  Improved power density with the addition of selenium
  Solid electrolyte
    Non-flammable
    Li dendrite suppression
    High ionic conductivity at room temperature
    Low interfacial resistance
R. Viggiano, D. Dornbusch, J. Wu, J. Connell, Y. Lin, V. Yamakov. “Solid-state Architecture Batteries for Enhanced Rechargeability and Safety (SABERS) - A Transformative Solution to Meet Challenging Aerospace Requirements”, 2021 AIAA Aviation Forum (Virtual), 06/15/20 – 06/19/20.

## Slide 5: Objectives
To learn about the ionic conductivity of solid electrolytes through computational modeling
  The models that are generated provide useful information that can be used during the experimental portion of this project.
To find the optimal composition of the solid electrolyte

## Slide 6: Methods
Solid Electrolyte Sphere Approximation Model – SESAM
Models were created for Al-doped LLZO electrolyte (lithium lanthanum zirconium oxide Li7La3Zr2O12)
    Hexagonal-close packing (HCP) models
    Random packing models
    For each system, HCP and random packing, different amounts of interfacial resistance were modeled
Spheres
Compress
Solver
Visualization

## Slide 7: Electrolyte Modeling
Hexagonal Close-Packing
Random Packing
Compress

## Slide 8: Electrolyte Modeling - Particle Size Affect
Particle size deviation 1 nm
Particle size deviation 4 nm
Particle size deviation 8 nm
Particle size deviation 25 nm
The small particle size deviation shows a packing system similar to HCP packing
The large particle size deviation allows for the smaller particles to fill the empty spaces thereby increasing the volume percent

## Slide 9: Analysis
Chart: Volume Percent
| 1 | 2 | 4 | 6 | 8 | 10 | 15 | 20 | 25 | 30
30 nm | 65.8922 | 65.8722 | 66.1211 | 66.5289 | 66.98 | 67.4178 | 68.24 | 68.8222 | 69.0944
40 nm | 65.63 | 65.51 | 65.5811 | 65.8433 | 66.1378 | 66.4911 | 67.2933 | 67.3511 | 67.8844
60 nm | 65.1656 | 64.9589 | 64.6278 | 64.6278 | 64.7239 | 65.0967 | 65.5806 | 66.1139 | 66.8356 | 67.2506
80 nm | 65.9885 | 65.4856 | 63.9998 | 63.9578 | 64.0178 | 64.1274 | 64.335 | 65.5841 | 64.8671 | 66.6293
Using smaller particle sizes increased the volume percent of the system
All particle sizes showed a drop in the volume percent going from 1 nm deviation to 4 nm deviations
There was an upward trend in the volume percent after a deviation of 4 nm, as the ratio of particle sizes increase. This allows for the smaller particles to fit inside the empty spaces

## Slide 10: Analysis
Chart: Case I – Conductivity (average of 9 trials)
| 1 | 2 | 4 | 6 | 8 | 10 | 15 | 20 | 25 | 30
30 nm | 0.00022068 | 0.00021987 | 0.00021601 | 0.00021159 | 0.00020744 | 0.0002059 | 0.00021688 | 0.00023688 | 0.00028271
40 nm | 0.00027564 | 0.00026898 | 0.00026683 | 0.00026249 | 0.00025555 | 0.00025404 | 0.00024785 | 0.00024764 | 0.00028247
60 nm | 0.0003769 | 0.00036596 | 0.00033602 | 0.00033508 | 0.00032311 | 0.00032788 | 0.00031537 | 0.00031856 | 0.00035134 | 0.00036747
80 nm | 0.00049668 | 0.00042008 | 0.00044959 | 0.00047575 | 0.00046049 | 0.00042534 | 0.00037361 | 0.00042741 | 0.00040582 | 0.00045584
Chart: Case II - Conductivity (average of 9 trials)
| 1 | 2 | 4 | 6 | 8 | 10 | 15 | 20 | 25 | 30
30 nm | 0.076145 | 0.075839 | 0.074695 | 0.073087 | 0.071241 | 0.069936 | 0.068961 | 0.069448 | 0.07333
40 nm | 0.079364 | 0.077859 | 0.077296 | 0.076148 | 0.074219 | 0.073219 | 0.069963 | 0.065822 | 0.068932
60 nm | 0.081778 | 0.0793 | 0.074822 | 0.074478 | 0.072438 | 0.073078 | 0.070678 | 0.069625 | 0.071878 | 0.071357
80 nm | 0.05535 | 0.076011 | 0.078804 | 0.082882 | 0.080607 | 0.0779 | 0.068367 | 0.075336 | 0.069827 | 0.076282
Chart: Case III - Conductivity (average of 9 trials)
| 1 | 2 | 4 | 6 | 8 | 10 | 15 | 20 | 25 | 30
30 nm | 0.00011869 | 0.0001182 | 0.00011668 | 0.00011429 | 0.00011127 | 0.00010871 | 0.0001039 | 0.00010065 | 0.00010151
40 nm | 0.00011347 | 0.00011153 | 0.0001108 | 0.00010933 | 0.00010673 | 0.00010507 | 9.9713e-05 | 0.00010866 | 0.0001153
60 nm | 0.00010618 | 0.00010299 | 9.7644e-05 | 9.7122e-05 | 9.4625e-05 | 9.54e-05 | 9.2489e-05 | 9.0475e-05 | 9.2022e-05 | 9.0186e-05
80 nm | 0.00010674 | 0.00012893 | 9.8092e-05 | 0.00010141 | 9.879e-05 | 9.3225e-05 | 8.4621e-05 | 9.2667e-05 | 8.5924e-05 | 9.2964e-05
Case I - Particle resistance is dominant
Case III - Interface resistance is dominant
Case I - Particle resistance is dominant
Case II - Particle resistance is equal to interface resistance
Case III - Interface resistance is dominant

## Slide 11
Pressure Dependent Study – HPC and Random packing, 30 nm particles
Chart: Case I
| 1 | 2 | 4 | 6 | 8 | 16 | 32 | 64 | 100
Random | 3.8224e-05 | 6.7972e-05 | 0.00011344 | 0.00015298 | 0.00018631 | 0.00030894 | 0.00051003 | 0.00085234 | 0.0014191
HCP | 0.00010523 | 0.00016686 | 0.00026448 | 0.0004189 | 0.00066266 | 0.0010463 | 0.0016472 | 0.0022013
Chart: Case II
| 1 | 2 | 4 | 6 | 8 | 16 | 32 | 64 | 100
Random | 0.019652 | 0.031686 | 0.046893 | 0.058382 | 0.06761 | 0.096867 | 0.13851 | 0.22891 | 0.28995
HCP | 0.054771 | 0.077276 | 0.1076 | 0.14792 | 0.20092 | 0.26993 | 0.3592 | 0.42988
Chart: Case III
| 1 | 2 | 4 | 6 | 8 | 16 | 32 | 64 | 100
Random | 4.2899e-05 | 6.0463e-05 | 8.1232e-05 | 9.5481e-05 | 0.0001082 | 0.0001444 | 0.00021679 | 0.0002973 | 0.00036529
HCP | 0.00011422 | 0.00014393 | 0.00018139 | 0.00022866 | 0.00028834 | 0.00036378 | 0.00045937 | 0.0005342
Experimental data:
Electrolyte – lithium phosphorous sulfide chloride (LPSCl)
The experimental data is in agreement with the simulation data from SESAM model
Particle resistance is dominant
Particle and interface resistance are equal
Interface resistance is dominant
SESAM Models:

## Slide 12: Conclusion
Models were generated using SESAM to show the effects of particle size distribution on the conductivity of the electrolyte
Models were also generated to show how pressure effects the conductivity of the electrolyte
  This pressure dependent study was validated by experimental results

## Slide 13: Acknowledgements
My Amazing Mentors:
Dr. Yamakov
Dr. Lin
Dr. Connell
NASA Internship Team
Images from nasa.gov
Lab mates:
Brandon Walker, Elizabeth A Barrios, Malik A Satterwhite, and Justyn Lewis

## Slide 14: Thank you
Image from nasa.gov