## Slide 1: Exploration of Scalable Methods to Fabricate Synthetic Lunar Minerals for Engineered Regolith Simulants
Dr. Holly Shulman1,2
C. Howard2, J. LaPaglia2, D.L. Rickman3, M.R. Effinger4
1DrHollyShulman, LLC, Belmont, NY, 14813
2Alfred University, Alfred, NY, 14802
3Jacobs Space Exploration Group/NASA Marshall Space Flight Center, Huntsville, AL 35812
4NASA Marshall Space Flight Center (MSFC), EM31, Huntsville, AL, 35812
Fundamental and Applied Lunar Surface Research in Physical Sciences August 18–19, 2021

## Slide 2: Overview
Goals
Scalable Methods
Laboratory Results
Conclusions and Next Steps

## Slide 3: Goals
Develop scalable methods to fabricate synthetic lunar simulants focused on Highlands
Characterization to confirm and/or modify as needed for high fidelity to lunar regolith
Ultimate goal sufficient materials for large scale construction experimentation focusing on microwave densification

## Slide 4: Scalable Methods: Solid State Reaction
Solid State Reaction- Mixed Oxide Method
  Oxides (and carbonates) powders intimately mixed, e.g. ball mill
  Powders heated to react
    Diffusion controlled; time and temp critical; must be in appropriate phase field
    Must avoid reaction with container
  Batch Kiln- powders in saggers
  Rotary Kiln- powders in large rotating tube

## Slide 5: Scalable Methods: Solid State Reaction
Toll firing examples: Harrop Industries
1A. Batch Furnace (Periodic)
Electric Kilns
  Volume up to 27 cu. ft., Temp to 1,600°C Controlled atm.
Gas Kilns
  Volume up to 57 cu. ft., Temp to 1,700°C
1B. Rotary Kiln (Continuous)
Ceramic tube
  Variable rotation speed, tube inclination angle
  Temp to 1,400°C
Elevator Kiln
Rotary Kiln

## Slide 6: Scalable Methods: Reaction from Melt
Toll firing example: Washington Mills
2. Fusion from Melt - Arc Electrode Method
Power supply, graphite electrodes and vessel
Arc generated between electrodes >3000°C

## Slide 7: Laboratory Challenge
Target:
  Anorthite (plagioclase CaAl2Si2O8)
  Diopside (pyroxene CaMgSi₂O₆)
  Enstatite (pyroxene Mg2Si2O6)
  Olivine (solid solution (Mg,Fe)2SiO4)
Variables:
  Process method
  Raw materials
  Temperature
  Dwell Time, Heating and Cooling Rate
  Container material
X-Ray Diffraction feedback
Ming, D. W. (1992). Lunar sourcebook, Endeavour 16(2). Data compiled from Table 5.1, pg 123

## Slide 8: Olivine (Mg,Fe)2SiO4)
High purity natural sources available
End member synthetic forsterite standard commercial product via arc fusion method
Olivine solid solution available custom commercial product with controlled Fe/Mg+Fe ratio to match Highlands range
Natural olivine- Titon Supply Company

## Slide 9: Anorthite (CaAl2Si2O8)
XRD Anorthite via solid state method 1300°C using CaCO3, high purity Al2O3, and highly reactive fumed SiO2. Appearance of minor spinel phase likely due to Mg impurity in the CaCO3. This can be replaced with high purity CaCO3. Use of a less reactive amorphous SiO2 showed residual unreacted Al2O3 at these process conditions.
XRD Anorthite via arc electrode method >3000°C, using CaO, Al2O3, SiO2. Appearance of minor Gehlenite phase likely due to short reaction time. More time can be applied to allow better mixing of the melt.

## Slide 10: Diopside (CaMgSi₂O₆)
XRD Diopside via solid state method 1250°C using MgCO3 + CaCO3 + amorphous SiO2. Appearance of minor phase forsterite. No reaction with alumina crucible. Slight reaction with alumina crucible occurred for fumed SiO2 blend, and reaction for both SiO2 sources with alumina crucible at higher calcination temperature.

## Slide 11: Enstatite (Mg2Si2O6)
Complicated due to polymorphs
Desired phase orthoenstatite, also referred to as enstatite
Protoenstatite converts slowly to orthoenstatite ~ 1080 °C, highly sensitive to cooling rate
Phase field of enstatite polymorphs: Orthoenstatite (Oen) is the desired phase (enstatite). Protoenstatite (Pen) Clinoenstatite (High Hcen and Low LCen). Oen is stable phase at RT, however, requires long holds and slow cooling to induce transition from Pen. Transition begins at ~1080 C 1 ATM, and is slow to reverse. Cen phases occur mostly due to mechanically induced transitions in Oen and Pen, as lamellae in the host crystal.
Ref. Clément, Padrón-Navarta et al. 2018

## Slide 12: Enstatite (Mg2Si2O6)
XRD orthoenstatite (enstatite), synthesized from Talc (Mg3Si4O10(OH)2) and MgCO3, at 1000 °C for 48 hours. Minor phases quartz and forsterite. Reaction to forsterite is favored in the the orthoenstatite phase field.

## Slide 13: Enstatite
Effect of temp on phase formation: 48 hr dwell
950 °C
1000 °C
1040 °C
Starting materials Talc (Mg3Si4O10(OH)2) + MgCO3
Higher enstatite peaks 1000 °C than 950 °C, no change at 1040 °C
Commercial method - Possible to remove quartz via a reduction to SiO and evaporation process
Phase pure protenstatite readily formed >1100 °C should convert to othoenstatite with long dwell time. Tests are ongoing.
Arc fusion method with controlled cooling to be investigated.

## Slide 14: Summary
Solid state reaction and arc fusion methods are commercial methods for making synthetic minerals at ton scale.
Olivine readily available as natural mineral and commercial synthetic product.
Demonstrated synthetic anorthite via solid state and arc fusion methods.
Demonstrated synthetic diopside via solid state method. High probability of arc fusion success based on phase stability.
Demonstrated synthetic enstatite, however need for further refinement to achieve phase pure orthoenstatite.

## Slide 15: Suggested next steps
1. Lab scale
  Down select scalable method and starting materials
  Prepare 3-5 Kg batches of synthetic lunar minerals
  Characterize and modify particle size distribution e.g. laser light scattering and BET, milling to change particle size
  Make glass melts and pseudo agglutinates from blends e.g. via arc electrode quenching
  Batch synthetic minerals + glass
  Add minor phases, e.g nano Fe
  Measure dielectric properties
2. Scale up
  Use same method from lab scale (solid state or arc electrode) 50-100 Kg batches of minerals
  XRD confirm phases
  Modify particle size distribution (e.g. milling)
  Same procedures to make synthetic lunar glasses from quenching mineral blends
  Add minor phases
  Measure dielectric properties and other characterization