## Slide 1
Plasma Reduction of Regolith for Oxygen Liberation
Ryan Gott, Elspeth Petersen, Kenneth Engeling, Nilab Azim, Carolina Franco, Joel Olson
Gaseous Electronics Conference, October 6th, 2021

## Slide 2: Background
Lunar regolith is composed of 40% oxygen (by weight)
  Need oxygen for fuel and life systems
Bonds holding the oxygen require high temperatures, large amounts of energy, or strong reducing agents to separate the oxygen from the regolith
Silicates, which are prevalent at the poles, require extreme high temperatures in the current state of the art
Path needed for producing oxygen
  At any lunar location
  Without consumables
  At temperatures below melting and sintering

## Slide 3: Plasma Treatment
Hydrogen plasma produces H+ ions, which reduce silicates
H2 reduction creates water
Electrolysis can extract O2
Avoids consumables and high temperatures

## Slide 4
Concept
4

## Slide 5
Experimental Setup
Gas Exit
Vent to hood
Sample line to RGA/Mass Spec
Vacuum pump
Regolith
Plasma Torch
Optical Emission Spectrometer (outside)
TC
Power supply
H2 gas inlet
Extract oxygen from regolith using H2 plasma
Reactor and regolith remain at near-ambient temperature
Reactor is at 5 Torr
High Voltage DC Power Supply from Applied Plasma Technologies Corp gave ~100 W of power
H2 plasma plume passes over regolith then pulled out to vacuum pump
Optical Emission Spectrometer and Mass Spec monitor reaction/plasma conditions
H2 gas inlet

## Slide 6: Measurements
Three Concurrent Measurements in Chamber
GoPro Video
Residual Gas Analyzer (RGA)
Optical Emission Spectroscopy (OES)
Chart: Silica OES Results
Chart: LHS RGA Results
H2 On | 1e-13 | 1.6e-09
H2 Off | 1e-13 | 1.6e-09
Plasma On | 1e-13 | 2e-10
Plasma Off | 1e-13 | 2e-10
OH
N2
Si I
N2+
N2+
H
H
Water
N2
Oxygen

## Slide 7
Plasma Treatment of Lunar Highland Simulant

## Slide 8: RGA Water Signal
Chart: Water (18 m/z)
LHS=flat layer of regolith High LHS= piled regolith, so substrate interacted with plasma cloud more directly

## Slide 9
Optical Emission Spectroscopy (OES)
Identify species
  H, OH, N2, Si, N2 +
Interference (N2 leak)
OES Interpretations
  OH from water dissociation
    Possible addition from air leak
  Si I/ Fe II suggests reduction
  N2 shows leak (air)
Chart: Lunar Highland Simulant (LHS)
| 309.5 nm | 315.6 nm | 336.8 nm | 357.7 nm | 391.1 nm | 427.5 nm | 486.1 nm | 493 nm | 501.1 nm | 539.6 nm | 656.3 nm | 729.5 nm
0 min | 29.12 | 82.61 | 66.44 | 76.17 | 49.01 | 51.3 | -10.91 | 27.93 | 41.47 | 52.93 | 62.59 | 38.41
1 min | 237.35 | 177.9 | 140.75 | 133.8 | 803.2 | 244.65 | 318.5 | 188 | 162 | 259.1 | 1391.85 | 124.55
5 min | 377.21 | 245.0433 | 166.7733 | 161.7967 | 764.8767 | 228.61 | 377.8033 | 238.3033 | 213.3867 | 333.2367 | 1863.59 | 145.45
10 min | 283.2567 | 246.5067 | 168.5633 | 164.34 | 797.9233 | 245.7033 | 360.6767 | 230.3267 | 208.95 | 336.13 | 1790.99 | 132.57
15 min | 312.7933 | 236.2667 | 222.7333 | 204.7633 | 1121.5467 | 344.2467 | 382.6533 | 214.8733 | 200.34 | 319.89 | 1821.1467 | 137.28
25 min | 490.6 | 517.1 | 648.3 | 588.8 | 3402.1 | 957 | 368.2 | 218.6 | 208.6 | 246.4 | 1744.3 | 131.8
30 min | 497.75 | 592.83 | 807.99 | 716.69 | 4263.44 | 1210.49 | 313.62 | 158.76 | 204.79 | 249.71 | 1480.24 | 129.535
OH
N2
Si I N2+
N2+
H
H
N2+

## Slide 10: OH Results
Chart: Fine Silica
OH
N2

## Slide 11: OH Comparison
Chart: Fine Silica
OH OES | 58.6 | 1473.4 | 1474.7 | 685.6 | 540.1 | 484.8 | 540 | 577 | 692.7 | 972 | 1296.6 | 1320.7 | 1419.7 | 1405.9

## Slide 12: OH Comparison
Chart: Time
| 1 min | 5 min | 10 min
Empty Chamber | 236.1667 | 240.1333 | 211.1667
LHS | 237.35 | 377.21 | 283.2567
Silica | 437.3422 | 543.7322 | 459.1289
Fine Silica | 1473.4 | 1474.7 | 685.6
High LHS | 286.3 | 339.5 | 140.8
The High LHS* partially blocked the plasma, causing a reduction in light intensity.
*
*
*Lunar Highland Simulant (LHS)

## Slide 13: Summary
RGA/Mass spec and OES measurements show clear production of water
Increasing plasma contact area increases reactions
Many variables left to explore
  Packing of regolith/torch orientation
  Chamber temperature
  Varying pressure
Need to quantify water production and O2 removal efficiency
  Compare to higher TRL systems: Carbothermal Reduction and Molten Regolith Electrolysis

## Slide 14: Thank you!

## Slide 15
Backup Slide: Substrates
←Silica gel (74-250μm) SiO2
← Fine Silica (32-63μm) SiO2
↓Lunar Highland Simulant (60μm) LHS-1 from Exolith
Silica selected as a regolith analog for ease of characterization

## Slide 16: Backup Slide: Testing Parameters
Chamber Pressure
Pump down to 200 mTorr
Flow 15-75 sccm H2
  25 sccm H2 brings pressure to ≈4.5 Torr
Thermodynamic behaviors increase with pressure to ≈ 7 Torr
Plasma Parameters
High Voltage DC Power Supply from Applied Plasma Technologies Corp.
0 – 10 kV, 8 Amp max supply
The resulting power draw was 80-100 W
Operating Temperature
Gas in chamber max 50°C
Torch housing max 250°C
Test Simulant Masses
Initial tests with 1.5 grams
‘Piled’ test of 17 grams
Silica Sample in Chamber (on watch glass)

## Slide 17: Backup Slides: RGA Results
Chart: LHS Hydrogen RGA Results
Plasma On | 1e-13 | 1.6e-09
Plasma Off | 1e-13 | 1.6e-09
Chart: LHS RGA Results
H2 On | 1e-13 | 1.6e-09
H2 Off | 1e-13 | 1.6e-09
Plasma On | 1e-13 | 2e-10
Plasma Off | 1e-13 | 2e-10
Water
N2/Si
Oxygen
Water
N2/Si
Oxygen
Chart: LHS Hydrogen RGA Results (zoom)
Plasma On | 1e-13 | 1.6e-09
Plasma Off | 1e-13 | 1.6e-09