## Slide 1
Addressing the Physics of Adsorption and Desorption of molecules from the sub-monolayer to multilayer films
John Canham
Peraton Inc.
(john.Canham@peraton.com)
Jennifer Eigenbrode
NASA Goddard Space Flight Center, Planetary Environments Laboratory
(jennifer.eigenbrode@nasa.gov)
Contamination Control for Life Detection Team:
Antonios Seas, John Canham, Erich Schulze, Chris Lorentson, Therese Errigo, David Kusnierkiewicz, Faith Kujawa, Alfonso Davila, Chris McKay, Anthony Dazzo, Michael Swift, Andrew, Santo, Charles Sandy, Tony Asti, John Lin
ELSAH Technology Study Team, funded by NASA’s New Frontiers Program, 2018-2020
NASA CCMPP 2021
Abstracted from Eigenbrode, Gold, Canham, et al., 2021, Frontiers in Space Technology, DOI: 10.3389/frspt.2021.734423

## Slide 2
Motivation
Molecular cleanliness of hardware is critical to life detection missions
Significant deviations from existing molecular transport models are seen with very clean hardware
Higher fidelity modeling is needed to evaluate molecular cleanliness
COSPAR 2021
High fidelity contamination transport modeling
is critical to life detection missions.

## Slide 3
Questions
How do we improve the fidelity of modeling of outgassing at extremely low molecular contamination levels for Astrobiology?
Can we reduce molecular contamination down to femtomole levels in a sample?
COSPAR 2021
High fidelity contamination transport modeling
is critical to life detection missions.

## Slide 4: Traditional, well proven techniques and operations  Not adequate for Ultra-Sensitive Life Detection Missions
COSPAR 2021
  Verification techniques - inadequate
  Standard Contamination Transfer Models - unrealistic
  Need new analysis techniques are required to demonstrate contamination transfer at less than monolayer levels
  New forms of hardware protection/cleaning must be used to meet these stringent levels
Ultra-clean surfaces: Molecular interaction with surfaces is governed by the chemistry and physics of each molecule (circles) and the material it is adjacent to (spacecraft surface or other molecule).
Graphics from “Eigenbrode et al., 2021, Frontiers in Space Tech.”

## Slide 5: Astrobiology and Contamination
Some instruments are sensitive down to femtomole levels of molecules (<0.001 ng) in a sample
Interested in specific classes of molecules
  Target molecules must be tightly controlled
  Non-target molecules that do not interfere with the measurement of the target molecules can be less controlled
  Need to determine the level of acceptable contaminant levels that can be transferred to a sample
Residue levels (mass per unit area) won’t work
Need to evaluate the transport details to higher fidelity

## Slide 6: Typical outgassing composition (a cold finger)
More than 50 different compounds detected, widely varying in adsorption energy

## Slide 7: Molecules and their environment
Molecular behavior is dependent upon the local environment
  Strictly thermodynamic effects
    In a bulk liquid or gas phase a molecule has three translational and three rotational degrees of freedom
    When adsorbed on an ideal surface it loses one translational degree of freedom and one or two rotational degrees of freedom
    At a given temperature, loss of degrees of freedom results in loss of energy
  Polarization
    Induced polarization by a surface lowers the energy of the molecule

## Slide 8: Molecules on Surfaces
Molecular behavior being dependent upon their environment, needs to be addressed
With many molecular layers, the behavior will approach bulk behavior
As the number of molecular layers decreases, the behavior will diverge from bulk behavior
In the case of water on inorganic oxides, the first 3-5 layers are ice-like at room temperature. A solid like structure is formed.
To more closely approximate real behavior, it is necessary to address the material stack up
Graphic from “Eigenbrode et al., 2021, Frontiers in Space Tech.”

## Slide 9: Approach to more closely model transport
Address the molecular composition of the contamination
  Estimate the actual contamination composition and physical properties through chemical analysis or statistical means
  Evaluate the behaviors of this contamination on surfaces of interest (surface and bulk sinks)
Address the number of molecular layers
Address the behavior of the contamination in the modeled contamination load

## Slide 10: Material-Material interactions
There is a scarcity of material-material interaction data for most common Aerospace Contaminants
Brunauer, Emmett and Teller’s 1938 paper discusses the behavior of molecules in multiple molecular layers
  They suggest an approximation of the first molecular layer adsorption energy as being the enthalpy of sublimation
    This is consistent with other models of non-reactive monolayer adsorption energies
  Their approach also addresses the treatment of additional layers with different adsorption energies
“Adsorption of Gases in Multimolecular Layers” Brunauer, Emmett and Teller
Journal of the American Chemical Society, 60 (2) 309-319, 1938

## Slide 11: Implementation
Particle-In Cell, LLC’s Contamination Transport Simulation Program (CTSP) v1.5 was used
Four discrete representative molecules were chosen for the simulations (n-dioctyl phthalate, n-hexadecane, n-eicosane and n-pentacosane)
Thermodynamic data for these species were utilized
A material-material interaction routine was developed to address what the interaction of the individual contaminant is with the different surfaces
In this work, only bare surface material and molecular contaminant surface interactions were chosen, however, the capability exists to expand the definitions further
Enthalpies of sublimation were used for the first molecular layer and enthalpies of vaporization were used for subsequent layers.

## Slide 12: Implementation (continued)
The model evaluated was for an in-flight bake out of a component (ramp up, time and temperature)
The Material-Material interaction and strictly enthalpy of vaporization models were run for comparison
CTSP utilized a meshed spacecraft model
  Initial loaded the four exemplary compounds onto each mesh element
  The coverage of the mesh elements were tracked for each compound
  Surface residence times were used for defining rates of desorption

## Slide 13: Residence time- sublimation and vaporization
There are significant differences in the surface residence times between sublimation and vaporization
Based upon

## Slide 14: Standard model (Collector cone only)
Time 0
30 minutes
60 minutes
Approximately 1x10-12 of loading remaining at 60 minutes
Graphics from “Eigenbrode et al., 2021, Frontiers in Space Tech.”
Notes: All surfaces loaded with a monolayer of the contaminants, transport only from

## Slide 15: Improved Physics Model (Collector cone only)
Time 0
30 minutes
60 minutes
Approximately 12% of contamination load remaining at 60 minutes, primarily the nC25 hydrocarbon
Graphics from “Eigenbrode et al., 2021, Frontiers in Space Tech.”

## Slide 16: Comparison of n-C16 loss between standard model and improved model
Graphics from “Eigenbrode et al., 2021, Frontiers in Space Tech.”

## Slide 17: Comparison of n-C20 loss between standard model and improved model
Graphics from “Eigenbrode et al., 2021, Frontiers in Space Tech.”

## Slide 18: Summary
Brunauer, Emmett and Teller’s development for multilayer adsorption was incorporated into molecular transport modeling
Their estimation of the adsorption energy for the first molecular layer and subsequent layers was utilized
Both models utilized the rate reduction due to the source area
The improved physics model is more consistent with long duration high temperature bake out of surface contaminated high vacuum systems

## Slide 19: Future work
Develop processes for evaluating the material-material interactions
General material-molecule interactions
  Are general surface-molecule interactions feasible
  When does it work when doesn’t it work
  Is single molecular layer and multiple molecular layer modeling adequate?
Specific material-molecule (or class of molecules) of interest

## Slide 20
Conclusions
The techniques developed in this study will enable future life detection and other highly contamination sensitive missions to provide scientific results with higher confidence in their validity.
The improved Physics model addressing the variation of adsorption energies has higher fidelity than standard approaches
Allows higher fidelity modeling for Astrobiology missions
Models containing multiple species are possible
Further improvements with additional data are possible
Treating specific material-material interactions is possible

## Slide 21: Backup Charts

## Slide 22: Detailed Molecular Adsorption/Desorption
Below about five monolayers of organic contamination on a surface, the behavior of molecules on the surface is significantly different from in the bulk material.
  In the case of water on an inorganic oxide surface, in the first three monolayers of water on the surface, the adsorbed water is “ice like” at room temperature. (David B. Asay, 2005)
Details of the equilibrium behavior of molecular adsorption on surfaces was described by Brunauer, Emmett and Teller (BET) in 1937.
  The equilibrium state is defined by the arrival rate and accommodation being equal to the source area and the evolution rate or surface residence time and area
  The energetics and thus rate behavior of the first or first few molecular layers is in virtually all cases different from any and all additional layers.
The propagation of the energy perturbation to additional molecular layers can be accounted for within the BET framework.
  Within the BET framework, Chemisorption as well as physisorption can be dealt with.
Divergence of the actual adsorption behavior on a real surface is to be expected due the dispersion in the surface energy.

## Slide 23: BET graphical description
Adsorption Energy
E1
E2
E3
…
EL
E1
E2
E3
~EL
The adsorption energy in the first monolayer is the highest
The adsorption energy in the second monolayer is second highest
This continues until the energy converges to vaporization energy of bulk liquid

## Slide 24: Adsorption Kinetics
The rate of adsorption of a material on a specific surface is based upon
  The rate of arrival of the material to the surface
    Material cannot accumulate faster than it is supplied to the surface
    This is in effect a function of the partial pressure of the material in the gas phase
    The numerical rate per unit area is often described by the Hertz-Knudsen equation
  The accommodation of the molecules
    This is the probability that the molecules at this energy will adsorb on the surface
  The area
    This area is the area of the specific type of target surface (whether this is bare, is a monolayer, a multilayer, etc.)
In the BET approach, the adsorption rate is represented as
  a1 is the accommodation or sticking factor, p is the partial pressure, and s0 is the bare exposed surface area
Source Wikipedia
a­1ps0

## Slide 25: Desorption Kinetics
The rate of desorption of a material from a specific surface is based upon
  The fractional area of the specific surface layer of molecules, in this case bare surface
  The frequency of potential desorption events, whether probable of not
  The energy of the specific desorption process
  The temperature, defines what proportion of the molecules exceed that energy
In the BET approach, the desorption rate is represented as
  b1 is the frequency of the potential desorption events, s1 is the fractional area of the specific surface, E1 is the energy of the specific desorption process, R is the gas constant, and T is the temperature
  This is basically the surface residence time multiplied by the fractional area
b1s1e-E1/RT

## Slide 26: Adsorption/ Desorption Equilibrium
The BET Equilibrium description adsorption and desorption is
Using the BET terminology, the subscripts describe the molecular layer property
  a1= 1-s1 The total area minus the area covered by one layer is the fraction that is bare
  E1 is the adsorption energy for the first molecular layer
The quantity material on a surface is the sum of the adsorption and desorption behavior of all the layers
  Due to the direct relation between one layer and the next layer in the definition of the rate of adsorption and desorption, it is possible to simplify the equation from the individual layer level to an infinite number of molecular layers
Known differentiation between layer behaviors can be accounted for
a­1ps0=b1s1e-E1/RT

## Slide 27: Points to Ponder
The accommodation of molecules is an average value
The desorption energy is a function of the surface energy
The surface energy is an average energy
  At the extremes of the levels of coverage for a layer, the adsorption behavior should be expected to diverge from the average
  A 2 eV point defect is equivalent to a 192 kJ per mole difference in surface energy, which is huge!
Physical constraints
  A molecule adsorbed onto a uniform clean surface loses at least one degree of freedom
  Addition of further restrictions in the physical adsorption process results in loss of additional degrees of freedom. Physical imperfections, lattice defects, excitons,…
Water adsorbed on silicon dioxide is locked into a solid like physical state (Ice like) at room temperature through at least three molecular layers
BET assumption: heat of desorption from a bare surface is approximately the heat of sublimation