## Slide 1: Effective Emissivity of Nonisothermal Isogrid for Spacecraft Radiator Applications
Seth Abramczyk
November 19th, 2021

## Slide 2: Abstract
Accurate knowledge of the optical properties of spacecraft components, especially external components, is critical for proper spacecraft thermal design. The effective emissivity of isogrid (an array of equilateral triangular cavities) is not well understood, which poses a challenge for spacecraft thermal management. In this thesis the effective emissivity of isogrid with a prescribed base temperature and nonisothermal walls is examined. The temperature profile of the cavity’s walls and the overall effective emissivity of the cavity are found using Thermal Desktop with Monte Carlo ray tracing. The effective emissivity’s dependence on the wall height, wall thickness, wall resistance, and surface emissivity are examined. The existence of a critical wall height, and the contributing factors to this critical height, are discussed. Comparisons between isogrid and cavities with different base geometries are made. A variable emissivity isogrid spacecraft radiator concept employing the cavity effect is proposed, and mechanisms for achieving this are discussed.

## Slide 3: Contents
About me
Background
  Effective-ε and Cavity effect
  Spacecraft Thermal Control Overview
  Spacecraft Radiators
  Roman Space Telescope
Method
  Thermal Desktop, RadCAD, and Finite Difference Method
  Problem Description
  Model Description
  Model Parameters
Results/Conclusion
  View Factors
  Temperature Profile & Gradient
  vs Wall Height
  Critical Wall Height
  Isothermal vs Nonisothermal Walls
  Wall Nodalization
  Wall Thickness
  Wall Resistance
  Edge Effects
  Isogrid vs Other Geometries
Variable-e Isogrid Radiator Concept
Summary
Future Work

## Slide 4: About me
Education
  M.S. Mechanical Engineering – Expected 2021
    University of Maryland Baltimore County
  B.S. Mechanical Engineering – 2019
    The University of Texas at Dallas
NASA Goddard Space Flight Center Pathways Co-op (2018 – Present)
  Thermal Engineering Branch (2019 – Present)
    Roman Space Telescope (2019 - Present)
    SNOOPI & Dione CubeSats (2020 - Present)
    MOMA (2019-2020)
  Operations & Maintenance Branch (2018)
Notes: Working on MS Mech Engineering UMBC (this is my thesis… duh)
BS Mech Eng at UTD
Pathways at GSFC
  In TEB since 2019
  In Operations & Maintenance Branch 2018

## Slide 5: Effective Emissivity & The Cavity Effect
Radiant emission
Emissivity ()
  Ratio of radiant emission compared to that of a blackbody,
The Cavity Effect
  Effective emissivity ()
  Emissivity from a cavity compared to a blackbody with the same cavity opening area

## Slide 6: Spacecraft Thermal Control Overview
Thermal design goal of is to keep all components within temperature limits during worst case extreme hot & cold cases
  Design for hot case and cold case extremes
  All components have hot & cold temperature limits
Spacecraft steady-state energy balance
Heat is transported from dissipating components (electronics boxes, instruments, etc.) to radiators which reject the waste heat to space
Internal generation
Direct Solar
Albedo (reflected solar)
Earth IR
Rejected to Space

## Slide 7: Spacecraft Radiator Sizing
Hot case: Radiators sized large enough to reject all waste heat without breaking hot temperature limit
Cold case: Heaters used to prevent breaking the cold temperature limit
Radiator Sizing Example
  Electronics box on radiator dissipation varies 10 to 50 ; radiator temperature limits of -10°C to 40°C; ; no environmental backloading; assume
  Area for 50 box dissipation at 40°C: 0.102
  Heater power to for 10box dissipation at -10°C: 14.9

## Slide 8: Variable Emissivity Radiators
Thermal control device which vary emissivity with temperature
  and are only variables that can be varied
Louvers
  Low-ε vanes cover a high-ε radiator surface
  Vanes open/close via bi-metallic strips, covering and exposing high-ε surface
  Low temperature
    Vanes closed, low , less heat dissipated
  High temperature
    Vanes open, high , more heat dissipated
  Able to maintain a setpoint temperature by tuning of bi-metallic strips
D. G. Gilmore et al., Spacecraft Thermal Control Handbook Volume I: Fundamental Technologies, 2nd ed. The Aerospace Press, 2002.

## Slide 9: Variable Emissivity Radiator Sizing Example
Same problem as before, but varies from 0.5 - 0.9
Area for 50 box dissipation at 40°C and is same as before:
Heater power to for 10box dissipation at -10°C and =0.5:
11.3 W (75.8%) heater power savings from using variable emissivity radiator
 | Typical Radiator | Variable-ε Radiator | Difference
Emissivity @ 40°C | 0.9 | 0.9 | 0.0
Emissivity @ -10°C | 0.9 | 0.5 | 0.4
Area | 0.102 | 0.102 | 0
Heater Power | 14.9 | 3.6 | 11.3
 | Typical Radiator | Variable-ε Radiator | Difference
Emissivity @ 40°C | 0.9 | 0.9 | 0.0
Emissivity @ -10°C | 0.9 | 0.5 | 0.4
Area |  |  | 
Heater Power |  |  | 

## Slide 10: Roman Space Telescope Overview
Launching mid-2020’s, RST will explore:
  Dark Energy
    Unknown energy causing the universe to expand at an increasing rate. Dark energy makes up 68% of the total energy in the cosmos.
  Dark Matter
    Unknown matter that does not interact with normal matter
    RST will look at weak gravitational lensing caused by dark matter
  Exoplanets
    Planets orbiting other stars
    Will be detected by RST via microlensing, transiting, and possibly direct imaging
Compared to Hubble Space Telescope
  Same resolution with 100x the field of view
  “Over the first five years of observations, Roman will image over 50 times as much sky as Hubble covered in its first 30 years.”
NASA, “Nancy Grace Roman Space Telescope,” NASA Goddard Space Flight Center. https://roman.gsfc.nasa.gov/observatory.html.
H. L. Peabody, “Tracking Critical Thermal Metrics throughout the Life Cycle of a Large Observatory Thermal Model,” 2020.

## Slide 11: Thermal Desktop & RadCAD
Thermal Desktop
  Software package made specifically for spacecraft thermal analysis
  Runs as an application within AutoCAD
  Builds thermal R-C network and passes to SINDA to solve. Displays and analyses SINDA results.
  Calculates radiation exchange factors via Monte Carlo ray tracing (RadCAD)
RadCAD
  TD’s built-in Monte Carlo ray tracer
  Used to calculate radiation exchange factors between surfaces
  Thousands of rays shot from each node in random directions. Deposits energy onto each surface it hits based on the receiving surface’s properties. Each ray is propagated throughout the model until it reaches space or is fully absorbed.
T. D. Panczak, S. G. Ring, M. J. Welch, D. Johnson, B. A. Cullimore, and D. P. Bell, Thermal Desktop User’s Manual, 6.0. C&R Technologies, Inc., 2017.

## Slide 12: Finite Difference Method
General steady state 3D heat diffusion equation without internal heat generation
Finite Difference Formulation
  Assuming only 1 element in the thickness () direction
F. P. Incropera, D. P. Dewitt, T. L. Bergman, and A. S. Lavine, Fundamentals of Heat and Mass Transfer, 6th ed. John Wiley & Sons, 2007.

## Slide 13: Problem Description
Isogrid
  Array of equilateral triangular cavities
Assumptions
  Single cavity within an arbitrarily large isogrid array
  Array is in space with no radiative backloading from sun, earth, etc.
  System is at steady state
  Base of array is isothermal at prescribed temperature
  Cavity walls are isothermal through their thickness
  Material & optical properties independent of temperature

## Slide 14: Thermal Desktop Isogrid Model
Made from thin finite difference elements with edge nodes
Base of array given boundary node at
Array is 22x11 cells
  Edge cells in at position are “half cells” (right triangles)

## Slide 15: Model Parameters
Wall Height ()
  Non-dimensional
  is used throughout this thesis because it corresponds to when
Wall Thickness ()
  Non-dimensional
Characteristic Wall Resistance ()
Notes: Wall height (eta)
  Ratio of inner wall area to base area
Wall thickness (lambda)
  Ratio of thickness to length
Char wall resistance (Rchar)
  Thermal resistance up wall (in Z direction)

## Slide 16: View Factor Across Surface 1
For η=3.46
View factors found with RadCAD
View factors are highly variable across surface 1
At any given point:
Notes: F1-2 & F1-3 are mirrored about X=L/2. Max is ~0.7 at X=0 and X=L
F1-space & F1-4 are mirrored about Z=H/2. Max is 0.5 at Z=H

## Slide 17: Temperature Profile Across Surface 1
Highest temperature along
  At base temperature
Lowest temperature at ,
For =0.7, =3.46, =0.010
x
z
0
L
H

## Slide 18: Temperature Gradient vs Wall Height
Chart: Maximum ΔT vs η for εsurf =0.7, λ=0.010
| 0 | 3.4641016151377546E-2 | 0.17320508075688773 | 0.34641016151377546 | 0.69282032302755092 | 1.0392304845413265 | 1.3856406460551018 | 1.7320508075688774 | 2.078460969082653 | 2.4248711305964283 | 2.7712812921102037 | 3.117691453623979 | 3.4641016151377548 | 4.156921938165306 | 4.8497422611928567 | 5.5425625842204074 | 6.2353829072479581 | 6.9282032302755097 | 7.6210235533030604 | 8.3138438763306119 | 9.0066641993581626 | 9.6994845223857133 | 10.392304845413264 | 12.124355652982141 | 13.856406460551019 | 15.588457268119896 | 17.320508075688775 | 20.784609690826528 | 24.248711305964282 | 27.712812921102039 | 31.176914536239792 | 34.641016151377549 | 38.105117766515299 | 41.569219381653056 | 45.033320996790813 | 48.497422611928563 | 51.96152422706632
0.70 | 0 | -0.000666 | -0.016411 | -0.064263 | -0.24289 | -0.51103 | -0.84114 | -1.2205 | -1.6267 | -2.0688 | -2.5252 | -3.0006 | -3.4851 | -4.5062 | -5.5414 | -6.5924 | -7.6594 | -8.7051 | -9.7513 | -10.7854 | -11.8202 | -12.8232 | -13.8158 | -16.2204 | -18.501 | -20.6732 | -22.7419 | -26.5544 | -29.9949 | -33.1824 | -36.0262 | -38.5744 | -40.8992 | -43.151 | -45.2564 | -47.2412 | -49.155
Larger temperature gradient with increased wall height ()

## Slide 19: Characteristic Regions of vs Wall Height
Chart: εeff vs η Regions
| 3.4641016151377546E-2 | 0.17320508075688773 | 0.34641016151377546 | 0.69282032302755092 | 1.0392304845413265 | 1.3856406460551018 | 1.7320508075688774 | 2.078460969082653 | 2.4248711305964283 | 2.7712812921102037 | 3.117691453623979 | 3.4641016151377548 | 4.156921938165306 | 4.8497422611928567 | 5.5425625842204074 | 6.2353829072479581 | 6.9282032302755097 | 7.6210235533030604 | 8.3138438763306119 | 9.0066641993581626 | 9.6994845223857133 | 10.392304845413264 | 12.124355652982141 | 13.856406460551019 | 15.588457268119896 | 17.320508075688775 | 20.784609690826528 | 24.248711305964282 | 27.712812921102039 | 31.176914536239792 | 34.641016151377549 | 38.105117766515299 | 41.569219381653056 | 45.033320996790813 | 48.497422611928563 | 51.96152422706632 | #N/A | #N/A | #N/A
0.7 | 0.70506 | 0.72537 | 0.74538 | 0.78232 | 0.80706 | 0.83256 | 0.84938 | 0.85887 | 0.86626 | 0.87078 | 0.87498 | 0.87456 | 0.87644 | 0.87109 | 0.8663 | 0.85976 | 0.84734 | 0.84106 | 0.82966 | 0.81919 | 0.80984 | 0.79852 | 0.77529 | 0.75552 | 0.73331 | 0.71329 | 0.68065 | 0.64991 | 0.62509 | 0.5992 | 0.58201 | 0.56653 | 0.55369 | 0.54316 | 0.53103 | 0.52015 | #N/A | #N/A | #N/A
: Surface emissivity
: Maximum effective emissivity
: Critical wall height
  for which
: Equivalent wall height
  for which
Analogous to critical insulation thickness for a pipe
Critical Wall Height

## Slide 20: Contributing Factors to Critical Wall Height
Chart: Wall Height, η
| 0 | 3.4641016151377546E-2 | 0.17320508075688773 | 0.34641016151377546 | 0.69282032302755092 | 1.0392304845413265 | 1.3856406460551018 | 1.7320508075688774 | 2.078460969082653 | 2.4248711305964283 | 2.7712812921102037 | 3.117691453623979 | 3.4641016151377548 | 4.156921938165306 | 4.8497422611928567 | 5.5425625842204074 | 6.2353829072479581 | 6.9282032302755097 | 7.6210235533030604 | 8.3138438763306119 | 9.0066641993581626 | 9.6994845223857133 | 10.392304845413264 | 12.124355652982141 | 13.856406460551019 | 15.588457268119896 | 17.320508075688775 | 20.784609690826528 | 24.248711305964282 | 27.712812921102039 | 31.176914536239792 | 34.641016151377549 | 38.105117766515299 | 41.569219381653056 | 45.033320996790813 | 48.497422611928563 | 51.96152422706632
Walls | 0 | 0.014841 | 0.070678 | 0.133 | 0.24136 | 0.33065 | 0.40583 | 0.46635 | 0.51855 | 0.5615 | 0.59671 | 0.62853 | 0.65072 | 0.69315 | 0.72022 | 0.73852 | 0.74916 | 0.75578 | 0.76098 | 0.76067 | 0.75998 | 0.75659 | 0.7529 | 0.74036 | 0.72882 | 0.71267 | 0.69705 | 0.66918 | 0.64152 | 0.61916 | 0.59419 | 0.57804 | 0.56348 | 0.55113 | 0.54107 | 0.52928 | 0.51859
Base | 0.70042 | 0.69065 | 0.65513 | 0.61282 | 0.54143 | 0.47689 | 0.42723 | 0.38355 | 0.34084 | 0.30528 | 0.27459 | 0.24698 | 0.22437 | 0.18382 | 0.15139 | 0.1283 | 0.11112 | 0.092069 | 0.080593 | 0.069492 | 0.059697 | 0.053735 | 0.046101 | 0.035403 | 0.027151 | 0.021083 | 0.01666 | 0.011872 | 0.0087787 | 0.0063087 | 0.0053789 | 0.0043258 | 0.0033896 | 0.0028938 | 0.002416 | 0.0020655 | 0.001874
Total | 0.70042 | 0.70549 | 0.72581 | 0.74583 | 0.78279 | 0.80754 | 0.83307 | 0.8499 | 0.85939 | 0.86678 | 0.8713 | 0.87551 | 0.87508 | 0.87697 | 0.87162 | 0.86683 | 0.86028 | 0.84785 | 0.84157 | 0.83016 | 0.81968 | 0.81033 | 0.799 | 0.77576 | 0.75597 | 0.73375 | 0.71372 | 0.68106 | 0.6503 | 0.62546 | 0.59956 | 0.58236 | 0.56687 | 0.55403 | 0.54348 | 0.53135 | 0.52046
At (wall height = 0) entire contribution is from base
As increases
  decreases
  increases, reaches a maximum, and begins to decrease

## Slide 21: vs Wall Height Results (1/2)
Chart: εeff vs η for Various εsurf and λ=0.010
| 0 | 3.4641016151377546E-2 | 0.17320508075688773 | 0.34641016151377546 | 0.69282032302755092 | 1.0392304845413265 | 1.3856406460551018 | 1.7320508075688774 | 2.078460969082653 | 2.4248711305964283 | 2.7712812921102037 | 3.117691453623979 | 3.4641016151377548 | 4.156921938165306 | 4.8497422611928567 | 5.5425625842204074 | 6.2353829072479581 | 6.9282032302755097 | 7.6210235533030604 | 8.3138438763306119 | 9.0066641993581626 | 9.6994845223857133 | 10.392304845413264 | 12.124355652982141 | 13.856406460551019 | 15.588457268119896 | 17.320508075688775 | 20.784609690826528 | 24.248711305964282 | 27.712812921102039 | 31.176914536239792 | 34.641016151377549 | 38.105117766515299 | 41.569219381653056 | 45.033320996790813 | 48.497422611928563 | 51.96152422706632 | #N/A | #N/A
0.9 | 0.9 | 0.90233 | 0.91004 | 0.91849 | 0.93243 | 0.94156 | 0.94156 | 0.94955 | 0.95129 | 0.95216 | 0.95498 | 0.94878 | 0.94453 | 0.93541 | 0.92989 | 0.91706 | 0.90888 | 0.89456 | 0.88263 | 0.87284 | 0.85425 | 0.84956 | 0.84001 | 0.81216 | 0.78469 | 0.76432 | 0.74344 | 0.70965 | 0.66946 | 0.64578 | 0.62586 | 0.60823 | 0.59367 | 0.58083 | 0.56943 | 0.55645 | 0.54693 | #N/A | #N/A
0.7 | 0.7 | 0.70506 | 0.72537 | 0.74538 | 0.78232 | 0.80706 | 0.83256 | 0.84938 | 0.85887 | 0.86626 | 0.87078 | 0.87498 | 0.87456 | 0.87644 | 0.87109 | 0.8663 | 0.85976 | 0.84734 | 0.84106 | 0.82966 | 0.81919 | 0.80984 | 0.79852 | 0.77529 | 0.75552 | 0.73331 | 0.71329 | 0.68065 | 0.64991 | 0.62509 | 0.5992 | 0.58201 | 0.56653 | 0.55369 | 0.54316 | 0.53103 | 0.52015 | #N/A | #N/A
0.5 | 0.5 | 0.50686 | 0.53218 | 0.56065 | 0.61075 | 0.65234 | 0.68394 | 0.71119 | 0.73253 | 0.75118 | 0.7617 | 0.77187 | 0.78075 | 0.78866 | 0.79291 | 0.79335 | 0.78936 | 0.78452 | 0.77807 | 0.77374 | 0.76476 | 0.75957 | 0.75143 | 0.73079 | 0.70995 | 0.69091 | 0.67136 | 0.64325 | 0.61574 | 0.59049 | 0.56902 | 0.5452 | 0.53294 | 0.51953 | 0.50759 | 0.49728 | 0.48823 | #N/A | #N/A
0.3 | 0.3 | 0.30636 | 0.33024 | 0.35785 | 0.40819 | 0.45175 | 0.4901 | 0.52403 | 0.55061 | 0.57481 | 0.59507 | 0.61178 | 0.62663 | 0.64877 | 0.66299 | 0.66935 | 0.67363 | 0.67903 | 0.67687 | 0.67622 | 0.67386 | 0.67136 | 0.66553 | 0.65564 | 0.64106 | 0.62502 | 0.61156 | 0.58517 | 0.56182 | 0.54066 | 0.52073 | 0.50405 | 0.48801 | 0.47443 | 0.45892 | 0.45085 | 0.43918 | #N/A | #N/A
0.1 | 0.1 | 0.10298 | 0.11458 | 0.12872 | 0.15565 | 0.18164 | 0.20561 | 0.22875 | 0.24983 | 0.26959 | 0.28855 | 0.30524 | 0.32155 | 0.34987 | 0.37333 | 0.39353 | 0.41057 | 0.42321 | 0.43517 | 0.44395 | 0.45012 | 0.45693 | 0.46068 | 0.46568 | 0.46792 | 0.46542 | 0.46208 | 0.4517 | 0.4391 | 0.42901 | 0.41537 | 0.40447 | 0.3916 | 0.38196 | 0.37254 | 0.36372 | 0.35543 | #N/A | #N/A
Larger leads to
  Larger
  Larger and
  Because
0.010 | 0.90 | 0.95 | 2.77 | 6.67
 | 0.70 | 0.88 | 4.16 | 18.73
 | 0.50 | 0.79 | 5.54 | >20
 | 0.30 | 0.68 | 6.93 | >20
 | 0.10 | 0.47 | 13.86 | >20
0.010 | 0.90 | 0.95 | 2.77 | 6.67
 | 0.70 | 0.88 | 4.16 | 18.73
 | 0.50 | 0.79 | 5.54 | >20
 | 0.30 | 0.68 | 6.93 | >20
 | 0.10 | 0.47 | 13.86 | >20

## Slide 22: vs Wall Height Results (2/2)
Chart: εeff/εsurf vs η for Various εsurf and λ=0.010
| 0 | 3.4641016151377546E-2 | 0.17320508075688773 | 0.34641016151377546 | 0.69282032302755092 | 1.0392304845413265 | 1.3856406460551018 | 1.7320508075688774 | 2.078460969082653 | 2.4248711305964283 | 2.7712812921102037 | 3.117691453623979 | 3.4641016151377548 | 4.156921938165306 | 4.8497422611928567 | 5.5425625842204074 | 6.2353829072479581 | 6.9282032302755097 | 7.6210235533030604 | 8.3138438763306119 | 9.0066641993581626 | 9.6994845223857133 | 10.392304845413264 | 12.124355652982141 | 13.856406460551019 | 15.588457268119896 | 17.320508075688775 | 20.784609690826528 | 24.248711305964282 | 27.712812921102039 | 31.176914536239792 | 34.641016151377549 | 38.105117766515299 | 41.569219381653056 | 45.033320996790813 | 48.497422611928563 | 51.96152422706632 | #N/A | #N/A
0.9 | 1 | 1.0026 | 1.0112 | 1.0205 | 1.036 | 1.0462 | 1.0462 | 1.0551 | 1.057 | 1.058 | 1.0611 | 1.0542 | 1.0495 | 1.0393 | 1.0332 | 1.019 | 1.0099 | 0.99396 | 0.9807 | 0.96982 | 0.94917 | 0.94395 | 0.93334 | 0.9024 | 0.87188 | 0.84925 | 0.82605 | 0.7885 | 0.74384 | 0.71753 | 0.6954 | 0.67581 | 0.65963 | 0.64536 | 0.6327 | 0.61828 | 0.60769
0.7 | 1 | 1.0072 | 1.0362 | 1.0648 | 1.1176 | 1.1529 | 1.1894 | 1.2134 | 1.227 | 1.2375 | 1.244 | 1.25 | 1.2494 | 1.2521 | 1.2444 | 1.2376 | 1.2282 | 1.2105 | 1.2015 | 1.1852 | 1.1703 | 1.1569 | 1.1407 | 1.1076 | 1.0793 | 1.0476 | 1.019 | 0.97235 | 0.92844 | 0.89298 | 0.856 | 0.83145 | 0.80933 | 0.79099 | 0.77594 | 0.75861 | 0.74307
0.5 | 1 | 1.0137 | 1.0644 | 1.1213 | 1.2215 | 1.3047 | 1.3679 | 1.4224 | 1.4651 | 1.5024 | 1.5234 | 1.5437 | 1.5615 | 1.5773 | 1.5858 | 1.5867 | 1.5787 | 1.569 | 1.5561 | 1.5475 | 1.5295 | 1.5191 | 1.5029 | 1.4616 | 1.4199 | 1.3818 | 1.3427 | 1.2865 | 1.2315 | 1.181 | 1.138 | 1.0904 | 1.0659 | 1.0391 | 1.0152 | 0.99457 | 0.97647
0.3 | 1 | 1.0212 | 1.1008 | 1.1928 | 1.3606 | 1.5058 | 1.6337 | 1.7468 | 1.8354 | 1.916 | 1.9836 | 2.0393 | 2.0888 | 2.1626 | 2.21 | 2.2312 | 2.2454 | 2.2634 | 2.2562 | 2.2541 | 2.2462 | 2.2379 | 2.2184 | 2.1855 | 2.1369 | 2.0834 | 2.0385 | 1.9506 | 1.8727 | 1.8022 | 1.7358 | 1.6802 | 1.6267 | 1.5814 | 1.5297 | 1.5028 | 1.4639
0.1 | 1 | 1.0298 | 1.1458 | 1.2872 | 1.5565 | 1.8164 | 2.0561 | 2.2875 | 2.4983 | 2.6959 | 2.8855 | 3.0524 | 3.2155 | 3.4987 | 3.7333 | 3.9353 | 4.1057 | 4.2321 | 4.3517 | 4.4395 | 4.5012 | 4.5693 | 4.6068 | 4.6568 | 4.6792 | 4.6542 | 4.6208 | 4.517 | 4.391 | 4.2901 | 4.1537 | 4.0447 | 3.916 | 3.8196 | 3.7254 | 3.6372 | 3.5543
Lower → larger relative increase in
  Lower has more “room to grow” until it reaches the limit
  still lower for smaller

## Slide 23: Isothermal vs Nonisothermal Cavity Walls
Chart: Isothermal vs Nonisothermal εeff for λ=0.010
| 0 | 3.4641016151377546E-2 | 0.17320508075688773 | 0.34641016151377546 | 0.69282032302755092 | 1.0392304845413265 | 1.3856406460551018 | 1.7320508075688774 | 2.078460969082653 | 2.4248711305964283 | 2.7712812921102037 | 3.117691453623979 | 3.4641016151377548 | 4.156921938165306 | 4.8497422611928567 | 5.5425625842204074 | 6.2353829072479581 | 6.9282032302755097 | 7.6210235533030604 | 8.3138438763306119 | 9.0066641993581626 | 9.6994845223857133 | 10.392304845413264 | 12.124355652982141 | 13.856406460551019 | 15.588457268119896 | 17.320508075688775 | 20.784609690826528 | 24.248711305964282 | 27.712812921102039 | 31.176914536239792 | 34.641016151377549 | 38.105117766515299 | 41.569219381653056 | 45.033320996790813 | 48.497422611928563 | 51.96152422706632
Isothermal | 0.7 | 0.70508 | 0.72442 | 0.74546 | 0.7814 | 0.80728 | 0.83068 | 0.85153 | 0.86595 | 0.87606 | 0.88648 | 0.89188 | 0.89565 | 0.90631 | 0.91378 | 0.91197 | 0.91709 | 0.91986 | 0.91922 | 0.92011 | 0.92126 | 0.92353 | 0.92241 | 0.92462 | 0.9245 | 0.9223 | 0.92206 | 0.92402 | 0.92355 | 0.92327 | 0.92299 | 0.92404 | 0.92264 | 0.92257 | 0.92266 | 0.92362 | 0.92472
Nonisothermal | 0.70506 | 0.72537 | 0.74538 | 0.78232 | 0.80706 | 0.83256 | 0.84938 | 0.85887 | 0.86626 | 0.87078 | 0.87498 | 0.87456 | 0.87644 | 0.87109 | 0.8663 | 0.85976 | 0.84734 | 0.84106 | 0.82966 | 0.81919 | 0.80984 | 0.79852 | 0.77529 | 0.75552 | 0.73331 | 0.71329 | 0.68065 | 0.64991 | 0.62509 | 0.5992 | 0.58201 | 0.56653 | 0.55369 | 0.54316 | 0.53103 | 0.52015 | #N/A | #N/A | #N/A
Isothermal walls at vs nonisothermal walls
Isothermal ≡ nonisothermal for small
Isothermal
  As ,
Nonisothermal
  Critical wall height phenomenon
  As ,

## Slide 24: Varying Wall Nodalization
Chart: Varying Nodalization for λ=0.010
| 0 | 3.4641016151377546E-2 | 0.17320508075688773 | 0.34641016151377546 | 0.69282032302755092 | 1.0392304845413265 | 1.3856406460551018 | 1.7320508075688774 | 2.078460969082653 | 2.4248711305964283 | 2.7712812921102037 | 3.117691453623979 | 3.4641016151377548 | 4.156921938165306 | 4.8497422611928567 | 5.5425625842204074 | 6.2353829072479581 | 6.9282032302755097 | 7.6210235533030604 | 8.3138438763306119 | 9.0066641993581626 | 9.6994845223857133 | 10.392304845413264 | 12.124355652982141 | 13.856406460551019 | 15.588457268119896 | 17.320508075688775 | 20.784609690826528 | 24.248711305964282 | 27.712812921102039 | 31.176914536239792 | 34.641016151377549 | 38.105117766515299 | 41.569219381653056 | 45.033320996790813 | 48.497422611928563 | 51.96152422706632 | #N/A | #N/A
5x3 | 0.7 | 0.70506 | 0.72537 | 0.74538 | 0.78232 | 0.80706 | 0.83256 | 0.84938 | 0.85887 | 0.86626 | 0.87078 | 0.87498 | 0.87456 | 0.87644 | 0.87109 | 0.8663 | 0.85976 | 0.84734 | 0.84106 | 0.82966 | 0.81919 | 0.80984 | 0.79852 | 0.77529 | 0.75552 | 0.73331 | 0.71329 | 0.68065 | 0.64991 | 0.62509 | 0.5992 | 0.58201 | 0.56653 | 0.55369 | 0.54316 | 0.53103 | 0.52015 | #N/A | #N/A
5x5 | 0.7 | 0.70519 | 0.72493 | 0.74602 | 0.78194 | 0.80939 | 0.83133 | 0.84639 | 0.85667 | 0.86504 | 0.8705 | 0.87335 | 0.87737 | 0.87537 | 0.87261 | 0.86602 | 0.85486 | 0.84713 | 0.83946 | 0.82726 | 0.81842 | 0.80904 | 0.79895 | 0.77694 | 0.75304 | 0.73033 | 0.7063 | 0.6734 | 0.64091 | 0.609 | 0.57686 | 0.55673 | 0.53884 | 0.52351 | 0.50906 | 0.49604 | 0.4787 | #N/A | #N/A
5x7 | 0.7 | 0.70574 | 0.72504 | 0.74603 | 0.78211 | 0.80973 | 0.83153 | 0.8459 | 0.85941 | 0.86625 | 0.87153 | 0.8733 | 0.87635 | 0.87465 | 0.87109 | 0.86394 | 0.85473 | 0.84759 | 0.84143 | 0.82592 | 0.8161 | 0.80801 | 0.79811 | 0.77318 | 0.75026 | 0.72821 | 0.70725 | 0.66795 | 0.63487 | 0.60211 | 0.57434 | 0.55065 | 0.5304 | 0.51232 | 0.49204 | 0.47824 | 0.46697 | #N/A | #N/A
5x9 | 0.7 | 0.70542 | 0.72448 | 0.74546 | 0.78339 | 0.80868 | 0.82874 | 0.84845 | 0.85655 | 0.86513 | 0.87035 | 0.87035 | 0.87529 | 0.87531 | 0.87014 | 0.8662 | 0.85549 | 0.84737 | 0.83633 | 0.82685 | 0.81719 | 0.8079 | 0.79913 | 0.77428 | 0.74812 | 0.72693 | 0.70291 | 0.66332 | 0.63152 | 0.59619 | 0.56991 | 0.54781 | 0.5271 | 0.50895 | 0.49138 | 0.47424 | 0.45988 | #N/A | #N/A
Varied wall nodalization from 5x3, 5x5, 5x7, and 5x9 nodes
Increased Z nodalization better captures nonlinear gradients
More accurate gradients → more accurate
Most plots shown for because good agreement up to that point

## Slide 25: Varying Wall Thickness
Chart: εeff vs η for Various λ
| 0 | 3.4641016151377546E-2 | 0.17320508075688773 | 0.34641016151377546 | 0.69282032302755092 | 1.0392304845413265 | 1.3856406460551018 | 1.7320508075688774 | 2.078460969082653 | 2.4248711305964283 | 2.7712812921102037 | 3.117691453623979 | 3.4641016151377548 | 4.156921938165306 | 4.8497422611928567 | 5.5425625842204074 | 6.2353829072479581 | 6.9282032302755097 | 7.6210235533030604 | 8.3138438763306119 | 9.0066641993581626 | 9.6994845223857133 | 10.392304845413264 | 12.124355652982141 | 13.856406460551019 | 15.588457268119896 | 17.320508075688775 | 20.784609690826528 | 24.248711305964282 | 27.712812921102039 | 31.176914536239792 | 34.641016151377549 | 38.105117766515299 | 41.569219381653056 | 45.033320996790813 | 48.497422611928563 | 51.96152422706632 | #N/A | #N/A
λ=0.0005 | 0.7 | 0.70515 | 0.72481 | 0.74589 | 0.77369 | 0.78799 | 0.78768 | 0.78023 | 0.76957 | 0.75217 | 0.73586 | 0.71761 | 0.69972 | 0.66204 | 0.6286 | 0.59594 | 0.56558 | 0.53997 | 0.51243 | 0.49031 | 0.47093 | 0.45104 | 0.43298 | 0.39374 | 0.36218 | 0.33422 | 0.30896 | 0.26821 | 0.23948 | 0.21161 | 0.19387 | 0.18279 | 0.17195 | 0.16354 | 0.15299 | 0.14691 | 0.13983 | #N/A | #N/A
λ=0.005 | 0.7 | 0.70502 | 0.72487 | 0.74595 | 0.78124 | 0.80688 | 0.82894 | 0.84103 | 0.85301 | 0.85675 | 0.86357 | 0.86187 | 0.85892 | 0.84892 | 0.84044 | 0.82733 | 0.81414 | 0.80057 | 0.78643 | 0.77033 | 0.75604 | 0.74352 | 0.73166 | 0.70033 | 0.67137 | 0.64553 | 0.62416 | 0.58864 | 0.55578 | 0.52793 | 0.50541 | 0.49171 | 0.47738 | 0.46701 | 0.45602 | 0.44806 | 0.44012 | #N/A | #N/A
λ=0.010 | 0.7 | 0.70535 | 0.72496 | 0.74572 | 0.78244 | 0.80872 | 0.83104 | 0.84753 | 0.85788 | 0.86567 | 0.87079 | 0.873 | 0.87589 | 0.87544 | 0.87123 | 0.86562 | 0.85621 | 0.84736 | 0.83957 | 0.82742 | 0.81773 | 0.8087 | 0.79868 | 0.77492 | 0.75173 | 0.7297 | 0.70744 | 0.67133 | 0.6393 | 0.6081 | 0.58008 | 0.5593 | 0.54072 | 0.52462 | 0.50891 | 0.49488 | 0.48142 | #N/A | #N/A
λ=0.015 | 0.7 | 0.70591 | 0.72487 | 0.74673 | 0.78084 | 0.8102 | 0.83116 | 0.84824 | 0.86104 | 0.87067 | 0.87329 | 0.88012 | 0.88366 | 0.88432 | 0.88373 | 0.87738 | 0.8732 | 0.86983 | 0.86189 | 0.85364 | 0.847 | 0.84089 | 0.83234 | 0.81227 | 0.79746 | 0.78038 | 0.76309 | 0.72999 | 0.70307 | 0.67502 | 0.65553 | 0.64162 | 0.62441 | 0.61139 | 0.59956 | 0.58667 | 0.57854 | #N/A | #N/A
Increased thickness → lower resistance → smaller gradients (more isothermal) → higher

## Slide 26: Varying Wall Resistance
Chart: εeff vs Rchar for Various εsurf
Plot of vs looks like vs
  Because

## Slide 27: Edge Effects
Chart: Cavity Array Edge Effect in the X Direction for εsurf=0.7, η=3.46, λ=0.010
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11
Y=5 | 0.88012 | 0.878 | 0.87784 | 0.87802 | 0.87918 | 0.87528 | 0.87984 | 0.87841 | 0.88157 | 0.87768 | 0.88167 | 0.89397
Y=4 | 0.87706 | 0.87736 | 0.87718 | 0.87594 | 0.87404 | 0.87877 | 0.8777 | 0.87752 | 0.87566 | 0.8781 | 0.87814 | 0.8911
Y=3 | 0.87798 | 0.87552 | 0.87514 | 0.87697 | 0.87632 | 0.87466 | 0.87382 | 0.8787 | 0.87593 | 0.8778 | 0.87822 | 0.89457
Y=2 | 0.87719 | 0.8739 | 0.88061 | 0.87712 | 0.87674 | 0.87799 | 0.87881 | 0.87912 | 0.87555 | 0.87778 | 0.87862 | 0.89276
Y=1 | 0.8787 | 0.87901 | 0.87691 | 0.87743 | 0.87577 | 0.87737 | 0.87687 | 0.87663 | 0.87703 | 0.87871 | 0.87817 | 0.89431
Y=0 | 0.87456 | 0.875 | 0.87625 | 0.87762 | 0.87585 | 0.87577 | 0.87757 | 0.8772 | 0.87571 | 0.87642 | 0.87725 | 0.89341
Slight increase in for edge cavities at but not
Because cavities at are right triangles, not equilateral
  Have a different value for the same height
  Higher → higher
27

## Slide 28: Isogrid vs Other Geometries (1/2)
Chart: εeff vs η for Single Cell of Different Geometries
| 0 | 0.5 | 1 | 2 | 3 | 4 | 5
Triangle | 0.7 | 0.76761 | 0.81027 | 0.85499 | 0.87153 | 0.88884 | 0.88876
Square | 0.7 | 0.76242 | 0.81341 | 0.85175 | 0.87513 | 0.85824 | 0.84148
Pentagon | 0.7 | 0.76361 | 0.81156 | 0.84878 | 0.84358 | 0.82858 | 0.80157
Hexagon | 0.7 | 0.76475 | 0.81022 | 0.84003 | 0.83311 | 0.80388 | 0.76314
Circle | 0.7 | 0.76552 | 0.80799 | 0.83104 | 0.81297 | 0.77389 | 0.73135
Compared single cell of different geometries
For small
  No difference in because
For larger

## Slide 29: Isogrid vs Other Geometries (2/2)
Chart: Perimeter/Area Ratio for Various Shapes
| Triangle | Square | Pentagon | Hexagon | Circle
P/B | 34.641 | 20 | 14.5309 | 11.547 | 10
Triangle has largest perimeter/area ratio
For a given
  Larger P/A → smaller → lower → larger
Cavities shown at

## Slide 30: Variable Emissivity Isogrid Radiator Concept
Variable-ε radiator using the cavity effect
“Propeller” design
  3 blades around central mast
  Mast raises/lowers with temperature

## Slide 31: Summary
Most other studies
  Cylindrical cavity
  Single cavity
  Isothermal walls
  If nonisothermal, then prescribed temperature profile
This thesis
  Isogrid cavity
  Arbitrarily large array of cavities
  Nonisothermal walls
  Solved for both temperature profile and effective emissivity
Parameters impacting effective emissivity
  Wall height
  Surface emissivity
  Wall thickness
  Wall resistivity
Critical wall height
  peaks at some critical wall height
  As ,
Proposed variable-ε isogrid radiator concept

## Slide 32: Future Work
Verify results in thermal-vacuum chamber
Investigate
  Need finer nodalization on walls to capture large gradients
Isogrid on curved surfaces
  Both concave and convex
  Very common in the real-world
Effect of varying base temperature
  If → smaller gradients on wall → higher ?
  If → larger gradients on wall → lower ?
Directionality of emission from cavity opening
  Cavity is likely not a diffuse emitter due to temperature gradients on the wall, even if each surface it itself diffuse

## Slide 33: Acknowledgements
UMBC
  Dr. Ruey-Hung Chen
  Connie Bailey
NASA GSFC
  Dr. Vivek Dwivedi
  John Hawk
  Rob Chalmers
  Roman Space Telescope project
Committee Members
  Dr. Ruey-Hung Chen
  Dr. Ronghui Ma
  Dr. Liang Zhu
  Dr. Vivek Dwivedi

## Slide 34: Backup Slides

## Slide 35: Spacecraft Thermal Control Coatings
D. G. Gilmore et al., Spacecraft Thermal Control Handbook Volume I: Fundamental Technologies, 2nd ed. The Aerospace Press, 2002.
= IR emissivity
= Solar absorptivity

## Slide 36: Temperature Profile Across Surface 1
Chart: Temperature Profile Across Z for εsurf=0.7, η=3.46, λ=0.010
| 1.0000000000000007 | 0.97959183673469463 | 0.95918367346938849 | 0.93877551020408234 | 0.9183673469387762 | 0.89795918367347005 | 0.87755102040816391 | 0.85714285714285776 | 0.83673469387755162 | 0.81632653061224547 | 0.79591836734693933 | 0.77551020408163318 | 0.75510204081632704 | 0.73469387755102089 | 0.71428571428571475 | 0.6938775510204086 | 0.67346938775510246 | 0.65306122448979631 | 0.63265306122449017 | 0.61224489795918402 | 0.59183673469387788 | 0.57142857142857173 | 0.55102040816326558 | 0.53061224489795944 | 0.51020408163265329 | 0.48979591836734715 | 0.469387755102041 | 0.44897959183673486 | 0.42857142857142871 | 0.40816326530612257 | 0.38775510204081642 | 0.36734693877551028 | 0.34693877551020413 | 0.32653061224489799 | 0.30612244897959184 | 0.2857142857142857 | 0.26530612244897955 | 0.24489795918367344 | 0.22448979591836732 | 0.2040816326530612 | 0.18367346938775508 | 0.16326530612244897 | 0.14285714285714285 | 0.12244897959183672 | 0.1020408163265306 | 8.1632653061224483E-2 | 6.1224489795918366E-2 | 4.0816326530612242E-2 | 2.0408163265306121E-2 | 0
X=0 | -3.1896 | -3.1868 | -3.1794 | -3.168 | -3.1529 | -3.1342 | -3.1121 | -3.0868 | -3.0582 | -3.0267 | -2.9922 | -2.9549 | -2.9148 | -2.872 | -2.8266 | -2.7787 | -2.7283 | -2.6755 | -2.6204 | -2.563 | -2.5033 | -2.4415 | -2.3775 | -2.3114 | -2.2433 | -2.1732 | -2.1011 | -2.0271 | -1.9512 | -1.8735 | -1.794 | -1.7127 | -1.6297 | -1.5451 | -1.4588 | -1.3709 | -1.2814 | -1.1904 | -1.0979 | -1.0041 | -0.909 | -0.81258 | -0.71492 | -0.61604 | -0.51598 | -0.4148 | -0.31256 | -0.2093 | -0.1051 | -1.6e-05
X=L/4 | -3.3609 | -3.3587 | -3.3522 | -3.3416 | -3.327 | -3.3085 | -3.2862 | -3.2604 | -3.2311 | -3.1985 | -3.1626 | -3.1237 | -3.0817 | -3.0368 | -2.9891 | -2.9386 | -2.8855 | -2.8298 | -2.7717 | -2.7111 | -2.6482 | -2.5829 | -2.5155 | -2.4458 | -2.374 | -2.3002 | -2.2243 | -2.1465 | -2.0667 | -1.985 | -1.9015 | -1.8161 | -1.729 | -1.6401 | -1.5495 | -1.4572 | -1.3632 | -1.2676 | -1.1704 | -1.0716 | -0.97124 | -0.86931 | -0.76585 | -0.66089 | -0.55441 | -0.44645 | -0.33702 | -0.22613 | -0.11379 | -1.7e-05
X=L/2 | -3.4775 | -3.4754 | -3.4692 | -3.459 | -3.4449 | -3.427 | -3.4054 | -3.3802 | -3.3514 | -3.3192 | -3.2837 | -3.2449 | -3.2029 | -3.1579 | -3.1099 | -3.059 | -3.0053 | -2.9488 | -2.8896 | -2.8278 | -2.7635 | -2.6967 | -2.6275 | -2.5559 | -2.482 | -2.4059 | -2.3276 | -2.2471 | -2.1646 | -2.0799 | -1.9933 | -1.9048 | -1.8142 | -1.7218 | -1.6275 | -1.5313 | -1.4333 | -1.3334 | -1.2318 | -1.1285 | -1.0234 | -0.91652 | -0.80794 | -0.69763 | -0.58561 | -0.47189 | -0.35647 | -0.23935 | -0.12052 | -1.8e-05
Chart: Temperature Profile Across X for εsurf=0.7, η=3.46, λ=0.010
| 0 | 2.0408163265306121E-2 | 4.0816326530612242E-2 | 6.1224489795918366E-2 | 8.1632653061224483E-2 | 0.1020408163265306 | 0.12244897959183672 | 0.14285714285714285 | 0.16326530612244897 | 0.18367346938775508 | 0.2040816326530612 | 0.22448979591836732 | 0.24489795918367344 | 0.26530612244897955 | 0.2857142857142857 | 0.30612244897959184 | 0.32653061224489799 | 0.34693877551020413 | 0.36734693877551028 | 0.38775510204081642 | 0.40816326530612257 | 0.42857142857142871 | 0.44897959183673486 | 0.469387755102041 | 0.48979591836734715 | 0.51020408163265329 | 0.53061224489795944 | 0.55102040816326558 | 0.57142857142857173 | 0.59183673469387788 | 0.61224489795918402 | 0.63265306122449017 | 0.65306122448979631 | 0.67346938775510246 | 0.6938775510204086 | 0.71428571428571475 | 0.73469387755102089 | 0.75510204081632704 | 0.77551020408163318 | 0.79591836734693933 | 0.81632653061224547 | 0.83673469387755162 | 0.85714285714285776 | 0.87755102040816391 | 0.89795918367347005 | 0.9183673469387762 | 0.93877551020408234 | 0.95918367346938849 | 0.97959183673469463 | 1.0000000000000007
Z=H | -3.1896 | -3.1941 | -3.2035 | -3.2161 | -3.2309 | -3.2472 | -3.2644 | -3.2822 | -3.3001 | -3.3181 | -3.3357 | -3.3527 | -3.3691 | -3.3847 | -3.3994 | -3.413 | -3.4254 | -3.4367 | -3.4466 | -3.4553 | -3.4626 | -3.4685 | -3.473 | -3.476 | -3.4775 | -3.4775 | -3.476 | -3.4731 | -3.4686 | -3.4627 | -3.4554 | -3.4468 | -3.4368 | -3.4255 | -3.4129 | -3.3993 | -3.3846 | -3.3689 | -3.3525 | -3.3355 | -3.318 | -3.3001 | -3.2823 | -3.2646 | -3.2474 | -3.2311 | -3.2164 | -3.2037 | -3.1941 | -3.1896
Z=3H/4 | -2.9148 | -2.9175 | -2.9248 | -2.9358 | -2.9495 | -2.9653 | -2.9824 | -3.0004 | -3.0187 | -3.0372 | -3.0554 | -3.0731 | -3.0902 | -3.1065 | -3.1218 | -3.1359 | -3.1489 | -3.1606 | -3.171 | -3.18 | -3.1876 | -3.1937 | -3.1984 | -3.2014 | -3.2029 | -3.2029 | -3.2014 | -3.1983 | -3.1937 | -3.1876 | -3.18 | -3.171 | -3.1605 | -3.1488 | -3.1358 | -3.1216 | -3.1063 | -3.0901 | -3.073 | -3.0553 | -3.0371 | -3.0187 | -3.0003 | -2.9824 | -2.9653 | -2.9495 | -2.9358 | -2.9248 | -2.9174 | -2.9147
Z=H/2 | -2.2433 | -2.2451 | -2.25 | -2.2577 | -2.2675 | -2.2792 | -2.2923 | -2.3064 | -2.3212 | -2.3364 | -2.3516 | -2.3667 | -2.3814 | -2.3955 | -2.4089 | -2.4215 | -2.4331 | -2.4436 | -2.4529 | -2.4611 | -2.468 | -2.4736 | -2.4778 | -2.4806 | -2.482 | -2.482 | -2.4806 | -2.4778 | -2.4736 | -2.468 | -2.4611 | -2.4529 | -2.4435 | -2.433 | -2.4214 | -2.4088 | -2.3953 | -2.3812 | -2.3664 | -2.3513 | -2.3361 | -2.321 | -2.3062 | -2.2921 | -2.279 | -2.2673 | -2.2574 | -2.2497 | -2.2447 | -2.2429
Z=H/4 | -1.2814 | -1.2825 | -1.2855 | -1.2903 | -1.2964 | -1.3036 | -1.3118 | -1.3206 | -1.3298 | -1.3393 | -1.349 | -1.3585 | -1.3679 | -1.377 | -1.3856 | -1.3937 | -1.4012 | -1.4081 | -1.4142 | -1.4196 | -1.4241 | -1.4277 | -1.4305 | -1.4323 | -1.4333 | -1.4333 | -1.4323 | -1.4305 | -1.4277 | -1.424 | -1.4195 | -1.4142 | -1.408 | -1.4011 | -1.3936 | -1.3854 | -1.3767 | -1.3676 | -1.3582 | -1.3487 | -1.3391 | -1.3296 | -1.3204 | -1.3116 | -1.3035 | -1.2962 | -1.2901 | -1.2853 | -1.2822 | -1.2811