## Slide 1: Mechanics of Structure Genome (MSG)-Based Nonlinear Shell Analysis
Yufei Long, Wenbin Yu
School of Aeronautics & Astronautics, Purdue University
Juan M. Fernandez, Andrew C. Bergan
NASA Langley Research Center
AIAA SciTech 2022, SCS-04/MAT-17, High Strain Composite Materials and Structures III
01/04/2022

## Slide 2: Introduction
Thin-ply High Strain Composite (TP-HSC) deployable booms
Coiled for stowage, long stowage time
Observed permanent deformation, yielding initiated during stowage
MSG-based nonlinear shell homogenization
High efficiency compared with solid models, incremental analysis
Avoid information loss from converting 3D models
[1]
[3]
[2]
[1] Coiled TP-HSC boom
[2] Permanent deformation of the boom cross section
[3] Permanent deformation in the boom longitudinal direction
Δh

## Slide 3: MSG-based Nonlinear Shell Analysis
SwiftComp
MSG-based general purpose constitutive modeling
3D solid & plate/shell analysis
Nonlinear homogenization, incremental analysis
Principle of minimum
information loss
Mechanics of structure genome
Structural elements
Microstructures

## Slide 4: Euler-Newton Combined method
Material model
Euler step
Newton step
Dehomogenization and updating state variables
From last increment
To next increment if converged
1st iteration
Other iterations
Functional to be minimized
Euler predictor step
Newton corrector step
3D strain rate

## Slide 5: 2-Step Homogenization of Plates/Shells
Independent analysis: load prescribing, multiple loading step
2-Step homogenization multiscale analysis: 1) 3D solid step for lamina/yarn; 2) shell step for laminate/woven composites
Read inputs for both plate/shell & 3D models
Preprocessing for both models
Shell model: call 3D model at each integration point
3D model: compute tangent stiffness at each integration point
3D model: compute homogenized tangent stiffness
3D model: solve fluctuating functions, dehomogenization
Shell model: fluctuating function, dehomogenization
Shell model: compute homogenized tangent stiffness
Output

## Slide 6: User-material for Nonlinear SwiftComp
Define nonlinear material model via user-material SCUMAT
Customize user-defined material properties & state variables
Minimize conversion efforts using Abaqus UMAT-like interface
Variables to be updated:
stress — stresses at each integration point
statev — user defined state variables
ddsdde — tangential stiffness

## Slide 7: User Material for Nonlinear SwiftComp
Multiscale Structural Mechanics
cdmhub.org/groups/yugroup
Validation with different existing nonlinear material models
Compared with Abaqus solid model with UMAT
Homogeneous material, thickness 1 mm
Section force N and moment M: calculated from the stresses at the center through the thickness

## Slide 8: User Material for Nonlinear SwiftComp
Multiscale Structural Mechanics
cdmhub.org/groups/yugroup
Simple viscoelastic model [1]
Continuum damage model [2]
[1] Abaqus, 2017 Documentation, Dassault Systèmes Simulia Corporation, 2017.
[2] Zhang, L., and Yu, W., “Constitutive modeling of damageable brittle and quasi-brittle materials,” International Journal of Solids and Structures, Vol. 117, 2017, pp. 80–90.

## Slide 9: Shell Analysis with Nonlinear Viscoelasticity Model
Multiscale Structural Mechanics
cdmhub.org/groups/yugroup
Model developed for analyzing permanent deformation of TP-HSC [1]
1 mm thickness polymethyl methacrylate (PMMA) plastic shell: compared with experiment [2]
30 N/mm creep – 25 N/mm creep recovery
Creep under different load magnitudes
Recovery under different load magnitudes
[1] Zhang, L., Klimm, W., Kwok, K., Fernandez, J. M., Bergan, A. C., and Yu, W., “A Nonlinear Viscoelastic-Viscoplastic Constitutive Model for Epoxy Polymers,” AIAA SciTech 2022 Forum, American Institute of Aeronautics and Astronautics, San Diego, California, 2022.
[2] Lai, J., and Bakker, A., “3-D Schapery representation for non-linear viscoelasticity and finite element implementation,” Computational mechanics, Vol. 18, No. 3, 1996, pp. 182–191.

## Slide 10: 3D Homogenization with Nonlinear Viscoelasticity Model
E1 (MPa) | E2 (MPa) | E3 (MPa) | ν23 | ν13 | ν12 | G23 (MPa) | G13 (MPa) | G12 (MPa)
2.94E5 | 2.91E4 | 2.91E4 | 0.2 | 0.2 | 0.46 | 1.13E4 | 1.13E4 | 1.00E4
Choose the 2D SG of a hexagonal pack
Fiber:
Orthotropic, linearly elastic with elastic constants listed below
Matrix:
Nonlinear viscoelastic model [1]
Compute effective 3D properties
Multiscale Structural Mechanics
cdmhub.org/groups/yugroup
[1] Zhang, L., Klimm, W., Kwok, K., Fernandez, J. M., Bergan, A. C., and Yu, W., “A Nonlinear Viscoelastic-Viscoplastic Constitutive Model for Epoxy Polymers,” AIAA SciTech 2022 Forum, American Institute of Aeronautics and Astronautics, San Diego, California, 2022.

## Slide 11: 3D Homogenization with Nonlinear Viscoelasticity Model
* Relaxation: load to 1% strain in fiber direction over 180 s, then keep for 1800 s
Multiscale Structural Mechanics
cdmhub.org/groups/yugroup

## Slide 12: Bending of Viscoelastic–Viscoplastic PMMA Plate/Shell
κ11 = 0.18 mm–1, thickness 0.2 mm, 9,000 vs. 18,000 s relaxation, 36,000 s recovery
Residual curvature during recovery
Moment–curvature
Multiscale Structural Mechanics
cdmhub.org/groups/yugroup

## Slide 13: 2-Step Homogenization Example
Simple viscoelastic material model from Abaqus manual for the matrix
3D homogenization:
hexagonal pack lamina
Shell homogenization:
for single-layer unidirectional laminate
Prescribed curvature 0.02 mm–1 in the normal direction to the fiber
Moments at different curvature rates
Multiscale Structural Mechanics
cdmhub.org/groups/yugroup

## Slide 14: SwiftComp with Surrogate Model
Same example viscoelastic material
Loaded in the normal direction to the fiber, 1.0% strain over 100 seconds
Construct surrogate model:
Polynomial based
Input — 3 strain components
Output — 3 stress components & 21 stiffness components
2-step homogenization: 6 hours
Surrogate model: 1 hour
Multiscale Structural Mechanics
cdmhub.org/groups/yugroup

## Slide 15: Summary
Nonlinear shell model: MSG-based, Euler-Newton combined method
Nonlinear SwiftComp: 3D solid & shell, load prescribing, multiple analysis steps, SCUMAT
  Validation with Abaqus UMAT: almost exact match
  Nonlinear viscoelastic-viscoplastic model: 4% error compared with experiments
Two-step homogenization: laminates & woven composites, 3D step for lamina/yarn, shell step for laminate/woven composites
Surrogate models: improve the computational efficiency, 6 hours to 1 hour in the example
Future work: Machine learning-based general-purpose surrogate modeling

## Slide 16: Thank You!