## Slide 1
Printed and Flexible Electronics
Devices
Jin-Woo Han
jin-woo.han@nasa.gov
Universities Space Research Association
NASA Ames Research Center
All images courtesy of NASA

## Slide 2
Motivation for Our Work

## Slide 3: In-Space Manufacturing (ISM) Program
In space
Electronic
Components
Space flight 2~3 / year
Significant cost as payload
On Ground
Not green
Energy waste
All images courtesy of NASA

## Slide 4: ISM in International Space Station (ISS)
The gas sensor on
my suit is not working 
Ok, I’ll print
new device 
Design and manufacturing of electronics in space
Images: www.nasa.gov
3D printer in ISS
All images courtesy of NASA

## Slide 5: Printable ‘Electronic’ Components
Sensors
Gas Sensor
Bio Sensor
Energy Generation
Solar Panel
Integrated Circuit
Logic
Memory
Display
Lightning
Energy Storage
Super-Capacitor
Communication
Antenna
Printer/
Material

## Slide 6: Printed Device Platform: A Universal Kit
Gas
sensor
Temp./RH sensor
Radiation
sensor
Energy harvester
User-defined
printing
Built-in heater
Non-volatile memory
Printing on demand
Plug and play based on the universal kit

## Slide 7
Gas Sensors
ACS Sensors, vol. 3, pp. 1782−1788, 2018.
ACS Applied Nano Materials, vol. 2, pp. 6445-6551, 2019.

## Slide 8: Ammonia Gas Leak Accident in ISS
Space Applications: cabin air quality in ISS, leak detection, planetary atmosphere
Societal Applications: Indoor/outdoor air quality, industrial leaks, breath analysis
All images courtesy of NASA

## Slide 9: Printing Process

## Slide 10: Multiport CNT Gas Sensor

## Slide 11: Sensor Experiments

## Slide 12: Ammonia Gas (NH3) Detection
Length normalization

## Slide 13: Variation Tolerance

## Slide 14: Electronic Nose (E-nose)

## Slide 15: Multiple-Gas Detection

## Slide 16
Radiation Sensors
ACS Sensors, vol. 4, pp. 1097-1102, 2018.
ACS Sensors, vol. 2, pp. 1679-1683, 2018.

## Slide 17: All-Printed UV Sensor
Exposed to Ambient Gas
Isolated Air (Oxygen) in Pocket
UV makes CNT less conductive.

## Slide 18: All-Printed Gamma Ray Sensor
Gamma ray makes CNT more conductive.

## Slide 19: Gamma Sensing Mechanism Experiment
Direct Ozon Exposure
Nitrogen Filled Ambient

## Slide 20
Resistive Switching Memory
Nanoscale Adv., Vol. 1, 2990-2998 (2019).

## Slide 21: Autonomous Inventory Management Control
All images courtesy of NASA

## Slide 22: Passive RFID
Printed Memory
16 bit memory = 65,536 IDs

## Slide 23: All Printed Resistive Switching Memory
Conventional Sandwich Type
Single Material Structural Type
Ag pattern
Top view

## Slide 24: All Printed Resistive Switching Memory

## Slide 25
All-Printed Resistive Switching Memory
25
Clever single Ag ink system to create Ag-AgO-Ag system using
an hourglass-shaped pattern and Joule heating.
Unipolar resistive switching with an on/off ratio of 108 at a
reading voltage of 0.02 V.
Bipolar resistive switching is also available, which is beneficial
in reducing switching current and power.
Nanoscale Advances 1, 2990 (2019)

## Slide 26
Mechanical Energy Harvester
Nano Energy, vol. 52, pp. 271-278, 2018.
Nano Energy, vol. 44, pp. 82-88, 2018.
Nano Energy, vol. 39, pp. 238-244, 2017.
For both small scale energy scavenging and large scale wind power generation
where the heavy conventional electromagnetic motors are not favored for launch

## Slide 27: Triboelectricity (Static Electricity)
27
Rubber
Fur
Triboelectricity is created at any contact interfaces.
Triboelectricity is an unwanted phenomenon because too strong voltage causes breakdown of electronics and fire in environments.
 Attractive energy source when properly managed
Notes: REF: http://whs.wsd.wednet.edu/
http://sciencevideosblog.blogspot.kr/
http://www.randrheating.com/humidifiers/
http://scienceblogs.com/startswithabang/2015/06/25/throwback-thursday-a-static-electricity-surprise-synopsis/

## Slide 28
Printable Mechanical Energy Harvester
 | Electromagnetic | Piezoelectric | Triboelectric
Material | Magnet and coil | PZT, BTO, PVDF | Polymers (PTFE, PDMS)
Mass | Heavy | Light | Ultralight
Power density | 0.29 – 1.85 mW/g | 0.35 – 0.43 mW/g | 0.48 – 8.8 mW/g
Cost | Low | High | Ultralow
Mechanical Durability | Good | Poor | Good
In-Space Manufacturability | No | No | Yes

## Slide 29: Operation Principle: Step 1
29
Step 1. Triboelectric charging (Contact electrification)
dielectric
Dielectric surface gains static charges by repeated contacts  Triboelectric layer
Silk
Aluminum
Paper
Cotton, woven
Steel, Nickel, Copper
Brass, Silver
Polyvinyl alcohol
Polyester
Natural rubber
Polyvinylidine chloride
Polyimide (Kapton)
Polyvinvi chloride (PVC)
Polydimethylsiloxane (PDMS)
Polytetrafluoroethylnene (PTFE)
Positive
Negative
Order of electrification (OE)
Positive OE material
Negative OE material
Strong triboelectricity!

## Slide 30: Operation Principle: Step 2
30
Step 2. Electrostatic induction
bot. electrode
top electrode
dielectric
Contact-separation mode
Sliding mode
I
I
I
I

## Slide 31: All 3D Printed TENG - Structure
3D printed TL
3D printed EL
3D printed case
(bottom to top)
q = 0
q = p / 24
q = 2p / 24
q = 3p / 24
QIE : QOE = 9:1
QIE : QOE = 7:3
QIE : QOE = 3:7
QIE : QOE = 1:9
Structure
Operation principle
 | Previous device | This device
Source type | Linear motion | Rotation
Manufacturing | 2D + 3D printing | 3D printing
31

## Slide 32: Grating Configuration Effect
Triboelectric layers
4B
8B
12B
16B
Electrode layers
4B
8B
12B
16B
More blades make more frequent charge movement  Higher energy generation
Accurate patterning by 3D printing is beneficial.
32

## Slide 33: Printable Material Effect
33
ABS
PLA
Nylon
MMA

## Slide 34
34
Printed Supercapacitors
CNT and other carbon inks, Ag ink for electrode
Specific capacitance ~ 170 F/g. Energy density ~ 15 Wh/Kg
Power density ~ 2 KW/Kg, 100,000 cycles without loss of performance

## Slide 35
Thank you