## Slide 1: Aluminum borohydride ammines as fuels for hybrid rocket motors: theoretical performance and particle synthesis
David Drewniak– david.drewniak@psu.edu
Ph.D. Student
Mechanical Engineering Department
NASA Space Technology Graduate Research Fellow ’21
JANNAF 51st Combustion Subcommittee, Session 1O, 6 June 2022
David L. Drewniak, J. Eric Boyer, Richard A. Yetter
Distribution Statement A: Approved for public release; distribution is unlimited.

## Slide 2: Outline
What are aluminum borohydride ammines?
Additives for upper stage hybrid motors
Safer storable
in-space thrusters
Aluminum borohydride hexammine,
Thermal decomposition properties
Synthesis
(g) | (1)
(s) | (2)
 | (1)
 | (2)
Applications

## Slide 3: Aluminum borohydride ammines,
Figures from: Dovgaliuk, I., & Filinchuk, Y. (2016). Aluminium Complexes of B- and N-Based Hydrides: Synthesis, Structures and Hydrogen Storage Properties. International Journal of Hydrogen Energy, 41(34), 15489–15504.
(l)
(s)
Distribution Statement A: Approved for public release; distribution is unlimited.

## Slide 4: Theoretical Performance

## Slide 5: Hydride particle additives can increase regression rate of hydrocarbon fuel binders
Hydride | Tdecomp (°C) |  | Comment
 | 530 | 10.6 | Poor theoretical performance
 | 320 | 18.4 | 
 | 200 | 10.5 | 3 steps to liberate all hydrogen
 | 650 | 11.5 | Boils at 210°C
 | 170 | 10.0 | Two-phase flow losses can be significant
 | 110 | 19.5 | Forms polymer
 | 110 | 17.1 | Liberates and
 | 170 | 17.2 | Liberates and
Hydride | Tdecomp (°C) |  | Comment
 | 530 | 10.6 | Poor theoretical performance
 | 320 | 18.4 | 
 | 200 | 10.5 | 3 steps to liberate all hydrogen
 | 650 | 11.5 | Boils at 210°C
 | 170 | 10.0 | Two-phase flow losses can be significant
 | 110 | 19.5 | 
 | 110 | 17.1 | 
 | 170 | 17.2 | 
Shark, S. C., Pourpoint, T. L., Son, S. F., & Heister, S. D. (2013). Performance of Dicyclopentadiene/H2O2-Based Hybrid Rocket Motors with Metal Hydride Additives. Journal of Propulsion and Power, 29(5), 1122–1129.
At lower additive loading, all hydrides increase regression rate. At high loading, regression rate can be attenuated due to agglomeration and blocking.

## Slide 6
Additives can increase specific impulse slightly and decrease O/F ratio
Calculated vacuum specific impulse (Isp,vac) for 50 wt% hydride particles with PDCPD binder and O2(L) oxidizer, Pchamber = 600 psi, ε = 50, equilibrium composition, B2O3(L) omitted, two-phase losses included, ηvel = 0.90
Poly(dicyclopentadiene) (C10H12, PDCPD) is a hydrophobic plastic binder that is compatible with metal hydrides and can protect them from hydrolyzing

## Slide 7: Al(BH4)3・2NH3 with non-toxic oxidizers has performance comparable to hydrazine/MON-3, but much lower temperature
Pchamber = 200 psi, ε = 15, frozen composition @ ε = 2, ηvel = 0.95
Calculated combustion chamber temperature, Pchamber = 200 psi
Requires powders to be pressed into a fuel grain so no binder is needed. Historical precedence with LiAlH4.*
*Osmon, R. V. (1966). An Experimental Investigation of LiAlH4-H2O2Hybrid Rocket. Chemical Engineering Progress, 62(61), 92–102.

## Slide 8: Particle Synthesis

## Slide 9: Aluminum borohydride ammine synthesis
(g) | Reactor 1
 | Reactor 1
Reactor 2
(s) | Reactor 2
 | Reactor 2
(s) | TBD
 | TBD

## Slide 10: TG/DSC analysis of
Ammonium perchlorate (NH4ClO4, AP) added to investigate effects of NH4 + ion on decomposition steps. Recent studies* found decomposition of NH3BH3 found significant effect of NH4 + inclusion.
*Biswas, P., Ghildiyal, P., Kwon, H., Wang, H., Alibay, Z., Xu, F., Wang, Y., Wong, B. M., & Zachariah, M. R. (2022). Rerouting Pathways of Solid-State Ammonia Borane Energy Release. The Journal of Physical Chemistry C, 126(1), 48–57.
Large value may be due to clathrate NH3 or N2

## Slide 11: Future Work
Opposed flow burner and motor tests with
  Visualize particle decomposition, reaction, and agglomeration
Synthesize
Analyze properties of
  TGA/DSC/MS, specific heat, density, heat of formation
Quantify advantages of based thruster
  LEO, Lunar, interplanetary
Develop injector for fuel rods
Lee, J., Weismiller, M., Connell, T., Risha, G., Yetter, R., Gilbert, P., & Son, S. (2008). Ammonia Borane Based-Propellants. In 44th AIAA/ASME/SAE/ASEE Joint Propulsion Conference \& Exhibit. American Institute of Aeronautics and Astronautics.

## Slide 12: Conclusion
This work was supported by a NASA Space Technology Graduate Research Opportunities Award.
Questions?
Aluminum borohydride ammines may increase the regression rate of conventional hybrid rocket motors due to high H2 content and favorable decomposition pathway
with non-toxic oxidizers is a low temperature alternative to hydrazine/MON-3
synthesized,
TGA/DSC verified full ammoniation,
NH4 + may aid decomposition

## Slide 13: Backup

## Slide 14: Combustion product species at = 2
Exhaust combustion mass fractions for /, frozen chemical composition, temperature = 1930 ± 20K for all O/F at ε = 2; all species gaseous unless labeled otherwise

## Slide 15: Derivation of two-phase flow losses
[1]
[2]
particles
gas
Particles don’t contribute to pressure

## Slide 16: Two-phases losses can have significant effects on performance
Al(BH4)3・2NH3/95%H2O2 with various levels of two-phase flow losses applied, Pchamber = 200 psi, ε = 15, frozen composition @ ε = 2

## Slide 17: Two-phase flow loss derivation
Al(BH4)3・2NH3/95%H2O2 with various levels of two-phase flow losses applied, Pchamber = 200 psi, ε = 15, frozen composition @ ε = 2