## Slide 1: A Data-Driven Bayesian Crack Nucleation Model for Fatigue in Nickel-based Superalloys
George R. Weber1, Max Pinz2, Somnath Ghosh2
Engineering Mechanics Institute Conference 2022
Johns Hopkins University, Baltimore, MD
June 2, 2022
1NASA Langley Research Center, Hampton, VA
(former postdoc at JHU where work was performed)
2Johns Hopkins University, Baltimore, MD

## Slide 2: Nickel (Ni)-based Superalloys
What makes superalloys “super”?
Blades rotate at 10,000 rpm
Tip velocity at 1,200 km/h (750 mph)
Stresses of 180 MPa
Equivalent to the weight of a heavy truck hanging from each blade
Alloy Chemistry
Multiscale Microstructure
Roger Reed. The Superalloys 2008
Gas stream at 1750K
Material of choice for the most extreme environments in jet turbine engine applications
Microstructure of Ni-based superalloy Rene 88DT

## Slide 3: Overview of Model Development Process
Objective
Combine experimental data and a multiscale simulation toolchain to develop a crack nucleation criteria based on material state for Ni-based superalloys
Pinz, Weber, Stinville, Pollock, Ghosh. NPJ Comput Mater 2022
Material State
Fatigue Experiments
Multiscale Simulation Toolchain
Crack Nucleation Probability
Bayesian Model
(Stinville, Pollock, UCSB)

## Slide 4: Experimental Data Sets and Crack Nucleation Observations
…
…
Data Set of 12 Microstructures
Image
Quality Maps
Electron Backscatter Diffraction (EBSD) Maps
Interrupted fatigue experiments with crack nucleation sites along twin boundaries
Type I Crack Nucleation
Stinville, et al. Acta Mater 2016
Digital image correlation fields indicate fatigue cracks at early cycles of deformation

## Slide 5: Concurrent Multiscale Model for Simulation of Polycrystals
Crystal Plasticity
Anisotropic elasticity
Thermally-activated flow rule
Self and latent hardening
Rate-dependent Elastoplasticity
Anisotropic elasticity
Power-law flow rule
Generalized von Mises plasticity
Exponential and linear hardening
Extruded Microstructure
Homogeneous Medium

## Slide 6: Comparison of Boundary Conditions for an Extruded Two-Dimensional Microstructure
Constant Strain Rate Loading to 1% Strain
Homogenized Medium
Elastic Medium
εp
10%
0%
Free Surfaces
What boundary conditions are sufficient for localization studies?

## Slide 7: Cyclic Loading and Assembling Mechanical Response Database
External Cyclic Loading
on all 12 microstructures
10 State Variable Output Fields Are Extracted
Von Mises Stress:
Principal Stresses:
Max. Plastic Slip:
Max. Resolved Shear Stress:
Elastic Helmholtz Energy:
Max. Normal Slip System Stress:
Plastic Defect Energy:
Equivalent Plastic Strain:

## Slide 8: Parallel Slip Configuration
Parallel slip
Out-of-plane slip
Parallel Slip occurs when slip along a parallel slip plane is favored over all other slip planes, and the slip plane is shared between adjacent grains
Parallel Slip Indicator
This is an empirical sufficiency condition for crack nucleation
Active parallel slip
Otherwise
A
B
C
Twin Boundary (111)
Shared Slip Plane
EBSD scan with marked
crack nucleation boundary

## Slide 9: A Bayesian Crack Nucleation Framework
Objective:
At every point, find
“Given the state of the material x, what is the probability of observing a crack?”
Bayesian Model
Can approximate priors from total observed cracked volumes
Large, highly covariant
joint distributions

## Slide 10: Nataf Transformation
Approximation of
To retain the covariance structure while gaining simplification, the joint distributions
are approximated by a Nataf Transformation
1) Transform to Marginally Uniform Random Variable
2) Transform to Marginally Standardized Random Variable
3) Determine Multivariate Normal

## Slide 11: Visualization of Nataf Transformation for Bivariate Case
Original Data
Marginally Uniform Data
Marginally Standard Data

## Slide 12: Nataf Model for Likelihood Probability Density Function (PDF)
Model Fit in Standard Space
Model Transformed to Original Space

## Slide 13: Crack Nucleation Probability Field on a Case Microstructure
Crack Nucleation
Von Mises Stress
Maximum Plastic Slip Rate
Plastic Defect Energy
Top 3 most significant state variables for crack nucleation prediction

## Slide 14: Scalar Crack Nucleation Indicator
Linear Discriminant Analysis
Cracked Regions
Uncracked Regions
Build up of dislocation structures
Directionally dependent shear
Building a Simple One-Dimensional Model

## Slide 15: Concluding Remarks
Probabilistic Crack Nucleation Model
Enables crack nucleation prediction based on local material state
Yields probabilistic output to allow direct comparison between potential sites for failure
Leads to simple scalar mechanistic indicator to explain precursors of nucleation events
Generalizable set of methods for other materials and problem sets
Pinz, Weber, Stinville, Pollock, Ghosh. NPJ Comput Mater 2022

## Slide 16: Additional Slides

## Slide 17: Concurrent Multiscale Model for Simulation of Polycrystals
Crystal Plasticity
Rate-dependent Elastoplasticity
Yield Function
Flow Rule
Anisotropic Elasticity
Hardening Evolution
Orowan Flow Rule
Hardening Law
Anisotropic Elasticity
Extruded Microstructure
Homogeneous Medium

## Slide 18: Homogenization of Crystal Plasticity Constitutive Model
Controlled Stress Loading: Mapping the Yield Function
For a given von Mises strain rate, incrementally load in a stress plane at a fixed stress ratio
Constant Strain Rate: Strain Hardening
θ
Crystal Plasticity
Homogenous
Crystal Plasticity
Homogenous

## Slide 19: Model Selection and Order Reduction
Instead of calculating at once, the model is incrementally built
Allows the assessment of relevance of each state variable
Reduces the order of the final model
Selection algorithm to determine top state variables from data set
(Build model with one new variable)
(Calculate the “average” probability of correctly predicting nucleation)
(Create a set for selected state variables to fill)
(Loop over number of variables needed)
(Loop over remaining variables, not already selected)
(Select the most predictive state variable)
(Add this state variable to the final set)

## Slide 20: Bayesian Crack Nucleation Model Development Pipeline
Experimental Testing
and Characterization
Module I
Concurrent Multiscale Model Development
with Embedded Microstructural RVE
Module II
Creating Database of
Microstructural State Variables
Module III
Development of a Bayesian
Crack Nucleation Model
Module IV