## Slide 1: Artemis 1 Recovery and Post-Flight Evaluations
Jeremy Vander Kam, Orion TPS Liaison for Artemis 1 Recovery
Aug, 2022

## Slide 2: Four Parts to this Story
Orion Background
The EFT-1 Manufacturing Experience
The EFT-1 Flight Test and Post Flight Analysis
Moving Forward to Artemis Missions

## Slide 3: The Orion Program and Ames’ Role
Orion started in 2006 as the Multi-Purpose Crew Vehicle (MPCV)
The TPS Advanced Development Project (ADP) ran from 2006 to 2009
  Purpose: Get started early on a large-scale ablative Heat Shield, technology that NASA had not pursued since the Apollo Program
  The ADP was based at Ames
The Orion contract was awarded in 2009 to Lockheed Martin
EFT-1 Flight Test flown in Dec 2014
Ames continues to provide arc jet testing, thermal and structural analysis, material development, and technical leadership

## Slide 4: The Orion Spacecraft
On-Orbit Configuration
Launch Abort System
Crew Module
Service Module
The Heat Shield

## Slide 5: Artemis 1 Mission Profile
Artemis 1: Un-crewed Distant Retrograde Orbit (DRO) test, late Summer 2022
  Demonstrate TPS at entry velocities of ~ 11 km/s (EFT-1 was 8.9 km/s)
  25,000 mph instead of 20,000 mph
Artemis 1

## Slide 6: Artemis 1 Crew Module and Heat Shield

## Slide 7: The Artemis 1 Heat Shield
186 Avcoat™ blocks bonded to the carrier structure
Seams filled with adhesive

## Slide 8: Orion on Descent

## Slide 10: Small Boats Approach, Assess Safety, and Hook Up Lines

## Slide 11: Recovery by US Navy MDS Units

## Slide 12: Underwater Imagery is Taken

## Slide 13: Orion is Winched Towards the LPD Ship

## Slide 14: Orion is Floated into the Flooded Well Deck

## Slide 15: Orion Guided Over a Recovery Cradle and the Well Deck is Drained

## Slide 16: Orion over the Recovery Cradle

## Slide 17: Initial Inspections and Photos Taken in the Well Deck

## Slide 18: Artemis 1 Test Objective: Evaluate Seam “Fencing”
Seam adhesive can “grow” during the entry trajectory

## Slide 19: EFT-1 Post Flight
Post-Flight Heat Shield
Transition Wakes
Recovery Damage
Stagnation Point – Off-center for a Lifting Entry
Manufacturing Repair Plugs
EFT-1 Heat Shield

## Slide 20: Post-Flight Evaluation
Progressive Machining Operations
~ 60 samples
> 200 Recession Measurements
Thermal, Material, and Mechanical Testing across the country

## Slide 21: Artemis 1: Summer 2022