## Slide 1
Predicting Skin/Stiffener Separation under Cyclic Loads
Carlos G Dávila
Durability, Damage Tolerance and Reliability Branch
NASA Langley Research Center
Hampton, VA
Simulation
Experimental
ONERA Invited Talk
Centre de Châtillon, Paris, FR
September 15, 2022

## Slide 2: Fatigue: Skin/Stiffener Separation

## Slide 3: Fatigue: Skin/Stiffener Separation
How to model the initiation and propagation of skin/stiffener separation under cyclic loads?

## Slide 4: Fatigue Testing – Single Stringer Compression Specimen

## Slide 5: Fatigue - Thermography

## Slide 6: Collapse Sequence
Flange debonding and tunneling
Stringer crippling
58 mm
Delamination inside skin
A
B
C
Infrared camera

## Slide 7: In-situ Ultrasonic Scanner (UT)
UT probe
Single stringer compression specimen (back)
Implanted defect
1000 cycles
2000 cycles
6750 cycles
40 mm
68 mm
72 mm
87 mm
Cycles

## Slide 8: Fatigue Damage Propagation
Typical fatigue propagation of indentation damage
Collapse at 78,135 cycles

## Slide 9: Morphology of Indentation Damage with Fatigue
A. Cross-section
B. Detail of indentation zone
C. Analysis of UT data
Indenter
Skin
Skin
Web
Skin
Flange
Flange
Web

## Slide 10: Separation - Nondestructive Evaluation (NDE)
Ultrasonic C-scanning (UT)
X-Ray Computed Tomography (CT)
Skin
Flange
Delaminations
Delaminations

## Slide 11: Fatigue Propagation Rate Using the Paris Law
Murri, NASA/TM–2013-217966
Paris data does not apply to crack initiation.
Characterization tests take a long time and expensive to conduct.
Tests must be conducted at different stress ratios R and mode mixities B.
Resistance curves induce multiple Paris laws (R-curve effect).
Implementation or Paris law into a cohesive law is difficult.
Paris Law:

## Slide 12: Turon Fatigue Cohesive Model (2006)
Turon Fatigue Damage Law
Both Gmax and lpz are “non-local” quantities, i.e, require data at other integration points
Issues with Paris Law
However:
(Composites A, 2006)
Paris Law

## Slide 13: What effect does an R-curve have on fatigue?
Yao, L., Composites Part A, 2014
d, F
Loading Cycle: Quasi-static Fatigue
QS: Quasi-static
NL: 1st point of nonlinearity
QS

## Slide 14: R-Curve In Fatigue
Yao, L., Composites Part A, 2014

## Slide 15: Characterization of Paris Law
Deobald et. al, NASA/TM–2017
Paris law data must be interpolated for mode mixity and stress ratio

## Slide 16: Fatigue: S-N or Paris Law?
S-N Curve
Paris Law
Can we develop a cohesive model based on S-N that can also predict crack propagation?
S-N Curve and Paris law are related:
b = 2m
Allegri, 2013

## Slide 17: S-N Cohesive Fatigue Damage Model
Consider case of bar subjected to cyclic load
Assume cohesive law is envelope of fatigue damage
F
Time
What damage law?

## Slide 18: CF20 Cohesive Fatigue Damage Model
A
B
S-N curve
Consider damage accumulation function at point P:
Number of cycles to failure obtained by integrating dN from A to B:
≈ 1
CF20, Dávila et al. NASA/TP–2020-220584

## Slide 19: Endurance limit vs. tensile strength (R = -1)
Motor
Specimen
+
-
N. Fleck, 1994
Rotating beam fatigue testing
For R = -1
Notes: Fleck, N. A., Kang, K. J., and Ashby, M. F., "Overview No. 112: The Cyclic Properties of Engineering Materials," Acta Metallurgica et Materialia, Vol. 42, No. 2, 1994

## Slide 20: Goodman Diagram (GD)
The GD is design tool that represents the locus of stress states corresponding to a runout stress or a given number of cycles to failure
R = s min/s max
e
0.58*e

## Slide 21: Determination of Damage Model Parameters
Fatigue model entirely defined by parameters h, e, and p
Endurance (Goodman diagram)
Endurance @ R=-1
Stress ratio
Brittleness
h = 0.95
h = 1
Mixed-mode factor
Mode mix
Affects slope of S-N and Paris law
Affects pre-factor “C” of Paris law

## Slide 22: Determination of Damage Model Parameters
Effect of the model parameters η, ε and p on: a) S-N diagram; b) crack propagation curve

## Slide 23: Palmgren-Miner (P-M) Rule
Does the CF20 fatigue model satisfy the P-M rule?
Recalling that the rate of damage in CF20 is:
It is easy to show that for any sequence of cycles and ,
Yes, the P-M rule is satisfied, i.e., no fatigue history effect on subsequent damage
,

## Slide 24: Implementation into a UMAT Subroutine
Quasi-static tearing damage
Loss of constitutive stiffness
QS mixed-mode parameters
(Turon)
Calculate incremental fatigue damage
Update damage
Relative displacement jump
Update damage with fatigue
Fatigue parameters
Fatigue damage
Fatigue Enabled?
Yes
No
Update damage

## Slide 25: Analysis of Double Cantilever Beam Specimen (DCB)
Applied load remains constant
Detail of propagation zone

## Slide 26: Propagation Rates for DCB Specimen
Test: Murri, NASA/TM–2013-217966
Analyses of DCB were conducted with 4 different applied loads (displacement control)
R = 0.1

## Slide 27: R-Curve Effect on DCB Specimen
Test: Murri, NASA/TM–2013-217966
R-curve
Quasi-static response of DCB using superposition of bridging laws

## Slide 28: Delamination Propagation Rates for DCB with R-Curve
Predicted delamination growth rates in a DCB specimen for several values of applied displacement (red) and applied force (green).
R = 0.1

## Slide 29: Delamination Propagation Rates for DCB with R-Curve
R = 0.1
Predicted delamination growth rates in a DCB specimen for several values of applied displacement (red) and applied force (green).

## Slide 30: R-Curve Effects with Superposition
Test: Murri, NASA/TM–2013-217966
R-curve
DCB
R-curve is captured by superposing two layers of elements with bilinear cohesive laws.
Analysis parameters:
h = 0.95, e = 0.2, p = b
DCB R = 0.1

## Slide 31: Effect of Stress Ratio R on Propagation Rates
(Allegri, 2013)
Analysis parameters:
h = 0.95, e = 0.2, p = b

## Slide 32: Mixed Mode Fatigue – Prediction of MMB Test
Test conducted under force control.
R = 0.1
Analysis parameters:
h = 0.95, e = 0.2, p = b
MMB 50% R = 0.1

## Slide 33: Three Point Bend (3PB) Doubler Specimen
Skin/doubler separation
Skin (tape laminate)
Doubler (fabric)
x
z
y
0°

## Slide 34: Simplified Shell Model of 3PB Doubler Specimen
Interface law w/ bridge
Interface law – nominal tape/tape
Bridge
d
s
Empirical cohesive properties capture the effects of all damage mechanisms
Continuum Shell Model
Skin (3 layers of elements)
Cohesive
Doubler (2 layers)

## Slide 35: Simplified Shell Model of 3PB Doubler Specimen
Predicted
Test
Shell Model
Initiation
Test
Analysis
 | Base | Bridge | 
GIc = | 0.45 | 0.60 | N/mm
GIIc = | 1.1 | 4.50 | N/mm
sc = | 105 | 3.5 | MPa
tc = | 97 | 10. | MPa
KI = | 5E+05 | 1.8E+04 | N/mm3
Ksh = | 1.6E+05 | 3.0E+04 | N/mm3
BK = | 2.07 | 3 | 
Initiation
Propagation
Computed (Turon’s constraints)
Before peak load (symmetric)
After peak load (unsymmetric)
Propagation
Peak load

## Slide 36: 3PB Fatigue – Experimental Results

## Slide 37: Delamination length in 3PB Doubler
3PB Doubler R = 0.1
Analysis parameters:
h = 0.95, e = 0.2, p = b

## Slide 38: Delamination length in 3PB Doubler
3PB Doubler R = 0.4
Analysis parameters:
h = 0.95, e = 0.2, p = b

## Slide 39: General Loading Conditions
R=smin/smax
RL=Fmin/Fmax
Stress ratio
Force ratio
Assume R = RL
Is this assumption always valid?

## Slide 40: General Loading Conditions
Postbuckled stiffened panel Negative load ratios Unsynchronized loads
Constant pressure
Cyclic force
Geometric nonlinearity induces non-proportional stresses in structure.
R varies throughout structure.
Load reversal causes crack closure.
Mode mixity changes during cycle.
R is undefined.
Orientation of interfacial tractions change during cycle.
R is undefined

## Slide 41: General Loading Conditions
Simplified Cyclic Loading Cycle Jump Analysis Min-Max Analysis
Valid if R = RL
Can be used with cycle count techniques for spectrum loading.
Valid if Min and Max are readily identifiable.
Can be used with cycle count techniques for spectrum loading.
Applies to all loads except possibly spectrum loading or block loading.

## Slide 42: General Loading Conditions
R=smin/smax
Calculate Stress ratio
Min-Max Technique
Twin Models
Raimondo, AIAA J., 2020
Max Load Model
Min Load Model
Share damage state

## Slide 43: Concluding Remarks
Fatigue Cohesive Constitutive Model:
  Based on S-N curve rather than Paris law.
  Relies on relationship between S-N and Paris.
  Simplified loading procedure keeps load constant during analysis.
  Fatigue model parameters obtained from DCB test data.
  Same fatigue parameters were used in all analyses (h = 0.95, e = 0.2, p = b ).
  Very simple to implement on top of a UMAT of a bilinear cohesive law
R-Curve Effects Modeled Using Cohesive Superposition
  R-curve represents effect of blunting, delving, bridging, and migrations.
  Shift in Paris lines is predicted.
Skin/Stiffener Separation: 3PB Doubler Test
  Specimen is initially pristine.
  Interface characterized by quasi-static R-curve.