## Slide 1
Ken Segal / NASA Goddard Space Flight Center
ASC 37th Annual Technical Conference
Sept 19-21, 2022
Tucson, Arizona
Composite Technology for Exploration (CTE) Project
Infusing Bonded Joint Technology into Space Launch System Block 1b Flight Structures
This material is a work of the U.S. Government and is not subject to copyright protection in the United States.

## Slide 2: Introduction: Who is Ken Segal ?
From Boston
TRMM
HST Repair Mission 2a
UMd / BSME 1988
FERMI
Pilot Vehicles
Mechanic to Engineer / USAF
JWST
POES
Technology Development: Composites Bonded Joint infusion in SLS

## Slide 3: Presentation Intent
Inform you about CTE Motivation, Objectives and Team
Share Longitudinal and Circumferential Joint (L-Joint and C-Joint) Advancements
Outline Relevant Analytical Tools
Identify Joints infused into SLS and other possibilities

## Slide 4: Composites at NASA: Over a decade working on Composites for Launch Vehicle Applications
CCM: Composite Crew Module (2007-2009)
ACT: Advanced Composites Project (2008-2010)
LSSM: Lightweight Spacecraft Structures and Materials (2011-2012)
CoEX: Composites for Exploration (2012-2013)
CCTD: Composite Cryotank Technology Development (2011-2015)
CEUS: Composites for Exploration Upper Stage (2014-2016)
CTE: Composite Technology for Exploration (2017-2021)
RAMPT: Rapid Analysis and Manufacturing Propulsion Technology (2017-2022)
FUTURE : Thermoplastic Development for Exploration Applications (2022-2024)
CCM: Composite Crew Module

## Slide 5: What Is CTE (The Project)
Y-Joint
CTE Grew From the Composite Cryotank Technology Demonstration Program
Analyses of Y-Joint failure mode and load was a significant challenge.
Ref: NASA TM 2015-218967, ‘Test and Analysis Correlation for a Y-Joint Specimen for a Composite Cryotank’; Brian Mason, et al
Notes: Cracks formed at .2*DLL

## Slide 6: CTE Team and Organizational Structure
1.0 Management
J. Fikes - Project Manager
M. Johnston - Deputy Project Manager
MSFC
3.0
Design/Analysis
D. Sleight/LaRC
K. Segal/GSFC
5.0
Manufacturing
W. Guin/MSFC
6.0
Testing/Evaluation
A. Finchum/MSFC
2.0
Materials
S. Miller/GRC
Notes: Talk about objective to advance joint technology. Acknowledgement verbally to team members.

## Slide 7: What Is CTE (The Project)
Configuration Studied
Circumferential Joint
Payload
EUS
Payload
r
PAF
USA
SLS Block 1b
S
Longitudinal Joint
Payload Attach Fitting (PAF)
Universal Stage Adapter (USA)
Exploration Upper Stage (EUS)
Payload I/F
2
PAF
EUS
USA
Joints Advanced
CTE’s goal is fully vetted designs demonstrating the light weight bonded joint technologies enabling flight mission infusions

## Slide 8: CTE Longitudinal Joint Design Development
CTE Point Design
SLS PLA Infusion
(Manufacturing Demo Shown)
Sub-Element Test
Design
Sub-element Tests and Analysis
Large-Scale Panel Tests and Analysis
Joint Sizing Analyses
Detail Joint Analyses
Material Selection and
Joint Design
Joint Manufacturing
Includes Pristine and damaged verification test analyses

## Slide 9: CTE Point Design
Loads
8.4 m Diameter, Based on SLS Size
1.58 m Diameter
Based on SpaceX Falcon 9 User guide
35 degrees conic angle results in highest membrane loads
Design Basis SLS Block 1b
Payload 10 metric tons
Based on Delta IV Launch Services User’s Guide
Stage / SLS Loads
Based on SLS-SPIE-SPEC-009
CTE Point Design is non-flight SLS scale structure design providing conservative joint development requirements
Notes: Launch Planners Guide

## Slide 10: L-Joint Design Down Select
ACT Industry studies by Boeing and Northrop- Grumman both concluded the double lap composite bonded joint is a preferred joint to advance:
Ref: Boeing’s ‘Composite Joint Concept Development and Evaluation for an ARES V Vehicle’; Final Report dated June 17,2010
Ref: Northrop’s ‘Lightweight Composite Joint Concept Development and Evaluation for an Ares V Vehicle’ , dated Oct 8 ,2010
CEUS Studies
CTE Designs
ACT Industry Studies
The double lap composite bonded joint was advanced for CTE design advancement and analyses studies due to its simplicity, and the abundance of past studies supporting this design and manufacturing.
Plug
Durable Redundant Joint
Metallic Double- Bolted with core densification
Metallic Clevis
Densified Core
Bonded Composite Doubler

## Slide 11: CTE Longitudinal Bonded Joint Design
1” Aluminum sandwich core
8-ply IM7/8552-1 face sheet
4-ply T650/5320-1 doubler
0.005” FM209-1M adhesive
EA9396.MD gap filler
CTE Longitudinal Bonded Joint Design
Compression is the critical load case
Max. compressive design line load is 2000 lb/in
CTE L-Joint designed to highest load in acreage area

## Slide 12: Joint Mass Comparison
Longitudinal Joint Mass and Part Count | Total Mass (lb-f) | # Fasteners | Part Count
Metallic Splice / Bolted with 1 Row of Bolts – Core Densification | 330 | 2100 | 2116
Metallic Splice / Bolted with 1 Row of Bolts – Bushings | 207 | 2100 | 4216
Composite Bolted with 1 Row of Bolts- Core Densified | 290 | 2100 | 2116
Composite Bolted with 1 Row of Bolts- Bushings | 167 | 2100 | 4216
Composite Bolted FailSafe – Core Densified | 234 | 530 | 546
Composite Bolted FailSafe – Bushings | 144 | 530 | 1076
All Bonded | 42 | N/A | 40
CTE Final Design, As Built Data | 27 | 0 | 40
MASS:
‘As modeled’ bonded joint mass 0.38 lb-f / ft
FY18 ‘as built’ mass 0.25 lb-f / ft
2.0 FoS Bonded longitudinal joint : 92% mass reduction and 98% part reduction.

## Slide 13: L-Joint Building Block
Coupons
Elements &
Sub-elements
Subcomponents
Component
~350
~50
2
Number of CTE specimens tested:
Manufacturing Process Development and Scale-up
Design Concepts and Analysis Development
Coupon Testing for Material Properties

## Slide 14: L- Joint Test Designs
Element test designs
Axial Strain Contours
Hoop Tension
24”L x 3” W
Axial and Hoop Edgewise Compression 7”L x 5” W
L-Joint Buckling Test 62”L x 30” W
L-Joint tests verified design and manufacturing, and quantify damage tolerance, and validate bonded joint analytical tools
Sub-component test designs
Notes: Transition, done for both pristine and damaged

## Slide 15: L-Joint Flawed Joint - Failure Analyses
HEWC: 2 inch flaw
Peak load: 15.1 kip
Delamination growth in axial direction
Flaw Growth
Disbonded
Bonded
Panel gap
Load [kip]
Displacement [in]
Initial Flaw
2”
Embedded Teflon insert

## Slide 16: L-Joint HEWC Flawed Test Results
Specimen 1
Specimen 2
Backside facesheet fractured near top of doubler
  Average peak load was 19.5 kip with 1.8% coefficient of variation.
  DIC Evidence of damage growth starting above 95% peak load.
    Primary failure mode was delamination near the midplane of the facesheet
    Delamination occurred at multiple interfaces
  The data shows good damage tolerance of the L-Joint / 9% knockdown compared with pristine
Specimen 3
Multiple interface delamination

## Slide 17: CTE L-Joint Flight Infusion
Shown on PAF MDA and on USA (Ruag)
Infusion: SLS Block 1b
Fiber Damage
in Face-sheet
Fiber Damage
in Face-sheet

## Slide 18: CTE C- Joint Development
Notes: Talk about objective to advance joint technology.

## Slide 19: CTE C-Joint Design Introduction
CTE Point Design Structure*
3D Woven C-channel: Woven by BRM,
Resin Transfer Molded (RTM) by Cornerstone Research Group (CRG)
3D Woven Pi-preform:
Woven by Bally Ribbon Mills (BRM) with B-stage resin impregnated.
Co-bonded to C-channel and Sandwich Panel
Film Adhesive
Conic Sandwich Panels
Composite facesheets with aluminum core
End-ring / Circumferential joint (C-Joint ) design

## Slide 20: FY19 Technical Assessment Periodic Review (TAPR) C-Channel Fiber and Weave Architecture
Two main 3D weave types
Leveraged prior ESA and NASA 3D weave work*: Selected IM7 Fiber and an orthogonal weave for C-channel development
Interlocked
weave
Z-Fiber / Orthogonal weave
*Jones, J., et al, “Comparative Study of 3-Dimensional Woven Joint Architectures for Composite Spacecraft Structures”

## Slide 21: 3D Woven Joints Efforts
TexGen
Illustration
Modeled in
Digimat
FEA Results
“Predicted” Elastic Properties
w/ Modeling & Test Correlation
Concept
BRM (ESA-Sonoca)
Prior Work
NASA / MSFC and GSFC
BRM
Weave flat panels
Northcoast
RTM panels
NASA/ GRC and NIAR
Properties testing
BRM: Design Inputs
NASA/ GSFC & GRC and MSC Software: Modeling Development
NASA/GSFC Joint Assembly
BRM: End Ring Weaving
CRG: Tool design and Fab
CRG: RTM C-Channel
NASA/MSFC and NIAR
Joint Verification Testing

## Slide 22: Partners, Collaborators
NASA MSFC
NASA LaRC
NASA GRC
North Coast Composites
NASA Center
Industry
Cornerstone Research Group (CRG)
Bally Ribbon Mills
NASA GSFC
MSC Software
Extreme Engineering
National Institute for Aviation Research
NASA/ GRC | NASA/ GSFC | MSC Software Extreme Engineering | Bally Ribbon Mills | North coast Composites | Cornerstone Research Group (CRG) | NASA/ LaRC | National Institute for Aviation Research (NIAR) | NASA/ MSFC
Cleveland, OH | Greenbelt, MD | Santa Anna, CA | Bally, PA | Cleveland OH | Miamisburg, OH | Hampton, VA | Wichita, KS | Huntsville, AL
Material Modeling, and Testing | Material Modeling | Material Model Support | 3D Weaving | Panel-Resin Transfer Molding | C-Joint -Tooling and RTM | Joint Sizing Analyses | Material Testing | Project Management and Joint Assembly

## Slide 23: C-Joint Building Block Effort
~200
~20
1
Number specimens tested:
Coupons
Elements &
Sub-elements
Subcomponent
CTE Point Design
Component
Manufacturing Process Development and Scale-up
Design Concepts and Analysis Development
Coupon Testing for Material Properties

## Slide 24: 3D Woven Joint Material Modeling
Modeling/ Analysis with DIGIMAT and GRC General Method of Cells
Weave Design
TexGen Model/ BRM
RVE
FE Mesh
FEA Results
Pi Preform Weave design and property predictions
Modeling DIGIMAT vs. MSGMC

## Slide 25: 3D Weave Progressive Failure Testing
Chart: Tension Dogbone – CTE-218-10-L 5 Load Cycles
Test Coupon
Test Setup
Repeated tension loads shows linear behavior up to ultimate failure
Flat
Panels
* Details of these tests are W. Jackson, et al "Experimental Observations of Damage States
in Unnotched and Notched 3D Orthogonal Woven Coupons Loaded in Tension," AIAA Scitech 2022

## Slide 26: 3D Weave Progressive Failure Testing
As manufactured
Failure in CTE-218-10-L. The arrow marks the edge termination of a warp tow. The circles mark the location of the z-tows along the failure surface.
Matrix Cracking
Run 2
30% Failure
Load
Run 4
93% Failure
Load
Matrix Cracks multiply under loading and are attenuated by fiber tows. Ultimate failure is Z- fiber rupture.

## Slide 27: 3D Weave C-Channel Verification Testing
C Channel Compression shows no damage indications until ultimate failure at an average of 8.2x DLL
Web Section
Compression failure
Chart: C-CHANNEL COMPRESSION - LOAD VS DISPLACEMENT CTE-400-36-A-B

## Slide 28: 3D Weave C-Channel Verification Testing
Test Setup
C Channel Tension shows initial indications of damage at 1.5x DLL and with ultimate failure at an average of 5.8x DLL
Chart: C-Channel TENSION - Load VS Displacement CTE-400-36-x-y
Flange to Web Junction
Failure is Z fiber rupture
Sub-Element

## Slide 29: 3D Weave C-Channel / L-Section Testing
C Channel –L Specimen tension tests shows damage indications at 1.3x DLL on one side and 1.6x DLL on the other side. Ultimate failure at 5.0x DLL
Right Edge @ 396 lbs
Right Edge Initiation DIC (396 lbs)
Left Edge Initiation DIC (525 lbs)
CTE-413-6: Significant damage at 1584 lbs
Edge damage characterization based on DIC ‘correlation measurement uncertainty’ metric
Test Coupon and setup
313.6 lbs is DLL
(224 ib/in x 1.4 inch)
* Details in A. Bergan, et al, "Challenges in Scaling Analysis from Coupons to Elements in 3D Woven Composites for a Launch Vehicle End-Ring Structure“, AIAA Scitech 2022

## Slide 30: Element Compression Test Results
Linear initial response to 7.4x DLL (12 kips)
The GoPro recorded audible events around the start of the nonlinearity (12 kip)
Smooth non-linearity to first load drop (> 21 kips)
Good repeatability
Ultimate compression strength > 10x DLL
Reduction in strain in right side region of PI-base indicating Damage at PI-base, confirmed with Xray CT
  3 coupons tested in Compression
    CTE-440 -1, -4 and -5

## Slide 31: Phase 3 Sub-Element Testing
Objective: Show the C-Joint could withstand 4 lifetimes of loading and sustain performance
3 Cycles load cycles performed with linear load vs displacement responses
Subsequent tests to failure initiation
  Tension -2
    9.28 Kips (10x DLL)
  Tension -9
    8.90 Kips (9.56x DLL)
  Compression -7
    17.84 Kips (11.0x DLL)
  Compression -8
    22.70 Kips (14.0x DLL)
Sub-element coupon tests show that after multiple life cycles C-joint Pi-Preform bond in tension and compression remain robust at loads 9x DLL

## Slide 32: Subcomponent Test and Setup
Test team and location: MSFC ET-30 / Bldg. 4655
Instrumentation
  4 Full Field DIC systems
  32 Foil Strain Gages
  10 LVDTs
  5 Go Pros
Sandwich Panel
Lower simulator
C-Joint
Upper simulator
Guided boundary condition
C-channel Load
Panel Load
Combined Loads Test Cases and Nomenclature
Panel Compression, C-channel Compression (PCCC)
Panel Tension, C-channel Compression (PTCC)
Panel Tension, C-channel Tension (PTCT)
Panel Compression, C-channel Tension (PCCT)
Sub-
component

## Slide 33: Subcomponent Load Cases
Load Case in order (top down and left to right) | 1.25xDLL | 2.00xDLL | 5.00xDLL
PCCC : Panel Compression C-Chanel Compression |  |  | Stopped Test at 3.7 x DLL
PTCC : Panel Tension C-Chanel Compression |  |  | No tests planned
PTCT : Panel Tension C-Chanel Tension |  | Tension stiffness change | 
PCCT :Panel Compression C-Chanel Tension | Bolted interface slip | Bolted interface slip | 
76 Load cases run encompassing the CTE Point Design Structure. Worst case superposition used to be conservative

## Slide 34: Test Results – Load vs. Actuator Displacement PCCC (Panel Compression C-channel Compression)
C-channel
Load (Kips)
Actuator Displacement (in.)
Linear behavior exhibited beyond 2 x DLL
No change in stiffness through testing (3.72 x DLL was last load case run)
During 500 PCCC test a side load actuator boundary condition change led to large deformation of the panel, which triggered a pre-programmed limit and stopped the test automatically.
Sandwich Panel
Load (Kips)
Actuator Displacement (in.)
Change in boundary condition
NOTE: Doted line is a reference line measuring the degree of linearity of test results for all charts.

## Slide 35: Test Results – Load vs. Actuator Displacement PTCT (Panel Tension C-channel Tension)
C-channel
Load (Kips)
Actuator Displacement (in.)
Sandwich Panel
Load (Kips)
Actuator Displacement (in.)
Initially linear behavior becomes nonlinear relatively early – expected based on previous sub-element tests
  C-channel flange stiffness in tension is nonlinear and that affects both the C-channel and Panel displacements
Good repeatability achieved with respect to loading of both C-channel and panel

## Slide 36: PTCT (Panel Tension C-Channel Tension) Indications of Damage via DIC
C-channel flange damage indicated by permanent deformation
  0.006 inch at end of 2x DLL loading
  Some additional recovery may occur due to viscoelasticity
Anticipated based on previous L-section tests
Carried full load, not a structural failure event
Relevant stiffness change may result at this level
Initial stiffness 1.25x DLL
Re-loads with reduced stiffness 2x DLL
Permanent deformation
Virtual extensometers defined in DIC
Left
Right
DIC contour showing permanent displacement after unloading

## Slide 37
Different initial stiffness in two loadings noticed.
Small displacement offset noticed at end of unloading cycle
Good repeatability in initial stiffness
Slippage at the interface of lower C-channel flange and bottom simulator flange observed visually and with DIC in both 1.25 & 2.0 x DLL cases
Slip expected as preload was low to prevent flange damage.
Displacement jump in 2.0 x DLL case as a result of boundary condition change for side actuator
C-channel
Load (Kips)
Actuator Displacement (in.)
Loading
Un-Loading
Permanent deformation
Test Results – Load vs. Actuator Displacement PCCT (Panel Compression C-channel Tension)
Sandwich Panel
Load (Kips)
Actuator Displacement (in.)
Un-Loading
Loading
Permanent deformation
Slip Range
Change in boundary condition
Relative Displacement Due to Slip
2.0 DLL PCCT Out of Plane Displacement
Lower flange bolt holes inspected- no damage found

## Slide 38: Final PCCC Test Comparison
C-channel
Load (Kips)
Actuator Displacement (in.)
Linear displacement behavior exhibited by C-channel to max load and in panel to 2.7 x DLL.
Abrupt change in boundary condition, predicted, at side load actuator and panel load tab intersection point (spherical bearing) led to large deformation of the panel and test stopped automatically.
Sandwich Panel
Load (Kips)
Actuator Displacement (in.)
Change in boundary condition
3.72 x DLL CASE
Last Test load achieved
PC – 23.58 Kips,
CC – 223.28 Kips

## Slide 39: Panel Rotation at ~3.7xDLL PCCC
Chart: Normal to Panel Z Displacement (in)
| 0 | 2.0708609246449499E-3 | 3.8384050222298495E-3 | 3.6633103942202497E-3 | 2.33610897165445E-3 | -2.0793961938718602E-4 | -4.1545536741902497E-3 | -9.7536682544822496E-3 | -1.7371720901203147E-2 | -2.754465389363215E-2 | -4.1086113646587145E-2 | -5.9293997154823148E-2
 | 0 | 2.1267 | 4.2533 | 6.38 | 8.5066 | 10.6333 | 12.7599 | 14.8865 | 17.0131 | 19.1397 | 21.2662 | 23.3928
+Z Panel Normal
in
The spherical- spherical bearing ended panel load line was not restrained potentially leading to instability under compressive loading
FEA pre-test shows panel out-of-plane displacement opposite to what observed in test and can be attributed to boundary condition uncertainties
The instability is sensitive to misalignments, C-channel axis roller contact status, etc. and these could have contributed to the direction of rotation (test vs. FEA)
Deformed shape exaggerated by 10x

## Slide 40: 3D Woven Light Weight Joints - Demonstrated
+Z Panel Normal
in
Ref, ‘3D Woven Composite End Ring Structure: Design Development and Verification Testing’. SciTech 2022, K. Segal, B.Farrokh, A.Bergan, R. Matarese, D. Sleight, A.Satyanarayana, and D. Myers
Deformed shape exaggerated by 10x
3D Woven joints in a primary load path has been demonstrated
3D Woven Design and analyses tools are proven capable though CTE work
Mass reduction of 100s of pound can be saved in future missions
For more information contact me
Kenneth.N.Segal@nasa.gov / 301-286-2895
or
Ken Segal on Linked in