## Slide 1: Lunar Thermal Analysis Guidebook (L-TAG): Thermo-physical and Optical Properties of Lunar Regolith Carlos Gomez, Brian Hamill, Greg Schunk NASA/Marshall Space Flight Center & Lisa Erickson NASA/Johnson Space Center
Presented By Lisa Erickson
Thermal & Fluids Analysis Workshop TFAWS 2022 September 6th-9th, 2022
Virtual Conference
TFAWS Short Course

## Slide 2: Background
The electromagnetic radiation spectrum is sub-divided into multiple bands based on differences in behavior. Of particular interest in radiation heat transfer is the “Thermal Radiation” band of the electromagnetic spectrum between 0.1 and 100 microns in wavelength.
Outside of the thermal waveband, electromagnetic energy generally passes through objects or has very little heat energy (based on temperature) under practical conditions.
Wavelengths beyond 100 microns may be of interest in measuring extremely low temperatures such as the far side of the Moon or perpetually shadowed craters. An object at a given temperature will emit energy over a spectrum of wavelengths.
Thermal analyses are typically conducted using a two waveband absorptance model which subdivides the thermal energy spectrum into solar (< 3.0 mm) and infrared (>3.0 mm) wavelengths.

## Slide 3: Solar Absorptivity/Albedo
Albedo is the fraction of incident light or radiation reflected by a surface and may be defined in several different ways.
Normal albedo is the reflectance of a surface when both viewed and illuminated in the local vertical direction (i.e. normal to the surface).
Directional hemispherical albedo is the reflectance in all directions resulting from direct illumination from a specific direction.
Total hemispherical albedo is the reflectance in all viewing directions integrated over all phase angles.
q
d
q
d
Normal Albedo
Directional
Hemispherical
Albedo
Total
Hemispherical
Albedo

## Slide 4: Bolometric Albedo
Bolometric albedos are obtained by integrating the wavelength dependent albedo over the waveband of interest as illustrated below for the lunar surface normal and hemispherical albedos.
A bolometric normal or hemispherical albedo would be averaged against the solar spectrum represented as a black body radiating at 5800K.
The hemispherical bolometric albedo is computed in two steps: first integrated over wavelength for a specific direction and then integrated over all incident directions.
Bolometric Normal Albedo
Bolometric Hemispherical Albedo

## Slide 5: Terrestrial Measurements of Lunar Albedo
Dollfus and Bowell [1] derived the normal albedo from telescopic observations of the near side lunar surface. The measurements were made and averaged for 14 different regions over a wavelength range of 0.327m to 1.05m. The following relation was derived to fit the normal albedo to the observations.
Since the observed waveband does not include the entire solar spectrum, the normal wavelength dependent albedo is integrated against the truncated waveband to obtain the bolometric normal albedo as shown below.
The bolometric normal albedo is recommended for orbital calculations involving a radiatively participating lunar surface as described in DSNE 3.3.9.1.2.
1A Dollfus and E. Bowell, “Polarimetric Properties of the Lunar Surface and its Interpretation”, Astronomy and Astrophysics 10, 29-53, 1971.

## Slide 6: Solar Incident Angle Albedo
For detailed thermal modeling of the lunar surface temperature, a solar incident angle albedo obtained from direct measurement of Apollo Sample Fines or correlations based on lunar surface temperature by a number of authors including Keihm, Williams, Vasvada, Hayne or Feng may be needed.

## Slide 7: Infrared Emittance
Directional, spectral, and total emittances of Apollo samples have been measured1
Equatorial emittances has been derived from Ch7 LRO Diviner brightness temperatures, which fairly represents actual kinetic temperatures2
Equatorial Emissivity from Vasavada 2012. Solid line is data smoothed over 3o of longitude every 0.05o (Ch7 is 25–41 μm, this is technically a spectral emittance) .2
1 Birkebak, “Thermal Radiation Properties of Lunar Materials from the Apollo Missions,” 1974.
2Vasavada et al., “Lunar equatorial surface temperatures and regolith properties from the Diviner,” 2012.
*Brightness temperatures measure total IR emission from the surface For more information see Supporting online Material for Paige et al., “Diviner Lunar Radiometer Observations of Cold Traps in the Moon’s South Polar Region,” 2010, doi: 10.1126/science.1187726
Total Emittance of Apollo 11 and 12 lunar fine samples from Birkebak 19742

## Slide 8: Infrared Emittance
Recommended values from DSNE:1
Location | Emissivity ε,
Highland mean (0O lat) | 0.95 – 0.98
Mare mean (0O lat) | 0.95 – 0.98
South Pole (84-90OS) nominal | Use Highland equatorial values. (No data available).
1 Cross-Program Design Specification for Natural Environments (DSNE), Rev G, 2019. Figure 3.4.6.2.1-1. Cremers and Birkeback 1971, Cremers et al. 1972, Cremers 1972, Cremers and Hsia 1974)
Notes: Note:

## Slide 9: Density,
Sample bulk density depends on:
  grain type, size, density
  sample porosity, compression
  ice content1
On the Lunar Surface, density depends on depth and location
  Global depth vs density models have been developed3,4,5
Bulk density vs depth. Apollo 15 site2
1 Reiss et al., "In-Situ Thermal Extraction of Volatiles from Lunar Regolith“ 2018.
2G. Heiken et al., Lunar sourcebook: A user’s guide to the moon. New York: Cambridge, Figure 9.19 p.499.
3 A. Vasavada et al., “Near-Surface Temperatures on Mercury and the Moon and the Stability of Polar Ice Deposits,” 1999.
4 Hayne et al., “Global Regolith Thermophysical Properties of the Moon From the Diviner Lunar Radiometer Experiment: Lunar Regolith Thermophysical Properties,” 2017.
5 Martinez and Siegler, “A Global Thermal Conductivity Model for Lunar Regolith at Low Temperatures,” 2021.

## Slide 10: Density,
Hayne 2017 – Global Density1
1 P. O. Hayne et al., “Global Regolith Thermophysical Properties of the Moon From the Diviner Lunar Radiometer Experiment: Lunar Regolith Thermophysical Properties,” 2017.
Table A1: Standard model parameters and physical constants
surface layer
deepest layer
z = depth (from surface) [m]
H = H-parameter, a location dependent scaling factor.
Determined H for ±70°LAT (typical range: 0 - 0.1 m)
Note: (,T),) were assumed constant – they vary locally but their variations manifest as different best fit H parameter values
average H for ±60°LAT is 0.068 m
Chart: Density, kg/m3

## Slide 11: Density: H - Parameter Map
https://quickmap.lroc.asu.edu/query?extent=136.6294561%2C71.9324346%2C-177.1800951%2C-76.0361511&proj=16&layerListFilter=&features=209.40000000%2C-89.59200000%7C6.95068337%2C32.16735885%7C-11.40643297%2C-42.98468575%7C43.52367024%2C42.87280373&selected=3&layers=NrBsFYBoAZIRnpEBmZcAsjYIHYFcAbAyAbwF8BdJAdgTpgDoAOAJknyNICIAnAQxwBzAKYAFPgWEAXKcK4AuLgHcAxgHsCeKdC6Uq5KsGSg22RCjgsz9DsQP69QA
Lunar QuickMap website

## Slide 12: Thermal Conductivity,
Bulk 𝑘 accounts for both conduction/radiation between/through grains
depends on:
  Material composition
  Temperature
  Density
Lunar surface vs temperature and density models have been developedincluding:1,2,3,4
Thermal conductivity of Apollo samples5
1 A. Vasavada et al., “Near-Surface Temperatures on Mercury and the Moon and the Stability of Polar Ice Deposits,” 1999.
2 Hayne et al., “Global Regolith Thermophysical Properties of the Moon From the Diviner Lunar Radiometer Experiment: Lunar Regolith Thermophysical Properties,” 2017.
3 Martinez and Siegler, “A Global Thermal Conductivity Model for Lunar Regolith at Low Temperatures,” 2021.
4Woods-Robinson et al., " A model for the Thermophysical Properties of Lunar Regolith at Low Temperatures" 2019.
5 Cross-Program Design Specification for Natural Environments (DSNE), Rev G, 2019. Figure 3.4.6.2.1-1. Cremers and Birkeback 1971, Cremers et al. 1972, Cremers 1972, Cremers and Hsia 1974)

## Slide 13: Thermal Conductivity,
Chart: Hayne 2017
| 20 | 40 | 60 | 80 | 100 | 120 | 140 | 160 | 180 | 200 | 220 | 240 | 260 | 280 | 300 | 320 | 340 | 360 | 380 | 400 | 420 | 440
1105.12 | 0.00075985 | 0.00076252 | 0.00076979 | 0.00078395 | 0.00080729 | 0.00084211 | 0.0008907 | 0.00095536 | 0.0010384 | 0.0011421 | 0.0012687 | 0.0014206 | 0.0016001 | 0.0018093 | 0.0020508 | 0.0023266 | 0.0026392 | 0.0029908 | 0.0033838 | 0.0038203 | 0.0043028 | 0.0048335
1198.20 | 0.0011137 | 0.0011177 | 0.0011283 | 0.0011491 | 0.0011833 | 0.0012343 | 0.0013055 | 0.0014003 | 0.001522 | 0.001674 | 0.0018596 | 0.0020822 | 0.0023453 | 0.002652 | 0.0030059 | 0.0034102 | 0.0038684 | 0.0043838 | 0.0049597 | 0.0055996 | 0.0063068 | 0.0070846
1348.08 | 0.0016836 | 0.0016895 | 0.0017056 | 0.001737 | 0.0017887 | 0.0018658 | 0.0019735 | 0.0021167 | 0.0023007 | 0.0025304 | 0.002811 | 0.0031476 | 0.0035452 | 0.0040089 | 0.0045438 | 0.005155 | 0.0058476 | 0.0066267 | 0.0074973 | 0.0084645 | 0.0095335 | 0.010709
1506.14 | 0.0022845 | 0.0022925 | 0.0023144 | 0.002357 | 0.0024271 | 0.0025318 | 0.0026779 | 0.0028723 | 0.0031219 | 0.0034337 | 0.0038144 | 0.0042711 | 0.0048106 | 0.0054398 | 0.0061657 | 0.006995 | 0.0079349 | 0.008992 | 0.010173 | 0.011486 | 0.012936 | 0.014532
1673.10 | 0.0029193 | 0.0029295 | 0.0029575 | 0.0030119 | 0.0031015 | 0.0032353 | 0.003422 | 0.0036704 | 0.0039894 | 0.0043877 | 0.0048743 | 0.0054579 | 0.0061473 | 0.0069513 | 0.0078789 | 0.0089387 | 0.01014 | 0.011491 | 0.013 | 0.014677 | 0.016531 | 0.01857
1774.40 | 0.0033044 | 0.003316 | 0.0033476 | 0.0034092 | 0.0035107 | 0.0036621 | 0.0038734 | 0.0041546 | 0.0045157 | 0.0049666 | 0.0055173 | 0.0061779 | 0.0069583 | 0.0078684 | 0.0089183 | 0.010118 | 0.011477 | 0.013006 | 0.014715 | 0.016614 | 0.018712 | 0.02102
1798.67 | 0.0033966 | 0.0034086 | 0.0034411 | 0.0035044 | 0.0036087 | 0.0037644 | 0.0039816 | 0.0042706 | 0.0046418 | 0.0051053 | 0.0056714 | 0.0063504 | 0.0071525 | 0.0080881 | 0.0091673 | 0.0104 | 0.011798 | 0.01337 | 0.015126 | 0.017078 | 0.019234 | 0.021607
1799.99 | 0.0034017 | 0.0034137 | 0.0034462 | 0.0035096 | 0.0036141 | 0.00377 | 0.0039875 | 0.004277 | 0.0046487 | 0.0051129 | 0.0056798 | 0.0063598 | 0.0071632 | 0.0081001 | 0.0091809 | 0.010416 | 0.011815 | 0.013389 | 0.015149 | 0.017103 | 0.019263 | 0.021639
1800.00 | 0.0034017 | 0.0034137 | 0.0034462 | 0.0035096 | 0.0036141 | 0.00377 | 0.0039875 | 0.004277 | 0.0046487 | 0.0051129 | 0.0056799 | 0.0063599 | 0.0071632 | 0.0081002 | 0.009181 | 0.010416 | 0.011815 | 0.01339 | 0.015149 | 0.017103 | 0.019263 | 0.021639
Suggested models for lunar surface modeling:
  Hayne 2017
  Martinez and Siegler 2019
  See references for full equations
1 Hayne et al., “Global Regolith Thermophysical Properties of the Moon From the Diviner Lunar Radiometer Experiment: Lunar Regolith Thermophysical Properties,” 2017.
2 Martinez and Siegler, “A Global Thermal Conductivity Model for Lunar Regolith at Low Temperatures,” 2021.
Sufficient in most cases
Chart: Martinez and Siegler 2021
| 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 | 120 | 130 | 140 | 150 | 160 | 170 | 180 | 190 | 200 | 210 | 220 | 230 | 240 | 250 | 260 | 270 | 280 | 290 | 300 | 310 | 320 | 330 | 340 | 350 | 360 | 370 | 380 | 390 | 400
1105.12 | 7.4468e-05 | 0.00010476 | 0.0001417 | 0.00018089 | 0.00022069 | 0.00026046 | 0.00029998 | 0.00033921 | 0.00037825 | 0.00041721 | 0.00045626 | 0.0004956 | 0.00053542 | 0.00057592 | 0.00061733 | 0.00065986 | 0.00070372 | 0.00074914 | 0.00079634 | 0.00084553 | 0.00089693 | 0.00095076 | 0.0010072 | 0.0010666 | 0.001129 | 0.0011947 | 0.001264 | 0.0013369 | 0.0014138 | 0.0014947 | 0.0015801 | 0.0016699 | 0.0017645 | 0.0018641 | 0.0019688 | 0.0020788 | 0.0021944 | 0.0023157 | 0.0024429
1198.20 | 0.00014265 | 0.00020059 | 0.0002712 | 0.00034597 | 0.00042176 | 0.00049731 | 0.00057216 | 0.00064623 | 0.00071963 | 0.00079258 | 0.00086537 | 0.00093832 | 0.0010118 | 0.0010862 | 0.0011618 | 0.0012391 | 0.0013184 | 0.0014001 | 0.0014847 | 0.0015724 | 0.0016638 | 0.0017591 | 0.0018588 | 0.0019632 | 0.0020728 | 0.0021879 | 0.0023088 | 0.002436 | 0.0025698 | 0.0027106 | 0.0028588 | 0.0030147 | 0.0031786 | 0.003351 | 0.0035321 | 0.0037223 | 0.003922 | 0.0041316 | 0.0043512
1348.08 | 0.00025244 | 0.0003549 | 0.0004797 | 0.00061177 | 0.00074552 | 0.00087868 | 0.0010104 | 0.0011406 | 0.0012693 | 0.001397 | 0.0015241 | 0.0016512 | 0.0017789 | 0.0019077 | 0.0020385 | 0.0021717 | 0.0023081 | 0.0024483 | 0.002593 | 0.0027429 | 0.0028985 | 0.0030607 | 0.0032299 | 0.003407 | 0.0035924 | 0.003787 | 0.0039912 | 0.0042058 | 0.0044313 | 0.0046684 | 0.0049177 | 0.0051799 | 0.0054554 | 0.005745 | 0.0060492 | 0.0063686 | 0.0067038 | 0.0070554 | 0.0074239
1506.14 | 0.00036822 | 0.00051763 | 0.00069959 | 0.00089209 | 0.001087 | 0.0012809 | 0.0014726 | 0.0016619 | 0.001849 | 0.0020344 | 0.0022188 | 0.002403 | 0.0025878 | 0.0027742 | 0.002963 | 0.0031553 | 0.0033518 | 0.0035537 | 0.0037619 | 0.0039772 | 0.0042007 | 0.0044333 | 0.004676 | 0.0049296 | 0.0051951 | 0.0054734 | 0.0057655 | 0.0060722 | 0.0063944 | 0.0067331 | 0.0070891 | 0.0074633 | 0.0078566 | 0.0082698 | 0.0087038 | 0.0091594 | 0.0096375 | 0.010139 | 0.010664
1673.10 | 0.00049052 | 0.00068952 | 0.00093186 | 0.0011882 | 0.0014476 | 0.0017057 | 0.0019608 | 0.0022126 | 0.0024613 | 0.0027077 | 0.0029526 | 0.0031971 | 0.0034423 | 0.0036894 | 0.0039396 | 0.0041942 | 0.0044544 | 0.0047214 | 0.0049966 | 0.0052811 | 0.0055762 | 0.0058833 | 0.0062034 | 0.0065379 | 0.0068879 | 0.0072548 | 0.0076396 | 0.0080437 | 0.0084681 | 0.0089141 | 0.0093828 | 0.0098754 | 0.010393 | 0.010937 | 0.011508 | 0.012107 | 0.012736 | 0.013396 | 0.014087
1774.40 | 0.00056472 | 0.00079382 | 0.0010728 | 0.0013679 | 0.0016664 | 0.0019635 | 0.0022571 | 0.0025467 | 0.0028329 | 0.0031162 | 0.0033978 | 0.0036789 | 0.0039607 | 0.0042447 | 0.0045322 | 0.0048245 | 0.0051233 | 0.0054299 | 0.0057457 | 0.0060722 | 0.0064108 | 0.006763 | 0.0071301 | 0.0075137 | 0.007915 | 0.0083356 | 0.0087767 | 0.0092398 | 0.0097262 | 0.010237 | 0.010774 | 0.011339 | 0.011932 | 0.012555 | 0.013209 | 0.013896 | 0.014617 | 0.015372 | 0.016164
1798.67 | 0.0005825 | 0.0008188 | 0.0011065 | 0.0014109 | 0.0017189 | 0.0020252 | 0.002328 | 0.0026268 | 0.0029219 | 0.0032141 | 0.0035045 | 0.0037943 | 0.0040849 | 0.0043777 | 0.0046741 | 0.0049755 | 0.0052835 | 0.0055996 | 0.0059251 | 0.0062617 | 0.0066107 | 0.0069737 | 0.0073521 | 0.0077474 | 0.0081611 | 0.0085945 | 0.0090491 | 0.0095264 | 0.010028 | 0.010554 | 0.011108 | 0.011689 | 0.012301 | 0.012943 | 0.013617 | 0.014324 | 0.015067 | 0.015846 | 0.016662
1799.99 | 0.00058347 | 0.00082017 | 0.0011084 | 0.0014132 | 0.0017217 | 0.0020286 | 0.0023319 | 0.0026312 | 0.0029267 | 0.0032194 | 0.0035103 | 0.0038006 | 0.0040917 | 0.004385 | 0.0046819 | 0.0049838 | 0.0052923 | 0.0056089 | 0.0059349 | 0.006272 | 0.0066216 | 0.0069852 | 0.0073643 | 0.0077602 | 0.0081745 | 0.0086087 | 0.009064 | 0.009542 | 0.010044 | 0.010572 | 0.011126 | 0.011709 | 0.012321 | 0.012964 | 0.013639 | 0.014348 | 0.015092 | 0.015871 | 0.016689
1800.00 | 0.00058347 | 0.00082017 | 0.0011084 | 0.0014133 | 0.0017217 | 0.0020286 | 0.0023319 | 0.0026312 | 0.0029267 | 0.0032194 | 0.0035103 | 0.0038007 | 0.0040917 | 0.004385 | 0.0046819 | 0.0049838 | 0.0052924 | 0.0056089 | 0.005935 | 0.0062721 | 0.0066217 | 0.0069853 | 0.0073643 | 0.0077603 | 0.0081746 | 0.0086087 | 0.0090641 | 0.0095421 | 0.010044 | 0.010572 | 0.011126 | 0.011709 | 0.012321 | 0.012964 | 0.013639 | 0.014348 | 0.015092 | 0.015872 | 0.016689
Improved analytical model fit for low temperatures
Density
Density

## Slide 14: Thermal Conductivity,
Chart: Hayne 2017
| 20 | 40 | 60 | 80 | 100 | 120 | 140 | 160 | 180 | 200 | 220 | 240 | 260 | 280 | 300 | 320 | 340 | 360 | 380 | 400 | 420 | 440
1105.12 | 0.00075985 | 0.00076252 | 0.00076979 | 0.00078395 | 0.00080729 | 0.00084211 | 0.0008907 | 0.00095536 | 0.0010384 | 0.0011421 | 0.0012687 | 0.0014206 | 0.0016001 | 0.0018093 | 0.0020508 | 0.0023266 | 0.0026392 | 0.0029908 | 0.0033838 | 0.0038203 | 0.0043028 | 0.0048335
1198.20 | 0.0011137 | 0.0011177 | 0.0011283 | 0.0011491 | 0.0011833 | 0.0012343 | 0.0013055 | 0.0014003 | 0.001522 | 0.001674 | 0.0018596 | 0.0020822 | 0.0023453 | 0.002652 | 0.0030059 | 0.0034102 | 0.0038684 | 0.0043838 | 0.0049597 | 0.0055996 | 0.0063068 | 0.0070846
1348.08 | 0.0016836 | 0.0016895 | 0.0017056 | 0.001737 | 0.0017887 | 0.0018658 | 0.0019735 | 0.0021167 | 0.0023007 | 0.0025304 | 0.002811 | 0.0031476 | 0.0035452 | 0.0040089 | 0.0045438 | 0.005155 | 0.0058476 | 0.0066267 | 0.0074973 | 0.0084645 | 0.0095335 | 0.010709
1506.14 | 0.0022845 | 0.0022925 | 0.0023144 | 0.002357 | 0.0024271 | 0.0025318 | 0.0026779 | 0.0028723 | 0.0031219 | 0.0034337 | 0.0038144 | 0.0042711 | 0.0048106 | 0.0054398 | 0.0061657 | 0.006995 | 0.0079349 | 0.008992 | 0.010173 | 0.011486 | 0.012936 | 0.014532
1673.10 | 0.0029193 | 0.0029295 | 0.0029575 | 0.0030119 | 0.0031015 | 0.0032353 | 0.003422 | 0.0036704 | 0.0039894 | 0.0043877 | 0.0048743 | 0.0054579 | 0.0061473 | 0.0069513 | 0.0078789 | 0.0089387 | 0.01014 | 0.011491 | 0.013 | 0.014677 | 0.016531 | 0.01857
1774.40 | 0.0033044 | 0.003316 | 0.0033476 | 0.0034092 | 0.0035107 | 0.0036621 | 0.0038734 | 0.0041546 | 0.0045157 | 0.0049666 | 0.0055173 | 0.0061779 | 0.0069583 | 0.0078684 | 0.0089183 | 0.010118 | 0.011477 | 0.013006 | 0.014715 | 0.016614 | 0.018712 | 0.02102
1798.67 | 0.0033966 | 0.0034086 | 0.0034411 | 0.0035044 | 0.0036087 | 0.0037644 | 0.0039816 | 0.0042706 | 0.0046418 | 0.0051053 | 0.0056714 | 0.0063504 | 0.0071525 | 0.0080881 | 0.0091673 | 0.0104 | 0.011798 | 0.01337 | 0.015126 | 0.017078 | 0.019234 | 0.021607
1799.99 | 0.0034017 | 0.0034137 | 0.0034462 | 0.0035096 | 0.0036141 | 0.00377 | 0.0039875 | 0.004277 | 0.0046487 | 0.0051129 | 0.0056798 | 0.0063598 | 0.0071632 | 0.0081001 | 0.0091809 | 0.010416 | 0.011815 | 0.013389 | 0.015149 | 0.017103 | 0.019263 | 0.021639
1800.00 | 0.0034017 | 0.0034137 | 0.0034462 | 0.0035096 | 0.0036141 | 0.00377 | 0.0039875 | 0.004277 | 0.0046487 | 0.0051129 | 0.0056799 | 0.0063599 | 0.0071632 | 0.0081002 | 0.009181 | 0.010416 | 0.011815 | 0.01339 | 0.015149 | 0.017103 | 0.019263 | 0.021639
should approach 0 as temperatures approach 0K
1 Hayne et al., “Global Regolith Thermophysical Properties of the Moon From the Diviner Lunar Radiometer Experiment: Lunar Regolith Thermophysical Properties,” 2017.
2 Martinez and Siegler, “A Global Thermal Conductivity Model for Lunar Regolith at Low Temperatures,” 2021.
Sufficient in most cases
Chart: Martinez and Siegler 2021
| 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 | 120 | 130 | 140 | 150 | 160 | 170 | 180 | 190 | 200 | 210 | 220 | 230 | 240 | 250 | 260 | 270 | 280 | 290 | 300 | 310 | 320 | 330 | 340 | 350 | 360 | 370 | 380 | 390 | 400
1105.12 | 7.4468e-05 | 0.00010476 | 0.0001417 | 0.00018089 | 0.00022069 | 0.00026046 | 0.00029998 | 0.00033921 | 0.00037825 | 0.00041721 | 0.00045626 | 0.0004956 | 0.00053542 | 0.00057592 | 0.00061733 | 0.00065986 | 0.00070372 | 0.00074914 | 0.00079634 | 0.00084553 | 0.00089693 | 0.00095076 | 0.0010072 | 0.0010666 | 0.001129 | 0.0011947 | 0.001264 | 0.0013369 | 0.0014138 | 0.0014947 | 0.0015801 | 0.0016699 | 0.0017645 | 0.0018641 | 0.0019688 | 0.0020788 | 0.0021944 | 0.0023157 | 0.0024429
1198.20 | 0.00014265 | 0.00020059 | 0.0002712 | 0.00034597 | 0.00042176 | 0.00049731 | 0.00057216 | 0.00064623 | 0.00071963 | 0.00079258 | 0.00086537 | 0.00093832 | 0.0010118 | 0.0010862 | 0.0011618 | 0.0012391 | 0.0013184 | 0.0014001 | 0.0014847 | 0.0015724 | 0.0016638 | 0.0017591 | 0.0018588 | 0.0019632 | 0.0020728 | 0.0021879 | 0.0023088 | 0.002436 | 0.0025698 | 0.0027106 | 0.0028588 | 0.0030147 | 0.0031786 | 0.003351 | 0.0035321 | 0.0037223 | 0.003922 | 0.0041316 | 0.0043512
1348.08 | 0.00025244 | 0.0003549 | 0.0004797 | 0.00061177 | 0.00074552 | 0.00087868 | 0.0010104 | 0.0011406 | 0.0012693 | 0.001397 | 0.0015241 | 0.0016512 | 0.0017789 | 0.0019077 | 0.0020385 | 0.0021717 | 0.0023081 | 0.0024483 | 0.002593 | 0.0027429 | 0.0028985 | 0.0030607 | 0.0032299 | 0.003407 | 0.0035924 | 0.003787 | 0.0039912 | 0.0042058 | 0.0044313 | 0.0046684 | 0.0049177 | 0.0051799 | 0.0054554 | 0.005745 | 0.0060492 | 0.0063686 | 0.0067038 | 0.0070554 | 0.0074239
1506.14 | 0.00036822 | 0.00051763 | 0.00069959 | 0.00089209 | 0.001087 | 0.0012809 | 0.0014726 | 0.0016619 | 0.001849 | 0.0020344 | 0.0022188 | 0.002403 | 0.0025878 | 0.0027742 | 0.002963 | 0.0031553 | 0.0033518 | 0.0035537 | 0.0037619 | 0.0039772 | 0.0042007 | 0.0044333 | 0.004676 | 0.0049296 | 0.0051951 | 0.0054734 | 0.0057655 | 0.0060722 | 0.0063944 | 0.0067331 | 0.0070891 | 0.0074633 | 0.0078566 | 0.0082698 | 0.0087038 | 0.0091594 | 0.0096375 | 0.010139 | 0.010664
1673.10 | 0.00049052 | 0.00068952 | 0.00093186 | 0.0011882 | 0.0014476 | 0.0017057 | 0.0019608 | 0.0022126 | 0.0024613 | 0.0027077 | 0.0029526 | 0.0031971 | 0.0034423 | 0.0036894 | 0.0039396 | 0.0041942 | 0.0044544 | 0.0047214 | 0.0049966 | 0.0052811 | 0.0055762 | 0.0058833 | 0.0062034 | 0.0065379 | 0.0068879 | 0.0072548 | 0.0076396 | 0.0080437 | 0.0084681 | 0.0089141 | 0.0093828 | 0.0098754 | 0.010393 | 0.010937 | 0.011508 | 0.012107 | 0.012736 | 0.013396 | 0.014087
1774.40 | 0.00056472 | 0.00079382 | 0.0010728 | 0.0013679 | 0.0016664 | 0.0019635 | 0.0022571 | 0.0025467 | 0.0028329 | 0.0031162 | 0.0033978 | 0.0036789 | 0.0039607 | 0.0042447 | 0.0045322 | 0.0048245 | 0.0051233 | 0.0054299 | 0.0057457 | 0.0060722 | 0.0064108 | 0.006763 | 0.0071301 | 0.0075137 | 0.007915 | 0.0083356 | 0.0087767 | 0.0092398 | 0.0097262 | 0.010237 | 0.010774 | 0.011339 | 0.011932 | 0.012555 | 0.013209 | 0.013896 | 0.014617 | 0.015372 | 0.016164
1798.67 | 0.0005825 | 0.0008188 | 0.0011065 | 0.0014109 | 0.0017189 | 0.0020252 | 0.002328 | 0.0026268 | 0.0029219 | 0.0032141 | 0.0035045 | 0.0037943 | 0.0040849 | 0.0043777 | 0.0046741 | 0.0049755 | 0.0052835 | 0.0055996 | 0.0059251 | 0.0062617 | 0.0066107 | 0.0069737 | 0.0073521 | 0.0077474 | 0.0081611 | 0.0085945 | 0.0090491 | 0.0095264 | 0.010028 | 0.010554 | 0.011108 | 0.011689 | 0.012301 | 0.012943 | 0.013617 | 0.014324 | 0.015067 | 0.015846 | 0.016662
1799.99 | 0.00058347 | 0.00082017 | 0.0011084 | 0.0014132 | 0.0017217 | 0.0020286 | 0.0023319 | 0.0026312 | 0.0029267 | 0.0032194 | 0.0035103 | 0.0038006 | 0.0040917 | 0.004385 | 0.0046819 | 0.0049838 | 0.0052923 | 0.0056089 | 0.0059349 | 0.006272 | 0.0066216 | 0.0069852 | 0.0073643 | 0.0077602 | 0.0081745 | 0.0086087 | 0.009064 | 0.009542 | 0.010044 | 0.010572 | 0.011126 | 0.011709 | 0.012321 | 0.012964 | 0.013639 | 0.014348 | 0.015092 | 0.015871 | 0.016689
1800.00 | 0.00058347 | 0.00082017 | 0.0011084 | 0.0014133 | 0.0017217 | 0.0020286 | 0.0023319 | 0.0026312 | 0.0029267 | 0.0032194 | 0.0035103 | 0.0038007 | 0.0040917 | 0.004385 | 0.0046819 | 0.0049838 | 0.0052924 | 0.0056089 | 0.005935 | 0.0062721 | 0.0066217 | 0.0069853 | 0.0073643 | 0.0077603 | 0.0081746 | 0.0086087 | 0.0090641 | 0.0095421 | 0.010044 | 0.010572 | 0.011126 | 0.011709 | 0.012321 | 0.012964 | 0.013639 | 0.014348 | 0.015092 | 0.015872 | 0.016689
Improved analytical model fit for low temperatures
Density
Density
Hayne 2017 vs Lab Data for NU-LHT-22

## Slide 15: Extra: Extension for Icy Regolith
Reiss 2018 gives a semi-empirical model for thermal conductivity of regolith samples with water vapor between voids + an extension for icy regolith1,2
Available water properties
  (vapor) Polynomial fit provided by D3.1 Table 10, VDI Heat Atlas. 2010.
  (ice) “Revised Release on the Equation of State 2006 for H2O Ice Ih,” IAPWS. 2009.
    https://iapws.readthedocs.io/en/latest/iapws.iapws95.html#iapws.iapws95.IAPWS95
1 Reiss, “In-Situ Thermal Extraction of Volatiles from Lunar Regolith,” 2018.
2 Siegler et. al,, “Laboratory Measurements of Thermal Properties of Icy Regolith Analogs,” 2011.
For Icy Regolith:1,2
Bulk thermal conductivity of regolith with water vapor/ice between voids using predicted with Reiss’s model
Notes: May skip this one

## Slide 16: Specific heat,
Bulk depends:
  Molecular structure
  Temperature
of many Apollo samples from have been measured at ~80K - 360K1
Lunar regolith vs temperature have been developedincluding:1,2,3
1 Hemingway et al., “Specific heats of lunar soils, basalt, and breccias from the Apollo 14, 15, and 16 landing sites, between 90 and 350°K,” Proceedings of the Lunar Science Conference, 1973..
2 Hayne et al., “Global Regolith Thermophysical Properties of the Moon From the Diviner Lunar Radiometer Experiment: Lunar Regolith Thermophysical Properties,” 2017. (Used data from Ledlow 1992 and Hemingway 1981)
3Woods-Robinson et al., " A model for the Thermophysical Properties of Lunar Regolith at Low Temperatures" 2019.
Specific heat of an Apollo Lunar Highlands sample1

## Slide 17: Specific heat,
Specific heat models:
  Hemingway 19731
    Empirical fit to Apollo measurements from 90K to 350K
  Hayne 20172
    Derived using Hemingway (1981) & Ledlow (1992)
  Woods-Robinson 2019 update for < 200K3
    Analytical model fit Apollo measurements from 90K – 350K and Breccia Rock at 3-4K
    Aimed for better accuracy near 0K since should nears as temperatures approach 0K4
Martinez and Siegler observed 2% difference in Lunar surface model results when using Hayne 2017 vs Woods-Robinson 20194
1 Hemingway et al., “Specific heats of lunar soils, basalt, and breccias from the Apollo 14, 15, and 16 landing sites, between 90 and 350°K,” Proceedings of the Lunar Science Conference, 1973..
2 Hayne et al., “Global Regolith Thermophysical Properties of the Moon From the Diviner Lunar Radiometer Experiment: Lunar Regolith Thermophysical Properties,” 2017. (Used data from Ledlow 1992 and Hemingway 1981)
3Woods-Robinson et al.," A model for the Thermophysical Properties of Lunar Regolith at Low Temperatures" 2019.
4Martinez and Siegler, “A Global Thermal Conductivity Model for Lunar Regolith at Low Temperatures,” 2021.
Chart: Temperature, K
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 | 120 | 130 | 140 | 150 | 160 | 170 | 180 | 190 | 200 | 210 | 220 | 230 | 240 | 250 | 260 | 270 | 280 | 290 | 300 | 310 | 320 | 330 | 340 | 350 | 360 | 370 | 380 | 390 | 400
Hayne 2017 | 24.0424 | 52.0968 | 80.48 | 109.1231 | 137.9597 | 166.9253 | 195.9576 | 224.9966 | 253.9841 | 282.8644 | 311.5837 | 340.0905 | 368.3351 | 396.2705 | 423.8513 | 451.0346 | 477.7795 | 504.0471 | 529.8009 | 555.0064 | 579.6312 | 603.6452 | 627.0202 | 649.7304 | 671.752 | 693.0632 | 713.6446 | 733.4788 | 752.5506 | 770.8468 | 788.3566 | 805.071 | 820.9834 | 836.0893 | 850.3862 | 863.8738 | 876.5541 | 888.4311 | 899.5108 | 909.8016
Woods-Robinson 2019 | 7.0517 | 26.4715 | 53.5142 | 84.7057 | 117.6203 | 150.6766 | 182.9538 | 214.0276 | 243.825 | 272.5 | 300.3277 | 327.6191 | 354.6547 | 381.6383 | 408.6703 | 435.7409 | 462.7421 | 489.5008 | 515.8297 | 555.0064 | 579.6312 | 603.6452 | 627.0202 | 649.7304 | 671.752 | 693.0632 | 713.6446 | 733.4788 | 752.5506 | 770.8468 | 788.3566 | 805.071 | 820.9834 | 836.0893 | 850.3862 | 863.8738 | 876.5541 | 888.4311 | 899.5108 | 909.8016
Hemmingway 1973 | 245.6125 | 279.4922 | 313.1907 | 346.5091 | 379.2717 | 411.326 | 442.5426 | 472.8153 | 502.061 | 530.22 | 557.2556 | 583.1542 | 607.9255 | 631.6025 | 654.241 | 675.9202 | 696.7426 | 716.8337 | 736.3421 | 755.4398 | 774.3217 | 793.2062 | 812.3346 | 831.9714 | 852.4045 | 873.9447 | 896.9261
Chart: 
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 | 120 | 130 | 140 | 150 | 160 | 170 | 180 | 190 | 200 | 210 | 220 | 230 | 240 | 250 | 260 | 270 | 280 | 290 | 300 | 310 | 320 | 330 | 340 | 350 | 360 | 370 | 380 | 390 | 400
Hayne 2017 | 24.0424 | 52.0968 | 80.48 | 109.1231 | 137.9597 | 166.9253 | 195.9576 | 224.9966 | 253.9841 | 282.8644 | 311.5837 | 340.0905 | 368.3351 | 396.2705 | 423.8513 | 451.0346 | 477.7795 | 504.0471 | 529.8009 | 555.0064 | 579.6312 | 603.6452 | 627.0202 | 649.7304 | 671.752 | 693.0632 | 713.6446 | 733.4788 | 752.5506 | 770.8468 | 788.3566 | 805.071 | 820.9834 | 836.0893 | 850.3862 | 863.8738 | 876.5541 | 888.4311 | 899.5108 | 909.8016
Woods-Robinson 2019 | 7.0517 | 26.4715 | 53.5142 | 84.7057 | 117.6203 | 150.6766 | 182.9538 | 214.0276 | 243.825 | 272.5 | 300.3277 | 327.6191 | 354.6547 | 381.6383 | 408.6703 | 435.7409 | 462.7421 | 489.5008 | 515.8297 | 555.0064 | 579.6312 | 603.6452 | 627.0202 | 649.7304 | 671.752 | 693.0632 | 713.6446 | 733.4788 | 752.5506 | 770.8468 | 788.3566 | 805.071 | 820.9834 | 836.0893 | 850.3862 | 863.8738 | 876.5541 | 888.4311 | 899.5108 | 909.8016
Hemmingway 1973 | 245.6125 | 279.4922 | 313.1907 | 346.5091 | 379.2717 | 411.326 | 442.5426 | 472.8153 | 502.061 | 530.22 | 557.2556 | 583.1542 | 607.9255 | 631.6025 | 654.241 | 675.9202 | 696.7426 | 716.8337 | 736.3421 | 755.4398 | 774.3217 | 793.2062 | 812.3346 | 831.9714 | 852.4045 | 873.9447 | 896.9261
At 10K
24.4 vs 7.05

## Slide 18: Thermal Wave / Skin Depth
Thermal wave – range in subsurface temperatures vs depth
Skin depth is the depth where diurnal thermal wave decays to
  Skin depth:
  Thermal diffusivity1
  Lunar Synodic rotation period
ranges from ~4 cm-10 cm 2
Annual thermal wave is deeper and has been derived from in-situ measurements at Apollo landing sites
Temperature as a function of depth at the Apollo 15 and 17 landing sites (From Lunar Sourcebook: A User’s Guide to the Moon
Langseth et al., “Revised lunar heat-flow values.,” 1976.Table 1.
2 P. Gläser and D. Gläser, “Modeling near-surface temperatures of airless bodies with application to the Moon,” 2019.

## Slide 19: Thermal Wave / Skin Depth
Thermal wave – range in subsurface temperatures vs depth
Skin depth is the depth where diurnal thermal wave decays to
  Skin depth:
  Thermal diffusivity1
  Lunar Synodic rotation period
ranges from ~4 cm-10 cm 2
Annual thermal wave is deeper and has been derived from in-situ measurements at Apollo landing sites
1 Langseth et al., “Revised lunar heat-flow values.,” 1976.Table 1.
2 P. Gläser and D. Gläser, “Modeling near-surface temperatures of airless bodies with application to the Moon,” 2019.
3 Hayne et al., “Global Regolith Thermophysical Properties of the Moon From the Diviner Lunar Radiometer Experiment: Lunar Regolith Thermophysical Properties,” 2017.
Lunar subsurface thermal wave predicted for different H parameters by Hayne 2017 3

## Slide 20: Ground Heat Flow
A geothermal heat flux is imposed on the top layer of lunar regolith from radioisotopes in the crust
Apollo heat-flow experiment data were used to calculated ground heat flux at the Apollo 15 and 17 (applied to top ~2m of regolith)
  Not globally applicable due to the ground’s higher thorium content 3
Langseth et al. estimated a global average heat flux, assuming it equaled the heat flux from radioisotopes beneath the surface
Subsurface temperatures in shadowed craters are likely very sensitive to ground heat flux 5
Quantifying global subsurface heat fluxes is still an active area of research
Region | Q [W/(m2K)] | Derived from
Hadley Rille | 0.021 | Apollo 15 heat probe data 1,2
Taurus-Littrow | 0.016 | Apollo 17 heat probe data 1,2
Global average | 0.018 | Adjusted from Apollo 15 and 17 values based on estimated concentrations of subsurface K, U, and Tr 1,2
Cabeus & Haworth Crater | 0.0112 | Chang׳E-2 microwave radiometer data 4
Shoemaker Crater | 0.0074 | Chang׳E-2 microwave radiometer data 4
LCROSS impact site (49.6W, 84.7S) | 0.01 | Chang׳E-2 microwave radiometer data 4
Lunar S. Pole | 0.009 | Chang׳E-2 microwave radiometer data and LRO Diviner data 6
1 Langseth et al., “Heat-flow experiment. In Apollo 17 Preliminary Science Report.,” NASA SP-330.
2 Langseth et al.,, “Revised lunar heat-flow values.,” Lunar and Planetary Science Conference Proceedings, vol. 3, p. 3143, Apr. 1976.
3 Siegler and Paige, “Lunar Global Heat Flow: Predictions and Constraints,” presented at the Lunar Science for Landed Missions Workshop, NASA Ames, 2018.
4 Wei et al, “Thermal behavior of regolith at cold traps on the Moon׳s south pole: Revealed by Chang׳E-2 microwave radiometer data,” 2016.
5 Glenar, et. al., “Earthshine as an Illumination Source at the Moon”, 2019.
6 Feng et al., “Thermal Gradient Of Regolith In Lunar South Polar Region Inferred From LRO Diviner And CE-2 MRM Data,” 2020.