## Slide 1
Role of NDE and In Situ Process Monitoring in Managing Risk of AM Space Hardware
Erin L. Lanigan, NASA Marshall Space Flight Center November 3rd, 2022

## Slide 2: Speaker Biography
Erin Lanigan
Native of Lenexa, Kansas (Kansas City metro)
Bachelor’s Degree in Mechanical Engineering from the University of Kansas
Non-Destructive Evaluation Team at NASA Marshall Space Flight Center since Oct. 2017
Completing Master’s in Mechanical Engineering at the University of Alabama in Huntsville
Focus Areas:
Infrared flash thermography
NDE of additive manufacturing
In situ process monitoring
AM certification
In-space manufacturing

## Slide 3: Outline
Qualification of NDE and in-situ monitoring
Certification framework
NASA’s involvement and approach
We will discuss NASA’s interest in qualifying NDE and in situ monitoring methods for certification of AM space hardware.

## Slide 4: Use Case – Inspectability Challenges
NASA is interested in qualifying in situ monitoring for complex, critical parts that are difficult to inspect using traditional NDE.
RS-25 Pogo Accumulator Z-Baffle
Over 100 Welds Eliminated
Nearly 35% Cost Reduction
28-Element Inconel® 625 Fuel Injector
Reduced 163 parts to 2
Schedule reduced from 1 year to 4 months
70% cost reduction
Injector Assembly
MSFC Project with Army Air and Missile Defense (AMD)
Cryogenic Heat Exchanger-Injector-Condenser Demo

## Slide 5: Investigating In Situ Monitoring Technologies
MSFC has investigated in situ process monitoring through various mechanisms.
Small Business Innovation Research
Monitoring Systems
ASTM WK73289 → E3353-22
“Standard Guide for In-Process Monitoring Using Optical and Thermal Methods for Laser Powder Bed Fusion”
ASTM AM Center of Excellence
Completed a landscape survey and workshop with road mapping session
EOS | Optical Tomography
& Meltpool Monitoring
ARCTOS | Thermal Tomography & High-Speed Spatter Imaging

## Slide 6: Variety of In Situ Technologies
There are many different in situ process monitoring technologies which observe different physical phenomena.
Ultrasonic Frequency Spectrum
Electromagnetic Frequency Spectrum
(No external excitation)
Monitor During Build Process
Inspection Between Build Layers
Passive
(Added excitation)
Active
Infrared/near-IR
melt pool monitoring
-
Visual
Laser profilometry
Laser ultrasonic
X-ray

## Slide 7: Monitoring Different AM Systems
There are also different additive manufacturing technologies that can be monitored.
Powder Bed Systems
Process:
Feedstock:
Freeform Fabrication
Laser Powder Bed Fusion (L-PBF)
Electron Beam Melting (EBM)
Selective Laser Sintering (SLS)
Metals: Nickel alloys, copper alloys, titanium alloys, etc.
Polymers: nylon, polyamide
Laser Directed Energy Deposition (DED)
Electron Beam Free Form Fabrication (EBF3)
Rapid Plasma Deposition
Additive Friction Stir Weld
Fused Filament Fabrication (FFF)
Metal powder/wire/chips
Filament: polymer, carbon fiber, biological, etc.

## Slide 8: Two Different Functions of In Situ Monitoring
There are two main functions of in situ process monitoring:
Process Control Function
Quantitative analysis of part quality
Requires a known correlation between indications, physics of the process, and actual defects in the finished part
Need to know probability of detection
  Extra step – verify actual size, location of created defects
Need to treat it like NDE – believe and investigate every indication
  Can’t dismiss anything as a false positive unless proven
vs.
Part Quality Function
Real-time warning of build problems
Use to check for process drift
Monitor effects of parameter changes, spatter, etc.
Not counting on it for quantitative part quality metrics or defect detection
  May help tell you where to look for a problem, but would require verification with NDE

## Slide 9: Challenging the Qualification Paradigm
When considering the use of in situ process monitoring for part qualification, there are a few aspects that challenge the current paradigm.
Closed-loop process control
Often, defect observations are indirect
  Directly observing process variation, inferring final defect
  Must understand physical basis for measured phenomena
  Need to prove a causal correlation from measured indications to defect state
Probability of detection (POD) study must include secondary verification of created defects
Current NASA qualification logic based on a locked process
For real-time parameter changes, a new approach is needed
In-process vs. post-process NDE
no longer nondestructive

## Slide 10: NASA AM Certification Approach
The current logic of additive manufactured part certification is outlined in NASA-STD-6016C, NASA-STD-6030, and NASA-STD-6033.
MSFC-SPEC-3717
MSFC-STD-3716
NASA-STD-6016C
General M&P requirements
NASA-STD-6030
NASA-STD-6033
Standard for Additively Manufactured Spaceflight Hardware by Laser Powder Bed Fusion in Metals
Specification for Control and Qualification of Laser Powder Bed Fusion Metallurgical Processes
NASA Technical Standard
NASA Technical Standard
Additive Manufacturing Requirements for Spaceflight Systems
Additive Manufacturing Requirements for Equipment and Facility Control
Handbook coming soon with more specifics on implementation.
Statement A: Approved for public release; distribution is unlimited.

## Slide 11: AM Part Classifications
Statement A: Approved for public release; distribution is unlimited.
Classifications for AM parts consider the risk of AM manufacturability and inspectability.
Catastrophic Failure?
Heavily Loaded?
Does the build have challenging aspects or areas that cannot be inspected?

## Slide 12: Class A Part NDE Requirements
The NASA standard requires quantitative NDE with full coverage of the surface and volume for Class A Parts.
Language:
“All Class A parts shall receive quantitative NDE with full coverage of the surface and volume of the part, including verifiable detection of critical initial flaw size in critical damage tolerant parts, with any coverage limitations due to NDE techniques(s) and/or part geometry documented in the PPP”
Rationale:
“NDE provides a necessary degree of quality assurance for AM parts in addition to the process controls of this NASA Technical Standard.”
“No methodology currently exists to preclude all AM process failure modes through the available manufacturing process controls.”
(emphasis added)
Statement A: Approved for public release; distribution is unlimited.

## Slide 13: Class A Part NDE Requirements (cont.)
Statement A: Approved for public release; distribution is unlimited.
For Class A parts, the NDE approach must comply with the Special NDE requirements in NASA-STD-5009.
Language:
“The NDE approach for Class A parts shall meet the Special NDE requirements of NASA-STD-5009, Nondestructive Evaluation Requirements for Fracture Critical Metallic Components, and be documented in the PPP.”
Rationale:
“The defects of interest in AM are of a different nature than those listed in Tables 1 and 2 of NASA-STD-5009, and AM microstructures can impact the effectiveness of NDE methods. Therefore, all inspection of fracture critical AM hardware should be treated as Special NDE.”
“Alternative flaw screening methods for Class A parts (e.g., proof testing) may be feasible with full justification provided in the PPP.”

## Slide 14: Class B Part NDE Requirements
Statement A: Approved for public release; distribution is unlimited.
The NASA standard requires NDE for process control with full coverage of the surface and volume for Class B Parts.
Language:
“All Class B parts shall receive NDE for process control with full coverage of the surface and volume of the part, including verifiable detection of critical initial flaw size in critical damage tolerant parts, with any coverage limitations due to NDE techniques(s) and/or part geometry documented in the PPP”
Rationale:
“NDE for process control requires the use of physical reference standards for calibration and acceptance criteria based on the capability of the NDE technique but does not require quantitative validation of flaw detection.
“Targeted approaches for NDE can be proposed and approved per the PPP.”
(emphasis added)

## Slide 15: Class B Part NDE Requirements (cont.)
Statement A: Approved for public release; distribution is unlimited.
For Class B parts, the NDE approach must meet the requirements in NASA-STD-5009.
Language:
“The NDE approach for Class B parts shall meet the Special NDE requirements of NASA-STD-5009 and be documented in the PPP.”
Rationale:
“The requirements in NASA-STD-5009 establish important controls, including the definition, validation, documentation, and approval of all NDE procedures, standards, methods, and acceptance criteria […]”
“Alternative post-build quality assurance methods for Class B parts (e.g., proof testing), as well as a reduction in NDE scope for Class B parts, may be feasible with full justification provided in the PPP."

## Slide 16: Qualified In Situ Process Monitoring
Passive in situ process monitoring may be used as a quantitative indicator of part quality, if qualified.
Language:
“Prior to use as a quantitative indicator of part quality for part acceptance, passive in-situ process monitoring technologies shall be qualified by the CEO to the satisfaction of NASA in a manner analogous to other NDE techniques.”
Rationale:
“All processes that are used to establish quantifiable quality assurance metrics are qualified against established criteria to verify detection reliability, calibration, and implementation. If in-situ monitoring techniques are employed for such purposes, the need for such qualification is unchanged.”
(emphasis added)

## Slide 17: Qualified In-Situ Process Monitoring (cont.)
Passive in situ process monitoring may NOT replace NDE.
Rationale (cont.):
“Certification of a passive in-situ monitoring technology relies upon a thorough understanding of the physical basis for the measured phenomena, a proven causal correlation of the measured phenomena to a well-defined defective process state, and a proven level of reliability for detection of the defective process state.”
“If qualified in the manner stated above, an in-situ process monitoring technique can be used to complement NDE in the Integrated Structural Integrity Rationale of the PPP. At this time, even a qualified in-situ process monitoring method cannot be considered a complete replacement for NDE.”
“Even if qualification is not desired, the use of in-situ process monitoring is encouraged as a source of process control data. This data can also be used to help guide targeted inspection.”
(emphasis added)

## Slide 18: Qualification Flow Chart
In situ monitoring can be used in several aspects of certification:
Qualification of Material Process (QMP)
Use with process development
Part Classification
Improve inspectability for better AM risk posture
Inspection process must be qualified by cognizant engineering organization (CEO)
Part Production Plan
Integrated Structural Integrity Rationale (ISIR):
  Can be specified as a defect screening action
  Must be qualified by CEO
Production Controls
Could develop certain metrics to track over time

## Slide 19: Adaptive (Closed-Loop) Systems
The current certification approach does not accommodate the use of adaptive systems.
Two issues for verification:
Monitor the process using sensors (e.g. meltpool thermal signature) and change a machine/process parameter (e.g. laser power) to optimize the response
Currently available in many directed energy deposition (DED) systems
Verify the sensor performance, algorithm and machine response
Verify the physics – does controlling this parameter result in a good part?
Adaptive (Closed-Loop) Systems
(control system)
(materials)
“Closed-loop process control based on adaptive in-situ monitoring technologies that alter the defined AM process in response to monitored phenomena are not currently applicable technology per this NASA Technical Standard and cannot be used without prior approved tailoring.”

## Slide 20: Control System Verification
For certifying closed-loop control systems, NASA can leverage the expertise of the spacecraft control systems community.
Black box issue:
Verify the accuracy of the sensor data
Verify the software/algorithm processing and response
Verify that the changed parameter responds correctly
For commercial systems, machine parameters may not be known, algorithms may not be accessible
Ideal approach: collaborate with machine manufacturers
Can also develop transfer function by studying inputs/outputs
Verification of a control system:

## Slide 21: Material Control Verification
Verifying that the adaptive system results in good material is a challenge that will require further study.
What parameter will you change?
Assume you’re monitoring the meltpool thermal emissions
Are you looking to keep it constant, or vary it based on part geometry?
More complex if monitoring multiple signals and/or changing multiple parameters
Qualify process for each different system, alloy, part?
What is being monitored, and to what end?
What does it really tell you about the process and the material?
Is this a good indicator of material quality?
Is the resulting microstructure/morphology consistent and repeatable?

## Slide 22: Conclusions
In summary, NDE and in situ monitoring both have a role in certification of AM space hardware.
To use for quantitative part quality function, monitoring system must be qualified.
→ Main challenge: developing correlation of indication to verified defect
Qualifying closed-loop, adaptive systems will require a new approach to the QMP.
NDE is still vital for verification of post-build quality.
Thank you for your time!
Questions?

## Slide 23
Thank you.
Erin L. Lanigan, NASA Marshall Space Flight Center November 3rd, 2022