## Slide 1: Evaluation of Ultrasonic Battery Inspection Techniques
Matt Webster1, Erik Frankforter1, Peter Juarez1, and Andrew Campbell2
1NASA Langley Research Center, Hampton, VA 2University of South Carolina, Columbia, SC
SPIE Smart Structures + NDE
March 13, 2023

## Slide 2: Motivation
Higher energy density batteries are needed to meet aerospace demands
Many high energy density configurations use lithium (Li) metal anodes
Non-uniform Li anode plating can lead to dendrite growth, short circuit, and thermal runaway
Research Goal: Identify local changes in structure that could lead to thermal runaway through nondestructive evaluation (NDE)
Illustration of lithium dendrite growth leading to internal short circuit
Increasing Charge Cycles

## Slide 3: Prior Work on Ultrasonic Testing (UT) of Batteries
Hsieh1 used elastic property changes due to ion transport to assess state of charge (SOC) and state of health (SOH)
Ladpli2 applied guided wave UT using external piezoelectric sensors to detect SOC and SOH
Huang3 applied time domain and resonance analysis to track changes in structure as a function of SOC and SOH
1A. G. Hsieh, et al., Energy and Environmental Science, 2015
2P. Ladpli et al., Journal of Power Sources, 2018
3M. Huang et al., Journal of Energy Storage, 2022
Battery NDE is an emerging field mostly focused on SOC and SOH
Notes: Hsieh pronounced “SHAY”
Nde of batteries is a relatively emerging field, but there has been significant progress over the past decade or so. Apart from monitoring electrical properties and temperature to deduce battery health, ultrasound has been the primary area of focus due to sensitivity to both changes in internal structure and mechanical properties
Hsieh et al in 2015 demonstrated the ability to monitor changes in elastic properties that occur during ion transport in operando in order to determine the state of charge and health in lithium ion batteries
Ladpli et al applied guided wave ultrasound using externally mounted piezoelectric wafers to determine state of health and

## Slide 4: Specimens for Evaluating Flaw Sensitivity
A pouch cell Li-metal battery was seeded with anode defects to test sensitivity of ultrasonic approaches
Pouch cell structure:
  Single battery cell (one anode/cathode pair)
  LiCoO2 cathode material
  Porous polymer separator
  Li metal anode with 80 um Li chips pressed onto the surface
  Liquid electrolyte
Focus area for inspections
Li chip Defects
Li metal anode with 80um thick lithium chip defects
Illustration of pouch cell defect locations
Pouch cell layup:
Image of Battery

## Slide 5: Overview of Guided Wave Approaches
Guided wave ultrasound involves propagation of waves along boundaries
Two guided wave ultrasound methods:
  Pitch-catch testing via piezoelectric wafer active sensor (PWAS)
  Laser Doppler vibrometry (LDV) – line scans
x
x
x
x
LDV Experimental Setup
Defective Cell
Baseline Cell
Example group velocity dispersion curve

## Slide 6: Pitch-Catch Guided Waves
PWAS bonded to battery pouch using cyanoacrylate adhesive
Excited using a 20 Vpp 300 kHz, 3-count sine wave
Clear wave mode measured at receiver with high signal-to-noise ratio (SNR)
  ‘Ringing’ observed due to large Li chip next to receiver in defective pouch cell
Transmitter
Receiver
Transmitter
Receiver
Embedded Lithium Chip Defects
Pristine pouch cell
Defective pouch cell

## Slide 7: Laser Doppler Vibrometry - Line Scans
PWAS excited by a 5 Vpp, 5-count Hanning windowed sine wave
LDV line scans
  Detection of out-of-plane velocity
  100 µm steps, 128 averages per point
Two wave modes present in pristine pouch
  Identified by two distinct slopes/velocities
Three wave modes present in defective pouch
  Rippling present for propagation over aberrations, may be due to factors such as defects and pouch wrinkling
LDV B-Scans
Pristine
Defective
excitation
excitation
Line scan across black dotted lines, in direction of purple arrow

## Slide 8: Laser Doppler Vibrometry – Waveforms
Waveforms via LDV at individual locations
  x=0 location beginning of scan line
Wave mode separation observed (probable fundamental symmetric / antisymmetric)
Significant attenuation over small propagation distances – electrolyte viscous effects
  Tradeoff with PWAS pitch-catch – LDV obtaining spatial data at lower SNR
Pristine
Defective
x = 80 mm
x = 95 mm
x = 60 mm
x = 50 mm

## Slide 9: Local Ultrasonic Resonance Spectroscopy (LURS)
Assesses through-thickness resonances, which are affected by layup and constituent properties
Demonstrated by Rus and Grosse4 on plate specimens and applied to battery inspection by Nelson5
Frequency-dependent reflection coefficient
Scanning gantry and custom fixturing used for collecting contact data
Constant force measurement probe
Transducer with delay line
4 J. Rus and C. Grosse, “Local Ultrasonic Resonance Spectroscopy: A Demonstration on Plate Inspection”, J. NDE, 2020.
5 W. Nelson, "Local Ultrasonic Resonance Spectroscopy of Lithium Metal Batteries for Aerospace Applications." Master’s Thesis, University of Virginia (2021).
Resonant frequencies

## Slide 10: Time-domain Amplitude
Time domain analysis data shows signatures from embedded flaws
Surface and edge effects present early in the received signal
TG1
TG2
TG3

## Slide 11: Resonance Frequency Analysis
Flaw cause shift in first and second resonance frequency with most dominant effects in second resonance
  Most dominant shift in the second resonance frequency (f2)
Some areas without known defects show signs of differences in structure as well

## Slide 12: Emerging Techniques – Model Parametric Exploration
Linking forward model with Dakota software, from Sandia National Laboratory https://dakota.sandia.gov/
  Simulated reflection spectrum in COMSOL using two-dimensional elastic-poroelastic media, technique via Nelson5
Sensitivity analysis, surrogate modeling, and inversion techniques for applications like material property, geometry, and flaw inverse analysis
Chart: 
viscosity | 0.75224
permeability_PE | -0.39946
permeability_LCO | 0.045719
Biot_willis_PE | -0.22777
Biot_willis_LCO | -0.16516
Tortuosity_PE | -0.22209
Tortuosity_PP | -0.10172
Tortuosity_LCO | -0.98645
porosity_LCO | 0.9213
Fundamental resonance, partial rank correlation
Resonance spectrum – 2D elastic-poroelastic simulation in COMSOL
5Nelson, William Charles. "Local Ultrasonic Resonance Spectroscopy of Lithium Metal Batteries for Aerospace Applications." Master’s Thesis, University of Virginia (2021).
Sensitivity of resonance to material parameters

## Slide 13: Discussion
This study demonstrates two candidates for identifying local changes in structure in lithium-metal batteries
Guided wave ultrasound is viable for in situ inspection, with pitch catch showing particularly good signal/noise and sensitivity to lithium defects
LURS provides much more information on the local structure than available from conventional pulse-echo inspection
  Inverse modeling framework established for calibration and sensitivity analysis
  Still needs to be implemented for inspection data
Currently working with battery subject matter experts to develop realistic damage so that these techniques can be evaluated for prognostic capability

## Slide 14: Acknowledgements
Funding provided by the NASA Convergent Aeronautics Solutions Project
Specimen development and management by Daniel Perey
Specimens manufactured by Cornerstone Research Group