## Slide 1: Ceramic aerogels for space high temperature applications
Haiquan Guo (USRA)
Jamesa L. stokes (NASA GRC)
MRS Spring meeting, April 2023
National Aeronautics and Space Administration
www.nasa.gov

## Slide 2
Acknowledgement
National Aeronautics and Space Administration
www.nasa.gov
Francis Hurwitz (NASA GRC retiree)
Elizabeth J. Young-dohe (NASA GRC)
Richard B. Rogers (NASA GRC)
Many intern students
Clay Klein
David Phan
Aileen Peer
Hayley Richardson
Helena Wood
Matthew K. Meyer
Kevin Yu
Eric Schmid
Diane Kjelby
Derek R. Miller
Katy N. Newlin
….
NASA fellowship students
Nathaniel Olson
Rebecca Walker

## Slide 3
National Aeronautics and Space Administration
www.nasa.gov
What are aerogels?
Made by removing solvent from wet gels without collapsing the structure
Highly porous solids with extremely small pore size
Low density
High surface area
Low thermal conductivity
  reduces heat transfer (convection, conduction, and radiation)
Sol
Aerogel
Gel

## Slide 4
Aerogels and their space applications
Collecting Comic Space Dust
Insulation on Rovers
Silica Aerogels
The first produced aerogel
Optically translucent
Silica aerogels begin to sinter about 700˚C
National Aeronautics and Space Administration
www.nasa.gov

## Slide 5
Actuators
Meteorite collector
Electrical insulation for CNT cable
Nanogenerators
IR scattering filter
Antenna
Mechanically stronger
Polymer aerogels degrade < 450˚C.
Aerogels and their space application
Polyimide aerogels
National Aeronautics and Space Administration
www.nasa.gov
Q. Zheng, et al., Adv. Fun. Mater. 2018, 28, 1706365.
H. Guo, et al., ACS Appl. Polym. Mater. 2019, 1, 7, 1680.
H. Guo, et al., ACS Appl. Mater. & Inter., 2020,12, 33288.
G. Sauti, et al., U.S. Patent 9,137,883.
M. A. B. Meador, et al., U.S. Patent 10428181.
https://www.scientia.global/fine-tuning-polymers-as-flexible-antenna-substrates-for-aircraft/
T. Essinger-Hileman, et al., Applied Optics, 59, 2020, 5439. (GSC-18207-1)
J.A. Del Corso et al., 9th International Planetary Probe Workshop June 2012, Toulouse.

## Slide 6
Many applications require higher temperature stability.
National Aeronautics and Space Administration
www.nasa.gov
Inflatable decelerator
Lower thermal conductivity: improve performance
Light weight: reduce cost, increasing payload
Reusable when possible
Mechanical durability
Heat shielding

## Slide 7
National Aeronautics and Space Administration
www.nasa.gov
Aluminosilicate aerogel synthesis
AlO6 octahedra
Boehmite [AlO(OH)]
+
hydrogel
supercritical CO2
Si
O
O
O
O
Tetraethyl orthosilicate (TEOS)
aerogel
S. Brühne, Cryst. Growth Des., 2008, 8, 489–493n
P. R. Aravind, et al Microporous and Mesoporous Mater. 2006, 96, 14–20
F. I. Hurwitz, M. Gallagher, T. Olin, M. K. Shave, M. Α. Ittes, K. N. Olafson, M.G. Fields, R. B. Rogers, and H. Guo, Inter. J. of Appl. Glass Sci. 2004, 1–11

## Slide 8
National Aeronautics and Space Administration
www.nasa.gov
Aluminosilicate aerogels and their composites
Aluminosilicate aerogels can be used >1100˚C (400˚C above silica aerogels)
Can be opacified to reduce radiation heat transfer
Reinforced with non-woven ceramic fiber papers or felts
Composites can be flexible
They can be modified to be hydrophobic
Composite densities of 0.07- 0.2 g/cm3, lighter than Microtherm HT (0.3428g/cm3), tailored with choice of reinforcement
Low thermal conductivity
Hydrogels with varying levels of TiO2 incorporation
F. I. Hurwitz, H. Guo, R.B. Rogers, E, J. Sheets, D. R. Miller, K. N. Newlin, M. K. Shave, A. R. Palczer, and M. T. Cox, J Sol-Gel Sci. Tech., 2012, 64, 367-374
Alumina paper impregnated with aluminosilicate aerogel
F. I. Hurwitz and H. Guo, U.S. Patent 10343131, 10343131 B1

## Slide 9
APA-2 alumina paper
Aluminosilicate aerogel/ APA-2 felt composite
Aerogel well bonded to fiber—does not “flake”
National Aeronautics and Space Administration
www.nasa.gov
Aluminosilicate Aerogel Composites
Thermal conductivity
J. Gembarovic and R. E. Taylor, Int J Thermophys, 2007, 2164–2175
F. I. Hurwitz and H. Guo, U.S. Patent 10343131, 10343131 B1

## Slide 10
Persistence of mesoporous structure heated at 1100 and 1200˚C
1100˚C, 24h
1200˚C, 24h
As supercritically dried
600˚C, 24h
National Aeronautics and Space Administration
www.nasa.gov

## Slide 11
Post-test Run 12 Loc 4
Post-test BF-20 layers removed
Underside, APA-2/aerogel layer 7
Aerogel microstructure is maintained
2 BF-20/7 AS-APA-2/Aluminized Kapton
17W/cm2 flux; 1435 psi @3300˚R combustor pressure
Temperature between aerogel composite and Kapton nominally 50˚C, a drop of 700˚C across 7 layers)
National Aeronautics and Space Administration
www.nasa.gov
LaRC 8’HTT test (to evaluate for EDL)

## Slide 12
National Aeronautics and Space Administration
www.nasa.gov
Hydrophobic aluminosilicate aerogel
Quartz felt /aluminosilicate/PTMS
600oC 1000oC 1100oC 1200oC
RT
1100oC
1200oC
F. I. Hurwitz and H. Guo, U.S. Patent 10343131, 10343131 B1

## Slide 13
National Aeronautics and Space Administration
www.nasa.gov
YSZ, Y/YbSZ, or YbSZ aerogels
Co-Doping YSZ with Ytterbia
•Ytterbium was chosen due its higher atomic mass and lower valence in comparison to Zr4+
•Produces lower thermal conductivities
•Higher sintering resistance at high temperatures than YSZ
•Stabilization of tetragonal zirconia formation
G. Witz et al., J. Am. Ceram. Soc., 2007, 90, 2935–2940
N. S. Olson, F. I. Hurwitz, H. Guo, N. J. Madden, J. L. Stokes, R. B. Rogers, J. A. Krogstad, J. Am. Ceram. Soc. 10.1111/jace.17792.
F. I. Hurwitz, R. B. Rogers, H. Guo, A. Garg, N. S. Olson, D. Phan, J. L. Cashman, J. Am. Ceram. Soc. 2020, 103, 6700-6711.
Thermal barrier coatings
•YSZ is a ceramic used in thermal insulating layers on super alloys in aircraft engines ZrO2-Y2O3
•Phases of zirconia changed by substitution of Zr4+ with Y3+
•Minimize surface area loss
•Low thermal conductivity 0.8-2.9 W/(m·K), would be much lower as an aerogel
•High thermal stability

## Slide 14
National Aeronautics and Space Administration
www.nasa.gov
With dopant increasing, surface area decreases, pore size increases

## Slide 15
National Aeronautics and Space Administration
www.nasa.gov
N. S. Olson, F. I. Hurwitz, H. Guo, N. J. Madden, J. L. Stokes, R. B. Rogers, J. A. Krogstad, J. Am. Ceram. Soc., 2021, 104, 4190-4202.
High additions (>20 mol% ) of dopant can keep mesoporous structure

## Slide 16
National Aeronautics and Space Administration
www.nasa.gov
•At 1000oC, 10% and 15% dopant both show tetragonal structure
•At 1100oC, 10% dopant shows tetragonal, 15% dopant shows cubic structure
•A cubic structure is present when dopant >20mol%
•Smaller crystallite size is indicated as the dopant concentration increases

## Slide 17
National Aeronautics and Space Administration
www.nasa.gov
SiO2 coating suppress the crystalline size growth, and maintains surface area > 100m2/g at 1100oC
SiO2-YSZ or YbSZ core-shell structure

## Slide 18
National Aeronautics and Space Administration
www.nasa.gov
600oC
1000oC
1100oC
10%Y-YSZ
10%Yb-YbSZ
A
A
A
A
A
A
A-air
A-air
B
B
B
B
B
B
C
C
C
C
C
C
A: no SiO2 coating B: SiO2 coating method 1 C: SiO2 coating method 2
SiO2 coating suppress the phase change and crystalline growth

## Slide 19
National Aeronautics and Space Administration
www.nasa.gov
Summary
Aluminosilicate aerogels
•Aluminosilicate aerogels can be used up to 1100oC.
•Their composites are not flakey and can be flexible.
•The aerogel and their composites can be modified to be hydrophobic.
Yttria and/or Ytterbia stabilized Zirconia aerogels
•The surface areas of the as dried aerogels depend on the total dopant level and water ratio, but no relationship with Y to Yb ratio.
•With increase dopant level, the pore size increases up to 20% dopant, and surface area decreases with the increased dopant.
•Dopant level and the choice of dopant can affect the phase change and crystalline size growth
•Increasing dopant above 20% can avoid the phase transformation and suppress the crystalline growth at 1100oC
•SiO2 coating can effectively suppress the crystalline growth and phase change.

## Slide 20
National Aeronautics and Space Administration
www.nasa.gov
Thank you!

## Slide 21
National Aeronautics and Space Administration
www.nasa.gov
SiO2 coating suppress the phase change and crystalline growth