Alternative MMOD Shielding Concepts

Eric L. Christiansen(1), Alan Davis(2), Dana Lear(1), Frankel Lyons(2)

(1)NASA Johnson Space Center, Mail Code XI5, 2101 NASA Parkway, Houston, TX 77058, USA

(2)Jacobs, NASA Johnson Space Center, Mail Code XI5-267, 2101 NASA Parkway, Houston, TX 77058, USA

ABSTRACT

The main types of meteoroid and orbital debris (MMOD) shields are single-layer “monolithic” shields, dual-wall “Whipple” shields, and multi-wall shields (“Stuffed Whipple” and “multi-shock” are common types). Aluminum alloys are typically used for the outer bumper layer and for the rear wall of the dual- and multi-wall shields, although carbon-composites are increasingly employed in MMOD shields given their low-mass and high-strength.  Ceramic (NextelTM) and KevlarTM fabrics are commonly used for the intermediate layers of Stuffed Whipple shields.

The NASA Johnson Space Center (JSC) Hypervelocity Impact Technology (HVIT) group is continuously working to improve NASA spacecraft MMOD shielding by evaluating new materials and shielding concepts by test and analysis. HVIT has performed many hypervelocity impact tests over several years to evaluate alternative MMOD shield materials and concepts. This paper will provide results of this work in the following areas:

- Material substitutions to improve radiation and MMOD protection within Stuffed Whipple shields,

- Metallic and ceramic foam bumper and intermediate layer materials,

- Self-sealing materials.

In the first two areas listed above, the candidate shield materials were tested under similar test conditions and with fixed shield standoff and mass.  Damage to the rear wall was quantified and compared to determine the best performing shield materials. In the self-sealing material evaluations, the test objective was to gauge the ability of different materials and techniques to stop leaks in a rear wall with a 1-atmosphere (air) delta-pressure across the wall. This paper provides results of the investigations and describes forward work to continue the development of the most promising MMOD shield alternatives.

KevlarTM is a trademark of DuPont de Nemours, Inc.

NextelTM is a trademark of 3M Corporation

Note, Trade names and trademarks are used in this report for identification only. Their usage does not constitute an official endorsement, either expressed or implied, by the National Aeronautics and Space Administration.