## Slide 1
Effects of Defects Analysis and Sizing Framework for Efficient Design of Composite Structures
August Noevere
Collier Aerospace

## Slide 2
Outline
Background and Introduction
Integration into Commercial Stress Analysis Tool
Approach
Example with Wrinkling Data
Conclusions

## Slide 3
Background: HiCAM Design for Manufacturing (DFM) Project
CAPP

## Slide 4
Introduction and Background
Previous work done in the Advanced Composite Consortium (ACC) Design for Manufacturing (DFM) project:
  Map as-manufactured fiber directions from VCP to analysis model
  Map lap and gap data from VCP to analysis model
  Map simulated wrinkles from COMPRO to VCP
The goal of the current work is to expand this defect mapping into a generalized tool that can import and analyze defects from any source
  Manufacturing process simulations
  Kinematic simulations
  Real defect data – recorded in-situ or via NDE

## Slide 5
Outline
Background and Introduction
Integration into Commercial Stress Analysis Tool
Approach
Example with Wrinkling Data
Conclusions

## Slide 6
Integration into HyperX
Defect data
  Imported from any source and mapped to the FEM
Custom analysis plugins
  (In work)
  Define custom analysis approaches using defect data
  View analysis results in HyperX
Structural design and loads
  Loads from FEA are stored in HyperX and used to optimize the composite design
Effect of Defects Framework
Wrinkle Analysis
Gap Analysis
Fiber Dev. Analysis
Custom Analysis Plugins
Defect Data Mapped to FEM
Structural Design and Loads
Analysis and Margin Writing

## Slide 7
Defects in HyperX

## Slide 8
Outline
Background and Introduction
Integration into Commercial Stress Analysis Tool
Approach
Example with Wrinkling Data
Conclusions

## Slide 9
Mapping Approach
A standard approach for mapping was implemented:
  Defect surface is tessellated
  Centroid of each triangle in the tessellation is projected to the FEM mesh
  Once a FEM element is found that has a successful projection, the defect data (length, width, etc) is associated with that element
Dproj
A1
A3
A2
Node 1
Node 2
Node 3
Tessellation Centroid
FEM Mesh
Defect Mesh
Mesh mapping with area coordinates

## Slide 10
Analysis Approach
Long-term goal is for the defect analysis approach to be fully customizable – still in work
Short-term: a knockdown based approach is used
  A knockdown curve is created to define the severity as a function of a defect trait (such as area or length)
  This curve is referenced during analysis and used to modify the composite strength allowable (ply based or laminate based)
Example knockdown for gaps as a function of gap width
Example knockdown for wrinkles as a function of wrinkle area

## Slide 11
Outline
Background and Introduction
Integration into Commercial Stress Analysis Tool
Approach
Example with Wrinkling Data
Conclusions

## Slide 12
Setup for Demonstration
The demonstration model has a “funnel” shape with double curvature
A FEM was built and FEA performed with three load cases to generate representative loads
  Tension on long axis
  Tension on short axis
  Pressure
Laminate optimization was performed in HyperX to generate plies

## Slide 13
Mapping of Wrinkling Data
Wrinkles were recorded in-situ at USC’s McNair center with the ACSIS system
Wrinkles were provided in a .stp file as surface patches
Mapping

## Slide 14
Analysis with Wrinkles
Strength knockdowns per element were applied according to the area of the wrinkle covering the element
Ply-based analysis revealed that the wrinkles could cause structural failure (negative margins)
Effected Elements
Wrinkles

## Slide 15
Resizing the Laminate
The laminate was resized to resolve negative margins generated by the wrinkles
Resizing was achieved by using the negative margins to establish “required” margins during resizing with pristine properties
  Example: element with -10% margin would be required to have a +10% margin during resizing
After resizing structure
After resizing structure
Added ply

## Slide 16
Outline
Background and Introduction
Integration into Commercial Stress Analysis Tool
Approach
Example with Wrinkling Data
Conclusions

## Slide 17
Conclusions
An effects of defects framework has been planned and initiated in HyperX
  Mapping of defects
  Analysis with a simple knockdown based approach
The process was demonstrated on a model with real wrinkle data captured from in-situ scans
Future work: improve HyperX analysis plugins to allow fully customizable analysis of defects

## Slide 18: Thank you! Questions?
Acknowledgements
The material contained in this paper is based upon work supported by NASA under award No. 80NSSC22M0157.
Any opinions, findings, and conclusions or recommendations expressed in this material are those of the author(s) and do not necessarily reflect the views of the National Aeronautics and Space Administration.
Thanks to the McNAIR Center at University of South Carolina for providing the CAD model and wrinkle scan data.