## Slide 1
Space Technology Mission Directorate
Technology Demonstration Mission Program
Space Nuclear Propulsion Project
Sarah L. Langston, Carl C. Poteet, Julia E. Cline
NASA Langley Research Center
2023 Nuclear and Emerging Technologies for Space (NETS)
The Challenges with Material Interfaces in a Nuclear Thermal Propulsion Engine Heat Exchanger

## Slide 2
Background and Motivation
Interface Challenges
Proposed Solutions
Concluding Remarks
Outline

## Slide 3: What is Nuclear Thermal Propulsion?
NASA is currently committed to developing critical technologies to send humans to cis-lunar space, Mars, and beyond
Nuclear Thermal Propulsion (NTP) is an enticing technology that would shorten crew transit time to Mars, as well as create additional abort options
REFLECTOR
NOZZLE
NUCLEAR REACTOR
CONTROL DRUM
PUMPS
H2
PROPELLANT
NTP Systems Work By:
Flowing a propellent through a nuclear reactor
Generating heat by nuclear fission to increase the temperature of the propellent
Exhausting the heated propellent through a nozzle to produce thrust

## Slide 4: NTP reactors operate at nearly 3000 K
Coating
C/C Tube
CerCer
H2 Gas
Flow
H2
Moderator Reactor Core
Fuel Element
Heat Exchange Tubes
REACTOR
H2
Challenge: design, analyze, and manufacture the heat exchange tubes used in the reactor
Moderator reactor core consists of many fuel elements
Fuel elements are comprised of ~90 individual heat exchange tubes

## Slide 5: Heat exchange tubes protect the fuel
Heat exchange tubes provide structural reinforcement and prevent corrosion of the nuclear fuel from the pressurized hydrogen propellent
Primary System Function: Nuclear Fuel (Ceramic-Ceramic, CerCer) heats hydrogen (H2) gas
Material / Layer Functions
Carbon-Carbon (C/C) tube – structural backbone to fuel, protect CerCer from H2 pressure
Coating – prevent H2 from corroding C/C tube and prevent H2 exposure to CerCer
H2 – heated propellent
Coating
C/C Tube
CerCer
H2 Gas
Flow
H2
Heat Exchange Tubes

## Slide 6: The use of dissimilar materials causes interface problems
Coating
CerCer
H2 Gas
Gap
Cracks
H2 Gas
C/C Tube
One
Temperature Cycle
Differences in material coefficients of thermal expansion (CTE) cause issues at two interfaces
CerCer to Tube Interface: A gap will open, cracks may form in CerCer
Tube to Coating Interface: Cracks will form
Pristine System
Cycled System
All issues are derived from material CTE mismatch at mating interfaces
Tailoring C/C tube layup can modify CTE, but a direct match over the temperature range is not feasible
(NTP operation requires ~10 cycles)

## Slide 7: Flowing helium eliminates one interface issue but requires system redesign
Coating
C/C Tube
CerCer
H2 Gas
He Gas
Flow
H2
Flowing helium (He) between the C/C tube and CerCer fuel
Utilize flowing He between CerCer and C/C tube to allow a gap while maintaining adequate heat transfer
  Pros: Eliminates CerCer to C/C interface issue
  Pitfalls: Helium must be hot and flowing – requires pumps/machinery that operate at these temperatures; may need an extra tank to carry helium; requires system redesign
No single solution listed solves all problems and may create new problems

## Slide 8: Restrained system reduces the fuel to C/C interface issue
Coating
C/C Tube
CerCer
H2 Gas
C/C Tube
Flow
H2
Restrained System
Add C/C tube to outside of system, which will restrain CerCer expansion
  Pros: Reduces CerCer to C/C interface issue
  Pitfalls: Requires thick outer C/C tube; generally high stresses; CerCer crushing and gap still likely; does not address C/C to coating interface; additional C/C tube reduces amount of nuclear fuel in assembly
No single solution listed solves all problems and may create new problems

## Slide 9: A melt layer can eliminate the fuel to C/C interface issues
Coating
C/C Tube
CerCer
H2 Gas
Melt Layer
Flow
H2
Melt Layer
Add an additional layer of material between CerCer and C/C that will melt prior to 1000K and expand prior to gap forming
  Pros: Eliminates CerCer to C/C interface issue; moderately simple to integrate
  Pitfalls: Have yet to identify a candidate melt layer material (matches neutronics, high thermal conductivity, appropriate CTE); does not address C/C to coating interface
No single solution listed solves all problems and may create new problems

## Slide 10: Inverting the system may improve both interface issues but requires major redesign
Coating
C/C Tube
CerCer
H2 Gas
Fuel Element
Heat Exchange Tubes
Inverted System
Have rods of CerCer fuel inside C/C tubes with H2 gas flowing around coated C/C tube exterior
  Pros: May improve both interface issues
  Pitfalls: Complicated; change that effects rest of engine integration (likely requires major system redesign); high hoop stress in C/C tube; crushing will occur but may not be uniform; coating cracks may open during cooling
No single solution listed solves all problems and may create new problems

## Slide 11: Concluding Remarks
Differences in CTE may lead to failure of the NTP system at material interfaces if not properly addressed
Multiple concepts have been presented to introduce additional compliance into the material system to prevent material cracking and/or failure with no clear solution
A better understanding of the mechanical behavior of the nuclear fuel material is needed to improve models and down select options