## Slide 1
NASA GRC – OSU
Advanced Materials and Manufacturing
GRC Magnetic Alloys
GRC Team
Alex Leary GRC LMA
Ron Noebe GRC LM
Maria Willard GRC LMA
Vladimir Keylin HX5
Grant Feichter HX5
5/18/2023

## Slide 2
• Power electronics: Conversion and Control
- AC/DC, DC/AC, voltage, frequency, etc…
- Reliability and redundancy
• MW of power managing kW of heat
• Turbine propulsion ~12kW/kg
- Hybrid Electric propulsion systems
must compete
- Magnetic materials can comprise
½ of inverter mass
- Breakdown voltage decreases with
altitude
- Aircraft EMI requirements
1 MW = 1341 HP
Modified from Madonna, et al. IEEE Trans Trans Elect (2018)
STARC-ABL concept
Boundary layer ingestion
Notes: Electrical requirements are increasing in aircraft and magnetic materials can account for large portions of the system mass

## Slide 3
Battery
Fuel Cell
Motor
Generator
AC / DC
Motor
Generator
AC / DC
DC / AC
DC / AC
DC / DC
Converter
Magnetics
Filter
Magnetics
High Voltage
Low Voltage
Example Aircraft Electrical System
Circuit Breakers
• Broad use of soft magnetic materials in subsystem components that in some cases, account for significant size / mass
• Many potential system configurations and subsystem component topologies available -> drives variety of magnetics requirements
• Power density – EMI – cost – reliability is a complex trade space
• Optimized system will be improved with advanced materials – GRC is working to make nanocomposites an option for designers
Common use of soft magnetic materials
DC
AC
DC

## Slide 4
Soft Magnetic Materials
Figures of merit:
- Saturation induction (Bsat)
- Power loss under operation conditions
- Power density (volume and/or mass)
- Temperature capability
- Tolerances
Local heating associated with air gaps
Target applications
Notes: Annealing options and anisotropy

## Slide 5
System level
requirements
Circuit
Topology
Magnetic requirements
GRC Magnetics
Feedback to system and circuit design
Planar flow casting (PFC)
Rapid solidification to form amorphous ribbon
Ceramic nozzle constrains puddle
Wheel speeds ~20-30 m/s
Ribbon thickness ~20 μm
Variable width up to 5 cm
Batch sizes 50g up to 3 kg
*Many unknown alloy melt properties
Prototype Inductors, Transformers, Chokes, etc…
Excellent magnetic properties,
Poor mechanical properties
Notes: Planar flow casting to make precursor material

## Slide 6
X-57 mounting locations
Firewall
Wing web
Prototype filter
Design requirements
L = 14μH, Ic = 10Ap, ID > 17 mm
Design comparison
Ferrite (SOA) Nanocomposite
Toroid 21x53x51 (mm) 21x40x25 (mm)
Bm (T) 0.3 0.8
μr 1600 5300
Mass (g) 454 145
cores
3X
Capabilities / Requirements
• Filter design by GRC LED
• Fast prototyping by GRC magnetics
* Integration and mechanical requirements
* GRC QA function prior to shipping
* AFRC determines flight worthiness
• Required for benchtop development
* Required for flight testing
X-57 EMI Filters
EMI is currently a significant challenge in aircraft power systems and nanocomposite chokes are not commercially available
Significant benefit – reduction in size and mass – compared to SOA

## Slide 7
  Distributed Gap
  Glued Arc/Bar Segments
  Edge-Wound Coil
  Liquid Cooling with Pump
  60 kg Total Mass
  Kool Mµ powder
  Gapless Design
  Oil Immersion
  12 kg Ribbon Mass
  20 kg Total Mass
  2 – 2.5X Smaller Volume
  Stress Annealed
  Distributed Gap
  Potted Assembly
  Liquid Cooling with Pump
  100 kg Total mass
  Iron-alloy powder
Low Permeability Application
Co-based nanocomposite: Tunable anisotropy gapless core
Filter inductor for MW scale gas compressor
GRC ribbon
Commercial core materials
Notes: Example application

## Slide 8: GRC Magnetics Collaboration Areas
1. Interaction with power electronics designers for prototypes requiring > 100kW
  GRC able to design/build/test custom prototype cores
  Application space relevant to many emerging grid/vehicle efforts
2. Material characterization and modelling under relevant conditions
  Excitation fields specific to converter topologies
  Scalable models for system level optimization
3. Structural characterization of nanocomposites with ~10nm grains
TEM: Typical nanocomposite