## Slide 1: Carbothermal Reduction Demonstration (CaRD) Project Status 2023
Water Electrolysis
Condenser
Methanation Reactor
Solar Concentrator Physical Sciences Inc.
Carbothermal Reactor
Orbitec
Heat
Excavator
Canadian Space Agency
Soil
Water Electrolysis Johnson Space Center
O2
LOX
H2O
Liquefaction Johnson Space Center
“Dust to Thrust” Demonstration 2010
Propulsion
Johnson Space Center
Past
Present
Future
Carbothermal Reactor Developed by Sierra Space Inside 15ft Dirty Thermal Vacuum Chamber at JSC
CaRD Prototype Test in FY24.
Targeting Payload on the Lunar Surface in 2027
End-to-end Lunar Carbothermal Oxygen From Regolith Process
O2 Liquefaction & Maintenance
O2 Dryer
Inlet Hopper
Soil Excavation
Outlet Hopper
Spent Soil Disposal
Carbothermal Reactor
CH4
H2
O2
CH4, CO, H2, CO2
CH4
Common to Mars ISRU, Carbothermal and ECLSS
Concentrated Solar Energy
Common to Mars ISRU and Carbothermal
CaRD project scope includes all of the subsystems necessary to determine the performance of the carbothermal reduction process (SiO2 + 2C  Si + 2CO) on the lunar surface.
Downstream components that convert CO into oxygen gas can be implemented at a larger scale once the yield is known.
Included in Digital Engineering Design Center Project
Included in CaRD Project
H2O
The current cost to land 1kg on the lunar surface is $1.2M. At that rate, landing 10 tonnes of LOX would cost $12B

## Slide 2: “Dust to Thrust” 2010
Solar Concentrator
Physical Sciences Inc.
Carbothermal Reactor
Orbitec (Now Sierra Space)
Heat
Excavator
Canadian Space Agency
Tephra
Water Electrolysis
Johnson Space Center
O2
LOX
H2O
Liquefaction
Johnson Space Center
Propulsion
Johnson Space Center
Heat
Plume
Sintered Pad
Physical Sciences Inc.
NORCAT

## Slide 3: Example of TRL 4 to 6 for the Moon
Component Vibration
Component Dust
Subsystem Vibration
Integrated Vibration
Component TVAC
Thermal Cycles
Component Thermal Vacuum
Integrated Thermal Vacuum
Torque Margin/Dust
Environmental Testing of the OVEN

## Slide 4: CaRD Environmental Test Unit (Brassboard)

## Slide 5: COMSOL Multiphysics Analysis
Lens Heating Analysis
Lens Stress Analysis

## Slide 6: CaRD Brassboard Test Results
Test Number | grams oxygen extracted/ kWh thermal
CaRD Ambient | 13.42
CaRD Vacuum 1 | 11.53
CaRD Vacuum 2 | 15.79
CaRD Vacuum 3 | 10.77
This test will be repeated in 2024 with an automated reactor being developed by Sierra Space through the Carbothermal Oxygen Production Reactor (COPR) Tipping Point project

## Slide 7: CaRD Prototype
Arm Mockup
Solar Concentrator
Reactor Fluid System
Gas Analysis
Avionics/Software
Thermal Management
Lander Mockup
Reactor

## Slide 8: Long Term Overview
Full Scale
10MT/yr
(2 kg/hr)
Pilot Plant
1MT/yr
(0.2 kg/hr)
Flight Demo
(single melt)
Ground Demo
(single melt)
Flight Demo
Pilot Plant
Full Scale Plant
Compass Study
3.5 MT/yr per module
SBIR Phase 3 (CTOP) (GRC-Sierra Space)
CaRD
Brassboard Reactor SBIR Phase 3 (Sierra Space)
Brassboard Waveguide, SBIR Phase 2 (Physical Sciences Inc.)
Prototype Reactor, COPR Tipping Point (Sierra Space)
Prototype Waveguide, SBIR Phase 3 ( Physical Sciences Inc.)
Studies/Development
Studies/Development
Ground Demo
Requirements
Demonstrations
Completed
Active
Needed

## Slide 9: Mars and ECLSS Commonality
End-to-end
Lunar Carbothermal O2FR Process
O2 Liquefaction & Maintenance
O2 Dryer
Inlet Hopper
Soil Excavation
Water Electrolysis
Condenser
Outlet Hopper
Spent Soil Disposal
Water Cleanup
Carbothermal Reactor
H2O
CH4
H2
H2O
O2
CH4, CO, H2, CO2
CH4
Sabatier Reactor
Methane Gas
Common to Mars ISRU and Carbothermal
End-to-end
Mars Propellant Production Process
O2 Liquefaction & Maintenance
O2 Dryer
Inlet Hopper
Soil Excavation
Water Electrolysis
Condenser
Outlet Hopper
Spent Soil Disposal
Water Cleanup
Regolith Dryer
H2O
CH4
H2
H2O
O2
Sabatier Reactor
CH4 Liquefaction & Maintenance
CH4 Dryer
CH4
CO2
CO2 Collection
Dust Filtration
H2O
Common to Mars ISRU, Carbothermal and ECLSS

## Slide 10: Scalability & Modularity
Notional packaging of Mars ISRU module sized for 40% of Mars LOX/Methane. 3 modules x 40% = 120% of full scale
Reference: Kleinhenz, J. E., & Paz, A. (2017). An ISRU propellant production system for a fully fueled Mars Ascent Vehicle. In 10th Symposium on Space Resource Utilization (p. 0423).
Components common to Mars ISRU module would easily fit inside of a flex rover cargo box
180” DIA = Falcon 9 payload fairing diameter
213” DIA = Minimum mirror diameter required for 1 tonne per year based on current results
 | Tonnes of O2 | days | kg/day | kg/hr
O2FR pilot plant | 1.000 | 182 | 5.49 | 0.23
O2FR full scale O2FR | 10.000 | 182 | 54.95 | 2.29
Mars ISRU LOX Methane | 27.912 | 480 | 58.15 | 2.42
Flex Rover cargo box volume

## Slide 11: Mars Commonality – Expanded to Lunar LOX/Methane
Modified Lunar Carbothermal Concept
O2 Liquefaction & Maintenance
O2 Dryer
Inlet Hopper
Soil Excavation
Water Electrolysis
Condenser
Outlet Hopper
Spent Soil Disposal
Water Cleanup
Carbothermal Reactor
H2O
CH4
H2
H2O
O2
CH4, CO, H2, CO2
CH4
Sabatier Reactor
Solid Carbon
Water from Icy Regolith
CH4 Liquefaction & Maintenance
CH4 Dryer
CH4
Methane Pyrolysis
Common to Mars ISRU and Carbothermal
Producing both LOX and LCH4 on the moon would be the best “Moon to Mars” architecture for propellant production and can be accomplished if solid carbon is combined with hydrogen sourced from lunar water
Current hydrogen liquefaction crycooler technology will have to operate for over a year in order to see a return on landed mass (assuming 183 days of sunlight per year)1
The use of solid carbon to drive a carbothermal reduction reaction has been demonstrated for terrestrial silicon production2
Methane pyrolysis technology is being developed for terrestrial hydrogen and carbon production3
References:
Nugent, B. T., Grotenrath, R. J., & Johnson, W. L. (2022). 20 Watt 20 Kelvin Reverse Turbo-Brayton Cycle Cryocooler Testing and Applications.
Maeng, S. H., Lee, H., Park, M. S., Park, S., Jeong, J., & Kim, S. (2020). Ultrafast carbothermal reduction of silica to silicon using a CO2 laser beam. Scientific reports, 10(1), 21730.
Methane Pyrolysis for Hydrogen-Opportunities and Challenges
Common to Mars ISRU, Carbothermal and ECLSS