## Slide 1
Printed Hybrid Electronics (PHE) in a Flight Environment: 3D Printed Electronics on Suborbital Technology Experiment Carrier 9 (SubTEC-9)
Beth Paquette/ NASA GSFC
Jason Fleischer/Laboratory for Physical Sciences
To be presented by Beth Paquette and Jason Fleischer at the Electronic Parts and Packaging (NEPP) Program’s Electronics Technology Workshop (ETW), Greenbelt, MD, June 12-15, 2023
1

## Slide 2
Printed Hybrid Electronics (PHE) – additive manufacturing technique where electronic circuits are fabricated by depositing materials onto an existing substrate without the use of masking or etching, and using existing electrical components
Advantages:
  Fine feature sizes down to 20-30 microns
  Variety of substrates – flexible, rigid, 3-dimensional non-planar
  Demand for increased sensitivity and performance
  Reduced size weight and power (SWaP)
  Subsystem miniaturization can increase the SWaP available for instruments, thereby increasing the science return for a mission
Applications:
  Hard Energy X-Ray Photoelectric Polarimeter (HXPP) detector strips
  Next Generation Microshutter Arrays (NGMSA) interconnects
  Microcontroller Circuitry providing telemetry data
EMI shield [Optomec]
Printed Hybrid Electronics (PHE)

## Slide 3
Additively Manufacture Arduino-type microcontroller Circuits, including temperature and Humidity sensors on the inside of a sounding rocket payload door in a waterproof section
Collect data and recover circuits from experiment to evaluate performance over flight and robustness of the circuits
Thermally connected, directly on door
Thermally connected, swappable
Thermally insulated, swappable
12 inch x 6 inch curved aluminum door panel
PHE Experiment Objective
3
To be presented by Beth Paquette and Jason Fleischer at the Electronic Parts and Packaging (NEPP) Program’s Electronics Technology Workshop (ETW), Greenbelt, MD, June 12-15, 2023
This experiment provides environmental data on the technology that we did not have before!
Notes: list of document section numbers, topics and presenters
3

## Slide 4
Accelerometer
Syringe Printed Temperature and Humidity Sensors
Voltage Regulators
Microcontroller bare die, unencapsulated
Passive Components (circled)
Cavities were milled out of or printed with the substrate
Components were placed upside down in the cavities
Insulating “moats” were added around the components
Traces were printed to the pads on the components to complete the circuit – multiple layers
PHE Circuit Details
To be presented by Beth Paquette and Jason Fleischer at the Electronic Parts and Packaging (NEPP) Program’s Electronics Technology Workshop (ETW), Greenbelt, MD, June 12-15, 2023
4

## Slide 5
Suborbital Technology Experiment Carrier 9 (SubTEC-9)
14 Experiments on board
20 ft long payload, Terrier-Improved Malemute Vehicle
181.5km altitude
Launched from Wallops Island, VA April 25, 2023
12 minute flight
Rocket and Flight Details
To be presented by Beth Paquette and Jason Fleischer at the Electronic Parts and Packaging (NEPP) Program’s Electronics Technology Workshop (ETW), Greenbelt, MD, June 12-15, 2023
Sub-TEC 9 Launch [Youtube]

## Slide 6
To be presented by Beth Paquette and Jason Fleischer at the Electronic Parts and Packaging (NEPP) Program’s Electronics Technology Workshop (ETW), Greenbelt, MD, June 12-15, 2023
Thermally connected, directly on door
Survived the entire flight
Thermally connected, swappable
Did not work since integration
Thermally insulated, swappable
Survived until T+47s
Post-Flight Analysis:
Flight Data
6
Monitored PHE circuit health during flight in real-time
Received telemetry data recorded from flight
Analyzing data from events leading up to flight, including vibration tests, payload buildup, and dress rehearsal
Notes: list of document section numbers, topics and presenters
6

## Slide 7
Preliminary findings from flight:
Thermally insulated, swappable circuit
  T+37 seconds: on the sensor data channels show a spike up prior to not functioning
T+47 seconds: The Main Payload PHE current increases
Thermally Connected Circuit printed directly on door:
  Rebooted at T+47 seconds
  Continued to function properly the rest of the flight
  Acceleration and sensor data follows main payload data
Post-Flight Analysis:
Flight Data
To be presented by Beth Paquette and Jason Fleischer at the Electronic Parts and Packaging (NEPP) Program’s Electronics Technology Workshop (ETW), Greenbelt, MD, June 12-15, 2023
7
Notes: Good accelerometer response

## Slide 8
Additional inspection and analysis in Goddard’s Parts Analysis Lab to have a complete picture of the flight
Independent functional testing
Visual External Inspection
X-Ray Inspection
Visual inspection of Connector and wiring
Report out any areas where further analysis may be required
To be presented by Beth Paquette and Jason Fleischer at the Electronic Parts and Packaging (NEPP) Program’s Electronics Technology Workshop (ETW), Greenbelt, MD, June 12-15, 2023
8
Post-Flight Analysis:
Next Steps

## Slide 9
Goddard Space Flight Center
  Parts, Packaging and Assembly Branch
  Brian Banks
  Sean Donohue
  Ahmed Ghalib
  Cathy Hesh
  Scott Hesh
  Peter Hughes
  Michael Johnson
  Matthew Morrow
  Tristan Epp-Schmidt
  Chris Green
  Wes Powell
  Margaret Samuels
  Joshua Yacobucci
Laboratory for Physical Sciences
  Donghun Park
  Dan Hines
  Edwin Quinn
Marshall Space Flight Center
  Curtis Hill
  Ian Small
  Jennifer Jones
Army Research Lab
  Harvey Tsang
  Sami Hawasli
Special Thanks

## Slide 10: Thank you!
Questions?
Contact:
beth.m.paquette@nasa.gov
Printed Hybrid Electronics Team: From left to right: Beth Paquette/GSFC, Brian Banks/GSFC, Jason Fleischer/Laboratory for Physical Sciences (LPS), Donghun Park/LPS. Photo by Berit Bland

## Slide 11
Acronyms
Acronym | Definition
PHE | Printed Hybrid Electronics
PCB | Printed Circuit Board
SWaP | Size Weight and Power
SubTEC | Suborbital Technology Experiment Carrier