## Slide 1
Vapor Growth of ZnSe-based Compound Semiconductors in Low Gravity environment on International Space Station
A physical science low-gravity experiment conducting in Low Gradient Furnace (LGF), Materials Science Research Rack (MSRR), on ISS
Principal Investigator: Dr. Ching-Hua Su, NASA/MSFC
Project Scientist: Dr. Martin Volz, NASA/MSFC

## Slide 2: Crystal growths of zinc selenide (ZnSe)–based ternary compound semiconductors by physical vapor transport
A list of II-VI compound semiconductors grown by PVT at MSFC
Compounds | CdTe | ZnTe | CdS | ZnSe | ZnS
Melting point (oC) | 1092 | 1292 | 1397 | 1526 | 1718
PVT growth temperature | 850 | 1000 | 985 | 1120 | 1150
Physical Vapor Transport (PVT) process consists of three steps:
(1) vapor species sublime from the source material at higher temperature,
(2) vapor species transport (diffusion/convection) through vapor phase to crystal site at lower temperature,
(3) condensation of vapor species on the crystal surface for its growth.
Main disadvantage of PVT process: Growth rates are low and inconsistent.

## Slide 3
Scientific objectives
To establish the effects of gravity-driven fluid flows to (1) crystalline structural quality, (2) the non-uniform incorporation of dopants, impurities and defects and (3) the compositional segregation in the ternary compounds grown by PVT – caused by the buoyancy-driven convection and irregular fluid-flows on Earth.
To assess self-induced strain effects developed during processing at elevated temperatures caused by the weight of the crystals.
To conduct theoretical simulation of heat transfer, mass transport and growth kinetics to obtain quantitative comparisons between the experimental and calculated results and, consequently, understand and simplify the complexity of the coupled mass transport and growth kinetics problem.

## Slide 4: Earth benefits/spin-off applications
Routine production of high-quality single crystals of high melting point semiconducting compounds requires a fundamental and in-depth understanding of the overall vapor growth processes.
Cr-doped ZnSe as efficient, tunable, diode-pumpable, mid-IR lasers operating at room temperature in the 2000-3000 nm range.
The growth of thick ZnSe film on GaAs substrate as quasi-phase matching media for the frequency converters of lasers.
Optical bistable characteristics of ZnSe for digital optical computer with bandgap tunability of ternary alloys of ZnSeTe and ZnSeS.

## Slide 5: Partial pressures along the three-phase curve for ZnSe
Zn sat.
At 1150oC, PZn varies from 8.4 to 1.3x10-4 atm, PSe2 varies from 20 to 5x10-9 atm
and a = PZn/ PSe2 varies from 1.7 x109 to 6.5x10-6
Zn sat.
Se sat.

## Slide 6: Analytical: one-dimensional diffusion on mass flux of AIIBVI
Mass flux of ZnSe as a function of DT for source temperature at 1080 oC and different values of a
Four parameters determine mass flux : source temperature, crystal temperature, a, the pressure ratio of A and B2 and pressures of residual gases, such as CO, CO2 H2, …
Mass flux of ZnSe as a function of PZ and different values of a(L)

## Slide 7: Maximizing transport rate by reducing residual gas and adjusting the stoichiometry
B. baking under vacuum to adjust a ~ 2.0
A. H2 reduction to reduce residual gases

## Slide 8: Heat treatment by baking under vacuum

## Slide 9: Crystal growth, thermal profile and initial ampoule positions
Growth was initiated by translating furnace to the right.
The peak with high temperature gradient confines the supersaturation position to a narrow region.
The peak reduces secondary nucleation by subliming any deposited material just ahead of growth interface.
horizontal
vertical
destabilized
vertical
stabilized
Gravity
direction

## Slide 10
ZnSe grown on (110) seeded
Unseeded growth
Seeded growth
Seeded grown ZnSe crystal on light table
ZnSe
Cr-ZnSe

## Slide 11: Flow chart of post-growth sample characterization plan

## Slide 12
Morphologies of grown ZnSe crystals
Vertical unseeded growth
x
g
g
g
x
g

## Slide 13: Horizontal unseeded growth
ZnSe-44
ZnSe-43
x
g
.
g
g

## Slide 14: Morphologies of the seeded grown ZnSe crystals Vertical growth
ZnSe(S)-9V
ZnSe(S)-12V
g

## Slide 15: Horizontal seeded growth
ZnSe(S)-8H
ZnSe(S)-11H
ZnSe(S)-13H
g
x
g
g

## Slide 16
SEM micrograph of the as-grown surface
vertical growth
horizontal growth
Step growth:
Shear convective vapor flow parallel to growing surface
Island growth:
Individual nucleus forming on growing surface

## Slide 17: Atomic force microscopy (AFM) on growth surface
Growth mechanism of island mode with nucleation of islands in the order of 10 nm in height and 10 mm in diameter.
Vertical growth
Horizontal growth
Step mode mechanism consists of (110) terraces of 10 mm with numerous steps of 10 nm height between the terraces.

## Slide 18
A growing surface contains the structures of terraces (T), steps (S) and kinks (K).
Zn and Se2 species reach surface to form adsorbed atoms (adatoms) which migrate on the surface.
A kink, K, makes an energy favorable site for the formation and attachment of adatom.
As kink filled to the edge of the surface, one step, S, is grown and the terrace extends one step to the right.
When the terrace, T, fills up the whole growing surface, the crystal grows upward by the step height.
Growth velocity R = dv/l where d: step height; l: distance between steps; v: growth velocity of the step.
From typical experimental values: R: 3-5 mm/day, d = 10 nm, l = 10 mm, v is estimated to be 50 mm/s.
Schematics of the step growth mechanism on a growing surface with terrace (T), kink (K) and step (S).
SEM micrograph of as-grown surface
Kinetics of step growth

## Slide 19: SWBXT on ZnSe crystals
Transmission images show twin lamellae and distortion caused by wall-wetting
Surface reflection images of 43H show alternate (111) twins

## Slide 20: Correlation between SWBXT and x-ray diffraction rocking curves

## Slide 21: Correlation between SWBXT, rocking curve and reciprocal space map
RSM differentiates mosaicity from strain
Double broaden
streaks: strain

## Slide 22: SWBXT on ZnSe crystals
Transmission images show twin lamellae and distortion caused by wall-wetting
Surface reflection images of 43H show alternate (111) twins

## Slide 23
gravity
growth
direction
[VZn]
[Al]
Effects of gravity on the grown crystals
Distribution of [VZn] and [Al] in ZnSe (horizontal)

## Slide 24
A(I1d)/A(Fx)
Distribution of [Al], [Na] and [VZn] in ZnSe (vertically stabilized)
x
g
[Al]
[Na]
[VZn]

## Slide 25
Distribution of [VZn] and [Al] in ZnSe (vertically destabilized)
x
g
[Al]
[VZn]

## Slide 26
growth direction
gravity
Impurities Distribution by secondary ion mass spectroscopy (SIMS)
(horizontally grown)
[Si]
[Fe]
[Cu]

## Slide 27
x
gravity and
growth direction
[Si]
[Fe]
[Cu]
Impurities Distribution by secondary ion mass spectroscopy (SIMS)
(vertically grown)

## Slide 28
Low Gradient Furnace, Materials Science Research Rack, U.S. Lab Module on ISS

## Slide 29
Low Gradient Furnace (LGF) built by ESA (European Space Agency)
Material Science Research Rack (MSRR)
Sample Cartridge Assembly (SCA)
Thermocouple
positions
source
seed
SCA X-ray image

## Slide 30
Schematics of Sample Cartridge Assembly (SCA) and thermal profile during growth

## Slide 31
Transmission X-ray to locate relative positions of seed, source and thermocouples

## Slide 32: Six flight samples, 3 unseeded and 3 seeded, processing on ISS
GTCS-C3 (unseeded Cr-doped ZnSe)
Processed on 3/3/23 after two failed attempts on 8/1/22 and 10/10/22
GTCS-C1 (unseeded ZnSe)
Process started on 3/21/23 and ended 11 hours before the planned 6 days growth
GTCS-C2 (seeded with ZnSe (110) crystal)
Process started on 4/25/23 and was disrupted during program cool-down after 5 days growth
GTCS-C4 (seeded with ZnSe (100) crystal)
Process planned on 8/7 -8/18/2023
GTCS-C5 (seeded with ZnSe (111) crystal)
Process planned on 9/11 -9/22/2023
GTCS-C6 (unseeded ZnSeTe)
Process planned on 11/20 -12/1/2023
unseeded growth ampoule
Seeded growth ampoule

## Slide 33
Measured thermal profile every 12 hours through the furnace translation for C2
saturation
temperature

## Slide 34
Acknowledgments
To my colleagues for their contributions to the project:
Drs. R. F. Brebrick, A. Burger, M. Dudley, S. Feth, M. A. George, D. G. Gillies, S. L. Lehoczky, R. Matyi, K. Mazuruk, W. Palosz, Balaji Raghothamachar, N. Ramachandran, Yi-Gao Sha, N. G. Singh, F. R. Szofran, M. P. Volz and Ling Jun Wang.
Technical supports: Curtis Bahr and Jeff Quick