## Slide 1: Solar White
Thermal Control Coating development with goals for solar absorptivity (α) of 0.01 and IR emissivity (ε) of 0.9
  These values would allow passive cooling to 90 K (on a sphere at 1 AU with no other heat loads)
  Applicability to in-space cryogenic storage, and cooling detectors for science
  May enable high temperature superconductors with applicability to active radiation shielding, and enhanced EP systems
 | SoA Paint (AZ-93) | Solar White Paint | SoA Tile | Solar White Tile
solar absorptivity (α) | ~0.15 | ~0.04 | ~0.06 | 0.01 – 0.04
IR emissivity (ε) | ~0.91 | ~0.99 | ~0.83 | ~0.99
Solar White Paint
Sprayed over aluminum
The Parker Solar Probe’s approach to the Sun is limited by its heat shield. A Solar White tile coating may allow substantially closer approach distances to the Sun, allowing scientific study and potentially allowing a spacecraft to slingshot around the Sun to reach interstellar velocities.
Angela Krenn
TFAWS, August 2023