## Slide 1
Window Material Database

## Slide 2: Brief History of Windows
Heritage (glass & ceramic) Window Designs
Apollo
ISS &
Shuttle
New (polymer) Window Designs
Orion
SpaceX – Crew Dragon
Gateway
Future Programs
Hybrid

## Slide 3: How did we get here?
Windows Material Database
  A database that provides flight relevant data to designers, allowing for quick trade studies between transparent materials.
    The database contains 4 types of materials: Acrylics, Polycarbonates, Glasses, and Ceramics (various brands), and each is tested using the same method.
      Acrylic (AC) brands
        GKN Cast, GKN Stretched, Plexiglass, Poly II, SAR (coated)
      Polycarbonate (PC) brands
        Lexan 9034, Lexan MR10 (coated), Makrolon (coated, also now Tuffak), & Zelux
      Glasses and Ceramic Brands
        Corning – Fused Silica (FS), Tosoh – Fused Quartz (FQ), & Surmet - ALON
  Each material is taken through a suite of material and environment testing
    Environments: Flammability, Atomic Oxygen, Hypervelocity Impact, Thermal Vacuum, and Radiation & UV
    Testing: Optical, Creep, Strength, and Thermal Property
      Materials are tested optically before and after exposure to determine if there was a degradation in optical quality after exposure. Then, the materials were tested for strength after exposure.

## Slide 4: Optical Testing
Test Parameters
  Transmission
    Visible spectrum
    Full spectrum (200-3000 nm)
  Reflectance
  Birefringence
  Wavefront
  Striae
  Haze
  Color Balance
  Wedge
  Imagery
No Pane
Fused Silica
GKN Stretched Acrylic
Makrolon Polycarbonate
400 mm Lens

## Slide 5: Wavefront Error
Test
  The purpose of the Transmitted Wavefront Error (TWE) Measurement is to determine the change in wavefront of a defined input light beam as it passes through an optically transparent material.
Test Setup
Notes: Convert this to a wavefront error only slide

## Slide 6: Wavefront Error Data
The pass/fail criteria of the wavefront error measurement is dependent on the optical quality desired.
Interferometer Wavefront Data
Category E windows do not have a wavefront error requirement
Allowable Wavefront Error for Category B, C, & D

## Slide 7: Thermal Property Testing
Properties Tested
  Degradation Temperature
    Q600 SDT Thermogravimetric Analyzer (TGA)
  Emittance (ASTM E408)
  Solar Absorptance (LPSR 300 Manual)
  Some more specific properties for materials currently in use
ET-100 Emissometer
LPSR 300 Sprectroreflectometer
 | AC – GKN Cast | AC – GKN Stretched | AC – Plexiglas | AC – SAR | AC – Poly II | PC – 9034 | PC – MR10 | PC – Makrolon | PC – Zelux | ALON | Fused Silica | Fused Quartz
Degradation Temperature (oC) | 370 | 368 | 324 | 326 | 366 | 457 | 463 | 486 | 485 | N/A | N/A | N/A
Emittance (HTE) | 0.93 | 0.93 | 0.94 | 0.96 | 0.93 | 0.92 | 0.83 | 0.95 | 0.92 | 0.85 | 0.94 | 0.95
Solar Absorptance | 0.33% | 0.32% | 0.28% | 0.29% | 0.29% | 0.38% | 0.31% | 0.27% | 0.35% | 0.30% | 0.20% | 0.19%
Results

## Slide 8: Strength Testing
Two Tests
  Tensile testing of dogbone-shaped specimen (polymers – ASTM D638)
  Biaxial flexure testing of brittle materials (glass and ceramics – ASTM C1499)
Test Setup
10 kip Load Cell
50 kip grips
Test Specimen & Alignment Tool
1.25” Dia Ring
2.5” Dia Ring
Test Specimen & Teflon Pucks
Alignment Tool (Wedding Cake)
Loading Rod

## Slide 9: Strength Testing: Prep Lesson Learned
Issue: Acrylic specimen would break outside of the gage length
  The issue was resolved by sanding the fillet areas
    Acrylic also exhibits some notch sensitivity like glass and ceramics
500 grit
Original

## Slide 10: Strength Testing Results
Calculated Parameters
  Young’s Modulus
  Yield Strength (1% Offset)
  Ultimate Strength
  Residual Strength
Chart: PC-9034-C0-T-1
Units: ksi | E | F_y | F_u
AC – GKN Cast | 546 | N/A | 9.0
AC – GKN S | 551 | N/A | 11.9
AC – Plexiglas | 512 | N/A | 8.4
AC – SAR | 477 | N/A | 8.1
AC – Poly II | 478 | N/A | 8.0
PC – 9034 | 358 | 7.9 | 9.0
PC – MR10 | 366 | 8.7 | 9.2
PC – Makrolon | 348 | 9.1 | 9.6
PC – Zelux | 362 | 8.4 | 9.1

## Slide 11: Creep Testing
Test Setup – ASTM D790
Tested Stressed: 3, 4, 6, 8, & 10 ksi

## Slide 12: Creep Data
Current data shows that the material remains in secondary creep. Some data points lay outside of this range due to test fixture slippage going unnoticed during quarantine.
Chart: Strain vs Days (MAKAR2-C2-C-1)
| 0 | 3.4722222335403785E-4 | 1.3888888861401938E-3 | 4.166666665696539E-3 | 6.9444444452528842E-3 | 1.1111111110949423E-2 | 1.6666666670062114E-2 | 3.0555555553291924E-2 | 0.11597222222189885 | 0.19374999999854481 | 0.26527777777664596 | 0.88402777777810115 | 1.1381944444437977 | 1.8638888888890506 | 1.9520833333299379 | 2.0208333333357587 | 2.1381944444437977 | 2.9000000000014552 | 3.2013888888905058 | 3.9131944444452529 | 4.1569444444467081 | 6.9124999999985448 | 7.2493055555532919 | 9.0027777777795563 | 13.908333333332848 | 18.19999999999709 | 25.120138888887595 | 32.216666666667152 | 44.918055555557657 | 52.161111111112405 | 63.909027777779556 | 74.061805555553292 | 99.145138888889051 | 155.02013888888905 | 220.02013888888905 | 268.02013888888905 | 372.02013888888905 | 421.02013888888905 | 490.02013888888905 | 529.02013888888905 | 570.02013888888905 | 893.02013888888905 | 1256.0201388888891 | 1404.0201388888891 | 1520.0201388888891 | 1877.0201388888891 | 1899.9784722222248 | 1907.1451388888891 | 1913.1034722222248
 | 0 | 0.60712 | 0.60862 | 0.61725 | 0.62625 | 0.62775 | 0.63338 | 0.63413 | 0.63825 | 0.64013 | 0.64163 | 0.648 | 0.64912 | 0.6495 | 0.65363 | 0.65363 | 0.65363 | 0.65363 | 0.65363 | 0.65512 | 0.65512 | 0.65963 | 0.67988 | 0.68062 | 0.68363 | 0.68588 | 0.68887 | 0.69187 | 0.69487 | 0.69863 | 0.69712 | 0.702 | 0.70538 | 0.71025 | 0.71438 | 0.71138 | 0.7155 | 0.71813 | 0.72038 | 0.72187 | 0.723 | 0.76313 | 0.77363 | 0.79462 | 0.81413 | 0.75787 | 0.75787 | 0.75863 | 0.75863
line | 0.70538 | 0.71025 | 0.71438 | 0.71138 | 0.7155 | 0.71813 | 0.72038 | 0.72187 | 0.723

## Slide 13: Flammability Testing
Test
  Each material had 3 test specimen
    Specimen 1 & 2: 20.9% oxygen at 14.7 psia
    Specimen 3: 30% oxygen at 10.2 psia (only if first two specimen pass)
  Pass/Fail Criteria
    Do not burn more than 6”
    Does not propagate the flame
AC – GKN Cast Results

## Slide 14: Flammability Test Results
Materials passing all 3 tests
  PC – 9034
  PC – MR10
  PC – Makrolon
  PC – Zelux
  AC – Poly II
Materials Passing 1st and/or 2nd tests
  AC – GKN Cast
  AC – SAR
  AC - Plexiglas
Materials Passing none
  AC – GKN Stretched
PC – Makrolon Results
AC – GKN Stretched

## Slide 15: Atomic Oxygen Exposure
Test Setup
Oxygen fluence goal: 1.64x1021 atoms/cm2

## Slide 16: Atomic Oxygen Results
Optical data was not collected due to loss of optics in the specimen
Further testing concluded that polysiloxane anti-scratch coatings at flight-like exposure levels protected the polymer materials
Typical Uncoated Specimen
PC – MR10

## Slide 17: Hypervelocity Impacting
Testing
  3 different projectile materials were used to represent different densities of potential impact material: Soda lime glass (lightest), Stainless steel (heaviest), and Ruby (middle)
  Projectile size and speed varied for a total of 35 shots (shortened to 12 shots for the polymers)

## Slide 18: Glass & Ceramics vs. Polymers
Shot 2 – Stainless Steel @ 5 km/s
Shot 1 – Soda Lime @ 5 km/s
The geometry of the defect for glasses and ceramics is unique with each shot.
  This led to a 35-shot matrix being used to cover any potential difference with material size, density, and speed.
Polymers do not have a unique response to HVI and are not as notch sensitive as glasses and ceramics
  A modified 12-shot matrix was used to cover different material sizes, density, and speeds.
  Shots chosen: # 2, 4, 5, 9, 12, 13, 17, 19, 21, 26, 32, & 33

## Slide 19: Hypervelocity Impact Residual Strength
Residual strength averages varied depending on material
  Polycarbonate: 98% - 99%
  Stretched Acrylic: 90% - 95%
  AC-GKN Cast: 57% - 97%
  AC-Poly II: 84% - 97%
  AC-SAR: 74% - 91%
  ALON: 12% - 35%
  Fused Silica: 9% – 20%
Typical Polycarbonate Break
Typical Glass or Ceramic Break

## Slide 20: Thermal Vacuum Exposure
Test Setup
  The objective of this test was to expose the polymer material to a vacuum and cycle from -100oF to +250oF for 3 cycles using the IR lamps above the specimen.

## Slide 21: Thermal Vacuum Results
Due to an anomaly with the thermal vacuum testing, strength testing was indefinitely post-poned.

## Slide 22: Radiation & UV Exposure
Test Setup
  Each material was exposed to a UV radiation environment and a proton and electron radiation environment. A single coupon was exposed to both environments to capture compounding effects.
  UV consisted of Near UV (NUV) and Vacuum UV (VUV), which was produced by a 1 kW Mercury-Xenon arc lamp and a Deuterium lamp respectively.

## Slide 23: Radiation & UV Results
Severe Lichtenberg lines and yellowing occurred on the specimen.
  Comparisons to flight data show that this does not occur in flight.
  Strength testing shows that radiation embrittlement has taken place, but a more testing in a moreflight-accurate environment is required.
Polycarbonate (PC – 9034)
Acrylic (AC – Poly II)
X-37 Samples 2500 ESH
Top: PC – 9034
Bottom: AC – Poly II

## Slide 24
Questions?