## Slide 1
Novel Ceramic Dispersion Strengthened Refractory Metals for Improved Printability and Properties
Carly J. Romnes
NASA Marshall Space Flight Center
Nuclear, Plasma, & Radiological Engineering, University of Illinois Urbana-Champaign
2023 Formnext Annual Expo
8 November 2023
Special thanks to:
Those working on RAAMBO at NASA; and at UIUC: Stubbins Group, SMEE Group, ETRL, and CPMI

## Slide 2
Motivation for work
Background on nanoparticle effects in AM
Our research goal, further background
Initial material down-selection process
Experimental methods used and initial results of some of those methods
Computational methods, results and approach for design of experiments
Experimental results, comparison with computational results
Presentation Overview

## Slide 3
Refractory alloy components are difficult and expensive to fabricate
These alloys have a variety of applications in extreme environments:
Nuclear fusion systems (divertors, plasma facing components)
Space nuclear power and propulsion
Elevated temperature environments (>1500C)
Aerospace systems
Hypersonic applications
Machining difficult
Fabrication expensive due to amount of waste
Next-generation nuclear energy systems require refractory materials
NASA’s Nuclear Thermal Propulsion Project Concept
Background
NASA.gov

## Slide 4
Additive manufacturing (AM) can help reduce fabrication expenses of refractory materials
Used to fabricate near-net-shape components
Powder recycling reduces material waste and cost associated with fabrication
AM promotes fabrication of particularly complex structures
AM of refractory metals has many benefits
L-PBF molybdenum lattice structures with different unit cell sizes
L-PBF tungsten, ultra-fine lattice, UC = 0.5 mm
Background
Courtesy of B. Colon, UTEP
C. Romnes et al., JMEP 31(8) (2022), pg. 6256-6269.
UC = 1.0 mm
UC = 1.5 mm
L-PBF tungsten test print of optimized heat exchanger design
NASA RAAMBO, unpublished.
Notes: AM promotes fabrication of particularly complex structures than can be achieved using traditional fabrication techniques

## Slide 5
After print parameter optimization, results still unfavorable
High thermal gradients and reheating result in residual stresses that can cause cracking
Brittleness of some metals results in stress-relief through microcracking
Porosity often due to lack of fusion
How to decrease cracking and porosity in AM refractory metals?
→ Grain refinement
AM of pure refractory metals shows microcracking and porosity
L-PBF Tungsten
L-PBF Molybdenum
NASA RAAMBO, unpublished.
Background
Build Direction
Microcracks
Notes: Add image of cracking in DED samples
High thermal gradients and reheating result in residual stresses that can cause cracking
Most AM metals are heat treated to relieve stresses before removal from build plate
Brittleness of some metals results in stress-relief through microcracking
Directional heat flow results in dendritic grains which promote crack propagation
Porosity often due to lack of fusion due to high melt temp of refractories, which overly-aggressive print parameters can reduce
Aggressive parameters result in issues with printing complex geometries
3 cracking mechanisms:
Hot cracking, solidification cracking
Thermal shock (large deltaT, deltaL = alpha*deltaT)
DBTT-shift
DBTT – smaller grains, lower DBTT. How to keep small? Zener Pinning
TL-TS = large, then hot cracking is a problem, steep Scheil curve (eutectic has low crack sus)

## Slide 6
Some work with adding ceramic dispersoids has shown promising results
A few studies have showed that adding ZrC and TaC to tungsten AM feedstock helped reduce cracking
No justification for why the ceramic or the composition was chosen
Current need for rigorous approach to AM refractory alloy design
Background
Direct impact of nanoparticle is unclear due to melting
Nanoparticle melting can be caused by:
Low nanoparticle melting temperature compared to base metal
Melting temperature suppression of nanoparticles
Aggressive print parameters
Result is different compounds form, as well as cellular structures if large amounts added
K. Li et al., IJRMHM 79 (2019), pg. 158-163.
J. Chen et al., JALCOM 897 (2022) 162978.
Notes: Issue is most studies only look at one composition
Need for rigorous approach to design AM refractory alloys with favorable properties
So is this good or bad? Well, the theory behind nanoparticle addition is based on the assumption that the nanoparticles DO NOT melt or form compounds fairly early on in the solidification process.

## Slide 7
The goal of this work is to prevent cracking and improve printability for AM of refractory metals
Identify and utilize computational tools to narrow down the experimental space
Develop a rigorous computational approach for AM alloy design utilizing feedback from experimental work
Want to add small amount of other material, prevent large changes in properties
Is melting good or bad??
Current need for rigorous approach to AM alloy design
L-PBF Pure W
Goal
NASA RAAMBO, unpublished.
J. Martin et al., Nature 549 (2017), pg. 365-369.
Notes: Well, the theory behind nanoparticle addition is based on the assumption that the nanoparticles DO NOT melt or form compounds fairly early on in the solidification process.

## Slide 8
Nanoparticles added to AM feedstock can have multiple effects:
Acts as grain nucleation sites
Promotes equiaxed grains during fabrication
Reduces grain size, promoting decreased DBTT
Prevents grain growth by Zener pinning
These effects can result in increased strength, nearing the values of wrought metals
Nanoparticles can act as grain nucleation sites, helping control solidification
Background
Notes: Fine, equiaxed grains more readily accommodate strain caused by thermal contraction
Helps prevent cracking by decreasing grain size:
Increases fracture toughness
Increases strength
Reduces brittleness

## Slide 9
Promising results but melting may result in smaller impact of nanoparticles
Bad because different phases formed, new phases could be undesirable
May be okay if secondary phase forms at beginning of solidification
How to predict nanoparticle influence?
Is melting good or bad?
Background
Notes: Issue is most studies only look at one composition
Need for rigorous approach to design AM refractory alloys with favorable properties

## Slide 10
Material Down-selection

## Slide 11
Used nanoparticle melt temperature as major selection criteria
Will allow us to show direct impact of solid nanoparticle vs. nanoparticle melting
Highest melting temperature materials are ceramics:
Carbides
Borides
Oxides
Material down-selection depends on application of interest
Methods

## Slide 12
Melting temperature was used to try to ensure ceramic particle survival during the print process
Initial computational selection criteria based on melting temperatures
Methods
 | Disqualified, Tm,ceramic < Tm,metal
 | Likely will melt, Tm,ceramic < Tm,metal + 100
 | Good candidate, Tm,ceramic > Tm,metal + 100
Color Legend
Notes: The highest melting temperature ceramics are carbides, borides, and oxides
This work focuses on carbides
Oxides eliminated due to poor oxidation resistance of refractory metals
Additionally, oxygen content of AM powders is fairly high, and oxygen is introduced during fabrication
Borides eliminated due to high neutron absorption cross-section

## Slide 13
Used nanoparticle melt temperature as major selection criteria
Will allow us to show direct impact of solid nanoparticle vs. nanoparticle melting
Highest melting temperature materials are ceramics:
Carbides
Borides
Oxides
Additional selection criteria:
Cost
Database availability for ICME design
Neutron absorption cross-section
Strength-to-weight ratio
Oxidation and corrosion resistance
Material down-selection depends on application of interest
Methods
Notes: Issue is most studies only look at one composition
Need for rigorous approach to design AM refractory alloys with favorable properties

## Slide 14
Initial Simulations

## Slide 15
Utilize computational tools to narrow trade space
Thermo-Calc Simulations:
Phase diagram modeling
Diffusion simulations
Precipitation simulations
Scheil solidification simulations
Crack susceptibility coefficient
Other models:
Kou crack susceptibility index
Rosenthal melt pool model
Many simulations have been proposed to help predict alloy behavior, printability, and nanoparticle survivability
Computational Methods
Big Question:
Do nanoparticles melt or survive printing?

## Slide 16
Thermo-Calc’s Material-to-Material calculator allows phase diagram calculations
Need to ensure that material system has been assessed for the database used
Can be used to identify unwanted phase formation
Biggest issue is ability to add oxygen to simulations
Not many databases have been well evaluated for oxygen in refractory metals
GRAINGER ENGINEERING
Thermo-Calc: first step is to calculate phase diagram information
Mo + ZrC Computational Results

## Slide 17
Thermo-Calc’s Scheil solidification simulations help predict dendrite behavior
Different types of Scheil simulations, classic Scheil typically the go-to
Crack susceptibility (Kou method) is estimated from the slope at the end of the Scheil solidification curve
Inclusion of C and O essential for accurate predictions of segregation behavior
GRAINGER ENGINEERING
Thermo-Calc: then perform Scheil solidification simulations
Mo + ZrC Computational Results

## Slide 18
Built in Crack Susceptibility Coefficient (CSC) property modeler is used to predict hot cracking
Several options for this module that is based on the work of Yan and Lin
Constant cooling rate likely most similar to what expected for Kou method performed with classic Scheil simulations
GRAINGER ENGINEERING
Thermo-Calc: crack susceptibility was calculated using several approaches
Constant Cooling Rate (dT/dt = C)
Constant Heat Flow (dQ/dt = C)
Heat Flow ∝ 1/sqrt(t)
*
*
*
*
Mo + ZrC Computational Results

## Slide 19
Experimental Methods

## Slide 20
Plasma spheroidization may be required to prevent inhomogeneities
Excess powder from printing is sieved to remove oversized powder
Nanoparticles may detach during powder recycling
Small L-PBF system used to reduce cost associated with alloy development
EOS M100 Metal L-PBF System with high accuracy oxygen meter
Experimental Methods
TEKNA TEKSPHERO-15 plasma spheroidizer

## Slide 21
Acoustic mixing prevents damage and deformation of spherical AM powder
Cooling fixture prevents powder overheating during mixing
Acoustic mixing promotes uniform nanoparticle distribution without AM powder damage
Resodyn LabRAMII Acoustic Mixer with Cooling Fixture
Experimental Methods

## Slide 22
Acoustic mixing prevents damage and deformation of spherical AM powder
Promotes uniform powder distribution without issues seen with mechanical mixing
Even after spheroidization, studies have seen irregular powder morphology
Ensures particle size distribution does not change
May eliminate need for spheroidization after mixing
Acoustic mixing promotes uniform nanoparticle distribution without AM powder damage
Spherical Mo + ZrC (400-1200nm) Acoustically Mixed
Experimental Methods/Results
0.15 mol %. ZrC
0.30 mol %. ZrC
0.60 mol %. ZrC
NASA RAAMBO, unpublished.
K. Li et al., IJRMHM 79 (2019), pg. 158-163.
J. Chen et al., JALCOM 897 (2022) 162978.

## Slide 23
Acoustic mixing does have limitations
NASA RAAMBO, unpublished.
10 µm
0.15 mol %. ZrC
0.30 mol %. ZrC
0.60 mol %. ZrC
1.35 mol %. ZrC
ZrC
ZrC
ZrC
Mo
ZrC
One issue seen is the saturation limit of powder homogenously mixed
ZrC caking on vessel walls seen after mixing 0.60 mol% in Mo
Spherical Mo + ZrC (400-1200nm) Acoustically Mixed
Experimental Methods/Results

## Slide 24
One issue seen is the saturation limit of powder homogenously mixed
ZrC caking on vessel walls seen after mixing 0.60 mol% in Mo
Saturation observed was dependent on nanoparticle size used
Not all nanopowders behave similarly
Acoustic mixing does have limitations
NASA RAAMBO, unpublished.
400 – 1200 nm
80 nm
20 nm
Zr
Mo
20 µm
BSE Image
EDS Overlay
Experimental Methods/Results
Notes: TaC nanopowder was more agglomerated and didn’t mix as well
May require some nanopowder pre-processing to remove large agglomerates

## Slide 25
L-PBF Molybdenum print parameter optimization showed fairly good results
L-PBF Pure Mo DOE1
TEKNA Spherical Powder
L-PBF Pure Mo DOE2
TEKNA Spherical Powder
Density (He Pycnometer): 99.6 %TD
Density (Archimedes): 95.1 %TD
Density (OM Image Analysis): 99.3 %RD
Density (He Pycnometer): 99.3 %TD
Density (Archimedes): 95.6 %TD
Density (OM Image Analysis): 99.2 %RD
Build Direction
After parameter optimization, few defects observed in pure molybdenum
EOS optimized parameters were not accurate for the particle size distribution of this powder
L-PBF Pure Mo EOS Parameters Optimized for Different Particle Size Distribution
Experimental Results
Parameter optimization sample geometry used
NASA RAAMBO, unpublished.

## Slide 26
Initial Results: Mo + ZrC
Mo + 0.15mol% ZrC
Notes: Maybe add image of full sample?

## Slide 27
Thermo-Calc’s CSC property modeler seems to reasonably predict results
Where hot cracking should be largest, see more defects in as-built samples
GRAINGER ENGINEERING
Initial results with 400-1200nm ZrC follow crack susceptibility trends
Mo + ZrC Results
*
*
*
Mo + 0.15 mol% ZrC
Mo + 0.30 mol% ZrC
Mo + 0.60 mol% ZrC
NASA RAAMBO, unpublished.
Build Direction

## Slide 28
One issue seen is the saturation limit of powder homogenously mixed
Caking of ZrC seen after mixing at 0.60 mol% in Mo
Acoustic mixing does have limitations
NASA RAAMBO, unpublished.
10 µm
0.15 mol %. ZrC
0.30 mol %. ZrC
0.60 mol %. ZrC
1.35 mol %. ZrC
ZrC
ZrC
ZrC
Mo
ZrC
Experimental Methods/Results

## Slide 29
Thermo-Calc’s CSC property modeler seems to reasonably predict results
Where hot cracking should be largest, see more defects in as-built samples
No large difference between 0.6 and 1.35 mol%
GRAINGER ENGINEERING
Initial results with 400-1200nm ZrC follow crack susceptibility trends
Mo + ZrC Results
Mo + 0.15 mol% ZrC
Mo + 0.30 mol% ZrC
Mo + 0.60 mol% ZrC
Mo + 1.35mol% ZrC
NASA RAAMBO, unpublished.
Build Direction

## Slide 30
As-built Density results using different methods all follow CSC trends
Mo + ZrC samples all had a higher porosity than pure Mo
Mo-optimized parameters used
Parameter optimization needed for adding carbides
Mechanical testing can help elucidate potential benefits of nanoparticles
GRAINGER ENGINEERING
Initial results with 400-1200nm ZrC show higher AB porosity
Mo + ZrC Results
Mo + 0.15 mol% ZrC
NASA RAAMBO, unpublished.
Pure Mo
Chart: Mol% ZrC
| 0 | 0.15 | 0.3 | 0.6 | 1.35
ρ He pyc (%TD) | 99.6268 | 98.53 | 97.31 | 98.47 | 98.71
ρ Archimedes (%TD) | 95.642 | 94.44 | 95.23 | 96.41 | 96.35
ρ Optical (% RD) | 99.324 | 98.19 | 96.9 | 98.07 | 98.73
CSC | 6.8365 | 6.3191 | 6.0847 | 6.3385 | 7.2629 | 7.5449 | 6.2985 | 5.5933 | 4.8139 | 4.2262 | 3.7609 | 3.4374 | 3.1316 | 2.8507 | 2.629 | 2.4392 | 2.2809 | 2.1074 | 1.9334 | 1.8187 | 1.8187 | 1.6759 | 1.539 | 1.4284 | 1.3017 | 1.2345 | 1.1278 | 1.0126
Density Measurements with CSC Overlaid
Build Direction
Notes: ZrC grain size reduction may improve mechanical properties and reduce crack propagation

## Slide 31
Chart: Mol% ZrC
| 0 | 0.15 | 0.3 | 0.6 | 1.35
AB | 99.324 | 98.19 | 96.9 | 98.07
HIP | 99.7 | 99.5323 | 99.3386 | 99.3515
CSC | 6.8365 | 6.3191 | 6.0847 | 6.3385 | 7.2629 | 7.5449 | 6.2985 | 5.5933 | 4.8139 | 4.2262 | 3.7609 | 3.4374
EBSD shows smaller grain size in Mo-ZrC sample both in AB and HIP conditions
Little to no grain growth observed after HIP heat treatment with ZrC added
Large change in density seen, obtaining values similar to pure Mo
Likely results in better mechanical properties
GRAINGER ENGINEERING
Initial results with 400-1200nm ZrC show promise regarding microstructure and response to heat treatment
Mo + ZrC Results
Mo + 0.15 mol% ZrC
NASA RAAMBO, unpublished.
Pure Mo
AB (Pre-HIP)
Post-HIP
Optical Density Measurements for AB and HIP
Build Direction
Notes: ZrC grain size reduction may improve mechanical properties and reduce crack propagation

## Slide 32
Goal of this work is to reduce/prevent AM refractory alloy cracking through material design utilizing computational approaches
Initial experimental validation of computer simulations started, issues identified
Pure metal print parameter optimization performed, in-process for Mo-carbide samples
Initial Mo + ZrC results show promising trends, particularly after heat treatment
Investigate effects of dispersoids on mechanical properties
Further investigate effects of nanoparticle size and print parameters
Extend work to W and Mo + other carbides
Summary and Future Work
Pure Mo
Chart: Mol% ZrC
| 0 | 0.15 | 0.3 | 0.6 | 1.35
AB | 99.324 | 98.19 | 96.9 | 98.07
HIP | 99.7 | 99.5323 | 99.3386 | 99.3515
CSC | 6.8365 | 6.3191 | 6.0847 | 6.3385 | 7.2629 | 7.5449 | 6.2985 | 5.5933 | 4.8139 | 4.2262 | 3.7609 | 3.4374
Mo + 0.15mol% ZrC
Thank you for your attention!
Feel free to contact me with additional questions: cromnes2@illinois.edu or carly.j.romnes@nasa.gov

## Slide 33
Goal of this work is to reduce/prevent AM refractory alloy cracking through material design utilizing computational approaches
Initial experimental validation of computer simulations started, issues identified
Pure metal print parameter optimization performed, in-process for Mo-carbide samples
Initial Mo + ZrC results show promising trends, particularly after heat treatment
Investigate effects of dispersoids on mechanical properties
Further investigate effects of nanoparticle size and print parameters
Extend work to W and Mo + other carbides
Summary and Future Work
Pure Mo
Thank you for your attention!
Feel free to contact me with additional questions: cromnes2@illinois.edu or carly.j.romnes@nasa.gov
Chart: Mol% ZrC
| 0 | 0.15 | 0.3 | 0.6 | 1.35
AB | 99.324 | 98.19 | 96.9 | 98.07
HIP | 99.7 | 99.5323 | 99.3386 | 99.3515
CSC | 6.8365 | 6.3191 | 6.0847 | 6.3385 | 7.2629 | 7.5449 | 6.2985 | 5.5933 | 4.8139 | 4.2262 | 3.7609 | 3.4374
Mo + 0.15mol% ZrC
This research is supported by a NASA Space Technology Research Fellowship, No. 80NSSC19K1168 and was carried out in part at the Materials Research Laboratory Central Research Facilities at the University of Illinois at Urbana-Champaign and the NASA Marshall Space Flight Center.
Special thank you to: Fernando Reyes-Tirado, Toren Hobbs, Jamelle Williams, Omar Mireles, Prof. James Stubbins, Prof. Jessica Krogstad, and the NASA RAAMBO team

## Slide 34
Backup Slides

## Slide 35
Specimen shape used for print parameter optimization ensured parameters useful for more complex shapes
Build plate with several samples for parameter optimization
Example of parameter optimization sample cross-section
Build Direction
Example of parameter optimization sample burnout at build plate interface
Experimental Methods/Results