## Slide 1
A Procedure to Quantify Interlaminar Damage in Refractory Composites by In-Situ Micro-X-Ray Computed Tomography
Bryan A. Kubitschek
NASA Langley Research Center, Hampton, VA 23681, USA
Bryson A. Marretta
Analytical Services & Materials, Hampton, VA 23666, USA
AIAA SciTech, 8-12 January 2024, Orlando Florida

## Slide 2
Outline
Introduction
Test setup
Data processing
Concluding remarks

## Slide 3
Introduction
Composite material maturation into a flight component is a lengthy and expensive process
Developing models to predict material properties requires improved empirical data at the unit cell level
Material databases will require fewer empirical tests if a feedback loop between a model and empirical observations can be improved

## Slide 4
Introduction, continued
Goal
Collect empirical data on the progressive failure of refractory composites to improve current simulations.
Objective
Develop a procedure to capture the progressive failure in ASTM-sized specimens throughout volume of the specimen.
Approach
Test and observe specimens utilizing a load frame located within a micro-x-ray computed tomography (CT) machine in an iterative manner.

## Slide 5
Specimens
Interlaminar Shear (ILS)
Double Notch Shear (DNS)
ASTM D3846
3.12 in. x 0.49 in.
warp align
8-Harness Satin Weave (HSW)
Gage area 0.169 in²
Flat-wise interlaminar tension (ILT)
ASTM D7291
1.0 in. x 1.0 in.
warp align
8-HSW
Gage area 0.99 in²

## Slide 6
Specimens, continued
Curve-Beam Interlaminar Tensile (CB-ILT)
ASTM D6415
warp align
8-HSW
SiC Coating

## Slide 7
Outline
Introduction
Test setup
Data processing
Concluding remarks

## Slide 8
Testing Procedure

## Slide 9
Materials used in the vicinity of the beam are x-ray friendly
Load frames are bolted to the CT platen
Tests were loaded incrementally by hand
  Interface 1201-BJ 10 Kip load cell
  Interface model 9840 data acquisition system
Test Stand Schematic

## Slide 10
X-Ray Scan Configuration
CT Scan Parameters
CT Technique Parameters
North Star Imaging (NSI) X3000 CT machine with Varian detector
Voxel resolution
Minimum voxel resolution for feature detection

## Slide 11
Outline
Introduction
Test setup
Data processing
Concluding remarks

## Slide 12
All ILT data required image filtering before performing an image analysis
Conducted adaptive Gaussian function
  A lowpass filter - focuses on the attenuation of grayscale intensity
  Linear - replaces the voxel with a weighted summation of the value from its surrounding neighbor
  Standard deviation in the grayscale value decreased 13.8% with the addition of the filter
Image Filtering

## Slide 13
Quantifies the uniformity of the grayscale value throughout the volume of the reconstruction
CT slice of the ILT baseline scan
X-directional variability of grayscale value
Y-directional variability of grayscale value
Z-directional variability of grayscale value
Directional Variability
A)
B)
C)
D)

## Slide 14
Used grayscale deviation for region of interest (ROI) placement for ILT analysis
  XY grayscale variability analysis heat map
Aspire to have the ROI mean and standard deviation (SD) grayscale value be close to the baseline scan
Directional Variability, continued

## Slide 15
Used VGStudioMax porosity inclusion analysis to capture pores and damage
Porosity Analysis

## Slide 16
While an uncertainty quantification has not yet been completed, identifying the sources is the first step
Sources of Uncertainty

## Slide 17
Outline
Introduction
Test setup
Data processing
Concluding remarks

## Slide 18
Developed a procedure to capture the progressive failure in ASTM-sized specimens throughout volume of the specimen
Discussed the details on
CT test stand configuration
Created a micro-x-ray CT configuration
  CT Scan Parameters
  CT Technique
Data processing
  Image filtering
  Directional variability
  Porosity analysis
Sources of uncertainty
Concluding Remarks

## Slide 19
Support was provided by:
NASA Langley Structural Mechanics and Concepts Branch
Acknowledgements